Supplemental File

Unraveling the fundamental mechanism of interface conductive network influence on the fast-charging performance of SiO-based anode for lithium-ion batteries

Ruirui Zhang1,2,#, Zhexi Xiao1,#,*, Zhenkang Lin1,3, Xinghao Yan4, Ziying He1, Hairong Jiang1, Zhou Yang2, Xilai Jia2, Fei Wei1,*

1 Beijing Key Laboratory of Green Chemical Reaction Engineering and Technology, Department of Chemical Engineering, Tsinghua University, Beijing, 100084, PR China

2 School of Materials Science and Engineering, University of Science and Technology Beijing, Beijing, 100083, PR China

3 Beijing Key Laboratory of Chemical Power Source and Green Catalysis, School of Chemistry and Chemical Engineering, Beijing Institute of Technology, Beijing, 100081, PR China

4 Institute of Polymer Science and Engineering, Department of Chemical Engineering, Tsinghua University, 100084, PR China

# Ruirui Zhang and Zhexi Xiao contributed equally to this work.

* Corresponding author. E-mail: xzx14@tsinghua.org.cn, wf-dce@tsinghua.edu.cn

Figure S1. XPS overall spectra of different SiO@C composites.

Figure S2. Si 2p XPS spectra of pristine SiO.

Figure S3. XRD patterns of SiO@C composites with different conductive network before cycling.

Figure S4. Dissolution rate change as the reaction time for different composites in 333 K.

Figure S5. The TG curves for different SiO@C composites.

Figure S6. STEM and corresponding EDS images of SiO@C-l composite.

Figure S7. STEM and corresponding EDS images of SiOx@C-m composite.

Figure S8. STEM and corresponding EDS images of SiOx@C-h composite.

Figure S9. CV curves of SiO@C-m composite from 0.1~0.5 mV s-1.

Figure S10. CV curves of SiO@C-h composite from 0.1~0.5 mV s-1.

Figure S11. EIS spectra of SiO@C-l composite under different temperature.

Figure S12. EIS spectra of SiO@C-m composite under different temperature.

Figure S13. EIS spectra of SiO@C-h composite under different temperature.

Figure S14. STEM and corresponding EDS images of SiOx@C-1 composite after cycling.

Figure S15. STEM and corresponding EDS images of SiOx@C-m composite after cycling.

Figure S16. STEM and corresponding EDS images of SiOx@C-h composite after cycling.

Fig. S17. Equilibrium potential of Li in SiO@C composites as a function of the state of lithiation ([Li+]/[Li+]max).

Fig. S18. Simulation of lithiation profiles of SiO@C-l with different rate.

Fig. S19. Simulation of lithiation profiles of SiO@C-m with different rate.

Fig. S20. Simulation of lithiation profiles of SiO@C-h with different rate.

Fig. S21. Distribution of the Li+ concentration in the electrolyte (a-c) and in solid phase (d-f) at the end of discharge for (a)(d) SiO@C-l, (b)(e) SiO@C-m and (c)(f) SiO@C-h.

Figure S22. The delithiated Cryo-TEM and corresponding selected area electro diffraction pattern of different SiO@C composites. (a) (d)SiO@C-l; (b) (e)SiO@C-m; (c) (f)SiO@C-h.

Figure S23. High-resolution XPS spectra of (a) F 1s, (b) O 1s for different alkali solubility composite (𝛼 decreases from left to right).

Figure S24. Top-view SEM images of electrode surface for different SiO@C composites under different cycling condition. (a-c) SiO@C-l (d-e) SiO@C-m (g-i) SiO@C-h correspond pristine electrode, after 1st cycling and after several rate cycling, respectively.

Figure S25. XRD of SiO@C composites with different conductive network after cycling.

Figure S26. Raman spectra of SiO@C composites with different conductive network after cycling.

Figure S27. EDS images with low and high magnification times of SiO@C-h.

Figure S28. EDS images with low and high magnification times of SiO@C-m.

Figure S29. EDS images with low and high magnification times of SiO@C-l.

Figure S30. GITT profiles and Li+ diffusion rate in different SOC of SiO@C-h, SiO@C-m, SiO@C-l composites during the 2nd cycle.

GITT-derived apparent lithium diffusion coefficient (DLi+) for SiO-based composites was calculated according to the below equation [1, 2, 3, 4]:

where mB and MB are the active and molar masses, respectively, VM is the molar volume, S is the active surface area of electrode, and τ, ΔES, and ΔEτ are respectively the pulse time, voltage change between steps, and voltage change during the pulse period.

Figure S31. Rate performance of SiO@C-h, SiO@C-m, SiO@C-l composites at 6 A g-1 and 8 A g-1.

Model description and parameters

Table S1. Governing equations and definite conditions of the 2D electrochemical model

| Lithium foil electrode |
| --- |
| Current on the surface |  |
| Boundary conditions |  |
| SiO@C electrode |
| Solid phase diffusion |  |
| Li-ion insertion kinetics |  |
| Charge balance |  |
| Boundary conditions | (interface of AM) (current collector) |
| Initial conditions | (inside of AM) |
| Electrolyte |
| Mass transport in electrolyte |  |
| Charge balance |  |
| Boundary conditions |  |
| Initial conditions |  |

Table S2. Parameters of the 2D electrochemical model

| Parameter | Symbol | Value/Definition |
| --- | --- | --- |
| Anodic charge transfer coefficient of SiO@C |  | 0.5 |
| Cathodic charge transfer coefficient of SiO@C |  | 0.5 |
| Anodic charge transfer coefficient of Li foil |  | 0.5 |
| Cathodic charge transfer coefficient of Li foil |  | 0.5 |
| Porosity of the separator |  | 0.4 |
| Electronic conductivity of AM |  | Measured |
| Ionic conductivity of the electrolyte |  | 0.95 S/m |
| Standard concentration in the electrolyte |  | 1000 mol/m3 |
| Li concentration in the AM |  | - |
| Maximal Li concentration in AM |  | 1e5 mol/m3 |
| Diffusion coefficient of Li+ in the electrolyte |  | 3.8e-10 m2/s |
| Li diffusion coefficient in AM |  | Measured |
| Faraday constant |  | 96485 C/mol |
| Exchange current density of SiO@C |  | Measured |
| Exchange current density of Li |  | 10 A/m2 |
| Li transference number |  | 0.251 |
| Equilibrium potential of Li |  | 0 V |
| Equilibrium potential of AM |  | Show as Fig. S17 |

Table S3. Electrical conductivity of the three SiO@C samples without pressure

| Samples | Conductivity/S·cm-1 |
| --- | --- |
| SiO@C-l | 0.136 |
| SiO@C-m | 0.120 |
| SiO@C-h | 0.112 |

References

1. Z. Zhao, J. Han, F. Chen, J. Xiao, Y. Zhao, Y. Zhang, D. Kong, Z. Weng, S. Wu, Q.-H. Yang. Liquid metal remedies silicon microparticulates toward highly stable and superior volumetric lithium storage. Adv. Energy Mater. 12(7), 2103565 (2022). https://doi.org/https://doi.org/10.1002/aenm.202103565

2. X. Wan, C. Kang, T. Mu, J. Zhu, P. Zuo, C. Du, G. Yin. A multilevel buffered binder network for high-performance silicon anodes. ACS Energy Lett. 3572-3580 (2022). https://doi.org/10.1021/acsenergylett.2c02030

3. Y. Huang, B. Shao, Y. Wang, F. Han. Solid-state silicon anode with extremely high initial coulombic efficiency. Energy Environ Sci. (2023). https://doi.org/10.1039/D2EE04057C

4. S. Kim, D.-Y. Han, G. Song, J. Lee, T. Park, S. Park. Resilient binder network with enhanced ionic conductivity for high-areal-capacity si-based anodes in lithium-ion batteries. Chem. Eng. J. 473(145441 (2023). https://doi.org/https://doi.org/10.1016/j.cej.2023.145441