Supporting Information for

Tracking Regulatory Mechanism of Trace Fe on Graphene Electromagnetic Wave Absorption

Kaili Zhang1, 2, Yuhao Liu1, 2, Yanan Liu1, 2, Yuefeng Yan1, 2, Guansheng Ma1, 2, Bo Zhong3, Renchao Che4, *, Xiaoxiao Huang1, 2, *

1 School of Materials Science and Engineering, Harbin Institute of Technology, Harbin, 150001, PR China

2 MIIT Key Laboratory of Advanced Structural-Functional Integration Materials & Green Manufacturing Technology, Harbin Institute of Technology, Harbin, 150001, PR China

3 School of Materials Science and Engineering, Harbin Institute of Technology at Weihai, Weihai, 264209, PR China

4 Laboratory of Advanced Materials, Shanghai Key Lab of Molecular Catalysis and Innovative Materials, Fudan University, Shanghai, 200438, PR China

*Corresponding authors.

E-mail: swliza@hit.edu.cn (Xiaoxiao Huang);

E-mail: rcche@fudan.edu.cn (Renchao Che)

S1 Experimental Section

S1.1 Preparation of Co2O3 nanosheets and the surface modification by CTAB

1.9 g CoCl2·6H2O and 0.8 g NaOH were added into the 160 mL deionized water and stirred till solid particle were completely dissolved. Next, the mixture was transferred to Teflon-lined stainless-steel autoclave for solvothermal reaction at 120 °C for 3 h. The autoclave was cooled to ambient temperature naturally. The product was successively washed by ethanol and distilled water for 3 times and then dried at 60°C. Co2O3 nanosheets were obtained when the as-synthesized Co(OH)2 nanosheets were put into the tube furnace and heat treated at 290 ℃ for 2h under air atmosphere. For the surface modification, Co2O3 nanosheets (1.0 g) and hexadecyltrimethylammonium bromide (CTAB, 0.5 g) were dispersed in deionized water (100 mL) with continuous magnetic stirring in a 60 °C water bath for 2 h. The product was washed with deionized water for several times and dried at 65 °C, and finally the modified hexagonal Co2O3 nanosheets were obtained.

S1.2 Preparation of Ni2O3 nanosheets and the surface modification by CTAB

2.0 g Ni(NO3)2·6H₂O was added into the 100 mL deionized water and stirred till solid particle were completely dissolved. With continuous magnetic stirring, 5 mL NH3·H2O was dropwise added to the solution. The mixture was transferred to Teflon-lined stainless-steel autoclave for solvothermal reaction at 150 °C for 12 h. The autoclave was cooled to ambient temperature naturally. The product was successively washed by ethanol and distilled water for 3 times and then dried at 60°C. Ni2O3 nanosheets were obtained when the as-synthesized Ni(OH)2 nanosheets were put into the tube furnace and heat treated at 350℃ for 2h under air atmosphere. For the surface modification, Ni2O3 nanosheets (1.0 g) and hexadecyltrimethylammonium bromide (CTAB, 0.5 g) were dispersed in deionized water (100 mL) with continuous magnetic stirring in a 60 °C water bath for 2 h. The product was washed with deionized water for several times and dried at 65 °C, and finally the modified hexagonal Ni2O3 nanosheets were obtained.

S1.3 Preparation of Co/RGO and Ni/RGO composite

GO suspension (100 mL, 10 mg·mL-1) were mixed with modified Co2O3 (4 mg) and Ni2O3 (4 mg) respectively, and the mixture was ultrasonic stirred evenly for 3 h by electrostatic adsorption process. Then the mixtures were sealed and refrigerated in the refrigerator, and treated by freeze-drying method (-65 ℃, 0.1 Pa) for 24 h. The above products were put into the tube furnace and heat treated at 350 ℃ for 2h under H2 atmosphere (60 mL·min-1). Finally, Co/RGO and Ni/RGO were obtained, respectively.

S1.4 Calculation details

All of the calculation results of Co/graphene and Ni/graphene were carried out by the Castep module of Materials Studio software based on density functional theory (DFT). The ion−electron interactions were described by the OTFG ultrasoft pseudopotential. The Generalized Gradient Approximation (GGA) method with Perdew−Burke−Ernzerhof (PBE) functional was adopted to solve the exchange and correlation functional energies. The cutoff energy and k-point mesh were determined as 500 eV and 2×3×1, respectively. The calculation accuracy was 1.0×10−5 eV per atom. The thickness of the vacuum layer along the c-axis is fixed at 20 Å.

S2 Supplementary Figures and Tables

Fig. S1. SEM images of a RGO, b Fe/RGO-1, c Fe/RGO-2, d Fe/RGO-3 and e Fe/RGO-4. f ICP measurement of samples.

Fig. S2. XRD patterns a, b and Raman spectra c, d of samples.

Fig. S3. a XPS survey, b C 1s spectra and c O 1s spectra of GO.

Fig. S4. Real part (µ') and imaginary part (µ") of permeability and permeability loss parameter (tan δμ) of a RGO composites and b Fe/RGO-2 composites at a low filling loading of 1-5 wt%.

Fig. S5. RL value versus frequency for specific thickness values of a RGO composites and b Fe/RGO-2 composites at a low filling loading of 1-5 wt%.

Fig. S6. Attenuation constant (ɑ) and intrinsic impedance ratio (Z) of a RGO composites and b Fe/RGO-2 composites at a low filling loading of 1-5 wt%.

From the attenuation point of view, the attenuation constant () can be expressed as follows and is an important factor to evaluate the dissipation effect for EMW [S1, S2].

(1)

Based on formula (1), the larger the imaginary part of EM parameters of the material is, the larger  is obtained, meaning more heat energy consumption are converted easily. From Fig. S6, the attenuation performance gradually increases with the increase of RGO and Fe/RGO filling ratio. The impedance matching ratio (Z) of samples can be calculated as [S3]:

(2)

and  are intrinsic impedance matches of the absorbing material and vacuum, respectively. The Z value of the absorbing material is closer to 1, the better the impedance match, so that more electromagnetic waves enter the material to promote the absorption of electromagnetic energy. The Z values exhibit the opposite trend compared to . With the increase of the filling ratio, the Z values gradually decrease due to the increase of electrical conductivity.

Fig. S7. Structure of Fe (110)/graphene (001) system (showing top view a and side view b) and charge density difference c, with purple and gray balls representing Fe atom and C atom, red contour denotes electron depletion region and blue contour refers to electron accumulation region.

Fig. S8. Microstructural characterizations of graphene and Fe/graphene. a Raman spectra, b TEM image, c-f SAED patterns and g AFM topography signals of graphene. h TEM and i SAED pattern of Fe/graphene.

Fig. S9. a µ' and b µ" of RGO, Fe/RGO-1, Fe/RGO-2, Fe/RGO-3 and Fe/RGO-4. c Magnetic hysteresis loops of Fe, Fe2O3, Fe/RGO-4.

Due to the low Fe content (0.32 ~1.22 wt%) in Fe/RGO composites, the u' and u" values of all samples are ≈1 and ≈0 (Fig. S9), and the saturation magnetization (Ms) value of Fe/RGO-4 was only 0.8 % of Fe (1.40 emu/g, 169.08 emu/g), indicating that Fe has no obvious magnetic loss at the measured frequency in the alternating EM field.

Fig. S10. The RL values versus frequency and thickness for a-c RGO, d-f Fe/RGO-1, g-i Fe/RGO-2, j-l Fe/RGO-3 and m-o Fe/RGO-4. The region confined in the black lines corresponds to RL≤−10 dB.

Fig. S11. RL values, simulated and experimental values of matching thicknesses under λ/4 condition, impedance matching values for a RGO, b Fe/RGO-2, c Fe/RGO-3 over 2-18 GHz.

Fig. S12. Cole-Cole curves of ε'-ε" and ε'- ε"p/f of a RGO, b Fe/RGO-1, c Fe/RGO-2, d Fe/RGO-3 and e Fe/RGO-4.

Based on the Debye relaxation theory, the existence of polarization can be proved by the Cole-Cole semicircle, each semicircle of Cole-Cole expresses a Debye relaxation process [S4]. The ԑ' and ε" can be expressed as follows:

(3)

(4)

(5)

where  is the static permittivity,  is the relative dielectric constant, τ is the relaxation time, respectively. To extract the τ of each polarization behavior, equation (3) and (4) can be further reduced to equation (6):

(6)

According to equation (6), each straight line in the plots of  versus  represents a kind of polarization behavior with different relaxation times [S5]. Fig. S12 shows the '-" and - curves of RGO, Fe/RGO-1, Fe/RGO-2, Fe/RGO-3 and Fe/RGO-4, it can be seen that the number of semicircles increases with the increase of Fe, indicating an enhanced relaxation process compared with GO. Fe/RGO-2 and Fe/RGO-3 have more polarization relaxation processes. The relaxation times are listed in Table S1.

Fig. S13. The tanδε a, α b, and Z c of RGO, Fe/RGO-1, Fe/RGO-2, Fe/RGO-3 and Fe/RGO-4.

Fig. S14. The electromagnetic parameters a-d and RL values e-h of Fe/RGO-1', Fe/RGO-2', Fe/RGO-3' and Fe/RGO-4'.

Fig. S15. The electrical conductivity of RGO, Fe/RGO-1, Fe/RGO-2, Fe/RGO-3 and Fe/RGO-4 powders.

Fig. S16. XRD patterns of Co, Ni, Co/RGO, Ni/RGO a. Eelectromagnetic parameters (ε', ε", μ' and μ") of Co/RGO and Ni/RGO composites with 2 wt% loading b, c. Charge density difference plots of Co (002)/graphene (001) and Ni (111)/graphene (001). The positive and negative charges are shown in blue and red (isovalue: 0.1) d. The σ e, Z and α f of Co/RGO and Ni/RGO. RL values with different thickness of Co/RGO g and Ni/RGO with 2 wt% loading h.

Fig. S17. Comparison of some typical RGO-based composites reported in the recent literature.

Table S1 Parameters of the local dielectric detection

| Parameters | value |
| --- | --- |
| Quality factor (Q) | 181 |
| Elastic coefficient (k) | 3 N/m |
| AC voltage (VAC) | 10 V |
| Lift height (z) | 15 nm |

Table S2 Relaxation times of the RGO, Fe/RGO-1, Fe/RGO-2, Fe/RGO-3 and Fe/RGO-4

| Samples | Frequency (GHz) | τ (s) |
| --- | --- | --- |
| RGO | 2 - 4.32 | 6.21×10-11 |
|  | 4.32 - 9.76 | 1.59×10-11 |
|  | 9.76 - 18 | 2.45×10-12 |
| Fe/RGO-1 | 2 - 4.79 | 8.22×10-11 |
|  | 4.79 - 11.27 | 2.142×10-11 |
|  | 11.27 - 14.52 | 4.17×10-12 |
|  | 14.52 - 18 | 3.54×10-12 |
| Fe/RGO-2 | 2 - 3.56 | 9.43×10-11 |
|  | 3.56 - 4.78 | 7.24×10-11 |
|  | 4.78 - 7.67 | 2.89×10-11 |
|  | 7.67 - 9.78 | 1.73×10-11 |
|  | 9.78 - 14.94 | 8.85×10-12 |
|  | 14.94 - 18 | 8.18×10-12 |
| Fe/RGO-3 | 2 - 2.52 | 9.36×10-11 |
|  | 2.52 - 3.74 | 6.41×10-11 |
|  | 3.74 - 5.67 | 5.37×10-11 |
|  | 5.67 - 8.73 | 1.77×10-11 |
|  | 8.73 - 14.85 | 7.15×10-12 |
|  | 14.85 - 18 | 3.72×10-12 |
| Fe/RGO-4 | 2 - 4.12 | 2.68×10-11 |
|  | 4.12 - 5.79 | 1.41×10-11 |
|  | 5.79 - 10.54 | 7.58×10-12 |
|  | 10.54 - 18 | 4.14×10-12 |

Table S3 The EMA performance in 2-18 GHz of typical absorbers

| Filler | Mass Ratio (wt%) | Thickness (mm) | RLmin (dB) | EAB (GHz) | Refs. |
| --- | --- | --- | --- | --- | --- |
| RGO/Cu | 8 | 5 | -50.4 | 4.1 | [S6] |
| FeCo/GNS | 50 | 2.5 | -40.2 | 4.3 | [S7] |
| NiFe2O4/rGO | 70 | 5 | -42 | 5.6 | [S8] |
| CoFe2O4/rGO | 50 | 2.8 | -57.7 | 5.8 | [S9] |
| Ti3C2Tx/rGO | 5 | 2.2 | -53.49 | 4.4 | [S10] |
| MnFe2O4/RGO | 10 | 3.0 | -29.0 | 4.88 | [S11] |
| rGO/CuS/PPy | 10 | 4 | -49.11 | 4.88 | [S12] |
| PVDF/RGO | 3 | 4 | -25.6 | 4.32 | [S13] |
| CoO-Co@RGO | 10 | 2.1 | -34.22 | 6.24 | [S14] |
| Graphene/Fe3O4/C | 25 | 1.8 | -30.1 | 5.4 | [S15] |
| SiC/FexOy/graphite | 66.67 | 5.5 | -41.8 | 4.64 | [S16] |
| ZnFe2O4@RGO@CuS | 20 | 2.2 | -55.4 | 7.5 | [S17] |
| Fe/RGO-2 | 2 | 2.45 | -53.38 | 6.56 | This work |
|  | 2 | 2.62 | -29.33 | 7.52 |  |

Supplementary References

- X. Liu, Y. Duan, Y. Guo, H. Pang, Z. Li et al., Microstructure design of high-entropy alloys through a multistage mechanical alloying strategy for temperature-stable megahertz electromagnetic absorption. Nano-Micro Lett. 14(1), 142 (2022). https://doi.org/10.1007/s40820-022-00886-6

- L. Zhang, X. Zhang, G. Zhang, Z. Zhang, S. Liu et al., Investigation on the optimization, design and microwave absorption properties of reduced graphene oxide/tetrapod-like ZnO composites. RSC Adv. 5(14), 10197-10203 (2015). https://doi.org/10.1039/c4ra12591f

- K. Zhang, J. Chen, S. Yue, H. Zhang, C. Meng et al., Facile synthesis of core-shell CI/SiO2 decorated RGO sheets composite for excellent electromagnetic wave absorption performance covering the whole x-band. Compos. Part A-Appl. S. 130, 105755 (2020). https://doi.org/10.1016/j.compositesa.2019.105755

- W. Liu, S. Tan, Z. Yang, G. Ji, Hollow graphite spheres embedded in porous amorphous carbon matrices as lightweight and low-frequency microwave absorbing material through modulating dielectric loss. Carbon 138, 143–153 (2018) https://doi.org/10.1016/j.carbon.2018.06.009

- X. Zhang, P. Guan, X. Dong, Multidielectric polarizations in the core/shell Co/graphite nanoparticles. Appl. Phys. Lett. 96, 223111 (2010). https://doi.org/10.1063/1.3446868

- H. Zhang, X. Tian, X. Zhang, S. Li, Y. Shen et al., Preparation and electromagnetic wave absorption of rgo/Cu nanocomposite. J. Phys. Chem. A 91(9), 1771-1774 (2017). https://doi.org/10.1134/s0036024417090126

- X. Li, J. Feng, Y. Du, J. Bai, H. Fan et al., One-pot synthesis of CoFe2O4/graphene oxide hybrids and their conversion into FeCo/graphene hybrids for lightweight and highly efficient microwave absorber. J. Mater. Chem. A 3(10), 5535-5546 (2015). https://doi.org/10.1039/c4ta05718j

- J. He, X. Wang, Y. Zhang, M. Cao, Small magnetic nanoparticles decorating reduced graphene oxides to tune the electromagnetic attenuation capacity. J. Mater. Chem. C 4(29), 7130-7140 (2016). https://doi.org/10.1039/c6tc02020h

- Y. Liu, Z. Chen, Y. Zhang, R. Feng, X. Chen et al., Broadband and lightweight microwave absorber constructed by in situ growth of hierarchical CoFe2O4/reduced graphene oxide porous nanocomposites. ACS Appl. Mater. Interfaces 10(16), 13860-13868 (2018). https://doi.org/10.1021/acsami.8b02137

- S. Shang, N. Zhao, Y. Chen, X. Wang, F. Hu et al., Ti3C2Tx/rgo aerogel towards high electromagnetic wave absorption and thermal resistance. CrystEngComm 24(25), 4556-4563 (2022). https://doi.org/10.1039/d2ce00578f

- F. Wen, H. Hou, J. Xiang, X. Zhang, Z. Su et al., Fabrication of carbon encapsulated Co3O4 nanoparticles embedded in porous graphitic carbon nanosheets for microwave absorber. Carbon 89, 372-377 (2015). https://doi.org/10.1016/j.carbon.2015.03.057

- B. Zhang, S. Lin, J. Zhang, X. Li, X. Sun, Facile synthesis of sandwich-like rGO/CuS/Polypyrrole nanoarchitectures for efficient electromagnetic absorption. Materials 13, 446 (2020). https://doi.org/10.3390/ma13020446

- X. Zhang, G. Wang, W. Cao, Y. Wei, M. Cao et al., Fabrication of multi-functional PVDF/RGO composites via a simple thermal reduction process and their enhanced electromagnetic wave absorption and dielectric properties. RSC Adv. 4(38), 19594-19601 (2014). https://doi.org/10.1039/c4ra02040e

- Y. Meng, S. Lu, Y. Wu, Z. Zi, Y. Ma et al., Efficient electromagnetic wave absorption of porous CoO–Co@RGO composites with optimized impedance matching derived from metal-organic frameworks. Nano 15(08), 2050104 (2020). https://doi.org/10.1142/s1793292020501040

- Y. Huang, L. Wang, X. Sun, Sandwich-structured graphene@Fe3O4@carbon nanocomposites with enhanced electromagnetic absorption properties. Mater. Lett. 144, 26-29 (2015). https://doi.org/10.1016/j.matlet.2015.01.015

- R. Meng, T. Zhang, P. Jiao, M. Zhang, X. Huang et al., Facile fabrication of SiC/FexOy embellished graphite layers with enhanced electromagnetic wave absorption. J. Alloys Compd. 798, 386-393 (2019). https://doi.org/10.1016/j.jallcom.2019.05.210

- Y. Wang, X. Gao, X. Wu, W. Zhang, Q. Wang et al., Hierarchical ZnFe2O4@RGO@CuS composite: strong absorption and wide-frequency absorption properties. Ceram. Int. 44(8), 9816-9822 (2018). https://doi.org/10.1016/j.ceramint.2018.02.220