Supporting Information for

Structural Engineering of Hierarchical Magnetic/Carbon Nanocomposites via In-Situ Growth for High-Efficient Electromagnetic Wave Absorption

Xianyuan Liu1, Jinman Zhou1, Ying Xue, Xianyong Lu1, *

Key Laboratory of Bio-Inspired Smart Interfacial Science and Technology of Ministry of Education, School of Chemistry, Beihang University, Beijing 100191, P. R. China

*Corresponding author. E-mail: xylu@buaa.edu.cn (Xianyong Lu)

Supplementary Figures and Table

Fig. S1 a Optical image of the surface of α-Fe2O3@ANFs/Al-α-Fe2O3 aerogel. SEM images of b α-Fe2O3@ANFs/Al-α-Fe2O3(1:1) aerogel, c α-Fe2O3@ANFs/Al-α-Fe2O3(1:2) aerogel, and d α-Fe2O3@ANFs/Al-α-Fe2O3(1:2.5) aerogel

Fig. S2 SEM images of a Al-Fe3O4 nanosheets, b Fe3O4-Fe@CNFs/Al-Fe3O4-Fe(1:1), c Fe3O4-Fe@CNFs/Al-Fe3O4-Fe(1:2), and d Fe3O4-Fe@CNFs/Al-Fe3O4-Fe(1:2.5)

Fig. S3 XRD patterns of Al-α-Fe2O3 nanosheets, and Al-Fe3O4 nanosheets

Fig. S4 TEM images of a α-Fe2O3@ANFs and b Fe3O4-Fe@CNFs

Fig. S5 TEM image of 0D@1D/2D Fe3O4-Fe@CNFs/Al-Fe3O4-Fe

Fig. S6 XPS spectra of Fe 2p of Fe3O4-Fe@CNFs

Fig. S7 DTG curves of ANFs, α-Fe2O3@ANFs, and α-Fe2O3@ANFs/Al-α-Fe2O3

Fig. S8 3D reflection loss curves maps of a Fe3O4-Fe@CNFs/Al-Fe3O4-Fe(1:1) and b Fe3O4-Fe@CNFs/Al-Fe3O4-Fe(1:2.5)

Table S1 Comparison of electromagnetic wave absorption of the samples

| Absorbers | Component, wt | RL, min |  | RL≤-10 dB |  |
| --- | --- | --- | --- | --- | --- |
|  | Fe3O4-Fe : Al-Fe3O4-Fe | RLmin (dB) | Thickness (mm) | EAB (GHz) | Thickness (mm) |
| CNFs | - | -3.8 | 0.9 | 0 | - |
| Fe3O4-Fe@CNFs | - | -24.2 | 1.9 | 5.9 | 1.9 |
| Al-Fe3O4 | - | -39.6 | 8.0 | 2.4 | 7.4 |
| Fe3O4-Fe@CNFs/Al-Fe3O4-Fe | 1: 3 | -59.3 | 4.3 | 5.6 | 2.2 |
| Fe3O4-Fe@CNFs/Al-Fe3O4-Fe(1:2.5) | 1 : 2.5 | -49.5 | 2.3 | 6.1 | 2.1 |
| Fe3O4-Fe@CNFs/Al-Fe3O4-Fe(1:2) | 1 : 2 | -49.5 | 2.1 | 6.4 | 2.2 |
| Fe3O4-Fe@CNFs/Al-Fe3O4-Fe(1:1) | 1 : 1 | -15.4 | 1.5 | 5.7 | 1.8 |