Supporting Information for

Dual-Defect Engineering Strategy Enables High-Durability Rechargeable Magnesium-Metal Batteries

Fuyu Chen1,2, Bai-Qing Zhao3, Kaifeng Huang1,2, Xiu-Fen Ma1,2, Hong-Yi Li1,2,*, Xie Zhang4, Jiang Diao1,2, Jili Yue1,2, Guangsheng Huang1,2, Jingfeng Wang1,2, Fusheng Pan1,2,5,*

1 National Innovation Center for lndustry-Education Integration of Energy Storage Technology, School of Materials Science and Engineering, Chongqing University, Chongqing 400044, P. R. China

2 National Magnesium Alloy Material Engineering Technology Research Center, Chongqing University, Chongqing 400044, P. R. China

3 Materials and Energy Division, Beijing Computational Science Research Center, Beijing 100193, P. R. China

4 School of Materials Science and Engineering, Northwestern Polytechnical University, Xi'an 710072, P. R. China.

5 National Key Laboratory of Advanced Casting Technologies, Chongqing University, Chongqing 400044, P. R. China

*Corresponding authors. E-mail: hongyi.li@cqu.edu.cn (Hong-Yi Li); fspan@cqu.edu.cn (Fusheng Pan)

Supplementary Figures and Tables

Fig. S1 Elemental mapping results of V, O, Mg, and C in MVOH/rGO

Fig. S2 The Electron Localization Function simulations results of (a) and Charge Density Difference of (b)

Electron Localization Function (ELF) results in Fig. S2a demonstrate strong localization of electrons around Mg, suggesting an increased tendency for these electrons to transfer from O, and the large ELF on MgO bond confirms the presence of strong interactions between Mg and O. Subsequently, the calculated Charge Density Difference (CDD) in Fig. S2b reveals charge accumulation around Mg (represented by the blue electron cloud) and corresponding electron loss around O (depicted by the yellow electron cloud), this suggests that O in VO layers can donate its lone pair electrons to the vacant orbitals of P-Mgd, indicating a strong tendency to generate coordination bonds between Mg and O from VO layers. Therefore, it is demonstrated that the bonding occurs between P-Mgd and O in the VO layers, leading to the generation of MgO5 polyhedra.

Fig. S3 Total Density of States (TDOS) of (a, b) MVOH and (c, d) VOH

The TDOS of MVOH (Fig. S3a and S3b) demonstrates a higher density of electronic states near the Fermi level compared to VOH (Fig. S3c and S3d), verifying the enhancement of conductivity attributed to the P-Mgd in V2O5·nH2O.

Fig. S4 Lamellar crystal structure of VOH

Fig. S5 TG profiles of (a) VOH, (b) MVOH, and (c) MVOH/rGO

Results show that pristine VOH contains 1.5 crystal water molecules per unit. The crystal water content of MVOH decreases to 1.0 because the interaction force between the pre-interalated Mg2+ and V–O layers shrinks the interlayer spacing. However, Od can greatly alleviate the interaction caused by P-Mgd, and the crystal water content of MVOH/rGO thus recovers to 1.4 per unit. Furthermore, the 3.1% weight loss observed in Fig. S5c between 270°C and 400°C can primarily be attributed to the thermal degradation of rGO in MVOH/rGO composite. The rGO content is thus deduced to be 11.4% in MVOH/rGO composite, with Mg0.07V2O5·1.4H2O content of 88.6%.

Fig. S6 XRD patterns of VOH, MVOH, and MVOH/rGO

Fig. S7 Raman spectra of (a) MVOH/rGO and (b) GO

Fig. S8 (ac) The pair distribution function results of MVOH/rGO at different midden range

The PDF analysis results at 5-10 Å in Fig. S8a reveal the typical characterization of V2O5 [S1], in which the peaks at 7.2 Å, 8.0 Å, and 11.0 Å in Fig. S8b represent the interatomic distance of VV along the b direction and the a direction, respectively.

Fig. S9 XPS survey spectra of MVOH/rGO at the Ar ion etching depth of 0, 10, 20 nm

In agreement with the ICP–OES and EDX analysis results, the XPS survey spectra in Fig. S9 shows the signals of V, Mg, O, and C. The signal intensity of C element decreases as the etching depth increasing from 0 to 20 nm, while the signals of V, Mg, and O elements increase, which verifies the surface contact between MVOH and rGO.

Fig. S10 (a) V 2p and (b) O 1s high-resolution XPS spectra of MVOH

Fig. S11 Initial GCD curves at 0.02 A g1 of (a) MVOH and (b) MVOH/rGO cathodes

Fig. S12 CV curves of MVOH/rGO at 0.1 mV s1 for the initial three cycles

Fig. S13 EPR spectrum of VOH-Od

As shown in Fig. S13, the characteristic peaks of Od were clearly observed, implying the existence of Od in VOH-Od.

Fig. S14 Long-term cycling performance at 0.5 A g1 of (a) MVOH/rGO, (b) VOH-Od, and (c) MVOH cathodes

Fig. S15 (a, b) Time-potential curves of MVOH/rGO cahode during long-term cycling at 1 A g1

Fig. S16 Fitting curves for Peaks AB in CV curves of MVOH/rGO at 0.10.8 mV s1

Fig. S17 Current contribution ratios of capacitive processes for VOH, MVOH, and MVOH/rGO cathodes at 0.10.8 mV s1

The contribution ratios of capacitive and diffusion processes in VOH, MVOH, and MVOH/rGO cathodes are calculated from the following equation [S2, S3]:

i = k1v+ k2v1/2                                          (S1)

Where ‘i’ represents the peak current, and k1 and k2 represent the capacitive and diffusion contribution coefficients, respectively.

Fig. S18 EIS spectra of VOH, MVOH, and MVOH/rGO cathodes

Mg2+ Diffusion coefficient (DMg2+) in the low-frequency region is calculated by the following equation [S4S7]:

DMg2+= R2T22A2n4F4C2σω2(ω≫2DMg2+L2)                     (S2)

Where R represents the gas constant, T is the absolute temperature, A denotes the electrode area, n stands for the amount of charge transferred per unit of molecule, F is the Faraday constant, C signifies the ion concentration in the electrolyte, and σω represents the Warburg coefficient. The low-frequency region σω and the real part of impedance (Z') are related by the following equation:

Z'= Rs + Rct +σω1/2                                    (S3)

Fig. S19 (ae) Interlayer spacing results of ex-situ TEM characterization

Fig. S20 Elemental mapping results of V, O, Mg, and C elements in MVOH/rGO at (a) fully charged, (b) charge states of D, (c) fully discharged, (d) discharg state of B, and (e) pristine states

Fig. S21 Cycling performance of Mg foil//MVOH/rGO full cell at 0.05 A g1

Table S1 ICP–OES results of Mg and V elements in MVOH/rGO and MVOH

| Samples | Elements | C1(mg/L) | RSD | Mg:V (atomic ratio) | Formula |
| --- | --- | --- | --- | --- | --- |
| MVOH/rGO-1 | Mg/V | 0.963/58.27 | 0.04%/1.14% | 0.07: 2 | Mg0.07V2O5 |
| MVOH/rGO-2 | Mg/V | 0.959/58.06 | 0.04%/1.14% | 0.07: 2 | Mg0.07V2O5 |
| MVOH-1 | Mg/V | 0.322/28.37 | 0.013%/0.56% | 0.05: 2 | Mg0.05V2O5 |
| MVOH-2 | Mg/V | 0.320/27.87 | 0.013%/0.55% | 0.05: 2 | Mg0.05V2O5 |

Table S2 XRD Rietveld refinement results of MVOH/rGO

| Samples | Rwp | Rp | GOF | χ² |
| --- | --- | --- | --- | --- |
| MVOH/rGO | 3.49% | 2.77% | 1.37 | GOF^2 |

Where, Rwp represents the Weighted Profile R-factor, Rp is the Profile R-factor, GOF denotes the Goodness of Fit, χ² stands for the Chi-squared, respectively.

Table S3 Comparison of cycling performance between MVOH/rGO and previously reported cathodes

| Cathode | Anode | Electrolyte | Cycling performance | Refs. |
| --- | --- | --- | --- | --- |
| V2O5-x | AC | 0.5 M Mg(ClO4)2 | ~78.2% after 400 cycles at 0. 1 A g−1 | [S7] |
| Mn0.04V2O5·1.17H2O | AC | 0.3 M Mg(TFSI)2 | 82% after 10,000 cycles at 2 A g−1 | [S8] |
| Mg0.3V2O5·1.1H2O | AC | 0.3 M Mg(TFSI)2 | 80% after 10,000 cycles at 2 A g−1 | [S9] |
| PANI-V2O5 | AC | 0.3 M Mg(TFSI)2 | ~80% after 500 cycles at 4 A g−1 | [S10] |
| SNVOX-CNT | AC | 0.5 M Mg(ClO4)2 | ~82% after 400 cycles at 0.1 A g−1 | [S11] |
| V2O5-PEDOT | AC | 0.3 M Mg(TFSI)2 | 67.3% after 500 cycles at 0.5 A g−1 | [S6] |
| NaV2O2(PO4)2F/rGO | AC | 0.3 M Mg(TFSI)2 | 76% after 9,500 cycles at 0.5 A g−1 | [S12] |
| (NH4)2V6O16·1.5H2O | AC | 0.5 M Mg(ClO4)2 | ~63% after 50 cycles at 0.1 A g−1 | [S13] |
| NaV8O20·nH2O | - | TEGDME/H2O | ~52.5% after 1,000 cycles at 1.5 A g−1 | [S14] |
| PANI/CC | AC | 0.3 M Mg(TFSI)2 | 97.3% after 1500 cycles at 1 A g−1 | [S15] |
| Mg(Mg0.5V1.5)O4 | AC | 0.3 M Mg(TFSI)2 | 71.4% after 500 cycles at 1 A g−1 | [S16] |
| MVOH/rGO | AC | 0.5 M Mg(TFSI)2 | 95% after 7,000 cycles at 1 A g−1 | This work |

Table S4 Comparison of cycling performance between Mg foil//MVOH/rGO full cell and previously reported RMMBs

| Cathode | Anode | Electrolyte | Cycling performance | Refs. |
| --- | --- | --- | --- | --- |
| Na2Ti6O13 | Mg foil | 0.4 M APC | 58.8% after 300 cycles at 0.1 A g−1 | [S17] |
| NiS@C-C | Mg foil | APC-LiCl | 65% after 45 cycles at 0.05 A g−1 | [S18] |
| Te@CSs | Mg foil | 0.4 M APC | 77.1% after 500 cycles at 0.5 A g−1 | [S19] |
| RFC/V2O5 | Mg foil | 0.2 M [Mg2(μ-Cl)2(DME)4][AlCl4]2 in DME | 67% after 100 cycles at 0.32 A g−1 | [S20] |
| PA-VOPO4 | Mg foil | 0.25 M APC | 70% after 500 cycles at 0.1 A g−1 | [S21] |
| PVO | Mg foil | 0.2 M Mg(CF3SO3)2- MgCl2-AlCl3 | 69.6% after 50 cycles at 0.1 A g−1 | [S10] |
| Ag2Se@C | Mg foil | 0.2 M APC | 65% after 500 cycles at 0.2 A g−1 | [S22] |
| Ti3C2Tx@C | Mg AZ31 | 0.4 M Mg2Cl3+ ·AlPh2Cl2-/THF | 85% after 400 cycles at 0.05 A g−1 | [S23] |
| Mo6S8 | Mg foil | PDEGVE@GF GPE | 80.3% after 500 cycles at 0.13 A g−1 | [S24] |
| MoS2/graphene | Mg foil | 0.25 M APC | 83% after 500 cycles at 0.5 A g−1 | [S25] |
| CuSe | Mg foil | 0.3 M Mg[B(hfip)4]2/DME-NaOTf | 84.0% after 100 cycles at 0.1 A g−1 | [S26] |
| V2O5-PEDOT | Mg foil | 0.4 M APC-CTAB | ~49.7% after 150 cycles at 0.1 A g−1 ~62.3% after 500 cycles at 0.5 A g−1 | [S27] |
| NaV3O8·1.69H2O | Mg foil | 0.4 M APC | 80% after 100 cycles at 0.05 A g−1 | [S28] |
| MVOH/rGO | Mg foil | 0.4 M APC-CTAB | 84% after 850 cycles at 0.1 A g−1 | This work |

Supplementary References

[S1]	X. Zhao, L. Li, L. Zheng, L. Fan, Y. Yi, et al., 3d‐orbital regulation of transition metal intercalated vanadate as optimized cathodes for calcium‐ion batteries. Adv. Funct. Mater. 34, 2309753 (2023). https://doi.org/10.1002/adfm.202309753

[S2]	Y. Zheng, Z. Yao, Z. Shadike, M. Lei, J. Liu, et al., Defect-concentration-mediated T-Nb2O5 anodes for durable and fast-charging Li-Ion batteries. Adv. Funct. Mater. 32, 2107060 (2021). https://doi.org/10.1002/adfm.202107060

[S3]	J. Liu, Y. Wang, C. Yang, K. Mu, S. Wang, et al., A microcapsule‐assistant self‐healing magnesium battery cathodes. Energy Technol. 9, 2100393 (2021). https://doi.org/10.1002/ente.202100393

[S4]	Q. Zong, Q. Wang, C. Liu, D. Tao, J. Wang, et al., Potassium ammonium vanadate with rich oxygen vacancies for fast and highly stable Zn-Ion storage. ACS Nano 16, 4588-4598 (2022). https://doi.org/10.1021/acsnano.1c11169

[S5]	D. Wu, J. Zeng, H. Hua, J. Wu, Y. Yang, et al., NaV6O15: A promising cathode material for insertion/extraction of Mg2+ with excellent cycling performance. Nano Res. 13, 335-343 (2020). https://doi.org/10.1007/s12274-019-2602-6

[S6]	Y. S. Joe, M. S. Kang, G. Jang, S. J. Lee, P. Nakhanivei, et al., Intercalation of bilayered V2O5 by electronically coupled pedot for greatly improved kinetic performance of magnesium ion battery cathodes. Chem. Eng. J. 460, 141706 (2023). https://doi.org/10.1016/j.cej.2023.141706

[S7]	D. Wu, Y. Zhuang, F. Wang, Y. Yang, J. Zeng, et al., High-rate performance magnesium batteries achieved by direct growth of honeycomb-like V2O5 electrodes with rich oxygen vacancies. Nano Res. 16, 4880–4887 (2023). https://doi.org/10.1007/s12274-021-3679-2

[S8]	X. Deng, Y. Xu, Q. An, F. Xiong, S. Tan, et al., Manganese ion pre-intercalated hydrated vanadium oxide as a high-performance cathode for magnesium ion batteries. J. Mater. Chem. A. 7, 10644–10650 (2019). https://doi.org/10.1039/c8ta11236c

[S9]	Y. Xu, X. Deng, Q. Li, G. Zhang, F. Xiong, et al., Vanadium oxide pillared by interlayer Mg2+ ions and water as ultralong-life cathodes for magnesium-ion batteries. Chem 5, 1194–1209 (2019). https://doi.org/10.1016/j.chempr.2019.02.014

[S10]	C. Zuo, Y. Xiao, X. Pan, F. Xiong, W. Zhang, et al., Organic-inorganic superlattices of vanadium oxide@polyaniline for high-performance magnesium-ion batteries. ChemSusChem 14, 2093–2099 (2021). https://doi.org/10.1002/cssc.202100263

[S11]	D. Wu, Z. Wen, H. Jiang, H. Li, Y. Zhuang, et al., Ultralong-lifespan magnesium batteries enabled by the synergetic manipulation of oxygen vacancies and electronic conduction. ACS Appl. Mater. Interfaces 13, 12049-12058 (2021). https://doi.org/10.1021/acsami.1c00170

[S12]	J. Wang, S. Tan, G. Zhang, Y. Jiang, Y. Yin, et al., Fast and stable Mg2+ intercalation in a high voltage NaV2O2(PO4)2F/rGO cathode material for magnesium-ion batteries. Sci. China Mater. 63, 1651–1662 (2020). https://doi.org/10.1007/s40843-020-1311-1

[S13]	L. Wei, R. Lian, D. Wang, Y. Zhao, D. Yang, et al., Magnesium ion storage properties in a layered (NH4)2V6O16·1.5H2O nanobelt cathode material activated by lattice water. ACS Appl. Mater. Interfaces 13, 30625–30632 (2021). https://doi.org/10.1021/acsami.1c06398

[S14]	X. Wang, X. Zhang, G. Zhao, H. Hong, Z. Tang, et al., Ether-water hybrid electrolyte contributing to excellent Mg ion storage in layered sodium vanadate. ACS Nano 16, 6093–6102 (2022). https://doi.org/10.1021/acsnano.1c11590

[S15]	P. Luo, Y. Xiao, J. Yang, C. Zuo, F. Xiong, et al., Polyaniline nanoarrays/carbon cloth as binder-free and flexible cathode for magnesium ion batteries. Chem. Eng. J. 433, 133772 (2021). https://doi.org/10.1016/j.cej.2021.133772

[S16]	C. Zuo, W. Tang, B. Lan, F. Xiong, H. Tang, et al., Unexpected discovery of magnesium-vanadium spinel oxide containing extractable Mg2+ as a high-capacity cathode material for magnesium ion batteries. Chem. Eng. J. 405, 127005 (2021). https://doi.org/10.1016/j.cej.2020.127005

[S17]	L. Luo, Y. Zhen, Y. Lu, K. Zhou, J. Huang, et al., Structural evolution from layered Na2Ti3O7 to Na2Ti6O13 nanowires enabling a highly reversible anode for Mg-ion batteries. Nanoscale 12, 230-238 (2020). https://doi.org/10.1039/c9nr08003a

[S18]	G. Zhu, G. Xia, H. Pan, X. Yu. Size-controllable nickel sulfide nanoparticles embedded in carbon nanofibers as high-rate conversion cathodes for hybrid Mg-based battery. Adv. Sci. 9, e2106107 (2022). https://doi.org/10.1002/advs.202106107

[S19]	Z. Chen, Q. Yang, D. Wang, A. Chen, X. Li, et al., Tellurium: a high-performance cathode for magnesium ion batteries based on a conversion mechanism. ACS Nano 16, 5349–5357 (2022). https://doi.org/10.1021/acsnano.1c07939

[S20]	Y. Cheng, Y. Shao, V. Raju, X. Ji, B. L. Mehdi, et al., Molecular storage of Mg ions with vanadium oxide nanoclusters. Adv. Funct. Mater. 26, 3446–3453 (2016). https://doi.org/10.1002/adfm.201505501

[S21]	L. Zhou, Q. Liu, Z. Zhang, K. Zhang, F. Xiong, et al., Interlayer-spacing-regulated VOPO4 nanosheets with fast kinetics for high-capacity and durable rechargeable magnesium batteries. Adv. Mater. 30, e1801984 (2018). https://doi.org/10.1002/adma.201801984

[S22]	J. H. Ha, B. Lee, J. H. Kim, B. W. Cho, S.-O. Kim, et al., Silver chalco-genides (Ag2X, X=S, Se) nanoparticles embedded in carbon matrix for facile magnesium storage via conversion chemistry. Energy Storage Mater. 27, 459–465 (2020). https://doi.org/10.1016/j.ensm.2019.12.008

[S23]	F. Liu, Y. Liu, X. Zhao, X. Liu, L.-Z. Fan. Pursuit of a high-capacity and long-life Mg-storage cathode by tailoring sandwich-structured Mxene@carbon nanosphere composites. J. Mater. Chem. A. 7, 16712–16719 (2019). https://doi.org/10.1039/c9ta02212k

[S24]	X. Ge, F. Song, A. Du, G. Sun, S. Zhang, et al., Stable anion-rectifying poly (alkoxide magnesium) electrolytes for reversible magnesium metal batteries. ACS Energy Lett. 8, 3685-3692 (2023). https://doi.org/10.1021/acsenergylett.3c01192

[S25]	C. Wu, G. Zhao, X. Yu, C. Liu, P. Lyu, et al., MoS2/graphene heterostructure with facilitated Mg-diffusion kinetics for high-performance rechargeable magnesium batteries. Chem. Eng. J 412, 128736 (2021). https://doi.org/10.1016/j.cej.2021.128736

[S26]	Y. Shen, Y. Wang, Y. Miao, Q. Li, X. Zhao, et al., Anion-incorporated Mg-ion solvation modulation enables fast magnesium storage kinetics of conversion-type cathode materials. Adv. Mater. 35, e2208289 (2023). https://doi.org/10.1002/adma.202208289

[S27]	Z. Yao, Y. Yu, Q. Wu, M. Cui, X. Zhou, et al., Maximizing magnesiation capacity of nanowire cluster oxides by conductive macromolecule pillaring and multication intercalation. Small 17, 2102168 (2021). https://doi.org/10.1002/smll.202102168

[S28]	M. Rashad, H. Zhang, M. Asif, K. Feng, X. Li, et al., Low-cost room-temperature synthesis of NaV3O8·1.69H2O nanobelts for Mg batteries. ACS Appl. Mater. Interfaces 10, 4757–4766 (2018). https://doi.org/10.1021/acsami.7b18682