Supporting Information for

Controlled Twill Surface Structure Endowing Nanofiber Composite Membrane Excellent Electromagnetic Interference Shielding

Dechang Tao 1, #, Xin Wen 1, 2, #, Chenguang Yang1, *, Kun Yan1, Zhiyao Li 1, Wenwen Wang1, *, Dong Wang1, 2, *

1 Key Laboratory of Textile Fiber and Products (Wuhan Textile University), Ministry of Education, Wuhan Textile University, Wuhan 430200, P. R. China

2 College of Chemistry, Chemical Engineering and Biotechnology, Donghua University, Shanghai 201620, P. R. China

# Dechang Tao and Xin Wen contributed equally to this work.

*Corresponding authors. E-mail: cgyang@wtu.edu.cn (Chenguang Yang); wwang@wtu.edu.cn (Wenwen Wang); wangdon08@126.com (Dong Wang)

S1 Experimental Section

S1.1 Preparation of nanofiber membrane

Polyvinyl alcohol-polyethylene copolymer (Pva-co-PE) and cellulose acetate butyrate (CAB) are uniformly mixed in a mass ratio of 2:8, and then extruded using a twin-screw extruder with a screw diameter of 28 mm and a length-to-diameter ratio of 35 to prepare new-born island fibers. The precursor fibers are extruded using a spinneret with a diameter of 1.8 mm and 12 holes, and spun under the conditions of 200~220°C, 1.5~2.5 MPa, and a winding speed of 1.5 m/s. After removing the sea phase with acetone, nanofibers are obtained, and the process diagram for the preparation of nanofibers is shown in Fig. S1.

Fig. S1 Schematic diagram of preparation of Pva-co-PE nanofibers

The nanofiber suspension membrane was prepared by using Pva-co-PE nanofibers with a diameter of 100-200 nm. The preparation process of nanofiber is shown in Fig. S1 and the SEM images of the nanofibers are shown in Fig. S2 c, c'. Ti3AlC2 (MAX) powder (98.7%) was obtained from Suzhou Kaifa New Material Technology Co., LTD. (Suzhou, China). Lithium fluoride (LiF), hydrochloric acid (HCl, 33wt.%), potassium hydroxide (KOH), silver nitrate (AgNO3), ethylene glycol (EG), copper chloride dihydrate (CuCl2·2H2O), ferric chloride (FeCl3), sodium bromide (NaBr) and polyvinylpyrrolidone (PVP, Mw=1300000 g/mol) were purchased from Sinopharm Chemical Reagent Co., Ltd. Nylon fabric (JRYS014, hole size: 25 μm×50 μm) provided by Suzhou Jurui textile strength Co., Ltd. The SEM images of the twill structure on the surface of nylon fabric are shown in Fig. S3.

S1.2 Synthesis of Ti3C2Tx MXene

Fig. S4 shows the preparation diagram of Ti3C2Tx MXene. First, 4g LiF was dissolved in a mixture of 60 mL HCl and 20 mL deionized water to make an etching solution. Under magnetic agitation, 2g Ti3AlC2 was added to the prepared etching solution and stirred at 35°C for 48 h. The mixture was centrifuged at 4000 r/min for 5 mins each time, and the product was repeatedly washed with deionized water until the pH was 6. Finally, the supernatant was collected by ultrasound for 30 min and centrifugation at a speed of 3500 r/min for 60 minutes, and a dark green colloidal solution of Ti3C2Tx MXene was obtained.

S1.3 Synthesis of Silver Nanowires

By magnetic stirring, 1.6g amount of PVP was fully dissolved in 100 mL EG in a three-necked flask at 150°C for 4 hours. Subsequently, 4 mL of 20 mM CuCl2·2H2O and 4 mM ferric chloride were added to PVP solution to achieve ultra-high aspect ratio AgNWs. A mixture of 40 mL of 0.70 M AgNO3 and 4 mM sodium bromide was then added to the solution and left for 2 hours at 150°C. After cooling to room temperature, filter acetone and ethanol with inhalation to wash completely. The obtained AgNWs were re-dispersed in deionized water at a concentration of 2.5 mg·mL−1 for future use. The optical photos of silver nanowire solution and microphotograph of the obtained AgNWs are shown in Fig. S2 a and a', respectively.

S1.4 Electromagnetic shielding effectiveness: theory and measurement

The EMI SE was analyzed using a vector network analyzer (Agilent, PNA-N5244A) in the frequency range of 8.2−12.4 GHz. Scattering parameters (S11 and S21) were recorded, and transmission (T), reflection (R), and absorption (A) coefficients were calculated. The total EMI SE (SET) and contributions from reflection (SER), absorption (SEA) and multiple internal reflections (SEM) are calculated as follows:

(S1)

(S2)

(S3)

(S4)

(S5)

(S6)

EMI SE depends on the dielectric and magnetic properties. At the same time, the EMI SE/t is normalized to eliminate the influence of thickness. In addition, the specific shielding efficiency (SSE) and SSE/t, taking into account density and thickness, are expressed as follows:

(S7)

(S8)

EMI shielding efficiency (%) is obtained by using the following equation:

(S9)

S1.5 Optimization model design

A typical square root optimization model (Eq. S10) is used in this work.

(S10)

The process sequence is executed according to the main effect. The optimal design software Design-Expert 12.0 was used to obtain the final equation (Eq. S11) according to the actual factors.

(S11)

S2 Supplementary Tables and Figures

Fig. S2 a Optical photos of silver nanowire solution and a' microphotograph of the AgNW. b Optical photos of Ti3C2Tx MXene solution. b' SEM image of the multi-layered MXene. b'' TEM images of the Ti3C2Tx MXene after ultrasonic dispersion. c-c' SEM images of the Pva-co-PE nanofibers

Fig. S3 SEM images of twill structure on nylon fabric surface

Fig. S4 Synthesis of Ti3C2Tx MXene via the etching and delamination method

Fig. S5 SEM image of surface morphology of the PMxAg nanofiber composite membranes. a-a'''' PM1.6Ag. b-b'''' PM2.2Ag. c-c'''' PM5.2Ag, and d-d'''' PM7.4Ag

Fig. S6 SEM images of surface morphology of the PM5.2Ag nanofiber composite membranes

Fig. S7 FTIR spectra of the Pva-co-PE membrane

Fig. S8 a High-resolution XPS spectra of C1s and b O1s for Pva-co-PE membrane

Fig. S9 SEM images of cross-section morphologies of the Pva-co-PE and PMxAg nanofiber composite membranes. a-a''' Pva-co-PE. b-b''' PM1.6Ag. c-c''' PM2.2Ag. d-d''' PM5.2Ag. e-e''' PM7.4Ag

Fig. S10 EDS spectra of the PM2.2Ag nanofiber composite membrane

Fig. S11 a-e EMI SE of Pva-co-PE and PMxAg nanofiber composite membranes when EM wave incidence from twill surface. f-i EMI SE of PMxAg nanofiber composite membrane when EM wave incidence from non-twill surface. j EMI STA and EMI STR of PMxAg nanofiber composite membranes when EM wave incidence from twill surface. k STA and STR of PMxAg nanofiber composite membranes when EM wave incidence from non-twill surface. l Comparison of the reflectance ratios of the EM wave at different incidence planes

Fig. S12 PMxAg nanofiber composite membrane materials prepared by different pumping pressure: a 20 kPa. b 40 kPa. c 60 kPa. d 80 kPa. e 100 kPa. f 120 kPa

Fig. S13 Circuit diagram of a Tesla coil device

Table S1 Performance comparison of PMxAg nanofiber membranes with previous reported EMI shielding materials

| EMI shielding materials | Filling Content (wt%) | Thickness (μm) | Density (g·cm-3) | EMI SE (dB) | EMI SSE (dB·cm−1) | EMI SSE/t (dB·cm2·g−1) | Ref. |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Pva-co-PE | 0 | 361.1 | 0.205 | / | / | / | This work |  |
| PM1.6Ag | 1.6 | 93.6 | 0.220 | 45.8 | 4893.2 | 22241.6 |  |  |
| PM2.2Ag | 2.2 | 164.5 | 0.239 | 78.9 | 4796.3 | 20068.2 |  |  |
| PM5.2Ag | 5.2 | 193.8 | 0.245 | 93.5 | 4824.5 | 19691.8 |  |  |
| PM7.4Ag | 7.4 | 264.7 | 0.253 | 103.9 | 3925.2 | 15514.6 |  |  |
| MXene/AgNWs/PVDF | 15 | 300 | 0.79 | 25.9 | 863.3 | 1091 | [S1] |  |
| FA-MXene/CNF | 30.5 | 120 | / | 63.9 | 5325 | / | [S2] |  |
| MXene/CNF film | 50 | 167 | 1.13 | 25 | 1497.0 | 884 | [S3] |  |
| MXene/PLA | / | 150 | / | 55.4 | 3693 | / | [S4] |  |
| MXene/CNF | 26 | 105 | / | 39 | 3714 | / | [S5] |  |
| MXene/AgNWs film | 20 | 120 | 1091 | 54.0 | 4500 | / | [S6] |  |
| MXene/FeCo/CNF | 55 | 340 | / | 58 | 1706 | / | [S7] |  |
| MXene/BC | 50 | 116 | / | 43.7 | 3767 | / | [S8] |  |
| MXene/Ni/PVDF | 20 | 100 | / | 19.5 | 1950 | / | [S9] |  |
| Ti3C2Tx/Wax | / | 800 | 2.03 | 70 | 875 | 431 | [S10] |  |
| Ti3C2Tx/PVA | 0.15 | 5000 | 0.011 | 28 | 56 | 5136 | [S11] |  |
| MXene | 100 | 11 | 0.001 | 68 | 28.4 | 25863 | [S12] |  |
| Graphene oxide/Fe3O4 paper | 50 | 300 | 0.78 | 24 | 800 | 1025.6 | [S13] |  |
| LPGF | 100 | 200 | 0.075 | 43.8 | 2190 | 29178 | [S14] |  |
| PPGF | 100 | 200 | 0.078 | 22 | 1100.0 | 14103 | [S14] |  |
| Ni@graphene/PVDF | 20 | 700 | / | 51.4 | 734 | / | [S15] |  |
| RGO/PEI | 1.38 | 2300 | 0.23 | 13 | 43.3 | 188 | [S16] |  |
| RGO/PU | 4.7 | 60000 | 6.01 | 57.7 | 1923 | 320 | [S17] |  |
| RGO/PS | 3.47 | 2500 | 0.25 | 45.1 | 41.9 | 167.5 | [S18] |  |
| RGO/PDMS | 0.36 | 1000 | 0.1 | 20 | 333.3 | 3333 | [S19] |  |
| RGO/WPU | 5 | 1000 | / | 34 | 33.8 | 338 | [S20] |  |
| RGO/Fe3O4 | 3.4 | 1800 | / | 13 | 8.9 | 49.5 | [S21] |  |
| RGO-γ-Fe2O3 | 2.3 | 360 | / | 20.3 | 15 | 416.7 | [S22] |  |
| RGO | 18.8 | / | / | 34.2 | 28.5 | 118.75 | [S23] |  |
| Graphene film | 50 | 10 | 1.49 | 43.8 | 43800 | 29396 | [S24] |  |
| Graphene film | / | 3.9 | 2.25 | 27.8 | 722078 | 320923 | [S25] |  |
| RGO/PMMA | 1.8 | 4000 | 0.79 | 19 | 47.4 | 60 | [S26] |  |
| Carbon nanotube/AgNWs/cellulose paper | 6.07 | 160 | 0.51 | 23.8 | 1487.5 | 2916.7 | [S27] |  |
| MWCNT/WPU | 76.2 | 100 | 0.04 | 21.1 | 211 | 5140 | [S28] |  |
| MWCNT/WPU | 76 | 320 | 0.45 | 49 | 1531 | 3408 | [S29] |  |
| MWCNT/SWCNT films | 30 | 130 | 0.8 | 65 | 500 | 625 | [S30] |  |
| MWCNT/WPU | 7.2 | 4500 | 0.126 | 50 | 111.1 | 881.8 | [S28] |  |
| MWCNT/PLLA | 1.47 | 2500 | 0.299 | 23 | 92 | 306.7 | [S31] |  |
| CNT/PS | 3.6 | 120 | 0.12 | 18.5 | 33 | 275 | [S32] |  |
| CNWs@G | 4.6 | 1600 | 0.159 | 36 | 370.7 | 2317 | [S33] |  |
| MWCNTs/Epoxy | 1.34 | 2000 | 0.2 | 40 | 20.1 | 100.5 | [S34] |  |
| CNTs/PC | 5 | 1850 | 0.185 | 25 | 20.8 | 112.6 | [S35] |  |
| CNTs/PP | 7.5 | 1000 | 0.1 | 35 | 37.2 | 372 | [S36] |  |
| SWCNTs/Pani | 15.5 | 2400 | 0.24 | 31.5 | 24.2 | 100.8 | [S23] |  |
| CNT/MLGEP | / | 1600 | 0.0089 | 47 | 293.8 | 32375 | [S37] |  |
| CNT/sponge | / | 2400 | 0.02 | 22 | 91.7 | 4583 | [S38] |  |
| MWCNT/CNF | / | 150 | 0.77 | 46.4 | 3093.3 | 4017.3 | [S39] |  |
| AgNWs/calcium alginate/PU film | 10 | 330 | 0.174 | 31.3 | 948.5 | 5451.1 | [S40] |  |
| AgNWs/PI | 4.5 | 5000 | 0.029 | 35 | 70 | 2416 | [S41] |  |
| AgNWs/PANI | 14 | 13 | / | 48 | 36923 | / | [S42] |  |
| AgNWs/cellulose papers | 0.53 | 160 | 0.53 | 48.6 | 3038 | 5585 | [S43] |  |
| Ag/Carbon fibers | 9 | 2500 | / | 38 | / | / | [S44] |  |
| AgNWs/PS | / | 800 | / | 33 | / | / | [S41] |  |
| AgNWs/Epoxy | / | 40 | / | 35 | / | / | [S45] |  |
| AgNWs/Epoxy | / | 13 | / | 50 | / | / | [S42] |  |

Fig. S14 SEM images of the microstructure of PM7.4Ag nanofiber composite membrane after combustion

Fig. S15 Water contact angle on the twill surface of the PM7.4Ag composite membrane after different bending times

Fig. S16 SEM images and water contact angle pictures of the PM7.4Ag composite membrane subjected to different compressive stresses, (a, a', a'') 2.5 MPa, (b, b', b'') 5.0 MPa, and (c, c', c'') 10.0 MPa

Fig. S17 Stability diagram of the PMxAg skeleton structure

Supplementary References

[S1]	 H. Cheng, Y. Pan, Q. Chen, R. Che, G. Zheng et al., Ultrathin flexible poly(vinylidene fluoride)/mxene/silver nanowire film with outstanding specific emi shielding and high heat dissipation. Adv. Composites Hybrid Mater. 4(3), 505-513 (2021). https://doi.org/10.1007/s42114-021-00224-1

[S2]	 Z. Guo, P. Ren, J. Wang, J. Tang, F. Zhang et al., Multifunctional sandwich-structured magnetic-electric composite films with joule heating capacities toward absorption-dominant electromagnetic interference shielding. Composites Part B: Engin. 236, 109836 (2022). https://doi.org/10.1016/j.compositesb.2022.109836

[S3] 	W.-T. Cao, F.-F. Chen, Y.-J. Zhu, Y.-G. Zhang, Y.-Y. Jiang et al., Binary strengthening and toughening of mxene/cellulose nanofiber composite paper with nacre-inspired structure and superior electromagnetic interference shielding properties. ACS Nano 12(5), 4583-4593 (2018). https://doi.org/10.1021/acsnano.8b00997

[S4]	 Z. Du, K. Chen, Y. Zhang, Y. Wang, P. He et al., Engineering multilayered mxene/electrospun poly(lactic acid) membrane with increscent electromagnetic interference (EMI) shielding for integrated joule heating and energy generating. Composites Commun. 26, 100770 (2021). https://doi.org/10.1016/j.coco.2021.100770

[S5]	 M. Ma, X. Liao, Q. Chu, S. Chen, Y. Shi et al., Construction of gradient conductivity cellulose nanofiber/mxene composites with efficient electromagnetic interference shielding and excellent mechanical properties. Composites Sci. Technol. 226, 109540 (2022). https://doi.org/10.1016/j.compscitech.2022.109540

[S6] L.-X. Liu, W. Chen, H.-B. Zhang, Q.-W. Wang, F. Guan et al., Flexible and multifunctional silk textiles with biomimetic leaf-like mxene/silver nanowire nanostructures for electromagnetic interference shielding, humidity monitoring, and self-derived hydrophobicity. Adv. Funct. Mater. 29(44), 1905197 (2019). https://doi.org/10.1002/adfm.201905197

[S7] M. Ma, W. Tao, X. Liao, S. Chen, Y. Shi et al., Cellulose nanofiber/mxene/feco composites with gradient structure for highly absorbed electromagnetic interference shielding. Chemical Engineering Journal. 452, 139471 (2023). https://doi.org/10.1016/j.cej.2022.139471

[S8]	 H. Liu, Z. Cui, L. Luo, Q. Liao, R. Xiong et al., Facile fabrication of flexible and ultrathin self-assembled Ti3C2Tx/bacterial cellulose composite films with multifunctional electromagnetic shielding and photothermal conversion performances. Chem. Engin. J. 454, 140288 (2023). https://doi.org/10.1016/j.cej.2022.140288

[S9] S.-J. Wang, D.-S. Li, L. Jiang, Synergistic effects between mxenes and ni chains in flexible and ultrathin electromagnetic interference shielding films. Adv. Mater. Interfaces 6(19), 1900961 (2019). https://doi.org/10.1002/admi.201900961

[S10] X. Li, X. Yin, S. Liang, M. Li, L. Cheng et al., 2d carbide mxene Ti2CTx as a novel high-performance electromagnetic interference shielding material. Carbon. 146, 210-217 (2019). https://doi.org/10.1016/j.carbon.2019.02.003

[S11] H. Xu, X. Yin, X. Li, M. Li, S. Liang et al., Lightweight ti2ctx mxene/poly(vinyl alcohol) composite foams for electromagnetic wave shielding with absorption-dominated feature. ACS Appl. Mater. Interfaces 11(10), 10198-10207 (2019). https://doi.org/10.1021/acsami.8b21671

[S12] F. Shahzad, M. Alhabeb, C.B. Hatter, B. Anasori, S. Man Hong et al., Electromagnetic interference shielding with 2d transition metal carbides (mxenes). Science 353(6304), 1137-1140 (2016). https://doi.org/10.1126/science.aag2421

[S13] W.-L. Song, X.-T. Guan, L.-Z. Fan, W.-Q. Cao, C.-Y. Wang et al., Magnetic and conductive graphene papers toward thin layers of effective electromagnetic shielding. J. Mater. Chem. A 3(5), 2097-2107 (2015). https://doi.org/10.1039/C4TA05939E

[S14] D. Lai, X. Chen, G. Wang, X. Xu, Y. Wang. Highly conductive porous graphene film with excellent folding resilience for exceptional electromagnetic interference shielding. J. Mater. Chem. C 8(26), 8904-8916 (2020). https://doi.org/10.1039/D0TC01346C

[S15] L. Liang, P. Xu, Y. Wang, Y. Shang, J. Ma et al., Flexible polyvinylidene fluoride film with alternating oriented graphene/ni nanochains for electromagnetic interference shielding and thermal management. Chem. Engin. J. 395, 125209 (2020). https://doi.org/10.1016/j.cej.2020.125209

[S16] J. Ling, W. Zhai, W. Feng, B. Shen, J. Zhang et al., Facile preparation of lightweight microcellular polyetherimide/graphene composite foams for electromagnetic interference shielding. ACS Appl. Mater. Interfaces 5(7), 2677-2684 (2013). https://doi.org/10.1021/am303289m

[S17] B. Shen, Y. Li, W. Zhai, W. Zheng. Compressible graphene-coated polymer foams with ultralow density for adjustable electromagnetic interference (emi) shielding. ACS Appl. Mater. Interfaces 8(12), 8050-8057 (2016). https://doi.org/10.1021/acsami.5b11715

[S18] D.X. Yan, H. Pang, B. Li, R. Vajtai, L. Xu et al., Structured reduced graphene oxide/polymer composites for ultra‐efficient electromagnetic interference shielding. Adv. Funct. Mater. 25(4), 559-566 (2015). https://doi.org/10.1002/adfm.201403809

[S19] Z. Chen, C. Xu, C. Ma, W. Ren, H.M. Cheng. Lightweight and flexible graphene foam composites for high‐performance electromagnetic interference shielding. Adv. Mater. 25(9), 1296-1300 (2013). https://doi.org/10.1002/adma.201204196

[S20] S.-T. Hsiao, C.-C. M. Ma, W.-H. Liao, Y.-S. Wang, S.-M. Li et al., Lightweight and flexible reduced graphene oxide/water-borne polyurethane composites with high electrical conductivity and excellent electromagnetic interference shielding performance. ACS Appl. Mater. Interfaces 6(13), 10667-10678 (2014). https://doi.org/10.1021/am502412q

[S21] K. Yao, J. Gong, N. Tian, Y. Lin, X. Wen et al., Flammability properties and electromagnetic interference shielding of pvc/graphene composites containing Fe3O4 nanoparticles. RSC Adv. 5(40), 31910-31919 (2015). https://doi.org/10.1039/C5RA01046B

[S22] B. Yuan, C. Bao, X. Qian, L. Song, Q. Tai et al., Design of artificial nacre-like hybrid films as shielding to mitigate electromagnetic pollution. Carbon 75, 178-189 (2014). https://doi.org/10.1016/j.carbon.2014.03.051

[S23] B. Yuan, L. Yu, L. Sheng, K. An, X. Zhao. Comparison of electromagnetic interference shielding properties between single-wall carbon nanotube and graphene sheet/polyaniline composites. J. Phys. D: Appl. Phys. 45(23), 235108 (2012). https://doi.org/10.1088/0022-3727/45/23/235108

[S24] Q. Wei, S. Pei, X. Qian, H. Liu, Z. Liu et al., Superhigh electromagnetic interference shielding of ultrathin aligned pristine graphene nanosheets film. Adv. Mater. 32(14), 1907411 (2020). https://doi.org/10.1002/adma.201907411

[S25] T. Zhou, C. Xu, H. Liu, Q. Wei, H. Wang et al., Second time-scale synthesis of high-quality graphite films by quenching for effective electromagnetic interference shielding. ACS Nano 14(3), 3121-3128 (2020). https://doi.org/10.1021/acsnano.9b08169

[S26] H.-B. Zhang, Q. Yan, W.-G. Zheng, Z. He, Z.-Z. Yu. Tough graphene−polymer microcellular foams for electromagnetic interference shielding. ACS Appl. Mater. Interfaces 3(3), 918-924 (2011). https://doi.org/10.1021/am200021v

[S27] H. Y. Choi, T.-W. Lee, S.-E. Lee, J. Lim, Y. G. Jeong. Silver nanowire/carbon nanotube/cellulose hybrid papers for electrically conductive and electromagnetic interference shielding elements. Composites Sci. Technol. 150, 45-53 (2017). https://doi.org/10.1016/j.compscitech.2017.07.008

[S28] Z. Zeng, H. Jin, M. Chen, W. Li, L. Zhou et al., Lightweight and anisotropic porous mwcnt/wpu composites for ultrahigh performance electromagnetic interference shielding. Adv. Funct. Mater. 26(2), 303-310 (2016). https://doi.org/10.1002/adfm.201503579

[S29] Z. Zeng, M. Chen, H. Jin, W. Li, X. Xue et al., Thin and flexible multi-walled carbon nanotube/waterborne polyurethane composites with high-performance electromagnetic interference shielding. Carbon 96, 768-777 (2016). https://doi.org/10.1016/j.carbon.2015.10.004

[S30] S. Lu, J. Shao, K. Ma, D. Chen, X. Wang et al., Flexible, mechanically resilient carbon nanotube composite films for high-efficiency electromagnetic interference shielding. Carbon 136, 387-394 (2018). https://doi.org/10.1016/j.carbon.2018.04.086

[S31] T. Kuang, L. Chang, F. Chen, Y. Sheng, D. Fu et al., Facile preparation of lightweight high-strength biodegradable polymer/multi-walled carbon nanotubes nanocomposite foams for electromagnetic interference shielding. Carbon 105, 305-313 (2016). https://doi.org/10.1016/j.carbon.2016.04.052

[S32] Y. Yang, M.C. Gupta, K.L. Dudley, R.W. Lawrence, Novel carbon nanotube−polystyrene foam composites for electromagnetic interference shielding. Nano Lett. 5(11), 2131-2134 (2005). https://doi.org/10.1021/nl051375r

[S33] L. Kong, X. Yin, M. Han, X. Yuan, Z. Hou et al., Macroscopic bioinspired graphene sponge modified with in-situ grown carbon nanowires and its electromagnetic properties. Carbon 111, 94-102 (2017). https://doi.org/10.1016/j.carbon.2016.09.066

[S34] Y. Chen, H.-B. Zhang, Y. Yang, M. Wang, A. Cao et al., High-performance epoxy nanocomposites reinforced with three-dimensional carbon nanotube sponge for electromagnetic interference shielding. Adv. Funct. Mater. 26, 447–455 (2016). https://doi.org/10.1002/adfm.201503782

[S35] M. Arjmand, M. Mahmoodi, G.A. Gelves, S. Park, U. Sundararaj Electrical and electromagnetic interference shielding properties of flow-induced oriented carbon nanotubes in polycarbonate. Carbon 49(11), 3430-3440 (2011). https://doi.org/10.1016/j.carbon.2011.04.039

[S36] M.H. Al-Saleh, U. Sundararaj Electromagnetic interference shielding mechanisms of CNT/polymer composites. Carbon 47, 1738–1746 (2009). https://doi.org/10.1016/j.carbon.2009.02.030

[S37] Q. Song, F. Ye, X. Yin, W. Li, H. Li et al., Carbon nanotube–multilayered graphene edge plane core–shell hybrid foams for ultrahigh-performance electromagnetic-interference shielding. Adv. Mater. 29, 1701583 (2017). https://doi.org/10.1002/adma.201701583

[S38] M. Crespo, M. González, A. L. Elías, L. Pulickal Rajukumar, J. Baselga, M. Terrones, J. Pozuelo. Ultra-light carbon nanotube sponge as an efficient electromagnetic shielding material in the ghz range. physica status solidi (RRL) – Rapid Research Letters. 8(8), 698-704 (2014). https://doi.org/10.1002/pssr.201409151

[S39] H. Zhang, X. Sun, Z. Heng, Y. Chen, H. Zou et al., Robust and flexible cellulose nanofiber/multiwalled carbon nanotube film for high-performance electromagnetic interference shielding. Ind. Eng. Chem. Res. 57, 17152–17160 (2018). https://doi.org/10.1021/acs.iecr.8b04573

[S40] L.-C. Jia, D.-X. Yan, X. Liu, R. Ma, H.-Y. Wu et al., Highly efficient and reliable transparent electromagnetic interference shielding film. ACS Appl. Mater. Interfaces 10, 11941–11949 (2018). https://doi.org/10.1021/acsami.8b00492

[S41] J. Ma, K. Wang, M. Zhan A comparative study of structure and electromagnetic interference shielding performance for silver nanostructure hybrid polyimide foams. RSC Adv. 5, 65283–65296 (2015). https://doi.org/10.1039/c5ra09507g

[S42] F. Fang, Y.-Q. Li, H.-M. Xiao, N. Hu, S.-Y. Fu. Layer-structured silver nanowire/polyaniline composite film as a high performance x-band EMI shielding material. J. Mater. Chem. C 4(19), 4193-4203 (2016). https://doi.org/10.1039/C5TC04406E

[S43] T.-W. Lee, S.-E. Lee, Y.G. Jeong Highly effective electromagnetic interference shielding materials based on silver nanowire/cellulose papers. ACS Appl. Mater. Interfaces 8, 13123–13132 (2016). https://doi.org/10.1021/acsami.6b02218

[S44] J. Li, S. Qi, M. Zhang, Z. Wang Thermal conductivity and electromagnetic shielding effectiveness of composites based on Ag-plating carbon fiber and epoxy. J. Appl. Polym. Sci. 132, 42306 (2015). https://doi.org/10.1002/app.42306

[S45] N.M. Abbasi, H. Yu, L. Wang, Zain-ul-Abdin, W.A. Amer et al., Preparation of silver nanowires and their application in conducting polymer nanocomposites. Mater. Chem. Phys. 166, 1–15 (2015). https://doi.org/10.1016/j.matchemphys.2015.08.056