Supporting Information for

Trunk-Inspired SWCNT-Based Wrinkled Films for Highly-Stretchable Electromagnetic Interference Shielding and Wearable Thermotherapy

Xiaofeng Gong 1,†, Tianjiao Hu1,†, You Zhang1, Yanan Zeng3, Ye Zhang1, Zhenhua Jiang1, Yinlong Tan2,*, Yanhong Zou3, Jing Wang1, Jiayu Dai1,* and Zengyong Chu1,*

1 College of Science, National University of Defense Technology, Changsha 410073, P. R. China

2 Beijing Interdisciplinary Research Center, National University of Defense Technology, Changsha 410073, P. R. China

3School of Physics and Electronics, Hunan University, Changsha 410082, P. R. China

†Xiaofeng Gong  and Tianjiao Hu contributed equally to the work.

*Corresponding authors. E-mail: tanyinlong15@nudt.edu.cn (Yinlong Tan); jydai@nudt.edu.cn (Jiayu Dai); chuzy@nudt.edu.cn (Zengyong Chu)

Supplementary Tables and Figures

Table S1 Construction parameters of the films

| Fabrication Parameters | DSWCNT0.08 | DSWCNT0.12 |
| --- | --- | --- |
| d1 (cm) | 6.4 | 6.4 |
| d2 (cm) | 42.0 | 41.6 |
| d3 (cm) | 6.8 | 7.2 |
| d4 (cm) | 41.5 | 41.0 |
| d5 (cm) | 7.6 | 8.0 |
| l1 (cm) | 20.0 | 20.0 |
| l2 (cm) | 66.0 | 66.0 |
| l3 (cm) | 21.5 | 22.0 |
| l4 (cm) | 65.0 | 65.0 |
| l5 (cm) | 21.5 | 22.0 |

d1:circumference of the uninflated substrate,

d2: circumference of the substrate after the first inflation,

d3: circumference of the substrate after the first deflation,

d4: circumference of the substrate after the second inflation,

d5: circumference of the substrate after the second deflation,

l1:length of the uninflated substrate,

l2: length of the substrate after the first inflation,

l3: length of the substrate after the first deflation,

l4: length of the substrate after the second inflation,

l5: length of the substrate after the second deflation.

Table S2 Comparison of the mechanical properties of related works

| Composites | Breaking elongation (%) | Tensile strength(MPa) | Thickness(mm) | Refs. |
| --- | --- | --- | --- | --- |
| PU-AgNW/CFF fabric | 15 | 9.6 | 0.36 | [S1] |
| TaS2 film | 5 | 125 | 0.003 | [S2] |
| MFEA/AgNWs film | 280 | 3.7 | 5 | [S3] |
| PEDOT:PSS/Li-TFSI/XSB film | 200 | 10 | 0.2 | [S4] |
| EMA/ TPO/RGO film | 653 | 7.1 | 1 | [S5] |
| LM/PDMS composite mesh | 150 | 0.4 | 0.4 | [S6] |
| AMLM/Ecoflex | 600 | 0.3 | 0.2-0.78 | [S7] |
| LM/PDMS lattice | 180 | 2.6 | 13 | [S8] |
| DSWCNT/Latex film | 660 | 9 | 0.27 | This work |

Table S3 Comparison of EMI shielding performance of related works

| Composites | Preparation method | Thickness (mm) | EMI(dB) | Refs. |
| --- | --- | --- | --- | --- |
|  |  |  | Original | Stretched (tensile strain) |  |
| MFEA/AgNWs film | polycondensation | 5 | 53 | 36(30%) | [S3] |
| PEDOT:PSS/XSB film | evaporation | 0.2 | 40.9 | 30.9(100%) | [S4] |
| PDMS/LM composite mesh | cast molding and mechanical sintering | 0.4 | 35 | 42(60%) | [S6] |
| LM/PDMS lattice | 3D printing | 3 | 37 | 36(100%) | [S8] |
| MXene/TPU film | uniaxial prestretching | >0.3 | 31 | 29(50%) | [S9] |
| Steel wool/rubber film | cast molding | 5 | 38 | 35(80%) | [S10] |
| MXene/PDMS film | thermal annealing and spin-coating | - | 30 | 26(50%) | [S11] |
| Cu mesh/PDMS film | self-forming and electroplating | - | 40.4 | 26(30%) | [S12] |
| MXene organohydrogel | solvent displacement | 1 | 32.8 | 21(100%) | [S13] |
| AgNWs/PDMS film | pre-stretching and spray coating | 0.2 | 32.2 | 22.5(100%) | [S14] |
| CNT/TPU film | microwave sintering | 2 | 35.5 | 26.5(100%) | [S15] |
| DSWCNT/Latex film | 3D pre-stretching and coating | 0.3 | 38.4 | 52.7(200%) | This work |
|  |  |  | 36 | 20.1(200%) |  |

Fig. S1 SEM and EDS images of the films. (a) Optical image of DSWCNT@latex, (b) SEM image of the latex substrate surface, (c) TEM image of SWCNT, (d) TEM image of GO, (e, f) EDS images of GO, (g-i) EDS images of SWCNT, and (j-l) EDS images of DSWCNT0.12

Fig. S2 FTIR and Raman spectra of the films. (a) FTIR spectrum of GO film, (b) FTIR spectrum of SWCNT film, (c) FTIR spectrum of DSWCNT0.12 film, (d) Raman spectrum of GO film, (e) Raman spectrum of SWCNT film, and (f) Raman spectrum of DSWCNT0.12 film

Fig. S3 Wrinkling scales observed from SEM images. (a-c) SEM images of DSWCNT0.08 film, and (d-f) SEM images of DSWCNT0.12 film

Fig. S4 Mechancial performance of the tape stripping test. (a) Illustration of the tape stripping test, (b) tensile force of the tape stripping test, (c) optical image of the tape stripping test, (d) SEM image of DSWCNT0.12 film, (e) cross-sectional SEM image of DSWCNT0.12 film, and (f) cross-sectional illustration of the interlocking structure

Fig. S5 Resistivity of the films. (a) Average resistivity of DSWCNT0.08 and DSWCNT0.12 films, and (b) assembly diagram of strain sensor

Fig. S6 EMI shielding measurement illustration of the anisotropic films. (a) A vector network analyzer, (b) the mapping of TE10 transverse wave in the waveguide, (c) the stretching direction is parallel to the polarization direction of the electric field, including A//E and C//E, and (d) the stretching direction is perpendicular to the polarization direction of the electric field, including A⊥E and C⊥E

Fig. S7 SET of the stretched DSWCNT0.08 film. (a) SET of the stretched DSWCNT0.08 film when A//E, (b) SET of the stretched DSWCNT0.08 film when C//E, (c) SET of the stretched DSWCNT0.08 film when A⊥E, and (d) SET of the stretched DSWCNT0.08 film when C⊥E

Fig. S8 SET of DSWCNT0.08 film at different strains. (a) SET of DSWCNT0.08 film when the axial and circumferential drawing direction is parallel to the electric field direction, and (b) SET of DSWCNT0.08 film when the axial and circumferential drawing direction is perpendicular to the electric field direction

Fig. S9 Comparison of SET of the films without stretching (at 0% strain)

Fig. S10 Cycling stability of DSWCNT0.12 film. (a) Comparison of SET of DSWCNT0.12 film before and after 10000 stretching cycles(A//E), (b) comparation of SET of DSWCNT0.12 film before and after punching(A//E), and (c) comparation of SET of DSWCNT0.12 film before and after vacuum impregnating with methyl silicone oil (A//E)

Fig. S11 Deicing performance of DWSCNT0.12 film. Optical images of the deicing performance of DWSCNT0.12 film under 5V-heating at (a) 0 s and (b) 60 s

Fig. S12 Mechanical property of the punched DSWCNT0.08 film. (a) SEM images of the punched DSWCNT0.08 film, on which a slit could be observed, (b) stress-strain curve of the punched DSWCNT0.08 film, (c) ΔR/R0-ε curve of the punched DWSCNT0.08 film during axial stretching

Fig. S13 Water resistance performance of the films. The film could withstand 60min-soaking under ultrasonic treatment, and 3day-soaking without ultrasonic treatment

Fig. S14 Microstructure of DSWCNT0.12 film impregnated with methyl silicone oil. (a) Optical image of DSWCNT0.12 film impregnated with methyl silicone oil, (b) SEM image of DSWCNT0.12 film impregnated with methyl silicone oil, (c) elemental distribution of Si on the surface of DSWCNT0.12 film impregnated with methyl silicone oil, (d) ΔR/R0-ε curve of DWSCNT0.12 film during axial stretching impregnated with methyl silicone oil

Movie S1 Elephant trunk-inspired fabrication process

Movie S2 Demonstration of EMI shielding effectiveness

Movie S3 Recording Joule heating with an infrared camera

Movie S4 Air bubbling using the punched film

Movie S5 Rolling droplets on the film impregnated with methyl silicone oil

Supplementary References

- L.-C. Jia, L. Xu, F. Ren, P.-G. Ren, D.-X. Yan et al., Stretchable and durable conductive fabric for ultrahigh performance electromagnetic interference shielding. Carbon 144, 101–108 (2019). https://doi.org/10.1016/j.carbon.2018.12.034

- F. Deng, J. Wei, Y. Xu, Z. Lin, X. Lu et al., Regulating the electrical and mechanical properties of tas2 films via van der waals and electrostatic interaction for high performance electromagnetic interference shielding. Nano-Micro Lett. 15, (2023), https://doi.org/10.1007/s40820-023-01061-1

- Y. Bai, B. Y. Zhang, G. Q. Fei, Z. L. Ma, Composite polymeric film for stretchable, self-healing, recyclable EMI shielding and Joule heating. Chem. Eng. J. 478, 147382 (2023). https://doi.org/10.1016/j.cej.2023.147382

- X. Jiang, J. W. Zhou, X. K. Zhong, Z. P. Hu, R. Hu et al., Stretchable PEDOT:PSS/Li-TFSI/XSB composite films for electromagnetic interference shielding. ACS Appl. Mater. Interfaces 15, 8521-8529 (2023), https://doi.org/10.1021/acsami.2c21604

- A. Katheria, P. Das, S. K. Ghosh, J. Nayak, K. Nath et al., Fabrication of 2D nanomaterial reinforced co-continuous binary blend composites for thermal management and EMI shielding applications. J. Polym. Res. 30, (2023). https://doi.org/10.1007/s10965-023-03843-y

- Z. F. Xu, J. L. Chen, G. Q. Wang, Y. Q. Zhao, B. Shen et al., Stretchable and translucent liquid-metal composite mesh for multifunctional electromagnetic shielding/sensing and Joule heating. Compos. Sci. Technol. 249, 110512 (2024). https://doi.org/10.1016/j.compscitech.2024.110512

- R. Zhu, Z. Li, G. Deng, Y. Yu, J. Shui et al., Anisotropic magnetic liquid metal film for wearable wireless electromagnetic sensing and smart electromagnetic interference shielding. Nano Energy 92, 106700 (2022). https://doi.org/10.1016/j.nanoen.2021.106700

- Z. Wang, X. Xia, M. Zhu, X. Zhang, R. Liu et al., Rational assembly of liquid metal/elastomer lattice conductors for high-performance and strain-invariant stretchable electronics. Adv. Funct. Mater. 32, 2108336 (2022). https://doi.org/10.1002/adfm.202108336

- J. Dong, S. Luo, S. Ning, G. Yang, D. Pan et al., MXene-coated wrinkled fabrics for stretchable and multifunctional electromagnetic interference shielding and electro/photo-thermal conversion applications. ACS Appl. Mater. Interfaces 13, 60478–60488 (2021). https://doi.org/10.1021/acsami.1c19890

- X. Hu, L. Mou, Z. Liu, Stretchable electromagnetic interference shielding and antenna for wireless strain sensing by anisotropic micron-steel-wire based conductive elastomers. Chin. Phys. B 30, 018401 (2021). https://doi.org/10.1088/1674-1056/abc2b3

- W. Chen, L.-X. Liu, H.-B. Zhang, Z.-Z. Yu Kirigami-inspired highly stretchable, conductive, and hierarchical Ti3C2Tx MXene films for efficient electromagnetic interference shielding and pressure sensing. ACS Nano 15, 7668–7681 (2021). https://doi.org/10.1021/acsnano.1c01277

- Z. B. Chen, S. D. Yang, J. H. Huang, Y. F. Gu, W. B. Huang et al., Flexible, transparent and conductive metal mesh films with ultra-high FOM for stretchable heating and electromagnetic interference shielding. Nano-Micro Lett. 16, (2024). https://doi.org/10.1007/s40820-023-01295-z

- Y. Yu, P. Yi, W. Xu, X. Sun, G. Deng et al., Environmentally tough and stretchable MXene organohydrogel with exceptionally enhanced electromagnetic interference shielding performances. Nano-Micro Lett. 14, 77 (2022). https://doi.org/10.1007/s40820-022-00819-3

- Y. Feng, J. Song, G. Han, B. Zhou, C. Liu et al., Transparent and stretchable electromagnetic interference shielding film with fence-like aligned silver nanowire conductive network. Small Meth. 7, 2201490 (2023). https://doi.org/10.1002/smtd.202201490

- D. Feng, D. Xu, Q. Wang, P. Liu, Highly stretchable electromagnetic interference (EMI) shielding segregated polyurethane/carbon nanotube composites fabricated by microwave selective sintering. J. Mater. chem. C 7, 7938-7946 (2019). https://doi.org/10.1039/c9tc02311a