Supporting Information for

MOFs Derived Strategy and Ternary Alloys Regulation in Flower-Like Magnetic-Carbon Microspheres with Broadband Electromagnetic Wave Absorption

Mengqiu Huang1,, Bangxin Li2,, Yuetong Qian3,, Lei Wang4, Huibin Zhang3, Chendi Yang1, Longjun Rao1, Gang Zhou1, Chongyun Liang2,* and Renchao Che1,5,6,*

1Laboratory of Advanced Materials, Shanghai Key Lab of Molecular Catalysis and Innovative Materials, Academy for Engineering & Technology, Fudan University, Shanghai 200438, P. R. China

2Department of Chemistry, Fudan University, Shanghai 200438, P. R. China

3Materials Genome Institute, Shanghai University, Shanghai 200444, P. R. China

4School of Materials Science and Engineering, Shanghai Institute of Technology, Shanghai 201418, P. R. China

5College of Physics, Donghua University, Shanghai 201620, P. R. China

6Zhejiang Laboratory, Hangzhou 311100, P. R. China

Mengqiu Huang, Bangxin Li, and Yuetong Qian contributed equally to this work.

*Corresponding authors. E-mail: cyliang@fudan.edu.cn (Chongyun Liang); rcche@fudan.edu.cn (Renchao Che)

Supplementary Figures

Fig. S1 XRD patterns of a CoNiZn-MOF, CoNiFe-MOF, CoNiCu-MOF precursors and b CoNiZn@C, CoNiFe@C, CoNiCu@C composites

Fig. S2 SEM images and EDX mapping of a-c CoNiCu@C, d-f CoNiFe@C, and g-i CoNiZn@C

Fig. S3 High resolution XPS spectra of a Co 2p, b Ni 2p, c Mn 2p, d Zn 2p, e Fe 2p and f Cu 2p for CoNiM@C microsphere

Fig. S4 Real and imaginary part of permeability of CoNi@C and CoNiFe@C

Fig. S5 Room-temperature hysteresis loops of CoNi@C and CoNiFe@C

Fig. S6 3D reflection loss mapping of a CoNi@C and b CoNiFe@C

Fig. S7 Effective absorption bandwidth of CoNi@C and CoNiFe@C

Fig. S8 Cole-Cole semicircular of CoNiM@C microspheres

Fig. S9 The magnetic loss tangent value of CoNiM composites

Fig. S10 The eddy current loss coefficient C0 value of CoNiM composites

Fig. S11 The simulated magnetic moments in smooth microspheres

Fig. S12 The simulated magnetic moments in sheets

Fig. S13 The simulated magnetic moments in flower-like microspheres

Supplementary Table

Table S1 The electromagnetic wave absorption performance comparison of CoNi-based composites

| Sample | Filler loading (wt %) | Thickness (mm) | EAB (GHz) | Refs. |
| --- | --- | --- | --- | --- |
| CoNi microspheres | 60 | 1 | 2.96 | [S1] |
| CoNi chains | 60 | 5.4 | 3.5 | [S2] |
| CoNi Nanoparticles | 65 | 1.4 | 4.4 | [S3] |
| CoNi@NC hollow microspheres | 30 | 3.08 | 4.5 | [S4] |
| CoNiMPC @CNT/MXene | 15 | 2.7 | 5.0 | [S5] |
| CoNi@graphite carbon@carbon | 70 | 2.0 | 5.51 | [S6] |
| CoNi/C hybrids | 20 | 2.1 | 5.7 | [S7] |
| CoxNiy@C nanocomposites | 20 | 1.8 | 5.7 | [S8] |
| CoNi@NC/rGO-600 | 25 | 2.5 | 6.7 | [S9] |
| CoNi microflowers | 16.7 | 2 | 6.8 | [S10] |
| CoNiMn@C flower | 40 | 2 | 5.8 | This work |

EAB: Efficient absorption bandwidth

Supplementary References

- Z. Wang, W. Yang, Q. Lv, S. Liu, Z. Fang, Ferromagnetic and excellent microwave absorbing properties of CoNi microspheres and heterogeneous Co/Ni nanocrystallines. RSC Adv. 9(24), 13365-13371 (2019). https://doi.org/ 10.1039/C9RA02013F

- M. Qiao, J. Li, S. Li, D. Wei, X. Lei, Hierarchical CoNi alloys toward microwave absorption application: Chain-like versus particle-like. J. Alloy Compd. 926, 166854 (2022). https://doi.org/10.1016/j.jallcom.2022.166854

- J. Park, D. Ahn, J. Ro, S. Suh, CoNi Nanoparticles with different compositions using a polyol method for a microwave absorber in high-frequency bands. Met. Mater. Int. 29(5), 1542-1554 (2023). https://doi.org/10.1007/s12540-022-01298-2

- W. Min, D.Xu, P. Chen, G. Chen, Q. Yu et al., Synthesis of novel hierarchical CoNi@NC hollow microspheres with enhanced microwave absorption performance. J. Mater. Sci-Mater El. 32, 8000-8016 (2021). https://doi.org/10.1007/s10854-021-05523-3

- T. Wu, F. Ren, Z. Guo, J. Zhang, X. Hou et al., Bayberry-like bimetallic CoNi-MOF-74 derivatives/MXene hybrids with abundant heterointerfaces toward high-efficiency electromagnetic wave absorption. J. Alloy. Compd. 976, 172984 (2024). https://doi.org/10.1016/j.jallcom.2023.172984

- X. Wu, W. Ma, J. Xu, P. He, Y. Du, et al., Hierarchical Multi-Core–Shell CoNi@Graphite Carbon@Carbon Nanoboxes for Highly Efficient Broadband Microwave Absorption. ACS Appl. Nano Mater. 5(5), 7300-7311 (2022). https://doi.org/10.1021/acsanm.2c01215

- J. Ge, Y. Cui, J. Qian, L. Liu, F. Meng et al., Morphology-controlled CoNi/C hybrids with bifunctions of efficient anti-corrosion and microwave absorption. J. Mater. Sci. Technol. 102, 24-35 (2022). https://doi.org/10.1016/j.jmst.2021.07.003

- X. Liang, Z. Man, B. Quan, J. Zheng, W. Gu et al., Environment-stable CoxNiy encapsulation in stacked porous carbon nanosheets for enhanced microwave absorption. Nano-Micro Lett. 12, 102 (2020). https://doi.org/10.1007/s40820-020-00432-2

- X. Xu, F. Ran, Z. Fan, Z. Cheng, T. Lv et al., Bimetallic metal-organic framework-derived pomegranate-like nanoclusters coupled with CoNi-doped graphene for strong wideband microwave absorption. ACS Appl. Mater. Interfaces 12(15), 17870-17880 (2020). https://doi.org/10.1021/acsami.0c01572

- Q. Liu, Qi Cao, X. Zhao, H. Bi, C. Wang, Insights into size-dominant magnetic microwave absorption properties of CoNi microflowers via off-axis electron holography. ACS Appl. Mater. Interfaces 7(7), 4233-4240 (2015) https://doi.org/10.1021/am508527s