Supporting Information for

Interpenetrated Structures for Enhancing Ion Diffusion Kinetics in Electrochemical Energy Storage Devices

Xinzhe Xue1, Longsheng Feng2, Qiu Ren1, Cassidy Tran1, Samuel Eisenberg1, Anica Pinongcos1, Logan Valdovinos1, Cathleen Hsieh1, Tae Wook Heo2, Marcus A. Worsley2, *, Cheng Zhu2, *, Yat Li1, *

1Department of Chemistry and Biochemistry, University of California, 1156 High Street, Santa Cruz, California 95064, United States of America

2Lawrence Livermore National Laboratory, 7000 East Avenue, Livermore, California 94550, United States of America

*Corresponding authors. E-mail: worsley1@llnl.gov (Marcus A. Worsley); zhu6@llnl.gov (Cheng Zhu); yatli@ucsc.edu (Yat Li)

Supplementary Figures

Fig. S1 GCD curves of 3 mm interpenetrated Zn//MnO2 devices obtained at 0.2 mA cm-2 in electrolytes with and without MnSO4

Fig. S2 SEM images of a a 3D-printed interpenetrated polymer substrate, and magnified images of b the bare substrate and after c Ni electroless plating, d Ni electro-plating, e Zn electro-plating, f electrodeposition of MnO2/PEDOT surface. Scale bars in b-f are 10 μm

Fig. S3 XRD patterns of an interpenetrated polymer substrate after Ni electroless (blue) and electro-plating (red). Dashed lines highlight the peak position of Ni (111) and (200). The arrow highlights the peak position of Ni2P

Fig. S4 EDS elemental analysis of a MnO2/PEDOT cathode and b Zn anode

Table S1 Structural data of interpenetrated devices with different feature sizes

| m value / mm | Number of unit cells | Geometric Area / cm2 | Unit Density / cm-2 | Average Inter-electrode Distance / μm | Volume / cm3 | Normalized Volume Ratio / % |
| --- | --- | --- | --- | --- | --- | --- |
| 8 | 4 | 2.56 | 1.56 | 1380 | 2.048 | 100 |
| 4 | 12 | 1.92 | 6.25 | 742.38 | 0.768 | 37.5 |
| 3 | 15 | 1.8 | 8.33 | 557.16 | 0.54 | 26.4 |

Fig. S5 a Electrochemical impedance spectra of Zn//MnO2 devices with different feature sizes, and b Magnified view of the spectra in the high-frequency region

Fig. S6 a Schematic illustration and optical images of the separate electrodes b before and c after the deposition of Zn and MnO2/PEDOT

Fig. S7 CV scans of both separate and interpenetrated devices collected at 1 mV s-1

Fig. S8 Normalized a charging and b discharging profiles of interpenetrated and separate device configurations via charging and discharging capacity collected at 0.2 mA cm-2

Fig. S9 a Cycling stability and b time of a 3 mm device obtained at 0.2 mA cm-2. c EIS spectra collected from the device before and after cycling test

Fig. S10 a EIS spectra of Zn//MnO2 devices with separate and interpenetrated configurations. Fitted data for b charge transfer controlled high frequency region, and c mass transfer controlled low frequency zones. The inset Figures are fitting equivalent circuits for lower and higher frequencies. The inset tables are b solid-state charge transfer controlled Rct, Rd, and c mass transfer-controlled ion diffusion resistance Rd

Fig. S11 Digital images showing the electrolyte under a 20 °C and b 0 °C. The electrolyte is composed of 2 M ZnSO4, 0.1 M MnSO4 in H2O/DMSO (v : v = 5 : 1)

Fig. S12 Representative Zn stripping/plating overpotentials of the interpenetrated and separate devices under a 20 °C and b 0 °C are selected for comparison

Table S2 Performance comparisons between 2D and 3D Zn//MnO2 battery devices

| Device Configurations | Electrolyte | Capacity / mAh cm-2 | Device Area / cm2 | Device thickness / cm | Device Volume / cm3 | References |
| --- | --- | --- | --- | --- | --- | --- |
| Zn//3D MnO2@nickel nanocone array | 2 M ZnSO4 + 0.2 M MnSO4 aq. | 3.959 | 0.48 | 7.4×10-3 | 3.55×10-3 | [S1] |
| Interdigitated 3D Zn//MnO2 battery | 2 M ZnSO4 + 0.1 M MnSO4 in PVA gel | 0.215 | 1 | 5×10-3 | 5×10-3 | [S2] |
| Quasi-solid-state 2D Zn//MnO2 battery | 3 M LiCl + 2 M ZnCl2 + 0.4 M MnSO4 in PVA gel | 2.2 | 0.5 | 0.08 | 0.04 | [S3] |
| 2D Zn//δ-MnO2 | 2 M ZnSO4 + 0.1 M MnSO4 in PAM gel | 0.58 | - | - | - | [S4] |
| 2D Zn//MnO2@CNT | 3 M LiCl + 2 M ZnCl2 + 0.4 M MnSO4 in PVA gel | 1.4 | 1 | 0.08 | 0.08 | [S5] |
| Interpenetrated Zn//MnO2 battery | 2 M ZnSO4 + 0.1 M MnSO4 aq. | 1.71 | 1.8 | 0.3 | 0.54 | This work |

Supplementary References

- W. Lai, Y. Wang, Z. Lei, R. Wang, Z. Lin, C.-P. Wong, F. Kang, C. Yang. High performance, environmentally benign and integratable Zn//MnO2 microbatteries. Journal of Materials Chemistry A 6(9), 3933-3940 (2018). https://doi.org/10.1039/C7TA10936A

- H. Wang, R. Guo, H. Li, J. Wang, C. Du, X. Wang, Z. Zheng. 2d metal patterns transformed from 3d printed stamps for flexible Zn//MnO2 in-plane micro-batteries. Chemical Engineering Journal 429(132196 (2022). https://doi.org/https://doi.org/10.1016/j.cej.2021.132196

- Y. Zeng, X. Zhang, Y. Meng, M. Yu, J. Yi, Y. Wu, X. Lu, Y. Tong. Achieving ultrahigh energy density and long durability in a flexible rechargeable quasi-solid-state Zn–MnO2 battery. Advanced Materials 29(26), 1700274 (2017). https://doi.org/https://doi.org/10.1002/adma.201700274

- D. Wang, L. Wang, G. Liang, H. Li, Z. Liu, Z. Tang, J. Liang, C. Zhi. A superior δ-MnO2 cathode and a self-healing Zn-δ-MnO2 battery. ACS Nano 13(9), 10643-10652 (2019). https://doi.org/10.1021/acsnano.9b04916

- X. Zhang, S. Wu, S. Deng, W. Wu, Y. Zeng, X. Xia, G. Pan, Y. Tong, X. Lu. 3d cnts networks enable MnO2 cathodes with high capacity and superior rate capability for flexible rechargeable Zn–MnO2 batteries. Small Methods 3(12), 1900525 (2019). https://doi.org/https://doi.org/10.1002/smtd.201900525