# Supporting Information for

Enhancing Defect-Induced Dipole Polarization Strategy of SiC@MoO3 Nanocomposite Towards Electromagnetic Wave Absorption

Ting Wang1, Wenxin Zhao2, Yukun Miao2, Anguo Cui3, Chuanhui Gao1, Chang Wang2, Liying Yuan2, Zhongning Tian2, Alan Meng4, Zhenjiang Li2, *, Meng Zhang2, *

1 College of Chemical Engineering, Qingdao University of Science and Technology, Qingdao, Shandong province, 266042, P. R. China

2 College of Materials Science and Engineering, Qingdao University of Science and Technology, Qingdao, Shandong province, 266042, P. R. China

3 Shandong Engineering Laboratory for Preparation and Application of High-Performance Carbon-Materials, College of Electromechanical Engineering, Qingdao University of Science and Technology, Qingdao 266061, P. R. China

4 Key Laboratory of Optic-electric Sensing and Analytical Chemistry for Life Science, MOE, Shandong Key Laboratory of Biochemical Analysis, College of Chemistry and Molecular Engineering, Qingdao University of Science and Technology, Qingdao, Shandong province, 266042, P. R. China

*Corresponding authors. E-mail: mengzhang@qust.edu.cn (Meng Zhang); zjli126@126.com (Zhenjiang Li)

Supplementary Figures and Table

Fig. S1 a~c SEM images of SiCNWS

Fig. S2 EDX spectrum of SiC@MoO3 nanocomposite

(a)

(b)

(c)

Fig. S3 a XPS spectra full spectrum, b C1s and c Si 2p spectra of SiC@MoO3, SiC@MO-t2, SiC@MO-t4, SiC@MO-t6 and SiC@MO-t8

Fig. S4 Two-dimensional graph of a SiC@MoO3, b SiC@MO-t2, c SiC@MO-t4, d SiC@MO-t6 and e SiC@MO-t8

Fig. S5 Three-dimensional graph of a SiC@MoO3, b SiC@MO-t2, c SiC@MO-t4, d SiC@MO-t6 and e SiC@MO-t8

(a)

(b)

(c)

(d)

(e)

Fig. S6 Absorption curves and corresponding 1/4 λ matching properties of a SiC@MoO3 nanocomposite and b SiC@MO-t2, c SiC@MO-t4, d SiC@MO-t6 and e SiC@MO-t8

Fig. S7 EAB and RLmin values of different samples under different matching thicknesses a SiC@MoO3 nanocomposite, b SiC@MO-t2, c SiC@MO-t4, d SiC@MO-t6 and e SiC@MO-t8

Fig. S8 a Magnetic permeability real and b magnetic permeability imaginary part of SiC@MoO3, SiC@MO-t2, SiC@MO-t4, SiC@MO-t6 and SiC@MO-t8

Fig. S9 a Polarization Loss and b Conduction Loss values of SiC@MoO3, SiC@MO-t2, SiC@MO-t4, SiC@MO-t6 and SiC@MO-t8

Fig. S10 Conductivity values of SiC@MoO3, SiC@MO-t2, SiC@MO-t4, SiC@MO-t6 and SiC@MO-t8

Fig. S11 Cole-Cole curve of SiC@MoO3 nanocomposites

Table R1 Comparison of RLmin and EAB values of the SiC@MO-t4 and SiC@MO-t6 samples with recent reports related absorbers

| Samples | EAB (GHz) | Matching thickness (mm) | RLmin (dB) | Matching thickness (mm) | References |
| --- | --- | --- | --- | --- | --- |
| o-MoO3/PPy | 6.40 | 2.30 | -31.80 | 2.30 | [45] |
| MoO3/TiO2/Mo2TiC2Tx | 8.60 | 1.80 | -30.76 | 2.30 | [46] |
| graphene/g-C3N4 | 4.60 | 4.50 | -34.69 | 4.50 | [47] |
| SnO/SnO2 | 4.3 | 1.40 | -37.60 | 1.40 | [48] |
| Fe3O4/Fe3S4 | 4.39 | 1.46 | −45.33 | 3.30 | [49] |
| Fe3O4@SiO2@MnO2 | 5.1 | 2.60 | -50.20 | 2.60 | [50] |
| Fe3O4@MnO2@Ni–Co/C | 7.1 | 2.00 | -41.2 | 4.00 | [51] |
| ZnFe2O4@MnO2@MXene | 4.7 | 1.40 | -50.4 | 1.40 | [52] |
| SiC@MO-t4 | 4.64 | 1.42 | -50.49 | 1.27 | This work |
| SiC@MO-t6 | 8.72 | 2.81 | -49.83 | 2.68 | This work |