Supporting Information for

Enhancing the Electrocatalytic Oxidation of 5-Hydroxymethylfurfural through Cascade Structure Tuning for Highly Stable Biomass Upgrading

Xiaoli Jiang1, Xianhui Ma2, Yuanteng Yang1, Yang Liu1, Yanxia Liu1, Lin Zhao1, Penglei Wang1, Yagang Zhang1,*, Yue Lin2,*, Yen Wei3,4,*

1 School of Materials and Energy, University of Electronic Science and Technology of China, Chengdu 611731, P. R. China

2 Hefei National Research Center for Physical Sciences at the Microscale, University of Science and Technology of China, Hefei 230026, P. R. China

3 The Key Laboratory of Bioorganic Phosphorus Chemistry & Chemical Biology (Ministry of Education), Department of Chemistry, Tsinghua University, Beijing 100084, P. R. China

4 School of Materials Science and Engineering, North Minzu University, Yinchuan 750021, P. R. China

*Corresponding authors. E-mail: ygzhang@uestc.edu.cn (Yagang Zhang);   linyue@ustc.edu.cn (Yue Lin); weiyen@tsinghua.edu.cn (Yen Wei)

Supplementary Figures and Tables

Fig. S1 SEM images of (a-c) Co3O4 and (d-f) NiCo2O4 at different magnifications

Fig. S2 SEM images of (a-c) Pd-NiCo2O4-1 and (d-f) Pd-NiCo2O4-3 at different magnifications

Fig. S3 TEM-EDS of Pd-NiCo2O4

Fig. S4 XRD pattern of (a) Co3O4 and (b) NiCo2O4 and Pd- NiCo2O4 with different Pd loading

Fig. S5 (a) XPS Survey spectra of Co3O4, NiCo2O4, Pd-NiCo2O4. (b) High-resolution XPS spectra of Pd 3d

Fig. S6 Ni3+/Ni2+ ratios obtained from XPS spectra of NiCo2O4 and Pd-NiCo2O4

Fig. S7 Ni K-edge XANES spectra of NiCo2O4, Pd-NiCo2O4

Fig. S8 LSV curves of NiCo2O4 with various Pd loading in 1 M KOH with 50 mM HMF

Fig. S9 LSV curves of NiCo2O4 and NiCo2O4 with various Pd loading in 1 M KOH with 100 mM HMF

Fig. S10 LSV curves of Pd-NiCo2O4 and Pd-Co3O4 in 1 M KOH with 50 mM HMF

Fig. S11 (a) LSV curves of Pd-NiCo2O4 in 1.0 M KOH with and without 100 mM HMF. (b) LSV curves of different samples in 1.0 M KOH with 100 mM HMF, and (c) corresponding overpotential at various current densities for HMFOR

Fig. S12 Electrochemical behavior of (a) furfuryl alcohol (R-OH) and (b) furfural (R-CHO) oxidation on Pd-NiCo2O4 and NiCo2O4 electrodes.

Fig. S13 Nyquist plots of Co3O4, NiCo2O4, and Pd-NiCo2O4

Fig. S14 Cyclic voltammograms (CVs) curves of (a) Co3O4, (b) NiCo2O4, (c) Pd-NiCo2O4 and (d) Pd/NF at different scan rates increasing from 20 to 120 mV s–1 with an interval point of 20 mV s–1

Fig. S15 ECSA-normalized LSV curves of samples in 1 M KOH with 50 mM HMF

Fig. S16 (a) HER LSV curves of samples and (b) stability (I-t) test at –150 mA cm–2

Fig. S17 HPLC standard curve measurements of pure (a, b) HMF, (c, d) HMFCA, (e, f) FFCA, (g, h) FDCA

Fig. S18 (a) HPLC curve measurements (b) the FDCA selectivity and Faradaic efficiency at different potentials for Pd-NiCo2O4

Fig. S19 HMF conversion, FDCA yield and Faradaic efficiency for different samples

Fig. S20 (a-c) SEM images (d) TEM, (e, f) HAADF-STEM images and (g) STEM-mapping of Pd-NiCo2O4 after HMFOR

Fig. S21 XPS Survey spectrum of Pd-NiCo2O4 after HMFOR

Fig. S22 High-resolution (a) Pd 3d, (b) Co 2p, (c) Ni 2p, (d) O 1s XPS spectra of Pd-NiCo2O4 after HMFOR

Fig. S23 CV curves of Co3O4, NiCo2O4, and Pd-NiCo2O4 in 1 M KOH with 50 mM HMF

Fig. S24 CV curves of Pd-NiCo2O4 in 1 M KOH with and without 50 mM HMF

Fig. S25 LSV curves of Pd-NiCo2O4 in 1 M KOH with different HMF concentration

Fig. S26 Schematic representation of the direct oxidation of HMF

Fig. S27 In situ ATR-FTIR spectra over Pd-NiCo2O4 and NiCo2O4 samples

Fig. S28 Multipotential-step curves of and (a) Co2O4 and (b) NiCo2O4 in 1 M KOH solution with and without 50 mM HMF addition

Fig. S29 Charge density difference for Pd-NiCo2O4

Fig. S30 PDOS of NiCo2O4

Fig. S31 Optimized stable adsorption configures (top review) for HMF and HMFCA on Pd-NiCo2O4

Fig. S32 FDCA yield and Faradaic efficiency of Pd-NiCo2O4 in coupled two-electrode cell at different voltages

Fig. S33 Long-term test of Pd-NiCo2O4 in two-electrode cell

Table S1 ICP results of Co, Ni and Pd elements in Pd-NiCo2O4

| Element | Wt% | At% |
| --- | --- | --- |
| Co | 19.54 | 0.33 |
| Ni | 32.94 | 0.56 |
| Pd | 10.80 | 0.10 |

Table S2 XPS results of Pd-NiCo2O4

| Name | Atomic% |  | PP Hgt (N) | PP At% |
| --- | --- | --- | --- | --- |
| C 1s | 35.23 |  | 31.88 | 40.52 |
| Co 2p | 2.9 |  | 0.56 | 0.71 |
| Ni 2p | 18.67 |  | 5.44 | 6.91 |
| O 1s | 42.7 |  | 40.65 | 51.67 |
| Pd 3d | 0.5 |  | 0.15 | 0.19 |

Table S3 XPS fitting results of samples

| Catalyst | Binding energy (eV) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Co2+ |  | Co3+ |  | Ni2+ |  | Ni3+ |  |
| Co3O4 | 796.38 | 781.46 | 794.80 | 779.83 | / | / | / | / |
| NiCo2O4 | 796.45 | 781.64 | 794.67 | 779.76 | 872.54 | 854.62 | 874.59 | 856.41 |
| Pd-NiCo2O4 | 797.28 | 781.29 | 792.73 | 775.42 | 873.32 | 855.64 | 874.92 | 857.09 |

Table S4 Comparison of the HMFOR performance between Pd-NiCo2O4 and recently reported advanced catalysts

| Catalysts | CHMF (mM) | Potential (V vs. RHE) | Current density (mA cm-2) | Faradaic efficiency (FE, %) | References |
| --- | --- | --- | --- | --- | --- |
| NiFe-1 | 50 | 1.5 | 630 | 92 | [S1] |
| CoOOH/CF | 50 | 1.5 | 420 | 99 | [S2] |
| CuCo2O4 | 50 | 1.5 | 225 | 94 | [S3] |
| Pd/NiCo | 50 | 1.5 | 81 | 95.9 | [S4] |
| Pt/Ni(OH)2 | 50 | 1.6 | 38 | 98.7 | [S5] |
| NiFeLDH/CPF | 10 | 1.45 | 20 | 99.4 | [S6] |
| Co0.4NiS@NF | 50 | 1.45 | 497 | 99.1 | [S7] |
| NF@Co3O4/CeO2 | 50 | 1.4 | 32 | 97.5 | [S8] |
| NiSx/β-Ni(OH)2/Ni | 50 | 1.38 1.4 | 120 392 | 98.3 | [S9] |
| Pd-NiCo2O4 | 50 | 1.44 1.5 | 596 800 | 99.6 | This work |

Table S5 Comparison of catalytic performance of the state-of-the-art catalysts reported in literatures and the catalyst in this work

| Catalysts | HMFOR//HER |  |  | HMFOR performance |  | References |
| --- | --- | --- | --- | --- | --- | --- |
|  | Ej10 (V) | Ej50 (V) | jF.E. | Ej100 (V) | F.E. (%) |  |
| MoO2-FeP@C | 1.49 | 1.6 | 20 | 1.42 | 97.8 | [S10] |
| E-CoAl-LDH-NSA | 1.5 | 1.74 | - | 1.59 | 99.4 | [S11] |
| NF@Mo-Ni0.85Se | 1.4 | 1.5 | - | 1.46 | 95 | [S12] |
| CuxS@NiCo-LDH | 1.34 | 1.49 | - | 1.36 | 99 | [S13] |
| NiSe/NiOx | 1.56 | 1.65 | - | 1.35 | 99 | [S14] |
| NiCu NTs | 1.3 | 1.47 | - | 1.38 | 96.4 | [S15] |
| NiCo2@MoO2/NF | 1.25 | 1.48 | - | 1.27 | 99.2 | [S16] |
| Rh-O5-Ni(Fe) | 1.32 | 1.42 | 40 | 1.39 | 98.5 | [S17] |
| Co9S8@Ni3S2/NF | 1.42 | 1.61 | - | 1.42 | 98.4 | [S18] |
| Pd-NiCo2O4 | 1.07 | 1.40 | 100 | 1.32 | 99.6 | This work |

Supplementary References

- C. Wang, Y. Wu, A. Bodach, M. L. Krebs, W. Schuhmann et al. A novel electrode for value-generating anode reactions in water electrolyzers at industrial current densities. Angew. Chem., Int. Ed. 62(7), e202215804 (2023). https://doi.org/https://doi.org/10.1002/anie.202215804

- R. Zhang, S. Jiang, Y. Rao, S. Chen, Q. Yue et al. Electrochemical biomass upgrading on CoOOH nanosheets in a hybrid water electrolyzer. Green Chem. 23(6), 2525-2530 (2021). https://doi.org/10.1039/D0GC04157B

- Y. Lu, C.-L. Dong, Y.-C. Huang, Y. Zou, Z. Liu et al. Identifying the geometric site dependence of spinel oxides for the electrooxidation of 5-hydroxymethylfurfural. Angew. Chem., Int. Ed. 59(43), 19215-19221 (2020). https://doi.org/https://doi.org/10.1002/anie.202007767

- G. Liu, T. Nie, Z. Song, X. Sun, T. Shen et al. Pd loaded nico hydroxides for biomass electrooxidation: Understanding the synergistic effect of proton deintercalation and adsorption kinetics. Angew. Chem., Int. Ed. 62(45), e202311696 (2023). https://doi.org/https://doi.org/10.1002/anie.202311696

- B. Zhou, Y. Li, Y. Zou, W. Chen, W. Zhou et al. Platinum modulates redox properties and 5-hydroxymethylfurfural adsorption kinetics of Ni(OH)2 for biomass upgrading. Angew. Chem., Int. Ed. 60(42), 22908-22914 (2021). https://doi.org/https://doi.org/10.1002/anie.202109211

- W.-J. Liu, L. Dang, Z. Xu, H.-Q. Yu, S. Jin et al. Electrochemical oxidation of 5-hydroxymethylfurfural with NiFe layered double hydroxide (LDH) nanosheet catalysts. ACS Cataly. 8(6), 5533-5541 (2018). https://doi.org/10.1021/acscatal.8b01017

- Y. Sun, J. Wang, Y. Qi, W. Li, C. Wang. Efficient electrooxidation of 5-hydroxymethylfurfural using Co-doped Ni3S2 catalyst: Promising for H2 production under industrial-level current density. Adv. Sci. 9(17), 2200957 (2022). https://doi.org/https://doi.org/10.1002/advs.202200957

- G. Zhao, G. Hai, P. Zhou, Z. Liu, Y. Zhang et al. Electrochemical oxidation of 5-hydroxymethylfurfural on CeO2-modified Co3O4 with regulated intermediate adsorption and promoted charge transfer. Adv. Funct. Mater. 33(14), 2213170 (2023). https://doi.org/https://doi.org/10.1002/adfm.202213170

- C. Liu, X.-R. Shi, K. Yue, P. Wang, K. Zhan et al. S-species-evoked high-valence Ni2+δ of the evolved β-Ni(OH)2 electrode for selective oxidation of 5-hydroxymethylfurfural. Adv. Mater. 35(12), 2211177 (2023). https://doi.org/https://doi.org/10.1002/adma.202211177

- G. Yang, Y. Jiao, H. Yan, Y. Xie, A. Wu et al. Interfacial engineering of MoO2-FeP heterojunction for highly efficient hydrogen evolution coupled with biomass electrooxidation. Adv. Mater. 32(17), 2000455 (2020). https://doi.org/https://doi.org/10.1002/adma.202000455

- Y. Song, Z. Li, K. Fan, Z. Ren, W. Xie et al. Ultrathin layered double hydroxides nanosheets array towards efficient electrooxidation of 5-hydroxymethylfurfural coupled with hydrogen generation. Appl. Catal., B. 299(120669 (2021). https://doi.org/https://doi.org/10.1016/j.apcatb.2021.120669

- C. Yang, C. Wang, L. Zhou, W. Duan, Y. Song et al. Refining d-band center in Ni0.85Se by Mo doping: A strategy for boosting hydrogen generation via coupling electrocatalytic oxidation 5-hydroxymethylfurfural. Chem. Eng. J. 422(130125 (2021). https://doi.org/https://doi.org/10.1016/j.cej.2021.130125

- X. Deng, X. Kang, M. Li, K. Xiang, C. Wang et al. Coupling efficient biomass upgrading with H2 production via bifunctional CuxS@NiCo-LDH core–shell nanoarray electrocatalysts. J. Mater. Chem. A 8(3), 1138-1146 (2020). https://doi.org/10.1039/C9TA06917H

- L. Gao, Z. Liu, J. Ma, L. Zhong, Z. Song et al. NiSe@NiOx core-shell nanowires as a non-precious electrocatalyst for upgrading 5-hydroxymethylfurfural into 2,5-furandicarboxylic acid. Appl. Catal., B. 261, 118235 (2020). https://doi.org/https://doi.org/10.1016/j.apcatb.2019.118235

- L. Zheng, Y. Zhao, P. Xu, Z. Lv, X. Shi et al. Biomass upgrading coupled with H2 production via a nonprecious and versatile cu-doped nickel nanotube electrocatalyst. J. Mater. Chem. A 10(18), 10181-10191 (2022). https://doi.org/10.1039/D2TA00579D

- J. Wu, J. Chen, T. Yu, Z. Zhai, Y. Zhu et al. Boosting electrochemical kinetics of NiCo2 via MoO2 modification for biomass upgrading assisted hydrogen evolution. ACS Catal. 13(20), 13257-13266 (2023). https://doi.org/10.1021/acscatal.3c03094

- L. Zeng, Y. Chen, M. Sun, Q. Huang, K. Sun et al. Cooperative Rh-O5/Ni(Fe) site for efficient biomass upgrading coupled with H2 production. J. Am. Chem. Soc. 145(32), 17577-17587 (2023). https://doi.org/10.1021/jacs.3c02570

- R. Zhang, F. Gao, C. Yang, Y. Bian, G. Wang et al. Boosting hydrogen evolution via anodic oxidation of 5-hydroxymethylfurfural in anion exchange membrane electrolyzer over a metallic heterostructure. Mater. Today Nano 23, 100373 (2023). https://doi.org/https://doi.org/10.1016/j.mtnano.2023.100373