Supporting Information for

“Zero-Strain” NiNb2O6 Fibers for All-Climate Lithium Storage

Yan Zhao1, 2, Qiang Yuan2, Liting Yang3, Guisheng Liang3, Yifeng Cheng4, Limin Wu5, *, Chunfu Lin1, 2, *, and Renchao Che1, 3, 4, *

1 College of Physics, Donghua University, Shanghai 201620, P. R. China

2 Institute of Materials for Energy and Environment, School of Materials Science and Engineering, Qingdao University, Qingdao 266071, P. R. China

3 Laboratory of Advanced Materials, Shanghai Key Lab of Molecular Catalysis and Innovative Materials, Academy for Engineering & Technology, Fudan University, Shanghai 200438, P. R. China

4 Zhejiang Laboratory, Hangzhou 311100, P. R. China

5 Inner Mongolia University, Hohhot 010021, P. R. China

*Corresponding authors. E-mail addresses: wlm@imu.edu.cn (Limin Wu); linchunfu@qdu.edu.cn (Chunfu Lin); rcche@fudan.edu.cn (Renchao Che)

Supplementary Figures and Tables

Fig. S1 Physical adsorption test of NiNb2O6 fibers: a) BET specific surface area plot. b) N2 adsorption−desorption isotherm. c) BJH pore-size distribution curve from desorption branch

Fig. S2 Electrochemical properties of NiNb2O6 at 0.1C and different temperatures. First three-cycle GCD profiles of NiNb2O6/Li half cells: a) 25, b) −10, and c) 60 °C. Reversible capacities of NiNb2O6/Li half cells: d) 25, e) −10, and f) 60 °C

Fig. S3 Nyquist plots of NiNb2O6/Li half cell after 0, 1, 10, 50, 100, 200, and 500 cycles at 25 °C

Fig. S4 Electrochemical properties of full cells. a) GCD profiles and b) cyclability of LiFePO4/NiNb2O6 full cell. c) GCD profiles and d) cyclability of LiFePO4/T-Nb2O5 full cell. e) GCD profiles and f) cyclability of LiFePO4/Li4Ti5O12 full cell

The T-Nb2O5 nanoparticles were synthesized through a hydrothermal method. 1.1 g of C10H5NbO20 (Macklin, 98%) was dissolved in 30 mL of deionized water. After stirring at 50 °C for 1 h, the solution was transferred to a 50 mL autoclave, which was then exposed to a 150 °C oven for 12 h for a hydrothermal reaction. The white product after the reaction was collected and washed with deionized water. The obtained paste was vacuum-dried at 80 °C for 10 h and calcined at 700 °C for 4 h in air.

Active materials (NiNb2O6 fibers, T-Nb2O5, and commercial Li4Ti5O12 (LTO-1, Shenzhen BTR)), conductive agent (Super-P carbon) or binder (polyvinylidene fluoride) in a mass ratio of 7.5:1.5:1 was mixed in 1-methyl-2-pyrrolidinone. The formed slurries were cast on Cu foils. These electrode films were placed in a vacuum oven and dried at 110 °C for 10 h, forming the working electrodes with loadings of ≈1.0 mg cm−2. Full cells were assembled into CR2032-type coin cells. LiFePO4 (P198, Shenzhen BTR) and active materials with an N/P ratio of 0.95 (cathode-limited configuration) were used as cathode and anode materials, respectively. The fabrication of the LiFePO4 cathodes was similar to that of the above anodes, except that LiFePO4, Super-P carbon, and polyvinylidene fluoride in a mass ratio of 8:1:1 was coated on Al foils.

Compared to the LiFePO4/T-Nb2O5 and LiFePO4/Li4Ti5O12 full cells, the LiFePO4/NiNb2O6 full cell exhibits better electrochemical properties. Especially, the reversible capacity of the LiFePO4/NiNb2O6 full cell (212 mAh g−1 at 1C) is 100 and 60 mAh g−1 larger than that of the LiFePO4/T-Nb2O5 and LiFePO4/Li4Ti5O12 full cells, respectively.

Fig. S5 Redox mechanism of NiNb2O6 fibers. Ex-situ Ni-2p XPS spectra: a) pristine, b) discharge (1.0 V), and c) charge (3.0 V) states. Ex-situ Nb-3d XPS spectra at pristine state: d) 25, e) −10, and f) 60 °C. Ex-situ Nb-3d XPS spectra at charge (3.0 V) states: g) 25, h) −10, and i) 60 °C

Fig. S6 Electrochemical kinetics of NiNb2O6 fibers. CV profiles of NiNb2O6/Li half cell at 0.2 mV s−1: a) 25, b) −10, and c) 60 °C. CV profiles of NiNb2O6/Li half cell at 0.4 mV s−1: d) 25, e) −10, and f) 60 °C. Capacitive contributions of NiNb2O6/Li half cell at different sweep rates: g) 25, h) −10, and i) 60 °C

Fig. S7 GITT tests of NiNb2O6 fibers. GITT curves (second cycle): a) 25, b) −10, and c) 60 °C. E versus t curves for a single step in GITT experiment: d) 25, e) −10, and f) 60 °C. Linear behavior of E versus τ0.5 relationship during a typical titration: g) 25, h) −10, and i) 60 °C

Calculations of apparent Li+ diffusion coefficients of NiNb2O6 fibers from GITT

The GITT tests are conducted on the NiNb2O6/Li cell to study the Li+ diffusivity in the NiNb2O6 fibers. Fig. S5a, Fig. S5b, and Fig. S5c respectively exhibit the typical GITT curves at 25, −10, and 60 °C during the first lithiation–delithiation cycle. For a clear observation, a single step of GITT is presented in Fig. S5d/Fig. S5e/Fig. S5f. Based on the Fick’s second law, the apparent Li+ diffusion coefficients (DLi) of the NiNb2O6 fibers can be calculated by using Eq. S1 [S1]:

DLi  GITT =4πmbVmMbS2ΔEsτdEτdτ2             τ≪L2DLi           (S1)

where, MB is the molar mass of NiNb2O6, Vm is the molar volume of NiNb2O6, mB is the mass of NiNb2O6, S is the NiNb2O6 electrode area, τ is the pulse duration time, L is the NiNb2O6 electrode thickness, and ΔEs and ΔEτ respectively represent the change in the equilibrium potential and the change in potential during the current pulse, which can be gained from the GITT curves (Fig. S5d/Fig. S5e/Fig. S5f). As the potential during a single titration delivers a linear relationship with τ0.5 (Fig. S5g/Fig. S5h/Fig. S5i), Eq. S1 can be simplified as Eq. S2:

DLi  GITT=4πτmbVmMbS2ΔEsΔEτ2τ≪L2DLi             (S2)

Based on Eq. S2, the apparent Li+ diffusion coefficients of the NiNb2O6 fibers during different states of discharge/charge at 25, −10, and 60 °C are obtained, and displayed in Fig. 3g-i, respectively.

Fig. S8 Relationship between peak current (Ip) and square root of sweep rate (v0.5) for intensive cathodic and anodic peaks of NiNb2O6/Li half cells: a) 25, b) −10, and c) 60 °C

Calculations of apparent Li+ diffusion coefficients of NiNb2O6 fibers by CV

The apparent Li+ diffusion coefficients of the NiNb2O6 fibers at 25, −10, and 60 °C are also determined from the CV data at different sweep rates (Fig. 3d, Fig. 3e, and Fig. 3f). It is found that the peak current of the intensive cathodic/anodic reaction Ip is in proportional to the square root of the sweep rate v0.5 (Fig. S6), which shows the linear semi-infinite diffusion in cathodic and anodic processes. Consequently, the Randles−Sevcik equation (Eq. S3) can be applied, based on which the Li+ diffusion coefficient DLi can be calculated [S2].

Ip = 2.69×105Sn1.5C(DLi  CVv)0.5                    (S3)

where, S is the electrode area, n is the charge transfer number, and C is the molar concentration of Li+ in solid. The obtained DLi values of NiNb2O6 fibers reach 2.3×10−13 cm2 s−1 (lithiation) and 3.0×10−13 cm2 s−1 (delithiation) at 25 °C, decrease to 1.0×10−13 cm2 s−1 (lithiation) and 1.1×10−13 cm2 s−1 (delithiation) at −10 °C, and increase to 4.2×10−13 cm2 s−1 (lithiation) and 7.3×10−13 cm2 s−1 (delithiation) at 60 °C, which match with the GITT results.

Fig. S9 In-situ XRD characterizations of NiNb2O6 fibers within 1.0−3.0 V (first cycle at 0.5C and 25 °C, at 0.1C and −10 °C, and at 0.5C and 60 °C). In-situ XRD patterns of NiNb2O6/Li half cell with discharge−charge curves: a) 25, b) −10, and c) 60 °C. 2D in-situ XRD patterns enlarged within 30.3−30.7°: d) 25, e) −10, and f) 60 °C. Variations in lattice parameters of NiNb2O6 during discharge−charge: g) 25, h) −10, and i) 60 °C. Solid and hollow symbols represent data for original phase and transformed phase, respectively

Fig. S10 Sudden movement of (311) peak after phase transformation from in-situ XRD patterns of NiNb2O6/Li half cell (first discharge): a) 25 and b) 60 °C

Fig. S11 In-situ XRD characterizations of NiNb2O6 fibers within 1.0−3.0 V (first four cycles at 0.5C and 25 °C, at 0.1C and −10 °C, and at 0.5C and 60 °C). 2D in-situ XRD patterns of NiNb2O6/Li half cell: a) 25, b) −10, and c) 60 °C. Variations in lattice constants of NiNb2O6: d) 25, e) −10, and f) 60 °C. PEEK: polyetheretherketone. Solid and hollow symbols represent data for original phase and transformed phase, respectively

Fig. S12 Rietveld-refined operando XRD patterns of NiNb2O6/Li operando cell at 1.0 V: a) 25 and b) 60 °C

Fig. S13 Ex-situ XRD pattern of NiNb2O6 electrode after 100 cycles

Fig. S14 “Zero-strain” mechanism of NiNb2O6 at −10 °C. Movement of ions from (a) initial stage to (b) partially lithiated stage, and finally to (c) final lithiated stage. Li, Ni, Nb, and O are colored by orange, grey, green, and red, respectively. Arrow lengths indicate movement distances

Fig. S15 “Zero-strain” mechanism of NiNb2O6 at 60 °C. Movement of ions from (a) initial stage to (b) partially lithiated stage, then to (c) phase-transformed stage, and finally to (d) final lithiated stage. Li, Ni, Nb, and O are colored by orange, grey, green, and red, respectively. Arrow lengths indicate movement distances.

Table S1 Comparisons of electrochemical properties of NiNb2O6 with previously-reported anode materials with intercalation characteristic

| Material | Rate capability | Cyclic stability | References |
| --- | --- | --- | --- |
| NiNb2O6 fibers | 164 mAh g−1 at 10C | capacity retention of 92.8% over 1000 cycles at 10C | this work |
| NiNb2O6 micron-sized particles | 126 mAh g−1 at 10C | capacity retention of 92.0% over 2500 cycles at 10C | [S3] |
| partially reduced TiNb24O62 nanofibers | 190 mAh g−1 at 10C | capacity retention of 86.4% over 500 cycles at 10C | [S4] |
| GaNb11O29 micron-sized particles | 121 mAh g−1 at 10C | capacity retention of 87.5% over 1000 cycles at 10C | [S5] |
| reduced MoxTi1−xNb2O7+y micron-sized particles | 192 mAh g−1 at 12C | capacity retention of 73.0% over 500 cycles at 12C | [S6] |
| 2D Nb2O5-C-rGO micron-sized sheets | ~165 mAh g−1 at 10C | capacity retention of 78.0% over 1500 cycles at 5C | [S7] |
| TiNb2O7 hierarchical microspheres | 100 mAh g−1 at 20C | capacity retention of 83.5% over 500 cycles at 10C | [S8] |
| Ti2Nb10O29 hollow nanofibers | 136 mAh g−1 at 20C | capacity retention of ~70% over 500 cycles at 10C | [S9] |
| TiNb2O7 nanoparticles | 87 mAh g−1 at 30C | capacity retention of ~83% over 500 cycles at 10C | [S10] |
| W3Nb14O44 nanowires | 131 mAh g−1 at 5C | capacity retention of ~64% over 1000 cycles at 10C | [S11] |
| Li4Ti5O12 nanorods | 136 mAh g−1 at 20C | capacity retention of ~61.5% over 1500 cycles at 10C | [S12] |
| Mo1.5W1.5Nb14O44 micron-sized particles | 198 mAh g−1 at 10C | capacity retention of 84.1% over 2000 cycles at 10C | [S13] |
| Nb14W3O44 nano-blocks | 160 mAh g−1 at 10C | capacity retention of 84.3% over 1000 cycles at 10C | [S14] |
| Cr0.2Fe0.8Nb11O29 micron-sized particles | 123 mAh g−1 at 10C | capacity retention of 86.9% over 500 cycles at 10C | [S15] |
| HfNb24O62 micron-sized particles | 78 mAh g−1 at 10C | capacity retention of 87.1% over 500 cycles at 10C | [S16] |
| 3D TiO2-QDs@C porous nanospheres | 108 mAh g−1 at 5A g−1 | capacity retention of 68.6% over 10000 cycles at 5A g−1 | [S17] |
| Mg2Nb34O87 micron-sized particles | 117 mAh g−1 at 10C | capacity retention of 83.9% over 2000 cycles at 10C | [S18] |
| AlNb11O29 micron-sized particles | 131 mAh g−1 at 10C | capacity retention of 93.2% over 500 cycles at 10C | [S19] |
| graphite micron-sized particles | 135 mAh g−1 at 10C | capacity retention of 73.0% over 1500 cycles at 10C | [S20] |
| carbon-coated Li3VO4 | 147 mAh g−1 at 0.3 A g−1 | 84.5% after 50 cycles at 0.02 A g−1 | [S21] |
| ω-Li3V2O5 nanoplates | 113 mAh g−1 at 10 A g−1 | 99.5% after 1000 cycles at 10 A g−1 | [S22] |
| Li2.98Cr0.04V0.98O4 microparticles | 147 mAh g−1 at 1.2 A g−1 | 86.6% after 1000 cycles at 1.2 A g−1 | [S23] |

Table S2 Comparisons of apparent Li+ diffusion coefficient (DLi) of NiNb2O6 with previously-reported M−Nb−O anode materials

| Material | DLi (cm2 s−1) | Test technique | References |
| --- | --- | --- | --- |
| NiNb2O6 fibers (25 °C) | 1.11×10−12 | GITT | this work |
| NiNb2O6 fibers (−10 °C) | 6.12×10−13 | GITT | this work |
| NiNb2O6 fibers (60 °C) | 1.29×10−13 | GITT | this work |
| NiNb2O6 fibers (25 °C) | 2.67×10−13 | CV | this work |
| NiNb2O6 fibers (−10 °C) | 1.10×10−13 | CV | this work |
| NiNb2O6 fibers (60 °C) | 5.73×10−13 | CV | this work |
| NiNb2O6 micron-sized particles (25 °C) | 1.36×10−12 | GITT | [S3] |
| W3Nb14O44 nanowires (25 °C) | 8.02×10−13 | CV | [S11] |
| Cu2Nb34O87 micron-sized particles (25 °C) | 3.50×10−13 | GITT | [S24] |
| VNb9O25 nanoribbons (25 °C) | 5.17×10−15 | EIS | [S25] |
| MoNb12O33 micron-sized particles (25 °C) | 3.90×10−14 | GITT | [S26] |
| Al0.5Nb24.5O62 micron-sized particles (25 °C) | 2.50×10−13 | GITT | [S27] |
| GeNb18O47 nanowires (25 °C) | 1.57×10−14 | CV | [S28] |
| W5Nb16O55 micron-sized particles (25 °C) | 1.0×10−13 | GITT | [S29] |
| TiNb6O17 micron-sized particles (25 °C) | 4.88×10−14 | CV | [S30] |
| TiCr0.5Nb10.5O29 nanoparticles | 2.07×10−14 | CV | [S31] |
| TiNb2O7 micron-sized particles (25 °C) | 1.05×10−15 | EIS | [S8] |
| HfNb24O62 micron-sized particles (25 °C) | 1.51×10−13 | GITT | [S16] |
| W16Nb18O93 nanowires (25 °C) | 1.31×10−14 | EIS | [S32] |
| TiO2/C composite nanospheres (25 °C) | 2.2×10−14 | CV | [S17] |
| Cr0.5Nb24.5O62 micron-sized particles (25 °C) | 4.57×10−14 | EIS | [S33] |
| TiNb2O7 nanorods (25 °C) | 3.24×10−14 | CV | [S34] |
| Nb2O5 nanorods (25 °C) | 3.66×10−17 | CV | [S35] |

Table S3 Comparisons of maximum unit-cell-volume change of NiNb2O6 with previously-reported M−Nb−O anode materials

| Material | Maximum unit-cell-volume change (%) | References |
| --- | --- | --- |
| NiNb2O6 (25 °C) | 0.53 (discharge to 1.0 V) | this work |
| NiNb2O6 (−10 °C) | 0.51 (discharge to 1.0 V) | this work |
| NiNb2O6 (60 °C) | 0.74 (discharge to 1.0 V) | this work |
| LaCeNb6O18 (25 °C) | 1.52 (discharge to 0.8 V) | [S36] |
| V3Nb17O12 (25 °C) | 3.46 (discharge to 0.8 V) | [S37] |
| BaNb3.6O10 (25 °C) | 5.96 (discharge to 0.8 V) | [S38] |
| NaNb13O33 (25 °C) | 6.02 (discharge to 0.8 V) | [S39] |
| Ni2Nb34O87 (25 °C) | 6.71 (discharge to 0.8 V) | [S40] |
| Ti2Nb10O29 (25 °C) | 6.8 (discharge to 1.0 V) | [S9] |
| GeNb18O47 (25 °C) | 6.83 (discharge to 0.8 V) | [S28] |
| TiNb2O7 (25 °C) | 7.22 (discharge to 1.0 V) | [S10] |
| MoNb13O33 (25 °C) | 7.8 (discharge to 0.8 V) | [S26] |
| Cu2Nb34O87 (25 °C) | 8.32 (discharge to 0.8 V) | [S24] |
| Al0.5Nb24.5O62 (25 °C) | 8.5 (discharge to 0.8 V) | [S27] |
| Zn2Nb34O87 (25 °C) | 8.58 (discharge to 0.8 V) | [S41] |
| VNb9O25 (25 °C) | 8.91 (discharge to 0.8 V) | [S25] |
| Mo3Nb14O44 (25 °C) | 10.6 (discharge to 0.8 V) | [S42] |
| PNb9O25 (25 °C) | 10.69 (discharge to 0.8 V) | [S43] |
| Mo4Nb26O77 (25 °C) | 12.8 (discharge to 0.8 V) | [S44] |

Table S4 Lattice parameters of delithiated NiNb2O6, partially lithiated NiNb2O6, lithiated NiNb2O6 after phase transformation, and lithiated NiNb2O6 states at 25 °C

| sample | a (Å) | b (Å) | c (Å) | V (Å3) | space group | Rwp | Uiso |
| --- | --- | --- | --- | --- | --- | --- | --- |
| delithiated NiNb2O6 | 14.03928 (58) | 5.68370 (16) | 5.02556 (12) | 401.015 (37) | Pbcn | 0.0152 | 0.01 |
| partially lithiated NiNb2O6 | 14.04520 (56) | 5.69151 (32) | 5.02825 (47) | 401.940 (78) | Pbcn | 0.0132 | 0.01 |
| lithiated NiNb2O6 after phase transformation | 14.05438 (84) | 5.69734 (24) | 5.03114 (18) | 402.839 (54) | Pbcn | 0.0126 | 0.01 |
| lithiated NiNb2O6 | 14.04300 (11) | 5.69445 (32) | 5.02986 (24) | 402.223 (72) | Pbcn | 0.0124 | 0.01 |

Table S5 Fractional atomic parameters of delithiated NiNb2O6 at 25 °C

| ion | site | x | y | z |
| --- | --- | --- | --- | --- |
| Ni2+ | 4c | 0 | 0.3324(14) | 0.25 |
| Nb5+ | 8d | 0.1604(62) | 0.1807(57) | 0.7482(28) |
| O2− | 8d1 | 0.0875(40) | 0.0807(43) | 0.0910(42) |
| O2− | 8d2 | 0.4205(11) | 0.1248(40) | 0.0867(35) |
| O2− | 8d3 | 0.7569(12) | 0.1199(39) | 0.0770(43) |

Table S6 Fractional atomic parameters of partially lithiated NiNb2O6 at 25 °C

| ion | site | x | y | z |
| --- | --- | --- | --- | --- |
| Ni2+ | 4c | 0 | 0.3328(18) | 0.25 |
| Nb5+ | 8d | 0.1594(79) | 0.1802(48) | 0.7598(42) |
| O2− | 8d1 | 0.0847(21) | 0.0643(04) | 0.1205(23) |
| O2− | 8d2 | 0.4211(14) | 0.1460(51) | 0.0796(43) |
| O2− | 8d3 | 0.7558(27) | 0.1090(19) | 0.0820(52) |

Table S7 Fractional atomic parameters of lithiated NiNb2O6 after phase transformation at 25 °C

| ion | site | x | y | z |
| --- | --- | --- | --- | --- |
| Ni2+ | 4c | 0 | 0.3304(16) | 0.25 |
| Nb5+ | 8d | 0.1606(18) | 0.1815(62) | 0.7654(09) |
| O2− | 8d1 | 0.0875(76) | 0.0599(54) | 0.1129(10) |
| O2− | 8d2 | 0.4211(56) | 0.1399(26) | 0.0867(35) |
| O2− | 8d3 | 0.7546(08) | 0.1045(62) | 0.0788(17) |

Table S8 Fractional atomic parameters of lithiated NiNb2O6 at 25 °C

| ion | site | x | y | z |
| --- | --- | --- | --- | --- |
| Ni2+ | 4c | 0 | 0.3269(22) | 0.25 |
| Nb5+ | 8d | 0.1608(10) | 0.1825(92) | 0.7673(29) |
| O2− | 8d1 | 0.0900(16) | 0.0552(74) | 0.1138(70) |
| O2− | 8d2 | 0.4215(16) | 0.1297(66) | 0.0965(55) |
| O2− | 8d3 | 0.7531(18) | 0.0995(72) | 0.0749(77) |

Table S9 Bond lengths of delithiated NiNb2O6, partially lithiated NiNb2O6, lithiated NiNb2O6 after phase transformation, and lithiated NiNb2O6 states at 25 °C

| bond | delithiated NiNb2O6 (Å) | partially lithiated NiNb2O6 (Å) | lithiated NiNb2O6 after phase transformation (Å) | lithiated NiNb2O6 (Å) |
| --- | --- | --- | --- | --- |
| Ni−O (8d1) | 2.0890(5) | 2.0894(6) | 2.1120(7) | 2.0820(8) |
| Ni−O (8d2) | 2.1290(5) | 2.1146(6) | 2.1020(7) | 2.1357(8) |
| Nb−O (8d1) | 2.0109(5) | 2.0267(6) | 2.0374(6) | 1.9910(7) |
| Nb−O (8d2) | 1.7811(5) | 1.7777(6) | 1.7546(6) | 1.7942(6) |
| Nb−O (8d3) | 2.0833(5) | 2.0907(6) | 2.0915(6) | 2.0929(7) |

Table S10 NiO6 and NbO6 polyhedron-volumes in delithiated NiNb2O6, partially lithiated NiNb2O6, lithiated NiNb2O6 after phase transformation, and lithiated NiNb2O6 states at 25 °C

| sample | NiO6 (Å3) | NbO6 (Å3) |
| --- | --- | --- |
| delithiated NiNb2O6 | 11.9050 | 10.4227 |
| partially lithiated NiNb2O6 | 12.0946 | 10.3599 |
| lithiated NiNb2O6 after the phase transformation | 12.4262 | 10.2432 |
| lithiated NiNb2O6 | 12.4922 | 10.1900 |

Table S11 Lattice parameters of delithiated and lithiated NiNb2O6 at −10 °C

| sample | a (Å) | b (Å) | c (Å) | V (Å3) | Space group | Rwp | Uiso |
| --- | --- | --- | --- | --- | --- | --- | --- |
| delithiated NiNb2O6 | 13.99453 (11) | 5.66938 (37) | 5.01653 (21) | 398.013 (75) | Pbcn | 0.0153 | 0.01 |
| lithiated NiNb2O6 | 14.02392 (11) | 5.68242(37) | 5.01954 (22) | 400.043 (76) | Pbcn | 0.0162 | 0.01 |

Table S12 Fractional atomic parameters of delithiated NiNb2O6 at −10 °C

| ion | site | x | y | z |
| --- | --- | --- | --- | --- |
| Ni2+ | 4c | 0 | 0.3430(21) | 0.25 |
| Nb5+ | 8d | 0.1606(85) | 0.1836(77) | 0.7526(24) |
| O2− | 8d1 | 0.0928(12) | 0.0851(62) | 0.1392(23) |
| O2− | 8d2 | 0.4271(15) | 0.1269(53) | 0.0675(90) |
| O2− | 8d3 | 0.7350(36) | 0.1122(75) | 0.9779(10) |

Table S13 Fractional atomic parameters of lithiated NiNb2O6 at −10 °C

| ion | site | x | y | z |
| --- | --- | --- | --- | --- |
| Ni2+ | 4c | 0 | 0.3393(21) | 0.25 |
| Nb5+ | 8d | 0.1616(95) | 0.1839(86) | 0.7609(11) |
| O2− | 8d1 | 0.0919(14) | 0.0802(66) | 0.1245(23) |
| O2− | 8d2 | 0.4266(16) | 0.1262(55) | 0.0725(97) |
| O2− | 8d3 | 0.7389(36) | 0.1219(73) | 0.1542(28) |

Table S14 Bond lengths of delithiated and lithiated NiNb2O6 states at −10 °C.

| bond | delithiated NiNb2O6 (Å) | lithiated NiNb2O6 (Å) |
| --- | --- | --- |
| Ni−O (8d1) | 2.0431(9) | 2.0493(11) |
| Ni−O (8d2) | 1.8907(7) | 1.8768(8) |
| Nb−O (8d1) | 2.0433(8) | 2.0907(8) |
| Nb−O (8d2) | 1.8802(8) | 1.8667(9) |
| Nb−O (8d3) | 1.8043(7) | 1.8102(9) |

Table S15 NiO6 and NbO6 polyhedron-volumes in delithiated and lithiated NiNb2O6 states at −10 °C

| sample | NiO6 (Å3) | NbO6 (Å3) |
| --- | --- | --- |
| delithiated NiNb2O6 | 10.7223 | 10.9830 |
| lithiated NiNb2O6 | 11.0163 | 10.8917 |

Table S16 Lattice parameters of delithiated NiNb2O6, partially lithiated NiNb2O6, lithiated NiNb2O6 after phase transformation, and lithiated NiNb2O6 at 60 °C

| sample | a (Å) | b (Å) | c (Å) | V (Å3) | Space group | Rwp | Uiso |
| --- | --- | --- | --- | --- | --- | --- | --- |
| delithiated NiNb2O6 | 14.04380 (86) | 5.68507 (21) | 5.02643 (16) | 401.287 (33) | Pbcn | 0.0151 | 0.01 |
| partially lithiated NiNb2O6 | 14.04408 (75) | 5.68917 (21) | 5.02945 (16) | 401.830 (49) | Pbcn | 0.0137 | 0.01 |
| lithiated NiNb2O6 after phase transformation | 14.03446 (17) | 5.69336 (49) | 5.03030 (39) | 401.938 (13) | Pbcn | 0.0118 | 0.01 |
| lithiated NiNb2O6 | 14.00864 (27) | 5.68940 (76) | 5.02191 (58) | 400.251 (72) | Pbcn | 0.0117 | 0.01 |

Table S17 Fractional atomic parameters of delithiated NiNb2O6 at 60 °C

| ion | site | x | y | z |
| --- | --- | --- | --- | --- |
| Ni2+ | 4c | 0 | 0.3350(20) | 0.25 |
| Nb5+ | 8d | 0.1581(82) | 0.1813(74) | 0.7710(26) |
| O2− | 8d1 | 0.0817(13) | 0.0651(51) | 0.1280(54) |
| O2− | 8d2 | 0.4217(16) | 0.1498(52) | 0.0727(42) |
| O2− | 8d3 | 0.7580(15) | 0.1226(49) | 0.0917(53) |

Table S18 Fractional atomic parameters of partially lithiated NiNb2O6 at 60 °C

| ion | site | x | y | z |
| --- | --- | --- | --- | --- |
| Ni2+ | 4c | 0 | 0.3352(77) | 0.25 |
| Nb5+ | 8d | 0.1603(04) | 0.1776(09) | 0.7546(29) |
| O2− | 8d1 | 0.0754(17) | 0.0514(33) | 0.1345(55) |
| O2− | 8d2 | 0.4176(20) | 0.1638(91) | 0.0566(06) |
| O2− | 8d3 | 0.7628(25) | 0.1130(59) | 0.0999(94) |

Table S19 Fractional atomic parameters of lithiated NiNb2O6 after phase transformation at 60 °C

| ion | site | x | y | z |
| --- | --- | --- | --- | --- |
| Ni2+ | 4c | 0 | 0.3250(37) | 0.25 |
| Nb5+ | 8d | 0.1582(34) | 0.1801(19) | 0.7419(27) |
| O2− | 8d1 | 0.0808(12) | 0.0422(33) | 0.1395(52) |
| O2− | 8d2 | 0.4206(22) | 0.1419(89) | 0.0732(16) |
| O2− | 8d3 | 0.7591(20) | 0.1029(53) | 0.0961(14) |

Table S20 Fractional atomic parameters of lithiated NiNb2O6 at 60 °C

| ion | site | x | y | z |
| --- | --- | --- | --- | --- |
| Ni2+ | 4c | 0 | 0.3247(59) | 0.25 |
| Nb5+ | 8d | 0.1588(25) | 0.1790(20) | 0.7335(53) |
| O2− | 8d1 | 0.0870(35) | 0.0677(16) | 0.1314(14) |
| O2− | 8d2 | 0.4198(39) | 0.1258(16) | 0.0734(13) |
| O2− | 8d3 | 0.7623(39) | 0.0853(20) | 0.1006(14) |

Table S21 Bond lengths of delithiated NiNb2O6, partially lithiated NiNb2O6, lithiated NiNb2O6 after phase transformation, and lithiated NiNb2O6 states at 60 °C

| bond | delithiated NiNb2O6 (Å) | partially lithiated NiNb2O6 (Å) | lithiated NiNb2O6 after phase transformation (Å) | lithiated NiNb2O6 (Å) |
| --- | --- | --- | --- | --- |
| Ni−O (8d1) | 2.0220(6) | 2.0362(9) | 2.0456(14) | 2.0230(2) |
| Ni−O (8d2) | 2.1282(7) | 2.1104(9) | 2.1062(14) | 2.1150(2) |
| Nb−O (8d1) | 2.0301(6) | 2.0765(7) | 2.1046(15) | 2.0695(3) |
| Nb−O (8d2) | 1.7745(6) | 1.7530(7) | 1.7237(11) | 1.7404(2) |
| Nb−O (8d3) | 2.0747(7) | 2.0864(7) | 2.0906(11) | 2.0956(3) |

Table S22 NiO6 and NbO6 polyhedron-volumes in delithiated NiNb2O6, partially lithiated NiNb2O6, lithiated NiNb2O6 after phase transformation, and lithiated NiNb2O6 states at 60 °C

| sample | NiO6 (Å3) | NbO6 (Å3) |
| --- | --- | --- |
| delithiated NiNb2O6 | 11.8765 | 10.4224 |
| partially lithiated NiNb2O6 | 11.9830 | 10.3433 |
| lithiated NiNb2O6 after phase transformation | 12.6139 | 10.1045 |
| lithiated NiNb2O6 | 12.3195 | 10.1537 |

Supplementary References

[S1] A.J. Bard, L.R. Faulkner, Electrochemical Methods: Fundamentals and Applications, second ed., Wiley, New York, USA 2001.

[S2] V. Augustyn, J. Come, M.A. Lowe, J.W. Kim, P.L. Taberna et al., High-rate electrochemical energy storage through Li+ intercalation pseudocapacitance, Nat. Mater. 12 (2013) 518-522. https://doi.org/10.1038/nmat3601

[S3] R. Xia, K. Zhao, Y. Kuo, L. Zhang, D. M. Cunha et al., Nickel niobate anodes for high rate lithium-ion batteries, Adv. Energy Mater. 12 (2021) 2102972. https://doi.org/10.1002/aenm.202102972

[S4] T. Jiang, S. Ma, J. Deng, T. Yuan, C. Lin et al., Partially reduced titanium niobium oxide: A high-performance lithium-storage material in a broad temperature range, Adv. Sci. 9 (2021) 2105119. https://doi.org/10.1002/advs.202105119

[S5] X. Lou, Q. Fu, J. Xu, X. Liu, C. Lin et al., GaNb11O29 nanowebs as high-performance anode materials for lithium-ion batteries, ACS Appl. Nano Mater. 1 (2018) 183-190. https://doi.org/10.1021/acsanm.7b00091

[S6] L. Zhao, S. Wang, Y. Dong, W. Quan, F. Han et al., Coarse-grained reduced MoxTi1−xNb2O7+y anodes for high-rate lithium-ion batteries, Energy Storage Mater. 34 (2021) 574-581. https://doi.org/10.1016/j.ensm.2020.10.016

[S7] P. Jing, K. Liu, L. Soule, J. Wang, T. Li et al., Engineering the architecture and oxygen deficiency of T-Nb2O5-carbon-graphene composite for high-rate lithium-ion batteries, Nano Energy 89 (2021) 106398. https://doi.org/10.1016/j.nanoen.2021.106398

[S8] H. Li, L. Shen, G. Pang, S. Fang, H. Luo et al., TiNb2O7 nanoparticles assembled into hierarchical microspheres as high-rate capability and long-cycle-life anode materials for lithium ion batteries, Nanoscale 7 (2015) 619-624. https://doi.org/10.1039/C4NR04847D

[S9] Q. Fu, J. Hou, R. Lu, C. Lin, Y. Ma et al., Electrospun Ti2Nb10O29 hollow nanofibers as high-performance anode materials for lithium-ion batteries, Mater. Lett. 214 (2018) 60-63. https://doi.org/10.1016/j.matlet.2017.11.076

[S10] L. Fei, Y. Xu, X. Wu, Y. Li, P. Xie et al., SBA-15 Confined synthesis of TiNb2O7 nanoparticles for lithium-ion batteries, Nanoscale 5 (2013) 11102-11107. https://doi.org/10.1039/c3nr03594h

[S11] L. Yan, J. Shu, C. Li, X. Cheng, H. Zhu et al., W3Nb14O44 nanowires: Ultrastable lithium storage anode materials for advanced rechargeable batteries, Energy Storage Mater. 16 (2019) 535-544. https://doi.org/10.1016/j.ensm.2018.09.008

[S12] L. Xi, H. Wang, S. Yang, R. Ma, Z. Lu et al., Single-crystalline Li4Ti5O12 nanorods and their application in high-rate capability Li4Ti5O12/LiMn2O4 full cells, J. Power Sources 242 (2013) 222-229. https://doi.org/10.1016/j.jpowsour.2013.04.020

[S13] R. Tao, T. Zhang, S. Tan, C. Jafta, C. Li et al., Insight into the fast-rechargeability of a novel Mo1.5W1.5Nb14O44 anode material for high-performance lithium-ion batteries, Adv. Energy Mater. 12 (2022) 2200519. https://doi.org/10.1002/aenm.202200519

[S14] C. Guo, Z. Liu, K. Han, L. Zhang, X. Ding et al., Nano-sized niobium tungsten oxide anode for advanced fast-charge lithium-ion batteries, Small 18 (2022) 2107365. https://doi.org/10.1002/smll.202107365

[S15] X. Lou, Z. Xu, Z. Luo, C. Lin, C. Yang et al., Exploration of Cr0.2Fe0.8Nb11O29 as an advanced anode material for lithium-ion batteries of electric vehicles, Electrochim. Acta 245 (2017) 482-488. https://doi.org/10.1016/j.electacta.2017.05.168

[S16] Q. Fu, H. Cao, G. Liang, L. Luo, Y. Chen et al., A highly Li+-conductive HfNb24O62 anode material for superior Li+ storage, Chem. Commun. 56 (2020) 619-622. https://doi.org/10.1039/C9CC07447C

[S17] W. Wang, J. Park, V. Nguyen, E. Jin, H. Gu, Hierarchical mesoporous rutile TiO2/C composite nanospheres as lithium-ion battery anode materials, Ceram. Int. 42 (2016) 598-606. https://doi.org/10.1016/j.ceramint.2015.08.153

[S18] X. Zhu, Q. Fu, L. Tang, C. Lin, J. Xu et al., Mg2Nb34O87 porous microspheres for use in high-energy, safe, fast-charging, and stable lithium-ion batteries, ACS Appl. Mater. Interfaces 10 (2018) 23711-23720. https://doi.org/10.1021/acsami.8b03997

[S19] X. Lou, R. Li, X. Zhu, L. Luo, Y. Chen et al., New anode material for lithium-ion batteries: Aluminum niobate (AlNb11O29), ACS Appl. Mater. Interfaces 11 (2019) 6089-6096. https://doi.org/10.1021/acsami.8b20246

[S20] C. Lv, C. Lin, X. Zhao, Rational design and synthesis of nickel niobium oxide with high-rate capability and cycling stability in a wide temperature range, Adv. Energy Mater. 12 (2022) 2102550. https://doi.org/10.1002/aenm.202102550

[S21] G. Shao, L. Gan, Y. Ma, H. Li, T. Zhai, Enhancing the performance of Li3VO4 by combining nanotechnology and surface carbon coating for lithium ion batteries, J. Mater. Chem. A 3 (2015) 11253-11260. https://doi.org/10.1039/C5TA02094H

[S22] X. Lan, L. Wang, L. Yu, Y. Li, X. Hu, Synergy of highly reversible ω-Li3V2O5 anodes and fluorine-containing additive electrolytes promises low-temperature-tolerant Li-ion batteries, ACS Mater. Lett. 3 (2021) 1394-1401. https://doi.org/10.1021/acsmaterialslett.1c00377

[S23] G. Liang, X. Jin, C. Huang, L. Luo, Y. Chen et al., Cr3+-doped Li3VO4 for enhanced Li+ storage, Funct. Mater. Lett. 13 (2019) 2050005. https://doi.org/10.1142/S1793604720500058

[S24] L. Yang, X. Zhu, X. Li, X. Zhao, K. Pei et al., Conductive copper niobate: superior Li+-storage capability and novel Li+-transport mechanism, Adv. Energy Mater. 9 (2019) 1902174. https://doi.org/10.1002/aenm.201902174

[S25] S. Qian, H. Yu, L. Yan, H. Zhu, X. Cheng et al., High-rate long-life pored nanoribbon VNb9O25 built by interconnected ultrafine nanoparticles as anode for lithium-ion batteries, ACS Appl. Mater. Interfaces 9 (2017) 30608-30616. https://doi.org/10.1021/acsami.7b07460

[S26] X. Zhu, J. Xu, Y. Luo, Q. Fu, G. Liang et al., MoNb12O33 as a new anode material for high-capacity, safe, rapid and durable Li+ storage: structural characteristics, electrochemical properties and working mechanisms, J. Mater. Chem. A 7 (2019) 6522-6532. https://doi.org/10.1039/C9TA00309F

[S27] Q. Fu, R. Li, X. Zhu, G. Liang, L. Luo et al., Design, synthesis and lithium-ion storage capability of Al0.5Nb24.5O62, J. Mater. Chem. A 7 (2019) 19862-19871. https://doi.org/10.1039/C9TA04644E

[S28] F. Ran, X. Cheng, H. Yu, R. Zheng, T. Liu et al., Nano-structured GeNb18O47 as novel anode host with superior lithium storage performance, Electrochim. Acta 282 (2018) 634-641. https://doi.org/10.1016/j.electacta.2018.06.109

[S29] K.J. Griffith, K.M. Wiaderek, G. Cibin, L.E. Marbella, C.P. Grey, Niobium tungsten oxides for high-rate lithium-ion energy storage, Nature 559 (2018) 556-563. https://doi.org/10.1038/s41586-018-0347-0

[S30] C. Lin, G. Wang, S. Lin, J. Li, L. Lu, TiNb6O17: a new electrode material for lithium-ion batteries, Chem. Commun. 51 (2015) 8970-8973. https://doi.org/10.1039/C5CC01494H

[S31] L. Hu, R. Lu, L. Tang, R. Xia, C. Lin et al., TiCr0.5Nb10.5O29/CNTs nanocomposite as an advanced anode material for high-performance Li+-ion storage, J. Alloys Compd. 732 (2018) 116-123. https://doi.org/10.1016/j.jallcom.2017.10.145

[S32] W. Ye, H. Yu, X. Cheng, H. Zhu, R. Zheng et al., Highly efficient lithium container based on non-Wadsley-Roth structure Nb18W16O93 nanowires for electrochemical energy storage, Electrochim. Acta 292 (2018) 331-338. https://doi.org/10.1016/j.electacta.2018.09.169

[S33] C. Yang, S. Yu, C. Lin, F. Lv, S. Wu et al., Cr0.5Nb24.5O62 nanowires with high electronic conductivity for high-rate and long-life lithium-ion storage, ACS Nano 11 (2017) 4217-4224. https://doi.org/10.1021/acsnano.7b01163

[S34] L. Hu, C. Lin, C. Wang, C. Yang, J. Li et al., TiNb2O7 nanorods as a novel anode material for secondary lithium-ion batteries, Funct. Mater. Lett. 9 (2016) 1642004. https://doi.org/10.1142/S1793604716420042

[S35] C. Shi, K. Xiang, Y. Zhu, W. Zhou, X. Chen et al., Box-implanted Nb2O5 nanorods as superior anode materials in lithium ion batteries, Ceram. Int. 43 (2017) 12388-12395. https://doi.org/10.1016/j.ceramint.2017.06.105

[S36] W. Wang, Q. Zhang, T. Jiang, S. Li, J. Gao et al., Conductive LaCeNb6O18 with a very open A-site-cation-deficient perovskite structure: A fast- and stable-charging Li+-storage anode compound in a wide temperature range, Adv. Energy Mater. 12 (2022) 2200656. https://doi.org/10.1002/aenm.202200656

[S37] Q. Fu, X. Zhu, R. Li, G. Liang, L. Luo et al., A low-strain V3Nb17O50 anode compound for superior Li+ storage, Energy Storage Mater. 30 (2020) 401-411. https://doi.org/10.1016/j.ensm.2020.05.012

[S38] X. Cheng, S. Qian, H. Yua, H. Zhua, Y. Xie et al., BaNb3.6O10 nanowires with superior electrochemical performance towards ultrafast and highly stable lithium storage, Energy Storage Mater. 16 (2019) 400-410. https://doi.org/10.1016/j.ensm.2018.06.018

[S39] J. Gao, L. Yang, C. Huang, G. Liang, Y. Lei et al., Sodium niobate with a large interlayer spacing: A fast-charging, long-life, and low-temperature friendly lithium-storage material, Adv. Sci. 10 (2023) 2300583. https://doi.org/10.1002/advs.202300583

[S40] C. Lv, C. Lin, X. Zhao, Rational design and synthesis of nickel niobium oxide with high-rate capability and cycling stability in a wide temperature range, Adv. Energy Mater. 12 (2021) 2102550. https://doi.org/10.1002/aenm.202102550

[S41] X. Zhu, H. Cao, R. Li, Q. Fu, G. Liang et al., Zinc niobate materials: crystal structures, energy-storage capabilities and working mechanisms, J. Mater. Chem. A 7 (2019) 25537-25547. https://doi.org/10.1039/C9TA07818E

[S42] R. Li, G. Liang, X. Zhu, Q. Fu, Y. Chen et al., Mo3Nb14O44: A new Li+ container for high-performance electrochemical energy storage, Energy Environ. Sci. 4 (2020) 65-71. https://doi.org/10.1002/eem2.12098

[S43] S. Patoux, M. Dolle, G. Rousse, C. Masquelier, A reversible lithium intercalation process in a ReO3-Type structure PNb9O25, J. Electrochem. Soc. 149 (2002) A391. https://doi.org/10.1149/1.1455647

[S44] S. Li, J. Gao, Y. Ou, W. Wang, Q. Zhang et al., A general strategy to enhance the electrochemical activity and energy density of energy-storage materials through using sintering aids with redox activity: A case study of Mo4Nb26O77, J. Mater. Chem. A 10 (2022) 19953-19962. https://doi.org/10.1039/D2TA02169B