Supporting Information for

Molecule-Level Multiscale Design of Non-Flammable Gel Polymer Electrolyte to Build Stable SEI/CEI for Lithium Metal Battery

Qiqi Sun1, Zelong Gong1, Tao Zhang1, Jiafeng Li1, Xianli Zhu1, Ruixiao Zhu1, Lingxu Wang1, Leyuan Ma1, Xuehui Li1, Miaofa Yuan1, Zhiwei Zhang1, Luyuan Zhang1, Zhao Qian1,*, Longwei Yin1,*, Rajeev Ahuja2 and Chengxiang Wang1,*

1 Key Laboratory for Liquid-Solid Structural Evolution and Processing of Materials (Ministry of Education), School of Materials Science and Engineering, Shandong University, Jinan 250061, P. R. China

2 Condensed Matter Theory, Department of Physics and Astronomy, Uppsala University, Uppsala 75120, Sweden

*Corresponding authors. E-mail: qianzhao@sdu.edu.cn (Zhao Qian); yinlw@sdu.edu.cn (Longwei Yin); wcxmat@sdu.edu.cn (Chengxiang Wang)

Supplementary Figures and Tables

Fig. S1 Molecular structures of TFMA (a) and HEMA (b)

Fig. S2 Optical photographs of in-situ prepared (a) 10TFMA-0.5LF-0.5LB, (b) 20TFMA-0.5LF-0.5LB, (c) 30TFMA-0.5LF-0.5LB, (d) 35TFMA-0.5LF-0.5LB and (e) 35HEMA -0.5LF -0.5LB within vials

Fig. S3 SEM images of a) original cellulose separator and b) obtained GPE with corresponding element mapping

Fig. S4 1H nuclear magnetic resonance (1H NMR) spectra of a) TFMA and b) HEMA monomer before and after polymerization

Fig. S5 Nyquist plots of various electrolytes obtained with SS|GPEs|SS at room temperatures

Fig. S6 Nyquist plots of a) SGPE electrolyte, b) CGPE electrolyte, c) 60TFMA-0.5LF-0.5LB electrolyte and d) 40TFMA-1.5LF-0.5LB electrolyte under various temperature

Fig. S7 Chronoamperometry profile collected from a symmetric Li|CGPE|Li cell (The inset corresponds to the EIS plots before and after chronoamperometry)

Fig. S8 TGA thermograms of the CGPE electrolyte

Fig. S9 Stress-strain curves of GPEs

Fig. S10 EIS spectra of a) Li|SGPE|Li and b) Li|CGPE|Li cells after 150 cycles

Fig. S11 Long-term cycling of Li|1MLF-35|Li symmetrical cells, with a current density of 0.1 mA cm-2 and 0.05 mAh cm-2 Li plated and stripped per cycle

Fig. S12 Cross-sectional SEM images and EDS mappings of the interface between SGPE and the LiFePO4 cathode

Fig. S13 Typical charge–discharge curves of a) LiFePO4/SGPE/Li cell at 0.5 C, b) LiFePO4/LE/Li cell at 0.3 C, c) LiFePO4/CGPE/Li cell at 0.3 C and at room temperature

Fig. S14 Long-term cycling performance for LiFePO4|SGPE|Li cell at a current density of (a) 1 C and (b) 2 C

Fig. S15 Typical charge/discharge curves of a) LiFePO4/LE/Li cell, b) LiFePO4/CGPE/Li cell under the varied rate from 0.1 C to 2 C

Fig. S16 Typical charge–discharge curves of a) LiCoO2|SGPE|Li cell, b) LiCoO2|LE|Li cell and c) LiCoO2|CGPE|Li cell at 0.2 C after being activated at 0.1 C at room temperature

Fig. S17 Contour plot of dQ/dV results of the LiCoO2|CGPE|Li cell from the 10th cycle to the 150th cycle

Fig. S18 The raw SEM images of Fig. 5a-d, respectively

Fig. S19 XRD patterns of pristine and cycled LiCoO2 cathodes after 30 cycles using SGPE, CGPE and LE electrolyte

Fig. S20 XPS spectra for B 1s and F 1s of the LiCoO2 cathodes cycled in a) SGPE electrolyte and b) CGPE electrolyte after 30 cycles

Fig. S21 FTIR spectra of –P=O peaks in TEP-based samples with different HEMA concentrations

Fig. S22 Deconvolution of peaks of the S-N-S stretching vibrational mode (CIP: contact ion pair, AGG: aggregated ion pair) in CGPE electrolyte

Table S1 The compositions of electrolyte used to optimize ionic conductivity

| Electrolytes | LiTFSI (mg) | TEP (μL) | TFMA (μL) | LiDFOB (mg) | RT Ionic conductivity (mS cm-1) |
| --- | --- | --- | --- | --- | --- |
| 35TFMA-0.2LF-0.5LB | 57.6 | 650 | 350 | 72 | 0.177 |
| 35TFMA-0.5LF-0.5LB | 144.0 | 650 | 350 | 72 | 0.933 |
| 35TFMA-1LF-0.5LB | 288.0 | 650 | 350 | 72 | 0.127 |
| 35TFMA-1.5LF-0.5LB | 432.0 | 650 | 350 | 72 | 0.070 |
| 35TFMA-2LF-0.5LB | 574.0 | 650 | 350 | 72 | 0.045 |
| 35TFMA-2.5LF-0.5LB | 718.0 | 650 | 350 | 72 | 0.021 |
| 40TFMA-0.5LF-0.5LB | 144.0 | 600 | 400 | 72 | 0.208 |
| 40TFMA-1.5LF-0.5LB | 432.0 | 600 | 400 | 72 | 0.041 |
| 10TFMA-0.5LF-0.5LB | 144.0 | 900 | 100 | 72 | 2.799 |
| 20TFMA-0.5LF-0.5LB | 144.0 | 800 | 200 | 72 | 1.495 |
| 30TFMA-0.5LF-0.5LB | 144.0 | 700 | 300 | 72 | 1.162 |
| 60TFMA-0.5LF-0.5LB | 144.0 | 400 | 600 | 72 | 0.009 |
| 60TFMA-1.5LF-0.5LB | 432.0 | 400 | 600 | 72 | 7.694E-04 |
| 80TFMA-0.5LF-0.5LB | 144.0 | 200 | 800 | 72 | 3.673E-06 |

Table S2 Comparison in LiFePO4||Li full cells performance (upper voltage, final capacity, cycle numbers, C rate, running temperature and LFP loading) with the SGPE electrolyte and other reported electrolytes

| Type | Electrolyte | Anode /Cathode | VR (V) | Electrochemical properties | Refs. | T | Loading (mg/cm2) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Liquid electrolyte | 1 M LiTFSI /EC/DEC | LiFePO4¦¦Li | 3.0-3.8 | 102.7 mAh g-1 for 125 cycles at 0.2 C, 65.2% capacity retention | [S1] | 25℃ | 2.08 |
| Gel electrolyte | PMLSE | LiFePO4¦¦Li | 3.0-3.8 | ~ 95 mAh g-1 for 200 cycles at 1 C, 85.5% capacity retention | [S1] | 25℃ | 2.08 |
| Gel electrolyte | PMLSE | LiFePO4¦¦Li | 3.0-3.8 | 127.7 mAh g-1 for 200 cycles at 0.2 C, 87.3% capacity retention | [S1] | 25℃ | 2.08 |
| Polymer electrolyte | PI/DBDPE /PEO/LiTFSI | LiFePO4¦¦Li | 2.5-3.8 | ~120 mAh g-1 for 300 cycles at 0.5 C, ~ 85% capacity retention | [S2] | 60℃ | 1.5 |
| Polymer electrolyte | PEO/LiTFSI | LiFePO4¦¦Li | 2.5-3.8 | ~100 mAh g-1 for 150 cycles at 0.5 C, ~78% capacity retention | [S2] | 60℃ | 1.5 |
| Gel electrolyte | CMP/MMT | LiFePO4¦¦Li | 3.0-4.2 | 140 mAh g-1 for 400 cycles at 0.3 C, >98% capacity retention | [S3] | RT | 5 |
| Gel electrolyte | CMP | LiFePO4¦¦Li | 3.0-4.2 | ~50 mAh g-1 for 400 cycles at 0.3 C, rapid capacity decay | [S3] | RT | 5 |
| Hybrid SSE | LIM-L | LiFePO4¦¦Li | 2.5-4.2 | ~130 mAh g-1 for 150 cycles at 0.1 C; 97% capacity retention; 37 mAh g−1 at 0.8 C | [S4] | RT | 12.4 |
| Composite electrolyte | PVDFHFP/ LiFSI/LLZTO | LiFePO4¦¦Li | 2.5-4.0 | 142.2 mAh g-1 for 300 cycles at 0.5 C, 97.2% capacity retention | [S5] | RT | 2 |
| Gel electrolyte | PDIL | LiFePO4¦¦Li | 2.0-4.5 | 127.2 mAh g-1 for 50 cycles at 0.3 C, ~87.1% capacity retention | [S6] | 25℃ | 1.5 |
| Gel electrolyte | PDIL | LiFePO4¦¦Li | 2.0-4.5 | 111.1 mAh g-1 for 150 cycles at 1 C, 90.6% capacity retention | [S6] | 25℃ | 1.5 |
| Quasi-solid-state electrolyte | CLSPE-IL4 | LiFePO4¦¦Li | 2.5-4.0 | 136.7 mAh g-1 for 500 cycles at 0.2 C, 91% capacity retention | [S7] | 25℃ | 1.94 |
| Gel electrolyte | FRSE | LiFePO4¦¦Li | 2.5-4.0 | 147 mAh g-1 for 500 cycles at 0.5 C, 98.7% capacity retention | [S8] | RT | ~5.8 |
| Quasi-solid-state electrolyte | PEMD | LiFePO4¦¦Li | 2.5-3.9 | 155.6 mAh g-1 for 85 cycles at 0.2 C, ~97% capacity retention | [S9] | 30 | 2.0-3.0 |
| Gel electrolyte | SGPE | LiFePO4¦¦Li | 2.5-4.0 | 110.4 mAh g-1 for 500 cycles at 0.5 C, ~65.8% capacity retention | this work | RT | 1.5-2.0 |

1 M LiTFSI/EC/DEC: 1 M LiTFSI/EC/DEC, 1:1 by volume

PMLSE: PVDF-HFP/MOF composite gel/LLZN nanowires solid electrolyte

PI: polyimide

DBDPE: decabromodiphenyl ethane

CMP: a solid composite electrolyte, UV initiated in situ cross-linked of poly (ethylene glycol) methyl ether acrylate (MPEGA) and poly (ethylene glycol) diacrylate (PEGDA) between cathodes and anodes of cell

CMP/MMT: a novel solid polymer/montmorillonite (MMT) composite electrolyte

LIM-L: LI-IL@MOF-LLZO hybrid electrolyte

PDIL: polymer dispersed ionic liquid‐based solid polymer electrolyte (PDIL‐SPE)

CLSPE-IL4: the EA and VC based polymer electrolytes, with 40% mass ratio of [PY13] [TFSI], denoted as CLSPE-IL4

FRSE: a flame-retardant solid-liquid hybrid electrolyte

PEMD: a unique solid electrolyte complexion consisted of polyethylene oxide, UiO-66-NH2, and deep eutectic solvents

Supplementary References

- J. Sun, X. Yao, Y. Li, Q. Zhang, C. Hou et al., Facilitating Interfacial Stability Via Bilayer Heterostructure Solid Electrolyte Toward High‐energy, Safe and Adaptable Lithium Batteries. Adv. Energy Mater. 10(31), 2000709 (2020). https://doi.org/10.1002/aenm.202000709

- Y. Cui, J. Wan, Y. Ye, K. Liu, L.-Y. Chou et al., A Fireproof, Lightweight, Polymer–Polymer Solid-State Electrolyte for Safe Lithium Batteries. Nano Lett. 20(3), 1686–1692 (2020). https://doi.org/10.1021/acs.nanolett.9b04815

- Y. Wang, X. Li, Y. Qin, D. Zhang, Z. Song et al., Local electric field effect of montmorillonite in solid polymer electrolytes for lithium metal batteries. Nano Energy 90, 106490 (2021). https://doi.org/10.1016/j.nanoen.2021.106490

- Z. Wang, Z. Wang, L. Yang, H. Wang, Y. Song et al., Boosting interfacial Li+ transport with a MOF-based ionic conductor for solid-state batteries. Nano Energy 49, 580–587 (2018). https://doi.org/10.1016/j.nanoen.2018.04.076

- J. Zhang, Y. Zeng, Q. Li, Z. Tang, D. Sun et al., Polymer-in-salt electrolyte enables ultrahigh ionic conductivity for advanced solid-state lithium metal batteries. Energy Storage Mater. 54, 440–449 (2023). https://doi.org/10.1016/j.ensm.2022.10.055

- S. Qin, Y. Cao, J. Zhang, Y. Ren, C. Sun et al., Polymer dispersed ionic liquid electrolytes with high ionic conductivity for ultrastable solid‐state lithium batteries. Carbon Energy 5, e316 (2023). https://doi.org/10.1002/cey2.316

- Z. Wang, Y. Wang, P. Zhai, P. Poldorn, S. Jungsuttiwong et al., A cation-dipole-reinforced elastic polymer electrolyte enabling long-cycling quasi-solid-state lithium metal batteries. J. Energy Chem. 75, 340–348 (2022). https://doi.org/10.1016/j.jechem.2022.08.042

- S.-J. Tan, J. Yue, Y.-F. Tian, Q. Ma, J. Wan et al., In-situ encapsulating flame-retardant phosphate into robust polymer matrix for safe and stable quasi-solid-state lithium metal batteries. Energy Storage Mater. 39, 186–193 (2021). https://doi.org/10.1016/j.ensm.2021.04.020

- S. Wang, Y. Chen, Q. Fang, J. Huang, X. Wang et al., Facilitating uniform lithium deposition via nanoconfinement of free amide molecules in solid electrolyte complexion for lithium metal batteries. Energy Storage Mater. 54, 596–604 (2023). https://doi.org/10.1016/j.ensm.2022.11.002