Supporting Information for

Defects-Rich Heterostructures Trigger Strong Polarization Coupling in Sulfides/Carbon Composites with Robust Electromagnetic Wave Absorption

Jiaolong Liu1, SiYu Zhang1, Dan Qu1, Xuejiao Zhou2, Moxuan Yin3, Chenxuan Wang3, Xuelin Zhang4, Sichen Li2, Peijun Zhang1, Yuqi Zhou1, Mengyang Li1,*, Bing Wei1,*, Hongjing Wu5,*

1 School of Physics, Xidian University, Xian 710071, P. R. China

2 School of Advanced Materials and Nanotechnology, State Key Discipline Laboratory of Wide Band Gap Semiconductor Technology, Xidian University, Xian 710071, P. R. China

3 School of Microelectronics, Xidian University, Xian 710071, P. R. China

4 School of Telecommunication Engineering, Xidian University, Xian 710071, P. R. China

5 MOE Key Laboratory of Material Physics and Chemistry under Extraordinary, School of Physical Science and Technology, Northwestern Polytechnical University, Xi’an 710072, P. R. China

*Corresponding authors. E-mail: limengyang@xidian.edu.cn (Mengyang Li), bwei@xidian.edu.cn (Bing Wei); wuhongjing@nwpu.edu.cn (Hongjing Wu)

Supplementary Figures and Tables

Fig. S1 Digital photographs of (a) carrageenan-M hydrogel, (b) after freeze drying; and (c, d) porous sulfides/carbon composites

Fig. S2 SEM and SAED images for (a-a2) CAs, (b-b2) Co-CAs, (c-c2) Ni-CAs, and (d-d2) Co/Ni-CAs

Fig. S3 (a) TEM images of Co/Ni-CAs; (b) Lattice information taken from the figure (a), showing that a number of (b1-b6) vacancy sites exist in Co9S8/Ni9S8 heterointerfaces for Co/Ni-CAs

Fig. S4 XPS spectra of (a) survey, (b) C 1s and (c) Ca 2p, and (d) Nyquist plots for M-CAs and CAs

Fig. S5 EMW absorption performance of samples. (a, a1) CAs; (b, b1) Co-CAs; (c, c1) Ni-CAs; (d, d1) Co/Ni-CAs

Fig. S6 EM parameters of samples. (a) ε′, (b) ε″, (c) Tanδε, (d) μ′, (e) μ″, and (f) Tanδμ

Fig. S7 (a) Cole-Cole semicircles of samples. (b) CAs, (c) Co-CAs, (d) Ni-CAs and (e) Co/Ni-CAs

Fig. S8 (a-d) 2D plots of impedance matching degree for samples

Generally, the normalized impedance Z can measure materials’ impedance matching level, and it is appraised by following equations according to the Maxwell′s equations:

Z = |Zin /Z0|=μrεrtanhj2πfdcμrεr

where Z0 and Zin embody the input impedance of the air and absorber, d is the thickness of absorber, f is the frequency of an electromagnetic wave and c represent the velocity of light in a vacuum.

The larger area between Z= 0.8 (black solid lines) and Z= 1.2 (red solid lines), the better impedance matching characteristic of absorber.

Fig. S9 Constructing Co9S8(220)/Ni9S8(114) heterointerface model by Quantum ATK software

Fig. S10 (a) Front and (b) top view, (c) charge density difference as well as (d) the planar-averaged charge density difference along the Z direction Δρ(z) and (e) electrostatic potential of Co9S8-Vs/Ni9S8 models

Table S1 Phase composition of M-CAs

| Samples | CAs | Co-CAs | Ni-CAs | Co/Ni-CAs |
| --- | --- | --- | --- | --- |
| Products | CaS | CaS Co9S8 | CaS Ni9S8 | CaS Ni9S8 Co9S8 |

Table S2 Binding energies (eV) of all samples and the shift values of binding energy of Co/Ni-CAs, Ni-CAs and Co-CAs relative to CAs

|  | Binding energy of samples |  |  |  | Shift values of binding energy relative to F-0 |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Samples | S 2p3/2 (eV) | Co 2p3/2 (eV) | Ni 2p3/2 (eV) | Ca 2p3/2 (eV) |  | ΔS2p3/2 (eV) | ΔCo 2p3/2 (eV) | ΔNi 2p3/2 (eV) | ΔCa 2p3/2 |
| CAs | 162.43 | -- | -- | 347.19 | 0 |  | -- | -- | 0 |
| Co-CAs | 162.26 | 780.23 | -- | 347.32 | -0.17 |  | 0 | -- | 0.13 |
| Ni-CAs | 161.62 | -- | 854.56 | 347.60 | -0.81 |  | -- | 0 | 0.41 |
| Co/Ni-CAs | 161.48 | 781.13 | 855.26 | 347.73 | -0.95 |  | 0.90 | 0.70 | 0.54 |

Table S3 Binding energies (eV) of S 2p and the calculated sulfur vacancy concentration, -C-S=C bond for samples

|  |  |  |  |  | S 2p |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 163.3(eV) | 162.5(eV) |  | 161.4 (eV) |  |  |  |  |  |
| Samples | -C-S=C- | S2p1/2 |  | S2p3/2 |  | S2p1/2/Total (%) |  |  | -C-S=C/Total (%) |
| CAs | 299.6 | 559.3 |  | 987.3 |  | 30.3 |  |  | 16.2 |
| Co-CAs | 95.6 | 163.6 |  | 252.7 |  | 32.0 |  |  | 18.7 |
| Ni-CAs | 84.2 | 156.3 |  | 154.5 |  | 39.6 |  |  | 21.4 |
| Co/Ni-CAs | 196.5 | 231.1 |  | 137.9 |  | 40.9 |  |  | 34.8 |

Table S4 Comparison of EMW absorption performance of some representative sulfides-based absorbers

| Absorber |  | RLmin (dB) | EAB (GHz) | Matching Thickness d (mm) | Refs. |
| --- | --- | --- | --- | --- | --- |
| NixSy/CoxSy@C | -47.20 |  | 3.70 | 2.50 | [S1] |
| WS2/NiO | -53.31 |  | 4.88 | 2.22 | [S2] |
| ZnO/ZnS/CuS | -43.88 |  | 5.10 | 1.59 | [S3] |
| CuS/MXene | -45.30 |  | 5.20 | 2.00 | [S4] |
| NiS2@MoS2 | -18.13 |  | 5.17 | 1.60 | [S5] |
| CuCo2S4/C | -52.60 |  | 6.00 | 2.00 | [S6] |
| Cu2S/Cu31S16 | -15.10 |  | 6.20 | 2.30 | [S7] |
| CoS2@MoS2/rGO | -58.00 |  | 6.24 | 2.40 | [S8] |
| CaS/Ni9S8/Co9S8@C | -48.30 |  | 6.76 | 1.80 | This work |

Table S5 Electrostatic potential of samples

| Samples | Ni9S8 | Co9S8 | electrostatic potential difference (eV) |
| --- | --- | --- | --- |
| Co9S8/Ni9S8 | -8.01 | -8.34 | 0.33 |
| Co9S8/Ni9S8-Vs | -7.52 | -9.65 | 2.13 |
| Co9S8-Vs/Ni9S8 | -7.998 | -9.52 | 1.52 |

Supplementary References

- L. Gai, G. Song, Y. Li, W. Niu, L. Qin et al., Versatile bimetal sulfides nanoparticles-embedded N-doped hierarchical carbonaceous aerogels (N-NixSy/CoxSy@C) for excellent supercapacitors and microwave absorption. Carbon 179, 111–124 (2021). https://doi.org/10.1016/j.carbon.2021.04.029

- D. Zhang, Y. Xiong, J. Cheng, J. Chai, T. Liu, X. Ba, S. Ullah, G. Zheng, M. Yan, M. Cao, et al., Synergetic dielectric loss and magnetic loss towards superior microwave absorption through hybridization of few-layer WS2 nanosheets with NiO nanoparticles. Sci. Bulletin 65, 138-146 (2020). https://doi.org/10.1016/j.scib.2019.10.011

- G. Chen, L. Zhang, B. Luo, H. Wu, Optimal control of the compositions, interfaces, and defects of hollow sulfide for electromagnetic wave absorption. J. Colloid Interface Sci. 607, 24–33 (2022). https://doi.org/10.1016/j.jcis.2021.08.186

- G. Cui, L. Wang, L. Li, W. Xie, G. Gu, Synthesis of CuS nanoparticles decorated Ti3C2Tx MXene with enhanced microwave absorption performance. Prog. Nat. Sci. Mater. Int. 30, 343–351 (2020). https://doi.org/10.1016/j.pnsc.2020.06.001

- X.-J. Zhang, S.-W. Wang, G.-S. Wang, Z. Li, A.-P. Guo et al., Facile synthesis of NiS2@MoS2 core-shell nanospheres for effective enhancement in microwave absorption, RSC Adv. 7, 22454-22460 (2017). https://doi.org/10.1039/C7RA03260A

- Q. Ma, Z. Xu, X. Li, X. Cheng, Core-shell CuCo2S4 based microspheres composited with carbon black nanoparticles for effective microwave absorption, J. Alloys Compd. 938, 168577 (2023). https://doi.org/10.1016/j.jallcom.2022.168577

- W. Li, J. Chen, P. Gao, MOFs-derived hollow Copper-based sulfides for optimized electromagnetic behaviors. J. Colloid Interface Sci. 606, 719–727 (2022). https://doi.org/10.1016/j.jcis.2021.08.019

- T. Zhu, W. Shen, X. Wang, Y.-F. Song, W. Wang, Paramagnetic CoS2@MoS2 core-shell composites coated by reduced graphene oxide as broadband and tunable high-performance microwave absorbers. Chem. Eng. J. 378, 122159 (2019). https://doi.org/10.1016/j.cej.2019.122159