Supporting Information for

Aligned Ion Conduction Pathway of Polyrotaxane-Based Electrolyte with Dispersed Hydrophobic Chains for Solid-State Lithium-Oxygen Batteries

Bitgaram Kim1, , Myeong-Chang Sung2, , Gwang-Hee Lee3, , Byoungjoon Hwang2, Sojung Seo1, Ji-Hun Seo1, *, and Dong-Wan Kim2, *

1Department of Materials Science and Engineering, Korea University, 145 Anam-ro, Seongbuk-gu Seoul, 02841, Republic of Korea

2School of Civil, Environmental and Architectural Engineering, Korea University, 145 Anam-Ro, Seongbuk-gu, Seoul, 02841, Republic of Korea

3Materials Science and Chemical Engineering Center, Institute for Advanced Engineering (IAE), Yongin 17180, Republic of Korea

Bitgaram Kim, Myeong-Chang Sung, Gwang-Hee Lee have contributed equally to this work.

*Corresponding authors. E-mail: seojh79@korea.ac.kr (Ji-Hun Seo); dwkim1@korea.ac.kr (Dong-Wan Kim)

S1 Supplementary Method

S1. 1 Materials

Poly(ethylene glycol) (Mn = 10,000), dimethyl sulfoxide (DMSO) (anhydrous, ≥ 99.9%), N,N-dimethylformamide (DMF) (anhydrous, 99.8%), chloroform (anhydrous, ≥99%), butyl acrylate (≥99%), poly(ethylene glycol) methacrylate (PEGMA, Mn=500), 2,2’-azobis(2-methylpropionitrile) (AIBN) and 1-hydroxycyclohexyl phenyl ketone (PI184, 99%) were purchased from Sigma-Aldrich. 1,1’-carbonyldiimidazole (CDI), α-cyclodextrin (α-CD), polyethylene glycol diacrylate (PDA, n=approx.9), ethylenediamine, 4-(4,6-dimethoxy-1,3,5-triazin-2-yl)-4-methylmorpholinium chloride (DMTMM) and N-carbobenzoxy-L-tyrosine (Z-Try-OH), dibutyltin dilaurate (DBTDL, >95%), hexamethylene diisocyanate (HDI), 4,4’-methylene diphyenyl diisocyanate (MDI) were purchased from TCI. Lithium bis(trifluoromethanesulfonyl)imide (LiTFSI, 98+%) was purchased from Alfa Aesar. 2-isocyanatoethyl acrylate was purchased from Showa Chemical Industry. All other organic solvents (HPLC grade) were purchased from Samchun Pure Chemical Co., Ltd. (Gyeonggi-Do, Korea). All chemicals were used as received without further purification.

S1.2 Synthesis of pristine polyrotaxane (pPR) and pPR-SPE

2 g poly (ethylene glycol) was completely dissolved in 30 ml chloroform. Subsequently, 0.2 g 1,1’-carbonyldiimidazole was added and stirred for 6 h. Following that, ethylene diamine was added, and the solution was stirred for 24 h. The resulting solution was precipitated in diethyl ether to obtain PEG-bis(amine) (PEGBA) powder. 3 g of α-CD, and 1 g of PEGBA were dissolved in 35 mL of distilled water and allowed to mix for 24 h. The resulting mixture was freeze-dried and dispersed in ethanol (35 mL). Subsequently, DMTMM (0.5 g) and Z-Try-OH (0.5 g) were added and the mixture was stirred vigorously for 24 h. The resulting solution was placed in a dialysis tube (MWCO 12k) and dialyzed, and freeze-dried to obtain pPR powder. pPR-SPE was synsthesized as described in a previous paper[1]. Speficially, 0.6 pPR were disolvend in 6 mL of DMSO with 0.1 M cross-linker (HDI:MDI= 4:1, molar ratio). Then, 0.75 M LiTFSI was added to the solution and stirred until the mixture was completely dissolved. The resultant solution was poured into a PTFE mold within argon-filled glass case ,and reacted in the oven at 70 °C for 48 h.

S1.3 Synthesis of modified polyrotaxane (mPR)

1 g pPR, 2-isocyanatoethyl acrylate and 0.1 g DBTDL were dissolved in 6 mL of DMSO. The mixture was stirred vigorously for 36 h. The resulting solution was placed in a dialysis tube (MWCO 12k), dialyzed, and freeze-dried to obtain the mPR powder.

S1.4 Synthesis of poly(α-cyclodextrin) (PCD)

1 g PEGMA was dissolved in 6 mL of chloroform and added in a solution in which 0.7 g of 1,4-phenylene diisocyanate was dissolved in 9 mL of chloroform, and resulting solution was stirred for 16 h. After the reaction, the mixture was precipitated in hexane and brown isocyanate-terminated PEGMA (I-PEGMA) was obtained. The collected I-PEGMA and 1 g of α-CD were dissolved in 10 mL of DMF and stirred for 24 h. The resulting solution was then precipitated in diethyl ether to obtain the resultant (CD-PEGMA). Subsequently, 1 g of CD-PEGMA and 0.3 mL AIBN were stirred in 8 mL of DMF and polymerized at 70 °C for 24 h. The solution was then precipitated in diethyl ether. Finally, a brown powder (PCD) was obtained and dried under vacuum.

S1.5 Optimization of lithium salt concentration of mPR-SPE

Extended Fig. 1 (a) Temperature-dependent ionic conductivity of the mPR-SPE at LiTFSI concentration of 0.375M, 0.5M, 0.625M, 0.75M, and 0.875M. (b) Bar graph of ionic conductivity of the mPR-SPEs at room temperature

Ionic conductivities were investigated to determine the optimal salt concentration (0.75 M) required in mPR-SPE.

S1.6 Preparation of RuO2-Graphene (RuO2-G)

To synthesize RuO2-G, graphene (0.02 g, Angstron Materials), ruthenium (III) chloride (RuCl3·xH2O; 0.015 g, Kojima Chemical, 99%), and cetrimonium bromide (1 g, Sigma Aldrich, 95%) were dispersed in 25 mL of distilled water and ethanol (4:1, v/v). The resulting solution was sealed in a 30 mL Teflon-lined stainless-steel autoclave and heated at 150 °C for 10 h. After cooling to room temperature, the particles were washed with distilled water, filtered multiple times using a nylon membrane (Durapore, 0.22 μm, Billerica, MA, USA), and dried at 70 °C for 24 h. Subsequently, the particles were subjected to thermal treatment at 500 °C for 2 h, followed by 800 °C for 5 h under a nitrogen flow of 100 sccm.

S2 Supplementary Figures and Tables

Fig. S1 (a) 1H NMR spectrum of pPR (400 MHz, DMSO-D6). (b) 1H NMR spectrum of mPR (400 MHz, DMSO-D6). (c) X-ray diffraction (XRD) of pPR and mPR. (d) Expected crystalline structure of mPR-SPE (In the view of one side of hexagonal lattice)

Fig. S2 Schematic of the crystalline structure by α-CD in polyrotaxane (PR)

Fig. S3 (a) Water contact angle of Teflon. (b) Geometrically optimized three-dimensional (3D) structure of H2O and PEFE unit of Teflon

Fig. S4 (a) Chemical structures of the three types of polymers containing acryl group. (b) 1H NMR spectrum (400 MHz, DMSO-d6) of PCD (c) FT-IR spectra of mPR-SPE, PCD-SPE and PDA-SPE before and after curing

Fig. S5 (a) Ionic conductivity of PDA-SPE, PCD-SPE, and mPR-SPE at 25 °C. (b) Li+ transference number of PCD-SPE. (c) Li+ transference number of PDA-SPE

Fig. S6 Comparison of the ionic conductivity and oxidation stability with those of recently reported polymer-based electrolytes

Table S1 Comparison of ionic conductivity of recently reproted polymer-based electrolytes

| Polymer | Salt | Ionic conductivity at 25 °C (S cm-1) | Oxidation stability (Voltage) | Refs. |
| --- | --- | --- | --- | --- |
| mPR | LiTFSI | 2.8E-3 (at 25 °C) | 4.8 | This study |
| PRX | LiNO3 | 5.93E-3 (at 2 5°C) | 4.7 | [S1] |
| PAN | LiTFSI | 2.0E-5 (at 30 °C) | 4.8 | [S2] |
| HFBA+MBAM | LiTFSI | 1.01E-3 (at 25 °C) | 4.58 | [S3] |
| Elastic epoxy | LiTFSI | 3.5E-4 (at 25 °C) | 4.4 | [S4] |
| P(VDF-HFP) | LiTFSI (EMIMTFSI) | 0.53E-3 (at 20 °C) | 4.9 | [S5] |
| PEGMA | LiDFOB | 1.3E-4 (at 30 °C) | 4.8 | [S6] |
| DOL + PEE | LiTFSI | 2.36E-3 (at 25 °C) | 4.5 | [S7] |
| PALE | LiTFSI | 0.84E-3 (at 25 °C) | 5.04 | [S8] |
| PVCM | LiDFOB | 8.61E-4 (at 25 °C) | 4.8 | [S9] |
| MEDP+EGMEA | LiTFSI | 1.1E-4 (at 25 °C) | 5 | [S10] |
| PEO+PMMA | LiTFSI | 1.08E-3 (at 25 °C) | 4.7 | [S11] |
| PEO+LLZTO | LiTFSI | 1.96E-4 (at 40 °C) | 5.1 | [S12] |
| P(VEC-CEA) | LiTFSI | 2.63E-4 (at 25 °C) | 5.0 | [S13] |
| PVDF-HFP | LiTFSI | 1.33E-3 (at 25 °C) | 4.5 | [S14] |
| PEO+PEGDE+BADGE | LiPF6 | 1.0E-3 (at 25 °C) | 4.37 | [S15] |
| PEGMA+UPyMA | LiTFSI | 3.8E-3 (at 25 °C) | 4.6 | [S16] |
| PEGDA+UPyMA | LiTFSI | 3.42E-4 (at 25°C) | 5.2 | [S17] |

Fig. S7 (a) DSC data of PDA-SPE, PCD-SPE, and mPR-SPE with and without salts. (b) XRD data of PDA-SPE, PCD-SPE, and mPR-SPE with and without salts

Table S2 Transition temperature and thermodynamic variables measured during the 2nd run of the DSC heat flow

| Sample | Tg (°C) | Tc (°C) | Tc (°C) |
| --- | --- | --- | --- |
| PDA-SPE | –47 | - | - |
| PDA-SPE (without LiTFSI) | –31 | - | - |
| PCD-SPE | –44 | - | 106.3 |
| PCD-SPE (without LiTFSI) | –12 | - | 105.6 |
| mPR-SPE | –45 | - | - |
| mPR-SPE (without LiTFSI) | –25 | - | - |
| Tg: Glass transition temperature Tc: Crystallization temperature Tm: Melting temperature |  |  |  |

Fig S8 Enlarged profiles of cycling performance of the symmetric Li cells with mPR-SPE at a current density of 0.2 mA cm-2 corresponding to (a) 75-80 cycles and (b) 345-350 cycles

Fig. S9 (a) Main component of solid-state lithium oxygen battery (LOB). SEM images of (b) RuO2-G catalyst, (c) carbon fibre film. Mass of cathode material loading (Wcat) was calculated by relevant electrode information

cathode surface area = 0.785 cm2

loading mass of catalyst = 0.35 mg

Specific capacity (Ah/gcat) = current density (A/gcat) × 1 h,

Wcat = 0.35mg0.785cm2 = 0.45 mg/cm2

Fig. S10 Galvanostatic discharge-charge curves of solid-state Li-O2 battery cell at a current rate of 500 mA g−1 and a fixed capacity limit of 1000 mA h g−1 in different polyelectrolytes of (a) mPR-SPE and (b) pPR-SPE

Table S3 Comparison of electrocatalytic performances of recently applied polymer-based solid-state LOBs

| Polymer | Catalysts | Limited capacity (mA h g–1) | Current density (mA g–1) | Cycle (number) | Lithium salt & solvent | Refs. |
| --- | --- | --- | --- | --- | --- | --- |
| mPR | RuO2-G Carbon fibre film | 500 | 100 [0.045 mA cm-2] | 300 | 0.75 M LiTFSI in DMSO | This study |
|  |  | 1000 | 500 [0.225 mA cm-2] | 202 | 0.75 M LiTFSI in DMSO | This study |
| PVDF-HFP @SiO2-SO3Li | Ru@C | 600 | 100 | 370 | 1.0 M LiTFSI in TEGDME | [S18] |
| PTFE @XPEG/SNPC | Super P | 1000 | 500 | 277 | 1.0 M LiTFSI in TEGDME | [S19] |
| MSTP-BQ | CNTs/LiFePO4 | 500 | 500 | 200 | LiTFSI in TEGDME | [S20] |
| SN-PCE (PVDF-HFP, BHT) | Ru-CNTs | 500 | 200 | 150 | 1.0 M LiCF3SO3 in DMSO | [S21] |
| PTFE@PS | Super P | 500 | 500 | 149 | 1.0 M LiTFSI in TEGDME | [S22] |
| P(VDF-HFP) + silica | Ru-CNTs | 1000 | 500 | 145 | LiTFSI in DMAc | [S23] |
| PEGMA +MTA | Pd3Co/MWCNT | 500 | 100 | 125 | 1.0 M LiCF3SO3 in TEGDME | [S24] |
| P(VDF-HFP) + silica | Ru@Super P | 1000 | 200 | 89 | 1.0 M LiTFSI in TEGDME | [S25] |
| P(VDF-HFP) | Super P | 500 | 100 | 56 | 1.0 M LiTFSI in TEGDME | [S26] |
| P(VDF-HFP) | Carbon black | 500 | 500 | 50 | 1.0 M LiTFSI in TEGDME | [S27] |
| FST-GPE | CNT | 1000 | 500 | 30 | 1.0 M LiTFSI in TEGDME | [S28] |
| P(VDF-HFP) | SGL Carbon (gas diffusion layer) | 198 | 200 | 89 | 1.0 M LiTFSI in TEGDME | [S29] |
| P(VDF-HFP) | Co3O4@CC | 0.125 (mA h cm-2) | 0.025 mA cm-2 | 101 | LiTFSI in DMF, THF | [S30] |
| PEO-based gel polymer (PG) | Carbon paper | 1.0 (mA h cm-2) | 0.2 mA cm-2 | 110 | 1.0 M LiTFSI in TEGDME | [S31] |
| PMMA/SiO2/PP | CNTs | 0.5 (mA h cm-2) | 0.1 mA cm-2 | 116 | LiTFSI in TEGDME | [S32] |
| P(VDF-HFP) | Co3O4/RuO2 | 0.1 (mA h cm-2) | 0.1 mA cm-2 | 553 | LiClO4 in TEGDME | [S33] |

Fig. S11 Galvanostatic discharge-charge curves of solid-state Li-O2 battery cell with (a) mPR-SPE and (b) pPR-SPE at 45 °C. (c) Cycling performance of mPR-SPE and pPR-SPE cell associated with Fig. S11a, b

Fig. S12 (a) Galvanostatic cycling of mPR-SPE cell at different capacity limits. (b) Galvanostatic cycling of mPR-SPE cell at different current densities at a fixed capacity limit of 500 mAh g−1

Fig. S13 Illustration of polymer infiltration and cell structure for in situ Raman analysis

Fig. S14 In situ Raman spectra from the discharge to the charge process of mPR-SPE cell recorded every 4 h in the galvanostatic discharge–charge curves

Supplementary References

- J. Seo, G.-H. Lee, J. Hur, M.-C. Sung, J.-H. Seo et al., Mechanically interlocked polymer electrolyte with built-in fast molecular shuttles for all-solid-state lithium batteries. Adv. Energy Mater. 11, 2102583 (2021). https://doi.org/10.1002/aenm.202102583

- C. Liu, R.L. Sacci, R. Sahore, G.M. Veith, N.J. Dudne et al., Polyacrylonitrile-based electrolytes: How processing and residual solvent affect ion transport and stability. J. Power Sources 527, 231165 (2022). https://doi.org/10.1016/j.jpowsour.2022.231165

- S. Qi, M. Li, Y. Gao, W. Zhang, S. Liu et al., Enabling scalable polymer electrolyte with dual-reinforced stable interface for 4.5 V lithium-metal batteries. Adv Mater. 35, 2304951 (2023). https://doi.org/10.1002/adma.202304951

- Z. Zeng, X. Chen, M. Sun, Z. Jiang, W. Hu et al., Nanophase-separated, elastic epoxy composite thin film as an electrolyte for stable lithium metal batteries. Nano Lett. 21, 3611-3618 (2021). https://doi.org/10.1021/acs.nanolett.1c00583

- M. Yao, Q. Ruan, Y. Wang, L. Du, Q. Li et al., A robust dual-polymer@inorganic networks composite polymer electrolyte toward ultra-long-life and high-voltage Li/Li-rich metal battery. Adv. Funct. Mater. 33, 2213702 (2023). https://doi.org/10.1002/adfm.202213702

- D. Zhang, Y. Liu, Z. Sun, Z. Liu, X. Xu et al., Eutectic-based polymer electrolyte with the enhanced lithium salt dissociation for high-performance lithium metal batteries. Angew. Chem. Int. Ed. 62, e202310006 (2023). https://doi.org//10.1002/anie.202310006

- J. Zhu, J. Zhang, R. Zhao, Y. Zhao, J. Liu et al., In situ 3d crosslinked gel polymer electrolyte for ultra-long cycling, high-voltage, and high-safety lithium metal batteries. Energy Storage Mater. 57, 92-101 (2023). https://doi.org/10.1016/j.ensm.2023.02.012

- S. Chai, Z. Chang, Y. Zhong, Q. He, Y. Wang et al., Regulation of interphase layer by flexible quasi-solid block polymer electrolyte to achieve highly stable lithium metal batteries. Adv. Funct. Mater. 33, 2300425 (2023). https://doi.org/10.1002/adfm.202300425

- M. Bai, X. Tang, M. Zhang, H. Wang, Z. Wang et al., An in-situ polymerization strategy for gel polymer electrolyte Si||Ni-rich lithium-ion batteries. Nat. Commun. 15, 5375 (2024). https://doi.org/10.1038/s41467-024-49713-z

- S. Wang, Q. Li, H. Gao, H. Cai, C. Liu et al., A polyzwitterion-mediated polymer electrolyte with high oxidative stability for lithium-metal batteries. Small 19, 2304677 (2023). https://doi.org/10.1002/smll.202304677

- X. Ye, J. Liang, J. Hu, D. Wu, Y. Li et al., An ultra-thin polymer electrolyte for 4.5 V high voltage LiCoO2 quasi-solid-state battery. Chem. Eng. J. 455, 140846 (2023). https://doi.org/10.1016/j.cej.2022.140846

- K. Khan, M.B. Hanif, H. Xin, A. Hussain, H.G. Ali et al., PEO-based solid composite polymer electrolyte for high capacity retention all-solid-state lithium metal battery. Small 20, 2305772 (2024). https://doi.org/10.1002/smll.202305772

- S. Ma, Y. Zhang, D. Zhang, Y. Zhang, W. Li et al., –C≡N functionalizing polycarbonate-based solid-state polymer electrolyte compatible to high-voltage cathodes. J. Energy Chem. 98, 422-431 (2024). https://doi.org/10.1016/j.jechem.2024.06.052

- Y. Zeng, L. Zhao, J. Zhang, Q. Li, D. Sun et al., La2O3 filler's stabilization of residual solvent in polymer electrolyte for advanced solid-state lithium-metal batteries. Small Sci. 3, 2300017 (2023). https://doi.org/10.1002/smsc.202300017

- S.H. Kim, N. Park, W. Bo Lee, J.H. Park, Functional sulfate additive-derived interfacial layer for enhanced electrochemical stability of PEO-based polymer electrolytes. Small. 20, 2309160 (2024). https://doi.org/10.1002/smll.202309160

- F. Chen, C. Guo, H. Zhou, M.W. Shahzad, T.X. Liu et al., Supramolecular network structured gel polymer electrolyte with high ionic conductivity for lithium metal batteries. Small 18, 2106352 (2022). https://doi.org/10.1002/smll.202106352

- H. Wang, J. Song, K. Zhang, Q. Fang, Y. Zuo et al., A strongly complexed solid polymer electrolyte enables a stable solid state high-voltage lithium metal battery. Energy Environ. Sci. 15, 5149-5158 (2022). https://doi.org/10.1039/D2EE02904A

- H. Wang, J. Song, K. Zhang, Q. Fang, Y. Zuo et al., A strongly complexed solid polymer electrolyte enables a stable solid state high-voltage lithium metal battery. Energy Environ. Sci. 15(12), 5149-5158 (2022). https://doi.org/10.1039/D2EE02904AG  Zheng, T. Yan, Y. Hong, X. Zhang, J. Wu et al., A non-newtonian fluid quasi-solid electrolyte designed for long life and high safety Li–O2 batteries. Nat. Commun. 14, 2268 (2023). https://doi.org/10.1038/s41467-023-37998-5

- J. Kim, A. Le Mong, D. Kim, Thin, flexible, and high-performance solid-state polymer electrolyte membranes for Li–O2 batteries. ACS Appl. Energy Mater. 6, 2877-2885 (2023). https://doi.org/10.1021/acsaem.2c03804

- M. Mushtaq, X. Guo, Z. Zhang, Z. Lin, X. Li et al., Dual-function redox mediator enhanced lithium-oxygen battery based on polymer electrolyte. J. Mater. Sci. Technol. 113, 199-206 (2022). https://doi.org/10.1016/j.jmst.2021.10.009

- J. Wang, G. Huang, K. Chen, X.-B. Zhang, An adjustable-porosity plastic crystal electrolyte enables high-performance all-solid-state lithium-oxygen batteries. Angew. Chem. Int. Ed. 59, 9382-9387 (2020). https://doi.org/10.1002/anie.202002309

- Z. Li, Y.-E. Liu, S. Weng, X. Wu, X. Yu et al., Oxygen-permeable and moisture-proof membrane for stable Li-O2/air batteries in humid working environment. Energy Storage Mater. 58, 94-100 (2023). https://doi.org/10.1016/j.ensm.2023.03.018

- C.-L. Li, G. Huang, Y. Yu, Q. Xiong, J.-M. Yan et al., Three birds with one stone: An integrated cathode–electrolyte structure for high-performance solid-state lithium–oxygen batteries. Small. 18, 2107833 (2022). https://doi.org/10.1002/smll.202107833

- S.M. Cho, J. Shim, S.H. Cho, J. Kim, B.D. Son et al., Quasi-solid-state rechargeable Li–O2 batteries with high safety and long cycle life at room temperature. ACS Appl. Mater. Interfaces 10, 15634-15641 (2018). https://doi.org/10.1021/acsami.8b00529

- C. Shu, J. Long, S.-X. Dou, J. Wang, Component-interaction reinforced quasi-solid electrolyte with multifunctionality for flexible Li–O2 battery with superior safety under extreme conditions. Small. 15, 1804701 (2019). https://doi.org/10.1002/smll.201804701

- T. Li, C. Wang, J. Cheng, J. Guo, A. Xiao et al., Janus polymer composite electrolytes improve the cycling performance of lithium–oxygen battery. ACS Appl. Mater. Interfaces 12, 12857-12866 (2020). https://doi.org/10.1021/acsami.9b23395

- W.-C. Lai, R.-W. Fan, A simple low-cost method to prepare gel electrolytes incorporating graphene oxide with increased ionic conductivity and electrochemical stability. J Electroanal. Chem. 907, 115889 (2022). https://doi.org/10.1016/j.jelechem.2021.115889

- X. Zou, Q. Lu, Y. Zhong, K. Liao, W. Zhou et al., Flexible, flame-resistant, and dendrite-impermeable gel-polymer electrolyte for Li–O2/air batteries workable under hurdle conditions. Small. 14, 1801798 (2018). https://doi.org/10.1002/smll.201801798

- M. Celik, A. Kızılaslan, M. Can, T. Cetinkaya, H. Akbulut, Electrochemical investigation of PVDF: HFP gel polymer electrolytes for quasi-solid-state Li-O2 batteries: Effect of lithium salt type and concentration. Electrochim. Acta 371, 137824 (2021). https://doi.org/10.1016/j.electacta.2021.137824

- M. Li, Y. Lian, Z. Li, M. Zhu, Q. Qiao et al., An integrated architecture of mutually infiltrated nanoarray cathode and polymer electrolyte improves the performances of solid-state lithium−oxygen batteries. Electrochim. Acta 453, 142360 (2023). https://doi.org/10.1016/j.electacta.2023.142360

- H.-S. Lim, W.-J. Kwak, S. Chae, S. Wi, L. Li et al., Stable solid electrolyte interphase layer formed by electrochemical pretreatment of gel polymer coating on li metal anode for lithium–oxygen batteries. ACS Energy Lett. 6, 3321-3331 (2021). https://doi.org/10.1021/acsenergylett.1c01144

- X. Liu, X. Xin, L. Shen, Z. Gu, J. Wu et al., Poly(methyl methacrylate)-based gel polymer electrolyte for high-performance solid state Li–O2 battery with enhanced cycling stability. ACS Appl. Energy Mater. 4, 3975-3982 (2021). https://doi.org/10.1021/acsaem.1c00344

- C. Zhao, J. Liang, Q. Sun, J. Luo, Y. Liu et al., Ultralong-life quasi-solid-state Li-O2 batteries enabled by coupling advanced air electrode design with li metal anode protection. Small Methods 3, 1800437 (2019). https://doi.org/10.1002/smtd.201800437