Supporting Information for

MoS2 Lubricate-Toughened MXene/ANF Composites for Multifunctional Electromagnetic Interference Shielding

Jiaen Wang1, #, Wei Ming1, #, Longfu Chen1, Tianliang Song1, Moxi Yele1, Hao Zhang1, Long Yang1, Gegen Sarula1, Benliang Liang1, *, Luting Yan 1, * and Guangsheng Wang 2, *

1 School of Physical Science and Engineering, Beijing Jiaotong University, Beijing 100044, P. R. China

2 Key Laboratory of Bio-Inspired Smart Interfacial Science and Technology of Ministry of Education, School of Chemistry, Beihang University, Beijing 100191, P. R. China

#Jiaen Wang and Wei Ming contributed equally to this work.

*Corresponding authors. E-mail: blliang@bjtu.edu.cn (Benliang Liang); ltyan@bjtu.edu.cn (Luting Yan); wanggsh@buaa.edu.cn (Guangsheng Wang)

Supplementary Figures and Tables

Fig. S1 (a) SEM image of Ti3AlC2. (b) SEM image of m-MXene. (c) TEM image of MXene. (d) TEM image of ANF

Fig. S2 TEM images of MoS2

Fig. S3 (a) Cross section SEM image of ternary MXene/ANF-MoS2 composite films. (b) Ternary MXene/ANF-MoS2 composite film digital picture

Fig. S4 (a) XRD spectrum of MoS2. (b) XRD spectrum of ANF-MoS2 composite films. (c) XRD spectrum of ANF/MXene-MoS2

Fig. S5 XPS spectrum of MoS2

Fig. S6 Fracture cross section EDS mapping images

Fig. S7 Tensile stress-strain curves of different composite films: (a) ANF/MoS2; (b) 2AMMO; (c) 4AMMO; (d) 5AMMO; (e) 6AMMO; (f) 7AMMO

Fig. S8 The tensile stress-strain curves of ternary MXene/ANF-MoS2 composite films and control samples: binary MXene/ANF composite films [S1]

Fig. S9 Fracture surface SEM images: (a) ANF/MoS2. (b) 2AMMO. (c) 4AMMO. (d) 5AMMO. (e) 6AMMO. (f) 7AMMO

Fig. S10 Fracture cross-section SEM images: (a) ANF/MoS2. (b) 2AMMO. (c) 4AMMO. (d) 5AMMO. (e) 6AMMO. (f) 7AMMO

Fig. S11 Fracture surface EDS mapping images

Fig. S12 Electrical conductivity of AMMO composite films

Fig. S13 EMI shielding effectiveness of ternary MXene/ANF-MoS2 composite films in 1-18 GHz

Fig. S14 EMI shielding result of a Bluetooth headset

Fig. S15 (a) I-V curve of ternary MXene/ANF-MoS2 composite films. (b) The linear fitting of temperature and U2

Fig. S16 Infrared thermal images of ternary MXene/ANF-MoS2 composite films under different electric heating voltages

Fig. S17 Infrared thermal images in photothermal conversion: (a) binary MXene/ANF composite films; (b) ternary MXene/ANF-MoS2 composite films

Fig. S18 The comparison between binary 5AM and ternary 5AMMO

Table S1 The detailed additive amounts of different components in the experimental preparation process

|  | MXene：ANF | MXene (0.29 wt%) | ANF (1 wt%) | MoS2 (0.55 wt%) | Filler content |
| --- | --- | --- | --- | --- | --- |
| ANF/MoS2 |  |  | 1.8 g | 1.4025 g | 0.3 |
| 2AMMO | 2:8 | 1.55 g | 1.8 g | 1.4025 g | 0.4041 |
| 4AMMO | 4:6 | 4.14 g | 1.8 g | 1.4025 g | 0.5228 |
| 5AMMO | 5:5 | 6.21 g | 1.8 g | 1.4025 g | 0.5883 |
| 6AMMO | 6:4 | 9.31 g | 1.8 g | 1.4025 g | 0.6585 |
| 7AMMO | 7:3 | 14.48 g | 1.8 g | 1.4025 g | 0.7341 |

Table S2 Mechanical performance of MXene/ANF and MXene/ANF-MoS2 composite films

|  | Tensile Strength (MPa) | Strain-to-failure (%) | Toughness (MJ∙m-3) |
| --- | --- | --- | --- |
| ANF | 60.02.9 | 44.03.7 | 16.82.8 |
| 2AM | 136.55.1 | 34.00.7 | 29.74.1 |
| 4AM | 140.91.8 | 26.32.5 | 20.32.1 |
| 5AM | 105.76.4 | 22.11.7 | 13.04.1 |
| 6AM | 85.54.4 | 18.31.9 | 8.81.8 |
| 7AM | 82.15.1 | 14.41.7 | 6.10.3 |
| ANF/MoS2 | 67.9±8.6 | 57.0±6.2 | 21.4±5.0 |
| 2AMMO | 181.8±1.4 | 32.2±2.4 | 36.5±2.6 |
| 4AMMO | 211.9±7.0 | 27.0±2.4 | 37.6±2.6 |
| 5AMMO | 167.3±9.1 | 25.8±0.7 | 26.3±0.8 |
| 6AMMO | 86.7±6.8 | 28.1±0.7 | 14.5±1.1 |
| 7AMMO | 68.1±4.4 | 24.5±1.6 | 9.4±1.0 |

Table S3 The comparison of toughness and strain-to-failure between ternary MXene/ANF-MoS2 composite films and other works

| Materials | Strain-to-failure (%) | Toughness (MJ∙m-3) | References |
| --- | --- | --- | --- |
| MMT/PVA-GA 70/30 | 0.33 | 0.5 | [S2] |
| MTM/PVA 70/30 | 1.7 | 2.1 | [S3] |
| MTM/CS 65/35 | 2.3 | 1.3 | [S4] |
| MTM/PDDA 70/30 | 2.1 | 1.4 | [S5] |
| MMT/CMC 20/80 | 2.6 | ~5.3 | [S6] |
| RGO/CS 95/5 | 10.4 | 17.7 | [S7] |
| RGO/MoS2-TPU 86/14 | 5.8 | 6.9 | [S8] |
| RGO/CS-Cu+ 91/9 | 4.4 | 14 | [S9] |
| RGO/CMC-Mn2+ 87/13 | 3.7 | 6.6 | [S10] |
| RGO/PVA 58/42 | 10.4 | 8.5 | [S11] |
| GO/Al2O3-CMC 8/92 | 5 | 8.2 | [S12] |
| GO/PAA 95/5 | 7.9 | 8.9 | [S13] |
| MTM/NFC 50/50 | 2.8 | 2.3 | [S14, S15] |
| MXene/NFC 50/50 | 16.7 | 14.8 | [S16] |
| Aminoclay/TOCN 33/67 | 11.7 | 20 | [S17] |
| RGO/TOCN 95/5 | 6.2 | 15.6 | [S18] |
| RGO/DWNT 95/5 | 7.9 | 9.2 | [S19] |
| Alumina/CMC/Cu2+ 13.3/20 | ~6.8 | 17.2 | [S20] |
| MXene/BN-PBO 25/75 | ~9.8 | ~8 | [S21] |
| MXene/ANF 20/80 | 15.3 | 21.87 | [S22] |
| MXene/ANF 20/80 | 12.45 | 19.97 | [S23] |
| MXene/ heterocyclic aramid 50/50 | 6.9 | 16.29 | [S24] |
| CuNW/ MXene/ANF 60/40 | 18.25 | 15.59 | [S25] |
| Al–Ti3C2Tx/ANF 40/60 | 8.05 | 9.96 | [S26] |
| Ti3C2Tx /BC | 11.2 | 8.1 | [S27] |
| 2AMMO | 32.19 | 36.54 | This Work |
| 4AMMO | 26.95 | 37.6 |  |
| 5AMMO | 25.78 | 26.27 |  |
| 6AMMO | 28.08 | 14.51 |  |
| 7AMMO | 24.47 | 9.44 |  |

Table S4 EMI SE of ternary MXene/ANF-MoS2 composite films

|  | Thickness(μm) | SER (dB) | SEA (dB) | SET (dB) |
| --- | --- | --- | --- | --- |
| 2AMMO | 19 | 7.10 | 11.32 | 18.42 |
| 4AMMO | 20 | 13.23 | 12.64 | 25.87 |
| 5AMMO | 25 | 14.33 | 26.62 | 40.95 |
| 6AMMO | 33 | 13.88 | 30.00 | 43.88 |
| 7AMMO | 48 | 14.95 | 30.05 | 45.00 |

Table S5 The comparison statistic between ternary MXene/ANF-MoS2 composite films and binary MXene/ANF composite films

| Material | SEA/SER | Strain-to-failure (%) | Toughness (MJ∙m-3) | Electric heating Temperature (℃) | Photothermal conversion temperature (℃) | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| 6AM | 1.54 | 18.80 | 8.82 | 88.6 | 43.8 | [S1] |
| 6AMMO | 2.16 | 28.08 | 14.51 | 91.6 | 53.7 | This work |

Table S6 The comparison statistic between ternary MXene/ANF-MoS2 composite films and binary MXene/ANF composite films

| Material | SEA/SER | Strain-to-failure (%) | Toughness (MJ∙m-3) | Tensile strength (℃)) | SET (℃) | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| 5AM | 1.49 | 21.86 | 12.83 | 104.65 | 40.02 | [1] |
| 5AMMO | 1.86 | 25.78 | 26.27 | 167.30 | 40.95 | This work |

Table S7 Comparison statistic about filler content, strain-to-failure and EMI SE of the MXene/ANF composite films with other reported materials.

| Material | Thickness(μm) | Fequen-cy Range(GHz) | Filler content (wt%) | Strain-to-failure (%) | EMI SE (dB) | Toughness (MJ∙m-3) | Refer-ences |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ti3C2TX/BC | 6.7 | 8.2-12.4 | 44.9 | 7.6 | 25 | - | [S28] |
|  | 5.2 |  | 55.8 | 6.6 | 27 | - |  |
|  | 4 |  | 76.9 | 2.4 | 38 | - |  |
| Ti3C2TX/PEDOT:PSS | 15.2 | 8.2-12.4 | 75.0 | 1.5 | 9 | - | [S29] |
|  | 12.5 |  | 80.0 | 0.82 | 24 | - |  |
| Ti3C2TX/PEDOT:PSS | 6.6 | 8.2-12.5 and 11.9-18 | 70 | 0.3 | 42 | - | [S30] |
| Ti3C2TX/CNF | 167 | 8.2-12.4 | 50 | 16.7 | 25 | 14.8 | [S16] |
|  | 74 |  | 80 | 4.9 | 26 | 2.0 |  |
|  | 47 |  | 90 | 3.1 | 24 | 1.2 |  |
| Ti3C2TX/CNF | 35 | 8.2-12.4 | 52.8 | 4.3 | 41 | - | [S31] |
| Ti3C2TX/PVA | - | 8-12 | 35.5 | 5.0 | 37 | - | [S32] |
| Ti3C2TX/TOCNF | 33 | 8.2-12.4 | 30 | 3.6 | 29 | 4.1 | [S33] |
|  | 38 |  | 50 | 2.1 | 35 | 1.7 |  |
| PIF/ Ti3C2TX | - | 8.2-12.4 | 13.8 | 10 | 22 | - | [S34] |
|  | 256 |  | 49.1 | 3 | 40 | - |  |
| Ti3C2TX /cellulose | - | 8.2-12.4 | 20.0 | 4 | 34.9 | - | [S35] |
| PVDF/Ti3C2TX/AgNWs | 300 | 8.2-12.4 | 15 | 9.47 | 25 | - | [S36] |
| Ti3C2TX /BCNFs | 11.4 | 8.2-12.4 | 50 | 2.6 | 42 | - | [S37] |
|  | - |  | 87.5 | 1.4 | 54 | - |  |
| Ti3C2TX /SA/Ca2+ | 2.8 | 0.3-18 | 80 | 3.8 | 46 | - | [S38] |
| MXene/BC/APP | - | 8.2-12.4 | 80 | 4.3 | 41 | 2.9 | [S39] |
| MXene/ heterocyclic aramid | 16 | 8.2-12.4 | 50 | 6.9 | 25.9 | 16.29 | [S24] |
|  | 14.4 |  | 60 | 3.51 | 34.2 | 5.81 |  |
| Al–Ti3C2Tx/ANF | - | 8.2-12.4 | 40 | 8.05 | 39.1 | 9.96 | [S26] |
| Ti3C2Tx /BC | - | 8.2-12.4 | 50 | 11.2 | 43.7 | 8.1 | [S27] |
| f-Ti3C2Tx /PNFs | 1705 | 8.2-12.4 | 50 | 16 | 28 | - | [S40] |
| MXene/MMT-CNF | - | 8.2-12.4 | 30 | 7 | 45 | - | [S41] |
| MXeneAgNW-CNF | 26 | 8.2-12.4 | 30 | 5.5 | 44 | - | [S42] |
| Ti3C2TX /CMC | 3 | 0.3-18 | 90 | 4.5 | 53 | - | [S43] |
| Ti3C2TX /ANF | 5.1 | 8.2-12.4 | 20 | 7 | 13 | 11 | [S44] |
|  | 4.5 |  | 40 | 2.8 | 28 | 4.5 |  |
|  | 3.9 |  | 60 | 1.5 | 33 | 2 |  |
|  | 3.2 |  | 80 | 1.7 | 39 | 1.8 |  |
| Ti3C2TX /ANF | 23 | 8.2-12.4 | 20 | 8.45 | 12.74 | - | [S45] |
|  | 22 |  | 40 | 7.23 | 19.43 | - |  |
|  | 20 |  | 60 | 2.20 | 28.54 | - |  |
|  | 17 |  | 80 | 1.80 | 30.0 | - |  |
| Ti3C2TX /ANF | - | 8.2-12.4 | 20 | 3.3 | 8 | 5.1 | [S46] |
|  | - |  | 40 | 3.0 | 26 | 5.3 |  |
|  | - |  | 60 | 1.74 | 35 | 1.2 |  |
|  | - |  | 80 | 1.75 | 42 | 1.1 |  |
| Ti3C2TX /ANF | 12 | 8.2-12.4 | 10 | 13.3 | 27 | 13.7 | [S47] |
|  | 12 |  | 20 | 11.9 | 30 | 9.5 |  |
|  | 9 |  | 30 | 12.4 | 33 | 9.9 |  |
|  | 9 |  | 40 | 8.1 | 41 | 6.3 |  |
| Ti3C2TX /ANF | - | 8.2-12.4 | 20 | 15.30 | 8 | 21.87 | [S22] |
|  | - |  | 40 | 7.52 | 19 | 13.39 |  |
|  | 40 |  | 60 | 5.41 | 39 | 6.01 |  |
|  | 37 |  | 80 | 3.26 | 50 | 2.37 |  |
| Ti3C2TX /ANF | 10 | 8.2-12.4 | 20 | 12.45 | 24.17 | 19.97 | [S23] |
|  | 12 |  | 40 | 7.17 | 35.09 | 17.35 |  |
|  | 15 |  | 60 | 5.25 | 46.89 | 7.71 |  |
|  | 28 |  | 80 | 5.03 | 53.48 | 5.77 |  |
| Pure MXene | 3.4 | 0.3-18 | 100 | 2.26 | 60.9 | - | [S43] |
| This work | 19 | 8.2-12.4 | 40.42 | 32.19 | 18.42 | 36.54 |  |
|  | 20 |  | 52.28 | 26.95 | 25.87 | 37.6 |  |
|  | 33 |  | 65.85 | 28.08 | 43.88 | 14.51 |  |
|  | 48 |  | 73.41 | 24.47 | 45.00 | 9.44 |  |

Supplementary References

- J. Wang, T. Song, W. Ming, M. Yele, L. Chen et al., High MXene loading, nacre-inspired MXene/ANF electromagnetic interference shielding composite films with ultralong strain-to-failure and excellent joule heating performance. Nano Res. 17, 2061-2069 (2024). https://doi.org/10.1007/s12274-023-6232-y

- P. Podsiadlo, A. K. Kaushik, E. M. Arruda, A. M. Waas, B. S. Shim et al., Ultrastrong and stiff layered polymer nanocomposites. Science 318, 80-83 (2007). https://doi.org/10.1126/science.1143176

- A. Walther, I. Bjurhager, J.-M. Malho, J. Pere, J. Ruokolainen et al., Large-area, lightweight and thick biomimetic composites with superior material properties via fast, economic, and green pathways. Nano Lett. 10, 2742-2748 (2010). https://doi.org/10.1021/nl1003224

- H.-B. Yao, Z.-H. Tan, H.-Y. Fang, S.-H. Yu, Artificial nacre-like bionanocomposite films from the self-assembly of chitosan–montmorillonite hybrid building blocks. Angew. Chem. Int. Ed. 49, 10127-10131 (2010). https://doi.org/10.1002/anie.201004748

- A. Walther, I. Bjurhager, J.-M. Malho, J. Ruokolainen, L. Berglund et al., Supramolecular control of stiffness and strength in lightweight high-performance nacre-mimetic paper with fire-shielding properties. Angew. Chem. Int. Ed. 49, 6448-6453 (2010). https://doi.org/10.1002/anie.201001577

- P. Das, S. Schipmann, J.-M. Malho, B. Zhu, U. Klemradt et al., Facile access to large-scale, self-assembled, nacre-inspired, high-performance materials with tunable nanoscale periodicities. ACS Appl. Mater. Interfaces 5, 3738-3747 (2013). https://doi.org/10.1021/am400350q

- S. Wan, J. Peng, Y. Li, H. Hu, L. Jiang et al., Use of synergistic interactions to fabricate strong, tough, and conductive artificial nacre based on graphene oxide and chitosan. ACS Nano 9, 9830-9836 (2015). https://doi.org/10.1021/acsnano.5b02902

- S. Wan, Y. Li, J. Peng, H. Hu, Q. Cheng et al., Synergistic toughening of graphene oxide–molybdenum disulfide–thermoplastic polyurethane ternary artificial nacre. ACS Nano 9, 708-714 (2015). https://doi.org/10.1021/nn506148w

- Y. Cheng, J. Peng, H. Xu, Q. Cheng, Glycera-inspired synergistic interfacial interactions for constructing ultrastrong graphene-based nanocomposites. Adv. Funct. Mater. 28, 1800924 (2018). https://doi.org/10.1002/adfm.201800924

- S. Gong, Q. Zhang, R. Wang, L. Jiang, Q. Cheng, Synergistically toughening nacre-like graphene nanocomposites via gel-film transformation. J. Mater. Chem. A 5, 16386-16392 (2017). https://doi.org/10.1039/C7TA03535G

- N. Zhao, M. Yang, Q. Zhao, W. Gao, T. Xie et al., Superstretchable nacre-mimetic graphene/poly(vinyl alcohol) composite film based on interfacial architectural engineering. ACS Nano 11, 4777-4784 (2017). https://doi.org/10.1021/acsnano.7b01089

- H. Zhao, Y. Yue, Y. Zhang, L. Li, L. Guo, Ternary artificial nacre reinforced by ultrathin amorphous alumina with exceptional mechanical properties. Adv. Mater. 28, 2037-2042 (2016). https://doi.org/10.1002/adma.201505511

- S. Wan, H. Hu, J. Peng, Y. Li, Y. Fan et al., Nacre-inspired integrated strong and tough reduced graphene oxide–poly(acrylic acid) nanocomposites. Nanoscale 8, 5649-5656 (2016). https://doi.org/10.1039/C6NR00562D

- A. Liu, A. Walther, O. Ikkala, L. Belova, L. A. Berglund, Clay nanopaper with tough cellulose nanofiber matrix for fire retardancy and gas barrier functions. Biomacromolecules 12, 633-641 (2011). https://doi.org/10.1021/bm101296z

- H. Sehaqui, A. Liu, Q. Zhou, L. A. Berglund, Fast preparation procedure for large, flat cellulose and cellulose/inorganic nanopaper structures. Biomacromolecules 11, 2195-2198 (2010). https://doi.org/10.1021/bm100490s

- W.-T. Cao, F.-F. Chen, Y.-J. Zhu, Y.-G. Zhang, Y.-Y. Jiang et al., Binary strengthening and toughening of MXene/cellulose nanofiber composite paper with nacre-inspired structure and superior electromagnetic interference shielding properties. ACS Nano 12, 4583-4593 (2018). https://doi.org/10.1021/acsnano.8b00997

- Y. Liu, S.-H. Yu, L. Bergström, Transparent and flexible nacre-like hybrid films of aminoclays and carboxylated cellulose nanofibrils. Adv. Funct. Mater. 28, 1703277 (2018). https://doi.org/10.1002/adfm.201703277

- Y. Wen, M. Wu, M. Zhang, C. Li, G. Shi, Topological design of ultrastrong and highly conductive graphene films. Adv. Mater. 29, 1702831 (2017). https://doi.org/10.1002/adma.201702831

- S. Gong, W. Cui, Q. Zhang, A. Cao, L. Jiang et al., Integrated ternary bioinspired nanocomposites via synergistic toughening of reduced graphene oxide and double-walled carbon nanotubes. ACS Nano 9, 11568-11573 (2015). https://doi.org/10.1021/acsnano.5b05252

- H. Li, X. Dai, X. Han, J. Wang, Molecular orientation-regulated bioinspired multilayer composites with largely enhanced mechanical properties. ACS Appl. Mater. Interfaces 15, 21467-21475 (2023). https://doi.org/10.1021/acsami.3c01647

- Y. Liu, N. Zhao, J. Xu, Mechanically strong and flame-retardant PBO/BN/MXene nanocomposite paper with low thermal expansion coefficient, for efficient EMI shielding and heat dissipation. Adv. Fiber Mater. 5, 1657-1670 (2023). https://doi.org/10.1007/s42765-023-00298-0

- J. Wang, X. Ma, J. Zhou, F. Du, C. Teng, Bioinspired, high-strength, and flexible MXene/aramid fiber for electromagnetic interference shielding papers with joule heating performance. ACS Nano 16, 6700-6711 (2022). https://doi.org/10.1021/acsnano.2c01323

- C. Liu, Y. Ma, Y. Xie, J. Zou, H. Wu et al., Enhanced electromagnetic shielding and thermal management properties in MXene/aramid nanofiber films fabricated by intermittent filtration. ACS Appl. Mater. Interfaces 15, 4516-4526 (2023). https://doi.org/10.1021/acsami.2c20101

- J. Xiong, R. Ding, Z. Liu, H. Zheng, P. Li et al., High-strength, super-tough, and durable nacre-inspired MXene/heterocyclic aramid nanocomposite films for electromagnetic interference shielding and thermal management. Chem. Eng. J. 474, 145972 (2023). https://doi.org/10.1016/j.cej.2023.145972

- F. Jia, J. Dong, X. Dai, Y. Liu, H. Wang et al., Robust, flexible, and stable CuNWs/MXene/ANFs hybrid film constructed by structural assemble strategy for efficient EMI shielding. Chem. Eng. J. 452, 139395 (2023). https://doi.org/10.1016/j.cej.2022.139395

- J. Wang, R. Zhai, X. Ma, W. Liu, C. Teng, Large flakes of Al–Ti3C2tx MXene constructing highly ordered layered MXene/ANF films with integrated multifunctionalities. Ceram. Int. 50, 11379-11391 (2024). https://doi.org/10.1016/j.ceramint.2024.01.038

- H. Liu, Z. Cui, L. Luo, Q. Liao, R. Xiong et al., Facile fabrication of flexible and ultrathin self-assembled Ti3C2tx/bacterial cellulose composite films with multifunctional electromagnetic shielding and photothermal conversion performances. Chem. Eng. J. 454, 140288 (2023). https://doi.org/10.1016/j.cej.2022.140288

- Y. Wan, P. Xiong, J. Liu, F. Feng, X. Xun et al., Ultrathin, strong, and highly flexible Ti3C2tx MXene/bacterial cellulose composite films for high-performance electromagnetic interference shielding. ACS Nano 15, 8439-8449 (2021). https://doi.org/10.1021/acsnano.0c10666

- R. Liu, M. Miao, Y. Li, J. Zhang, S. Cao et al., Ultrathin biomimetic polymeric Ti3C2tx MXene composite films for electromagnetic interference shielding. ACS Appl. Mater. Interfaces 10, 44787-44795 (2018). https://doi.org/10.1021/acsami.8b18347

- Y.-J. Wan, X.-M. Li, P.-L. Zhu, R. Sun, C.-P. Wong et al., Lightweight, flexible MXene/polymer film with simultaneously excellent mechanical property and high-performance electromagnetic interference shielding. Composites, Part A 130, 105764 (2020). https://doi.org/10.1016/j.compositesa.2020.105764

- B. Zhou, Z. Zhang, Y. Li, G. Han, Y. Feng et al., Flexible, robust, and multifunctional electromagnetic interference shielding film with alternating cellulose nanofiber and MXene layers. ACS Appl. Mater. Interfaces 12, 4895-4905 (2020). https://doi.org/10.1021/acsami.9b19768

- W. Wang, A. C. Y. Yuen, H. Long, W. Yang, A. Li et al., Random nano-structuring of PVA/MXene membranes for outstanding flammability resistance and electromagnetic interference shielding performances. Composites, Part B 224, 109174 (2021). https://doi.org/10.1016/j.compositesb.2021.109174

- Z. Zhan, Q. Song, Z. Zhou, C. Lu, Ultrastrong and conductive MXene/cellulose nanofiber films enhanced by hierarchical nano-architecture and interfacial interaction for flexible electromagnetic interference shielding. J. Mater. Chem. C 7, 9820-9829 (2019). https://doi.org/10.1039/C9TC03309B

- K. Sun, F. Wang, W. Yang, H. Liu, C. Pan et al., Flexible conductive polyimide fiber/MXene composite film for electromagnetic interference shielding and joule heating with excellent harsh environment tolerance. ACS Appl. Mater. Interfaces 13, 50368-50380 (2021). https://doi.org/10.1021/acsami.1c15467

- M. Zhu, X. Yan, H. Xu, Y. Xu, L. Kong, Highly conductive and flexible bilayered MXene/cellulose paper sheet for efficient electromagnetic interference shielding applications. Ceram. Int. 47, 17234-17244 (2021). https://doi.org/10.1016/j.ceramint.2021.03.034

- H. Cheng, Y. Pan, Q. Chen, R. Che, G. Zheng et al., Ultrathin flexible poly(vinylidene fluoride)/MXene/silver nanowire film with outstanding specific emi shielding and high heat dissipation. Adv. Compos. Hybrid Mater. 4, 505-513 (2021). https://doi.org/10.1007/s42114-021-00224-1

- X. Xu, S. Wu, J. Cui, L. Yang, D. Liu et al., Insights into the microstructures and reinforcement mechanism of nano-fibrillated cellulose/MXene based electromagnetic interference shielding film. Cellulose 28, 3311-3325 (2021). https://doi.org/10.1007/s10570-021-03765-2

- S. Wan, X. Li, Y. Wang, Y. Chen, X. Xie et al., Strong sequentially bridged MXene sheets. Proc. Natl. Acad. Sci. U.S.A. 117, 27154-27161 (2020). https://doi.org/10.1073/pnas.2009432117

- S. Luo, Q. Li, Y. Xue, B. Zhou, Y. Feng et al., Reinforcing and toughening bacterial cellulose/MXene films assisted by interfacial multiple cross-linking for electromagnetic interference shielding and photothermal response. J. Colloid Interface Sci. 652, 1645-1652 (2023). https://doi.org/10.1016/j.jcis.2023.08.177

- L. Wang, Z. Ma, Y. Zhang, H. Qiu, K. Ruan et al., Mechanically strong and folding-endurance Ti3C2tx MXene/PBO nanofiber films for efficient electromagnetic interference shielding and thermal management. Carbon Energy 4, 200-210 (2022). https://doi.org/10.1002/cey2.174

- R. Cheng, Y. Wu, B. Wang, J. Zeng, J. Li et al., Fireproof ultrastrong all-natural cellulose nanofiber/montmorillonite-supported mxene nanocomposites with electromagnetic interference shielding and thermal management multifunctional applications. J. Mater. Chem. A 11, 18323-18335 (2023). https://doi.org/10.1039/D3TA03798C

- R. Cheng, B. Wang, J. Zeng, J. Li, J. Xu et al., Janus-inspired flexible cellulose nanofiber-assisted MXene/silver nanowire papers with fascinating mechanical properties for efficient electromagnetic interference shielding. Carbon 202, 314-324 (2023). https://doi.org/10.1016/j.carbon.2022.10.079

- S. Wan, X. Li, Y. Chen, N. Liu, Y. Du et al., High-strength scalable MXene films through bridging-induced densification. Science 374, 96-99 (2021). https://doi.org/10.1126/science.abg2026

- C. Weng, T. Xing, H. Jin, G. Wang, Z. Dai et al., Mechanically robust ANF/MXene composite films with tunable electromagnetic interference shielding performance. Composites, Part A 135, 105927 (2020). https://doi.org/10.1016/j.compositesa.2020.105927

- F. Xie, F. Jia, L. Zhuo, Z. Lu, L. Si et al., Ultrathin MXene/aramid nanofiber composite paper with excellent mechanical properties for efficient electromagnetic interference shielding. Nanoscale 11, 23382-23391 (2019). https://doi.org/10.1039/C9NR07331K

- C. Lei, Y. Zhang, D. Liu, K. Wu, Q. Fu, Metal-level robust, folding endurance, and highly temperature-stable MXene-based film with engineered aramid nanofiber for extreme-condition electromagnetic interference shielding applications. ACS Appl. Mater. Interfaces 12, 26485-26495 (2020). https://doi.org/10.1021/acsami.0c07387

- D. Hu, S. Wang, C. Zhang, P. Yi, P. Jiang et al., Ultrathin MXene-aramid nanofiber electromagnetic interference shielding films with tactile sensing ability withstanding harsh temperatures. Nano Res. 14, 2837-2845 (2021). https://doi.org/10.1007/s12274-021-3297-z