Supporting Information for

A Flexible Smart Healthcare Platform Conjugated with Artificial Epidermis Assembled by Three-Dimensionally Conductive MOF Network for Gas and Pressure Sensing

Qingqing Zhou1, Qihang Ding2, Zixun Geng1, Chencheng Hu1, Long Yang1, Zitong Kan1, Biao Dong1, Miae Won2,3, Hongwei Song1, Lin Xu1,※, Jong Seung Kim2,3,※

1 State Key Laboratory of Integrated Optoelectronics, College of Electronic Science and Engineering, Jilin University, Changchun 130012, People's Republic of China

2 Department of Chemistry, Korea University, Seoul 02841, Republic of Korea

3TheranoChem Incorporation, Seoul 02856, Republic of Korea

※Corresponding authors. E-mail: linxu@jlu.edu.cn (Lin Xu); jongskim@korea.ac.kr  (Jong Seung Kim)

S1 Experimental captions

S1.1 Chemicals

Copper acetate (Cu(AC)2) and 2,3,6,7,10,11-Hexahydroxytrimethylene hydrate (HHTP) were purchased from Shanghai Aladdin Biochemical Technology Co., LTD. Methyl methacrylate (MMA, 99%) and lithium fluoride (LiF, AR) were obtained from Shanghai Macklin Biochemical Technology Co., Ltd (China). TI3AlC2 chunk was supplied by the Yiyi Technology Co., LTD. Potassium persulfate (K2S2O8, 99.5%) and 2,2'-Azobis(2-methylpropionitrile) (AIBN), toluene (C7H8, AR), formaldehyde (HCHO, AR), ethanol (C2H5OH, AR), methanol (CH3OH, AR), formaldehyde (HCHO, AR) and acetone (CH3COCH3, AR) were purchased from Beijing Chemical Plant of China. Hydrochloric acid (HCl, AR) was acquired from Tianjin Fengchuan Chemical Reagent Technology Co., LTD. Standard NO2, H2S and NH3 gases for the sensing measurement were obtained from Dalian Special Gases Co., Ltd (China). No further purification was performed for all chemical reagents and the deionized (DI) water was utilized in the whole experimental process.

S1.2 Synthesis of the Ti3C2Tx MXene nanosheets

For delamination, 2 g of LiF powder was firstly added into the 20 mL of HCl (9 M) aqueous solution and constantly stirred for 15 min at 35℃. Then, 1 g of Ti3AlC2 powder was decanted in the above solution and kept etching at 35℃ for 24 h. After the etching procedure, the collected precipitates were dispersed in DI water and further purified by repetitive centrifugation (3500 rpm for 10 mins) until the PH value of centrifuge supernatant approached to 6. To fabricate the delaminated Ti3C2Tx flakes, the as-produced precipitates were redispersed into 200 mL of DI water and continuously sonicated for 1 h in the ice-water bath. Finally, after centrifugation (3500 rpm) for 30 mins, the upper supernatant is collected as the few-layered Ti3C2Tx flakes, and the resultant sediment is multi-layered Ti3C2Tx nanosheets.

S1.3 Preparation of the 3D maroporous Ti3C2Tx foam

Firstly, the as-prepared monodispersed polymethylmethacrylate (PMMA) macro-spheres with 430 nm diameters were synthesized by emulsion polymerization according to the previous literature [S1]. To facilitate the electrostatic assembly between Ti3C2Tx flakes and PMMA spheres, the 40 mL of above-fabricated Ti3C2Tx flakes colloid suspension (2.5 mg/mL) was added into 6 mL of PMMA aqueous solution (70 mg/mL) and sonicated for 10 mins. After that, the Ti3C2Tx/PMMA hybrid film were prepared by filtering through a Celgard 3501 polypropylene membrane and then peeled off after drying for 10 h at RT. Finally, the Ti3C2Tx/PMMA hybrid film were annealed at 450°C under N2 atmosphere for 1.5 h with a heating rate of 10°C /min to remove the PMMA spheres, yielding the hollow Ti3C2Tx foam.

S1.4 Preparation of the 3D maroporous Ti3C2Tx@Cu3(HHTP)2 composite

To fabricate Cu3(HHTP)2 nanosheets, 0.6 mmol of Cu(AC)2 and 0.5 mmol of HHTP were respectively solved into 5 mL of ethanol and then vigorously stirred at 45°C for 30 mins to form the uniform mixture solution. The resultant Cu3(HHTP)2 were collected by vacuum filtrated through the polypropylene membrane. Afterwards, macroporous hollow Ti3C2Tx films and Cu3(HHTP)2 with mass ratio of 1:10, 1:20 and 1:40 were separately mixed, respectively, to optimize the gas sensing performance of the Ti3C2Tx@Cu3(HHTP)2 composite. They were marked as Ti3C2Tx@Cu3(HHTP)2-1/10, Ti3C2Tx@Cu3(HHTP)2-1/20 and Ti3C2Tx@Cu3(HHTP)2-1/40. As revealed from the sensing performance tests, the Ti3C2Tx@Cu3(HHTP)2-1/20 composite displayed the optimal sensing behavior, it is mainly investigated and discussed, which further abbreviated as Ti3C2Tx@Cu3(HHTP)2 composite for convenience.

S1.5 Characterizations of various samples

The morphological architecture of various samples is confirmed by field-emission scanning electron microscope (FESEM, JEOL JSM-7500F, Japan), Transmission electron microscopy (TEM) and high-resolution transmission electron microscopy (HRTEM). To determine the structure of the samples, X-ray diffractometer (Tokyo, Japan) with a monochromatised Cu target radiation source (λ= 1.5406 Å) are conducted. Fourier transform infrared spectroscopy (FTIR) spectra are recorded on a Vertex 80 V (Bruker) FTIR spectrometer in the range of 400-4000 cm-1. The thermal decomposition behavior of samples is analyzed by thermogravimetric analysis (TGA, Q500, TA) and differential thermogravimetry analysis (DTG). The chemical composition of samples is confirmed by X-ray photoelectron spectra (XPS, Thermo Fisher Scientific, Waltham, MA, USA).

S1.6 Computational details

Density functional theory (DFT) calculations were performed using the CP2K package. [S2] We have chosen the DZVP-MOLOPT-SR-GTH as basis set and pseudopotential to describe the ionic cores with a cutoff energy of 400 Rydberg in all relaxation processes. The convergence criterion for the maximum force is set as 1×10−3 atomic units. The k-points were 1×1×1 for geometry optimization and energy calculation. The atomic structures were analyzed by using the VESTA code [S3].

The adsorption energy (Eads) is calculated via the following formula (S1):

Eads = Etotal – Eslab –ENO2

where Etotal, Eslab and ENO2 represent the DFT energies of adsorbates with substrates, the substrates and NO2 gas adsorbates, respectively. The more negative this Eads value is, the stronger the adsorption.

Supplementary Figures

Fig. S1 SEM and TEM images of few Ti3C2Tx flakes

Fig. S2 SEM image and size statistics of the PMMA spheres

Fig. S3 The size statistics of the Cu3(HHTP)2 particles

Fig. S4 HRTEM image of the Cu3(HHTP)2 particles

Fig. S5 F 1s orbits in Ti3CTx foam and Ti3C2Tx@Cu3(HHTP)2 composite

Fig. S6 The flexible Ti3C2Tx@Cu3(HHTP)2 gas sensor

Fig. S7 The response of the flexible Ti3C2Tx@Cu3(HHTP)2 sensor to 1, 5 and 20 ppm NO2 gas, respectively, and the different ratios of Ti3C2Tx and Cu3(HHTP)2 is 1/10, 1/20 and 1/40

Fig. S8 The linear relationship of the Ti3CTx sensors to 1-200 ppm of the NO2 gas

Fig. S9 (a) The recovery time of the Ti3C2Tx@Cu3(HHTP)2 and Cu3(HHTP)2. Note that the Ti3C2Tx sensor cannot recover, thus the recovery time isn’t given; (b) The response, (c) response time and (d) recovery time of the L-Ti3C2Tx@Cu3(HHTP)2 sensor with lamellar structure of Ti3C2Tx to 10, 20, and 40 ppm of NO2 gas

Fig. S10 The selectivity coefficient of Ti3C2Tx@Cu3(HHTP)2 sensor to NO2 gas compared to other interfering gas molecules at RT. G1-G7 is NH3, H2S, CH3OCH3, C6H7, HCHO, CH3OH, C2H5OH gas, respectively

Fig. S11 Water contact angle test of the Ti3C2Tx@Cu3(HHTP)2 sensitive material

Fig. S12 (a) The response of the Ti3C2Tx@Cu3(HHTP)2 sensor to 3 ppm of NO2 which bent at different angles (0-60°); (b) The response curves of the sensor to 2 ppm of NO2 gas after bending 10 times

Fig. S13 (a-d) The C and O (side and top) adsorption sites of Cu3(HHTP)2 in Ti3C2Tx@Cu3(HHTP)2 composites; (e, f) The partial enlarged image of C (top) and O (top) adsorption sites of Cu3(HHTP)2 in Ti3C2Tx@Cu3(HHTP)2 composite

Fig. S14 (a-e) Resistance-response to different pressure variables, i.e., 0.3 kPa, 0.4 kPa, 1.8 kPa, 3.8 kPa and 5.5 kPa

Fig. S15 (a) The response and (b) the linear curve of the L-Ti3C2Tx@Cu3(HHTP)2 pressure sensor to different pressure variables from 0.6 to 6.1 kPa; (c) The response of the spherical Ti3C2Tx pressure sensor to 6.1 kPa pressure

Fig. S16 The total strain distribution simulation of the flexible Ti3C2Tx@Cu3(HHTP)2 sensor when increased the pressure exertions

Fig. S17 The strain distribution of the interface between microsphere and panel in the Ti3C2Tx@Cu3(HHTP)2 material. Note that the strain stress increases, as the degree of deformation increases

Fig. S18 The Schematic illustration of the sensing mechanism of the pressure sensor.

πr2=πab

For the circle,

η1=h1/r, (0<η1<1)

x1=2[ r2-(h1)2]1/2

For the ellipse,

η2=h2/b, (0<η2<1)

x2=f (η2, b),

R=μd2/(πx22/4)，A=πx22/4

Where r is the radius of a circle; a and b are the major and minor axes of the ellipse; h1 is the distance from the center of the circle to any string; η1 is the coefficient applicable to circles; x1 is the length of any string in the circle; h2 is the distance from the center of the ellipse to any string; η2 is the coefficient applicable to ellipse; x2 is the length of any string in the ellipse; A, d1 and d2 are contact area and the distance between Ti3C2Tx and Cu3(HHTP)2. R is the contact resistance between Ti3C2Tx and Cu3(HHTP)2.

Fig. S19 (a) The response of the flexible Ti3C2Tx@Cu3(HHTP)2 sensor to 120 Pa of pressure; (b) The sensing curve of the Ti3C2Tx@Cu3(HHTP)2 sensor under no pressure load

Fig. S20 (a) long-term stability tests of the Ti3C2Tx@Cu3(HHTP)2 sensor to 1.2 kPa pressure; (b) The actual photograph of the flexible sensor after bending and (c) the response curves of the Ti3C2Tx@Cu3(HHTP)2 sensor after bending 20 times to 1.8 kPa pressure

Fig. S21 The pressure response of the Ti3C2Tx@Cu3(HHTP)2 device to different exertions of pressing, such as (a) blowing, (b) tapping and (c) pressing

Fig. S22 (a) Twenty-six letters are expressed by using different definitions of Morse code; (b) Coding of the acronyms “JLU” and “SCI” by via short-time and long-time heavily pressing; (c) Coding of the words “MOF” and “SENSING” by lightly and heavily pressing on the Ti3C2Tx@Cu3(HHTP)2 sensor

Fig. S23 Schematic illustration of the Ti3C2Tx@Cu3(HHTP)2 sound sensor mounted on commercial speaker to detect classic “canon” audio

Fig. S24 The response comparison of the dual-mode flexible sensor to pressure with and without NO2 gas atmosphere

Fig. S25 The actual response of the wearable alarming system integrated with a flexible sensor to 1 ppm NO2 gas

Fig. S26 The actual response of a flexible smart wearable warning system integrated with a biomimetic sensor to diverse breathing patterns, including light and heavy breathing

Fig. S27 The real-time response of the flexible sensor to the normal writing and dysgraphia

Fig. S28 The real-time dynamic response of the flexible smart healthcare system integrating with a bionic dual-mode sensor under light and heavy pressing exertions as well as dysgraphia

Fig. S29 (a) Training and validation accuracy versus 1000 epochs. (b) Training and validation loss versus 100 epochs

Note that the physiological motor signals were respectively normalized through the functional Eq. (S2):

xi=xi−μσ                   (S2)

where xi and xi are the normalized and original signal values of each batch, respectively, while μ and σ express the mean and standard deviation, respectively.

Table S1 The binding energy (BE) and proportion of the Ti element in the Ti3C2Tx, and Ti3C2Tx@Cu3(HHTP)2 composite sensing materials

| Samples | BE (eV)/proportion |  |  |
| --- | --- | --- | --- |
|  | Ti-C | Ti-O | Ti-F |
| Ti3C2Tx | 459.1(455.6)/ 28.71% | 462.0(456.3)/ 41.56% | 464.5(457.3)/ 31.35% |
| Ti3C2Tx@Cu3(HHTP)2 composite | 459.0(455.0)/ 47.28% | 462.0(456.6)/ 21.96% | 464.4(457.2)/ 30.76% |

Table S2 A comparison of the sensing properties of recently reported NO2-based sensors with the as-prepared Ti3C2Tx@Cu3(HHTP)2 sensor in this work

| Sensing Materials | Temp (°C) | Ra res / Conc. (ΔR/Ra/ppm) | Tb res (s) | RH | Refs. |
| --- | --- | --- | --- | --- | --- |
| alkalized V2CTx | 25 | 57.6%/50 | 76 | 51.9% | [S4] |
| Cu3(HHTP)2-NF | RT | 68.9%/5 | 1800 | 50% | [S5] |
| Fe2O3/Cu3(HHTP)2-NF | 20 | 63.5%/5 | 1800 | 50% | [S5] |
| Pd@Cu3(HHTP)2 | RT | 13.5%/1 | 828 | 5% | [S6] |
| Pt@Cu3(HHTP)2 | 50/75 | 12.1%/1 | 14.0 | 5% | [S6] |
| Cu3(HHTP)2 | RT | 5%/1 | 1080 | N.R.c | [S6] |
| Ni3(HITP)2 | RT | 71%/100 | 135 | N.R.c | [S7] |
| HIOTP-Cu | RT | 55.6%/100 | 30.6 | N.R.c | [S7] |
| ZIF-8/Au NW | RT | 0.9%/20 | 7.2 | N.R.c | [S8] |
| MOF derivant | RT | 1%/5 | N.R.c | N.R.c | [S9] |
| MXene spheres | RT | 12.1%/5 | 180 | 30 | [S10] |
| WS2@Co-N-HCNCsd | RT | 48.2%/5 | 1200 | 5% | [S11] |
| Ti3C2Tx@Cu3(HHTP)2 | RT | 86%/100 | 7 | 35 | This work |

Where Ra res is the response; Ra and R g represent the resistance of the sensor to the air and the target gas, respectively; Tb res is the response times; N.R.c means not reported; WS2@Co-N-HCNCsd, WS2 is confined in Co, N-doped hollow carbon nanocages; Temp: Temperature; RT: Room temperature; Conc.: Concentration; RH: Relative Humidity.

Table S3 The adsorption energy (Eads) of Ti3C2Tx@Cu3(HHTP)2 to NO2 gas, (1 Hartree =27.2114eV)

| Samples | Edft/Hartree | Eads/Hartree | Eads/eV |
| --- | --- | --- | --- |
| NO2 | -41.88074553 | - | - |
| slab | -11246.92171 | - | - |
| slab-NO2 | -11288.80885 | -0.006395889 | -0.174041105 |

Table S4 Summary sensing performance results of recently reported pressure sensors as compared to the Ti3C2Tx@Cu3(HHTP)2 pressure sensor in this work

| Samples | Type of sensor | Sensitivity (kPa−1) | Linear detection Range (kPa) | Refs. |
| --- | --- | --- | --- | --- |
| Crumpled Ti3C2Tx | Resistive | 0.22 | 22.22–140 | [S10] |
| MXene/tissue paper | Current | 0.55 | 0.023−0.982 | [S12] |
| MWCNT/PDMS | Current | 0.7 | 0-200 | [S13] |
| PDMS/MXene | Voltage | 0.06 | 0.1-0.8 | [S14] |
| Graphene/PDMS | Current | 1.2 | 0.2-25 | [S15] |
| Graphene paper | Resistive | 0.1 | 2–20 | [S16] |
| ZnO nanowires | Current | 1.2 | 120–260 | [S17] |
| PVDF@lead zirconate titanate | Voltage | 0.06 | 1.79-22.41 | [S18] |
| Cellulose@carbon black | Current | 0.1 | 2–3.8 | [S19] |
| Ecoflex/CNTs | Capacitive | 0.39 | 1-10 | [S20] |
| Ti3C2Tx@Cu3(HHTP)2 | Resistive | 15.5/1.7 | 0-6.1 | This work |

Supplementary References

- L. Zhang, B. Dong, L. Xu, X. Zhang, J. Chen et al., Three-dimensional ordered ZnO-Fe3O4 inverse opal gas sensor toward trace concentration acetone detection. Sensor Actuat. B Chem 252, 367-374 (2017). https://doi.org/10.1016/j.snb.2017.05.167

- J. VandeVondele, M. Krack, F. Mohamed, M. Parrinello, T. Chassaing et al., Quickstep: Fast and accurate density functional calculations using a mixed gaussian and plane waves approach. Comput. Phys. Commun. 167(2), 103-128 (2005). https://doi.org/10.1016/j.cpc.2004.12.014

- K. Momma, F. Izumi, vesta: A three-dimensional visualization system for electronic and structural analysis. J. Appl. Crystallogr. 41, 653-658 (2008). https://doi.org/10.1107/s0021889808012016

- Y. Zhang, Y. Jiang, Z. Duan, Q. Huang, Y. Wu et al., Highly sensitive and selective NO2 sensor of alkalized V2CTx MXene driven by interlayer swelling. Sensor Actuat. B Chem. 344((2021). https://doi.org/10.1016/j.snb.2021.130150

- Y.-M. Jo, K. Lim, J. W. Yoon, Y. K. Jo, Y. K. Moon et al., Visible-Light-Activated Type II Heterojunction in Cu3(hexahydroxytriphenylene)2/Fe2O3 Hybrids for Reversible NO2 Sensing: Critical Role of π-π* Transition. ACS Central Sci. 7(7), 1176-1182 (2021). https://doi.org/10.1021/acscentsci.1c00289

- W.-T. Koo, S.-J. Kim, J.-S. Jang, D.-H. Kim, I.-D. Kim, Catalytic metal nanoparticles embedded in conductive metal-organic frameworks for chemiresistors: Highly active and conductive porous materials. Adv. Sci. 6(21), (2019). https://doi.org/10.1002/advs.201900250

- P. Chen, X. Su, C. Wang, G. Zhang, T. Zhang et al., Two-dimensional conjugated metal-organic frameworks with large pore apertures and high surface areas for NO2 selective chemiresistive sensing. Angew. Chem. Int. Ed. 62(40), (2023). https://doi.org/10.1002/anie.202306224

- P. Li, H. Zhan, S. Tian, J. Wang, X. Wang et al., Sequential ligand exchange of coordination polymers hybridized with in situ grown and aligned au nanowires for rapid and selective gas sensing. ACS Appl. Mater. Interfaces 11(14), 13624-13631 (2019). https://doi.org/10.1021/acsami.9b02286

- K. Rui, X. Wang, M. Du, Y. Zhang, Q. Wang et al., Dual-function metal-organic framework-based wearable fibers for gas probing and energy storage. ACS Appl. Mater. Interfaces 10(3), 2837-2842 (2018). https://doi.org/10.1021/acsami.7b16761

- Z. Yang, S. Lv, Y. Zhang, J. Wang, L. Jiang et al., Self-assembly 3d porous crumpled mxene spheres as efficient gas and pressure sensing material for transient all-mxene sensors. Nano-Micro Lett. 14(1), (2022). https://doi.org/10.1007/s40820-022-00796-7

- W. T. Koo, J. H. Cha, J. W. Jung, S. J. Choi, J. S. Jang et al., Few-layered WS2 nanoplates confined in Co, N-doped hollow carbon nanocages: Abundant WS2 Edges for Highly Sensitive Gas Sensors. Adv. Funct. Mater. 28(36), (2018). https://doi.org/10.1002/adfm.201802575

- Y. Guo, M. Zhong, Z. Fang, P. Wan, G. Yu. A wearable transient pressure sensor made with mxene nanosheets for sensitive broad-range human-machine interfacing. Nano Lett. 19(2), 1143-1150 (2019). https://doi.org/10.1021/acs.nanolett.8b04514

- Z. Xu, D. Wu, Z. Chen, Z. Wang, C. Cao et al., A flexible pressure sensor with highly customizable sensitivity and linearity via positive design of microhierarchical structures with a hyperelastic model. Microsyst. Nanoeng. 9(1), (2023). https://doi.org/10.1038/s41378-022-00477-w

- Y.-W. Cai, X.-N. Zhang, G.-G. Wang, G.-Z. Li, D.-Q. Zhao et al., A flexible ultra-sensitive triboelectric tactile sensor of wrinkled pdms/mxene composite films for e-skin. Nano Energy 81, (2021). https://doi.org/10.1016/j.nanoen.2020.105663

- J. Shi, L. Wang, Z. Dai, L. Zhao, M. Du et al., Multiscale hierarchical design of a flexible piezoresistive pressure sensor with high sensitivity and wide linearity range. Small 14(27), (2018). https://doi.org/10.1002/smll.201800819

- L.-Q. Tao, K.-N. Zhang, H. Tian, Y. Liu, D.-Y. Wang et al., Graphene-paper pressure sensor for detecting human motions. ACS Nano 11(9), 8790-8795 (2017). https://doi.org/10.1021/acsnano.7b02826

- P. Lei, Y. Bao, W. Zhang, L. Gao, X. Zhu et al., Synergy of zno nanowire arrays and electrospun membrane gradient wrinkles in piezoresistive materials for wide-sensing range and high-sensitivity flexible pressure sensor. Adv. Fiber Mater. 6(2), 414-429 (2024). https://doi.org/10.1007/s42765-023-00359-4

- C. Chen, G. Xie, J. Dai, W. Li, Y. Cai et al., Integrated core-shell structured smart textiles for active NO2 concentration and pressure monitoring. Nano Energy. 116((2023). https://doi.org/10.1016/j.nanoen.2023.108788

- Y. Zhang, P. Zhu, H. Sun, X. Sun, Y. Ye et al., Superelastic cellulose sub-micron fibers/carbon black aerogel for highly sensitive pressure sensing. Small. 20(13), (2024). https://doi.org/10.1002/smll.202310038

- Y. Ma, Z. Li, S. Tu, T. Zhu, W. Xu et al., An asymmetric interlocked structure with modulus gradient for ultrawide piezocapacitive pressure sensing applications. Adv. Funct. Mater. 34(8), (2024). https://doi.org/10.1002/adfm.202309792