Supporting Information for

Efficient and Stable Photo-Assisted Lithium-Ion Battery Enabled by Photocathode with Synergistically Boosted Carriers Dynamics

Zelin Ma1,‡, Shiyao Wang2,‡, Zhuangzhuang Ma5, Juan Li3, Luomeng Zhao1, Zhihuan Li3, Shiyuan Wang1, Yazhou Shuang1, Jiulong Wang1, Fang Wang1, Weiwei Xia1, Jie Jian1, Yibo He3, 4,* Junjie Wang2, Pengfei Guo1,4,* and Hongqiang Wang1,*

1State Key Laboratory of Solidification Processing, Center for Nano Energy Materials, School of Materials Science and Engineering, Northwestern Polytechnical University and Shaanxi Joint Laboratory of Graphene (NPU), Xi’an 710072, P. R. China

2State Key Laboratory of Solidification Processing, School of Materials Science and Engineering Department, Northwestern Polytechnical University, Xi’an 710072, P. R. China

3State Key Laboratory of Solidification Processing, Center of Advanced Lubrication and Seal Materials, School of Materials Science and Engineering, Northwestern Polytechnical University, Xi’an, Shaanxi 710072, P. R. China

4Research& Development Institute of Northwestern Polytechnical University in Shenzhen, Shenzhen, 518063, P. R. China

5Key Laboratory of Applied Surface and Colloid Chemistry, Shaanxi Key Laboratory for Advanced Energy Devices, Shaanxi Engineering Lab for Advanced Energy Technology, School of Materials Science and Engineering, National Ministry of Education, Shaanxi Normal University, Xi'an 710119, P. R. China

‡ Zelin Ma and Shiyao Wang contributed equally to this work.

*Corresponding authors. E-mail: heyibo@nwpu.edu.cn (Yibo He); guopengfei@nwpu.edu.cn (Pengfei Guo); hongqiang.wang@nwpu.edu.cn (Hongqiang Wang)

Supplementary Figures and Tables

Fig. S1 Optimized structure models of (a) TiO2 and (b) Au-TiO2

Fig. S2 Schematic diagram of preparation process for Au nanocrystals-embedded TiO2 nanofibers

Fig. S3 (a) TEM image of Au nanocrystals prepared by laser irradiation (insert, Mie-scattering image of laser-manufactured Au colloidal solution), (b) HRTEM image of Au nanocrystal and (c) particle size distribution histogram of Au nanocrystals

Fig. S4 XRD patterns and Rietveld plots of TiO2

Fig. S5 XPS spectra of Ti-2p peaks of TiO2 and Au-TiO2

Fig. S6 SEM images of TiO2 and Au-TiO2 nanofibers

Fig. S7 SEM image of TiO2 nanofibers with Au nanoparticles prepared by the traditional method with surfactants

Fig. S8 TEM and HRTEM images of TiO2 nanofibers

Fig. S9 EDX mapping images of TiO2 nanofibers (Ti and O elements)

Fig. S10 Schematic diagram of the photodetector measurement system

Fig. S11 LSV curves of TiO2 and Au-TiO2 in illuminated conditions

Fig. S12 I-t curves of TiO2 and Au-TiO2 in illumination conditions at an external bias voltage of 1V

Fig. S13 UPS spectra of (a) Au-TiO2 and (b) TiO2

Fig. S14 Structure diagram (a) and optical photograph (b) of photo-assisted coin cell

Fig. S15 Discharge-charge curves of TiO2 samples at 0.2 A g-1 in the dark and light conditions

Fig. S16 dQ/dV versus voltage of TiO2 samples at 0.2 A g-1 in the dark and light conditions

Fig. S17 Photo-conversion efficiency of TiO2 and Au-TiO2 photocathodes under illumination at 3.0 A g-1

Fig. S18 Z′ vs ω−1/2 curves of TiO2 and Au-TiO2 in the dark and light conditions

Fig. S19 TEM images of Ag (a) and Pt (b) nanocrystals prepared by laser irradiation

Fig. S20 UV-vis absorption spectra of the Ag nanocrystals, Pt nanocrystals, Ag-TiO2 nanofiber and Pt-TiO2 nanofiber

Fig. S21 SEM images of (a) Ag-TiO2 and (b) Pt-TiO2 nanofibers

Fig. S22 EDX mapping images of (a) Pt-TiO2 nanofiber (Ti, O and Pt elements) and (b) Ag-TiO2 nanofiber (Ti, O and Ag elements)

Table S1 Refinement results of TiO2 and Au-TiO2

| Phase |  | TiO2 | Au-TiO2 |
| --- | --- | --- | --- |
| Symmetry |  | anatase | anatase |
| Space group |  | I41/amd | I41/amd |
| Cell parameters | a(Å) | 3.7771 (1) | 3.7779 (0) |
|  | b(Å) | 3.7771 (1) | 3.7779 (0) |
|  | c(Å) | 9.4550 (3) | 9.4559 (1) |
|  | () | 90 (0) | 90 (0) |
|  | () | 90 (0) | 90 (0) |
|  | () | 90 (0) | 90 (0) |
|  | V (Å3) | 134.892 (1) | 135.013 (0) |
|  | Rwp(%) | 6.61 | 7.23 |
| Agreement factors | Rp(%) | 5.18 | 5.52 |
|  | 2 | 1.536 | 1.668 |

Table S2 ICP data of Au-TiO2

| Sample | Au | Ti | O |
| --- | --- | --- | --- |
| Au-TiO2 | ~4.1% | ~95.9 % | / |
| TiO2 | / | ~100 % | / |

Table S3 Specific capacities of TiO2 and Au-TiO2 in dark and light condition at different current densities

| Current density | Capacity (mAh g-1) | TiO2 |  | Au-TiO2 |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Dark | Illuminated | Dark | Illuminated |
| 0.2 A g-1 | discharge | 185 | 218 (18 %) | 203 | 276 (34 %) |
|  | charge | 178 | 208 | 199 | 267 |
| 0.5 A g-1 | discharge | 165 | 198 (21 %) | 182 | 251 (38 %) |
|  | charge | 154 | 187 | 175 | 243 |
| 1 A g-1 | discharge | 144 | 182 (27 %) | 164 | 233 (42 %) |
|  | charge | 136 | 175 | 158 | 226 |
| 2 A g-1 | discharge | 125 | 162 (30 %) | 143 | 204 (45 %) |
|  | charge | 116 | 151 | 135 | 197 |
| 3 A g-1 | discharge | 88 | 121 (37 %) | 105 | 163 (55 %) |
|  | charge | 79 | 112 | 96 | 153 |

Table S4 Discharge-charge voltages of TiO2 and Au-TiO2 in dark and light condition at different current densities

| Current density | Voltage (V) | TiO2 |  | Au-TiO2 |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Dark | Illuminated | Dark | Illuminated |
| 0.2 A g-1 | discharge | 1.710 | 1.741 | 1.738 | 1.755 |
|  | charge | 1.967 | 1.931 | 1.958 | 1.896 |
| 0.5 A g-1 | discharge | 1.710 | 1.727 | 1.715 | 1.745 |
|  | charge | 1.988 | 1.959 | 1.980 | 1.918 |
| 1 A g-1 | discharge | 1.696 | 1.721 | 1.698 | 1.739 |
|  | charge | 2.053 | 2.008 | 2.046 | 1.954 |
| 2 A g-1 | discharge | 1.644 | 1.663 | 1.655 | 1.693 |
|  | charge | 2.110 | 2.071 | 2.100 | 2.030 |

Table S5 Photo-conversion efficiency of Au-TiO2 photocathodes under dark and illuminated at different current densities

| Current density (A g-1) | Charge capacity (mAh g-1) |  | Energy (mW h) |  | Illuminated Time (h) | Photo-coversion efficiency (%) |
| --- | --- | --- | --- | --- | --- | --- |
|  | Dark | Illuminated | Dark | Illuminated |  |  |
| 0.2 | 199 | 267 | 0.239 | 0.267 | 1.34 | 0.042 |
| 0.5 | 175 | 243 | 0.210 | 0.243 | 0.49 | 0.135 |
| 1.0 | 158 | 226 | 0.190 | 0.226 | 0.23 | 0.313 |
| 2.0 | 135 | 197 | 0.162 | 0.207 | 0.11 | 0.818 |
| 3.0 | 96 | 153 | 0.115 | 0.153 | 0.06 | 1.267 |

Table S6 Photo-conversion efficiency of TiO2 photocathodes under dark and illuminated at different current densities

| Current density (A g-1) | Charge capacity (mAh g-1) |  | Energy (mW h) |  | Illuminated Time (h) | Photo-coversion efficiency (%) |
| --- | --- | --- | --- | --- | --- | --- |
|  | Dark | Illuminated | Dark | Illuminated |  |  |
| 0.2 | 178 | 208 | 0.214 | 0.228 | 1.04 | 0.027 |
| 0.5 | 154 | 187 | 0.185 | 0.196 | 0.38 | 0.058 |
| 1.0 | 136 | 175 | 0.163 | 0.175 | 0.18 | 0.133 |
| 2.0 | 116 | 151 | 0.139 | 0.151 | 0.08 | 0.300 |
| 3.0 | 79 | 112 | 0.095 | 0.112 | 0.04 | 0.850 |

Table S7 EIS fitting data of TiO2 and Au-TiO2 in the dark and light condition

|  | Rs () | Rct () | DLi+ (cm2 s-1) |
| --- | --- | --- | --- |
| TiO2 (dark) | 3.35 | 232.1 | 4.2510-8 |
| TiO2 (light) | 2.03 | 98.4 | 7.1810-8 |
| Au-TiO2 (dark) | 2.22 | 136.6 | 5.8410-8 |
| Au-TiO2 (light) | 1.49 | 45.0 | 8.7210-8 |

Table S8 Comparison of this work and other related work in literatures

| Number | Sample | Type | Specific capacity | Rate | Light | References |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | TiO2 | anatase/rutile | 180 mAh g-1 (0.2 A g-1) | 180 mAh g-1140 mAh g-1 (0.2~3 A g-1) | / | [S1] |
| 2 | TiO2 | anatase | 110 mAh g-1 (0.2 A g-1) | 110 mAh g-145 mAh g-1 (0.2~2 A g-1) | / | [S2] |
| 3 | TiO2 | anatase | 130 mAh g-1 (0.15 A g-1) | 130 mAh g-185 mAh g-1 (0.15~0.6 A g-1) | / | [S3] |
| 4 | TiO2 | anatase | 150 mAh g-1 (0.5 A g-1) | 130 mAh g-1115 mAh g-1 (0.5~1.5 A g-) | / | [S4] |
| 5 | TiO2 | anatase | 90 mAh g-1 (0.15 A g-1) | 90 mAh g-125 mAh g-1 (0.15~3 A g-1) | / | [S5] |
| 6 | TiO2 | anatase | 210 mAh g-1 (0.2 A g-1) | 210 mAh g-1160 mAh g-1 (0.2~2 A g-1) | / | [S6] |
| 7 | TiO2 | anatase | 160 mAh g-1 (0.1 A g-1) | 160 mAh g-150 mAh g-1 (0.1~3 A g-1) | / | [S7] |
| 8 | Ag/TiO2 | anatase | 150 mAh g-1 (0.1 A g-1) | 150 mAh g-155 mAh g-1 (0.1~1 A g-1) | / | [S8] |
| 9 | TiO2 | anatase | 140 mAh g-1 (0.15 A g-1) | 140 mAh g-155 mAh g-1 (0.15~1.5 A g-1) | / | [S9] |
| 10 | TiO2 | anatase | 130 mAh g-1 (1.84 uA cm-2) | / | / | [S10] |
| 11 | TiO2 | anatase | 190 mAh g-1 （0.3 A g-1） | / | 230 mAh g-1 (0.3 A g-1) | [S11] |
| 12 | TiO2 | anatase | 185 mAh g-1 (0.2 A g-1) | 185mAh g-188 mAh g-1 (0.2 A g-1~3 A g-1) | 218 mAh g-1121 mAh g-1 (0.2 A g-1~3 A g-1) | This work |
| 13 | Au-TiO2 | anatase | 205 mAh g-1 (0.2 A g-1) | 205 mAh g-1105 mAh g-1 (0.2 A g-1~3 A g-1) | 276 mAh g-1163 mAh g-1 (0.2 A g-1~3 A g-1) | This work |

Supplementary References

- W. Song, Q. Jiang, X. Xie, A. Brookfield, E.J.L. McInnes et al., Synergistic storage of lithium ions in defective anatase/rutile TiO2 for high-rate batteries. Energy Storage Mater. 22, 441-449 (2019). https://doi.org/10.1016/j.ensm.2019.07.025

- Y. Chen, J. Chen, J. Liu, Z. Lin, X. Hu et al., Metal-organic framework-derived mixed-phase anatase/rutile TiO2 towards boosted lithium storage: Surface engineering and design strategy through crystal phase transition. Mater. Today Nano 22, 100265 (2022).  https://doi.org/10.1016/j.mtnano.2022.100265

- J. Ma, K.G. Reeves, A.-G.P. Gutierrez, M. Body, C. Legein et al., Layered lepidocrocite type structure isolated by revisiting the sol–gel chemistry of anatase TiO2: A new anode material for batteries. Chem. Mater. 29, 8313-8324 (2017). https://doi.org/10.1021/acs.chemmater.7b02674

- Y. Cai, H.-E. Wang, X. Zhao, F. Huang, C. Wang et al., Walnut-like porous core/shell TiO2 with hybridized phases enabling fast and stable lithium storage. ACS Appl. Mater. Interfaces 9, 10652 (2017). https://doi.org/10.1021/acsami.6b16498

- M. Zhang, K. Yin, Z.D. Hood, Z. Bi, C.A. Bridges et al., In situ TEM observation of the electrochemical lithiation of N-doped anatase TiO2 nanotubes as anodes for lithium-ion batteries. J. Mater. Chem. A 5, 20651-20657 (2017). https://doi.org/10.1039/C7TA05877B

- D.-H. Lee, B.-H. Lee, A.K. Sinha, J.-H. Park, M.-S. Kim et al., Engineering titanium dioxide nanostructures for enhanced lithium-ion storage. J. Am. Chem. Soc. 140, 16676-16684 (2018). https://doi.org/10.1021/jacs.8b09487

- Y. Qiu, K. Yan, S. Yang, L. Jin, H. Deng et al., Synthesis of size-tunable anatase TiO2 nanospindles and their assembly into anatase@titanium oxynitride/titanium nitride−graphene nanocomposites for rechargeable lithium ion batteries with high cycling performance. ACS Nano 11, 6515-6526 (2010). https://doi.org/10.1021/nn101603g

- Y. Zhang, J. Li, W. Li, D. Kang, Synthesis of one-dimensional mesoporous Ag nanoparticles-modified TiO2 nanofibers by electrospinning for lithium ion batteries. Materials 12, 2630 (2019). https://doi.org/10.3390/ma12162630

- D.T. D, S. Mohapatra, S.V. Nair, A.S. Nair, A.K. Ra, Surfactant-assisted synthesis of porous TiO2 nanofibers as an anode material for secondary lithium ion batteries. Sustainable Energy Fuels 1, 138-144 (2017). https://doi.org/10.1039/C6SE00030D

- D. Imazeki, C.C. Gils, K. Nishio, R. Shimizu, T. Hitosugi, Effects of anisotropy in rutile TiO2 on the performance of solid-state lithium batteries. ACS Appl. Energy Mater. 3, 8338-8343 (2020). https://doi.org/10.1021/acsaem.0c00910

- O. Nguyen, E. Courtin, F. Sauvage, N. Krins, C. Sancheza et al., Shedding light on the light-driven lithium ion de-insertion reaction: towards the design of a photo-rechargeable battery. J. Mater. Chem. A 5, 5927-5933 (2017). https://doi.org/10.1039/C7TA00493A