Supporting Information for

Understanding the Decoupled Effects of Cations and Anions Doping for High Performance Perovskite Solar Cells

Tianxiang Hu1, Yixi Wang3, Kai Liu1, Jia Liu4, Haoyang Zhang1, Qudrat Ullah Khan5, Shijie Dai1, Weifan Qian1, Ruochen Liu3, Yanyan Wang1, Chongyuan Li1, Zhenru Zhang1, Mingxiang Luo1, Xiaofei Yue1, Chunxiao Cong1, Yuan Yongbo4, Anran Yu1*, Jia Zhang2*, Yiqiang Zhan1,2*

1 Center of Micro-Nano System, School of Information Science and Technology, Fudan University, Shanghai 200438, People’s Republic of China

2 The State Key Laboratory of Photovoltaic Science and Technology, Institute of Optoelectronics, Fudan University, Shanghai 200438, People’s Republic of China

3 Institute for Electric Light Sources, School of Information Science and Technology, Fudan University, Shanghai 200438, People’s Republic of China

4 Hunan Key Laboratory of Nanophotonics and Devices, School of Physics, Central South University, Changsha, Hunan 410083, People’s Republic of China

5 Vanced materials Technology (Zhongshan) Co., Ltd. Guangdong, 528437, People Republic China

*Corresponding authors. E-mail: jia.zhang0219@gmail.com (Jia Zhang); aryu@fudan.edu.cn (Anran Yu); yqzhan@fudan.edu.cn (Yiqiang Zhan)

Note S1 Calculation of the Lattice Constants

To get detailed understanding of the doped perovskite structure, we further calculate the lattice constant of Mg(CF3SO3)2, Ca(CF3SO3)2, Ba(CF3SO3)2 doped perovskite, respectively. We use the peaks with highest intensity to get the lattice constant in consideration of minimizing computational error.

We firstly calculate the interplanar spacing d using the equation:

d=nλ2sinθ

Where λ = 1.542 Å (The wavelength of the incident X-ray)

θ = peak position (In radians)

n = 1 (Order of diffraction)

As our doped perovskites keep the cubic structure, the lattice constants can be further calculated with the following equation:

a=b=c=d·h2+k2+l2

where (hkl) represents the crystal indices.

Supplementary Figures and Tables

Fig. S1 The top-surface EDS mapping of (a) Mg2+ elements in 1% Mg(CF3SO3)2 doped, (b) Ca2+ elements in 1% Ca(CF3SO3)2 doped and (c) Ba2+ elements in 1% Ba(CF3SO3)2 doped perovskite films

Fig. S2 XRD pattern of fabricated perovskite film with (a) MgI2, (b) BaI2 dissolved in DMF, (c) CaI2 first dissolved in H2O then added to precursor and FACF3SO3 additive

Fig. S3 Top-view SEM images of (a) pristine PbI2 film and PbI2 film with (b) 0.05%, (c) 0.4%, (d) 1% Ca(CF3SO3)2 dopant

Fig. S4 (a) XRD pattern of control and 0.15% Ca(CF3SO3)2 doped PbI2 films. (b) Extracted PbI2 (001) peak intensity and FWHM from the XRD results

Fig. S5 Top-view SEM images of (a) control perovskite film and perovskite film with (b) 0.3%, (c) 0.5%, (d) 0.8% FACF3SO3 additive

Fig. S6 Cross-sectional SEM images of (a) control perovskite film and (b) perovskite film with 0.15% Ca(CF3SO3)2

Fig. S7 UV-vis absorption spectra of perovskite films with and without 0.15% Ca(CF3SO3)2

Fig. S8 Statistical distribution of JSC for perovskite solar with cells with different Ca(CF3SO3)2 doping ratio

Fig. S9 Statistical distribution of (a) JSC, (b) VOC, (c) FF and (d) PCE of control, 0.15% Mg(CF3SO3)2, 0.15% Ca(CF3SO3)2, 0.15% Ba(CF3SO3)2, 0.15% Calcium dobesilate doped devices, respectively

Fig. S10 Temperature dependent conductivity measurements of lateral devices (Au/perovskite/Au) with (a) 0.15% Mg(CF3SO3)2 and (b) 0.15% Ba(CF3SO3)2

Fig. S11 Cross-sectional EDS mapping of iodide and Pb elements in perovskite with and without 0.15% Ca(CF3SO3)2

Table S1 Fitted parameters for the data in Fig. 1h

|  | (001) position | (001) width | (111) position | (111) width |
| --- | --- | --- | --- | --- |
| control | 13.88741 | 0.11417 | 24.24165 | 0.10738 |
| 1% Mg(CF3SO3)2 | 13.86796 | 0.09622 | 24.19939 | 0.10718 |
| 0.4% Ca(CF3SO3)2 | 13.88395 | 0.01157 | 24.21797 | 0.02818 |
| 1% Ba(CF3SO3)2 | 13.8496 | 0.1235 | 24.17839 | 0.14418 |

Table S2 Calculated lattice constants for control, 1% Mg(CF3SO3)2 doped, 0.4% Ca(CF3SO3)2 doped and 1% Ba(CF3SO3)2 doped perovskites based on the method described in Note S1

|  | From (001) | From (111) |
| --- | --- | --- |
| control | 6.37748 Å | 6.35989 Å |
| 1% Mg(CF3SO3)2 | 6.38638 Å | 6.37083 Å |
| 0.4% Ca(CF3SO3)2 | 6.37907 Å | 6.36602 Å |
| 1% Ba(CF3SO3)2 | 6.39481 Å | 6.37628 Å |