Supporting Information for

Quantum Dots Mediated Crystallization Enhancement in Two-Step Processed Perovskite Solar Cells

Heng Liu1,2, , Geyu Jin3, , Jiantao Wang2*, Weihai Zhang4, Long Qing2, Yao Zhang3,  Qiongqiong Lu1, Pengfei Yue1, Guoshang Zhang1, Jing Wei3*, Hongbo Li3*, Hsing-Lin Wang2*

1Henan Key Laboratory of Advanced Conductor Materials, Institute of Materials, Henan Academy of Sciences, Zhengzhou 450046, P. R. China

2Department of Materials Science and Engineering, Southern University of Science and Technology, Shenzhen 518055, Guangdong, P. R. China

3Beijing Key Laboratory of Construction-Tailorable Advanced Functional Materials and Green Applications, Experimental Center of Advanced Materials, School of Materials Science and Engineering, Beijing Institute of Technology, Beijing 100081, P. R. China

4College of New Energy, Ningbo University of Technology, Ningbo 315336, P. R. China

Heng Liu and Geyu Jin contributed equally to this work.

*Corresponding authors. jwangdz@connect.ust.hk (Jiantao Wang); weijing@bit.edu.cn (Jing Wei); hongbo.li@bit.edu.cn (Hongbo Li); wangxl3@sustech.edu.cn (Hsing-Lin Wang)

S1 Experimental Section

Materials: The ITO glass substrates were purchased from Advanced Electronic Technology Company in China. SnO2 was acquired from Alfa Aesar. Formamidinium Iodide (FAI), Methylammonium Bromide (MABr), Methylammonium Chloride (MACl), and Lithium-bis(trifluoromethanesulfonyl)imide (Li-TFSI) were obtained from Advanced Electronic Technology Company in China. Spiro-OMeTAD, Lead (II) iodide (PbI2), and 4-tert-butylpyridine were procured from Xi'an Polymer Light Technology Corp (Xi'an p-OLED). N,N-dimethylformamide (DMF), isopropyl alcohol (IPA), acetonitrile (ACN), chlorobenzene (CB), and dimethylsulfoxide (DMSO) were purchased from Sigma-Aldrich. Gold (Au, 99.99%) was obtained from commercial sources. Cesium carbonate (Cs2CO3, 99.99%), PbBr2 (99.99%), PbI2 (99.99%) were purchased from Aladdin. 1-octadecene (ODE, 90%), oleic acid (OA, 90%), oleylamine (OAm, 80–90%) were purchased from Alfa Aesar.

Solution Preparation: The 12 wt% SnO2 colloidal solution was diluted in deionized water (1:3, v:v) and stirred for 10 minutes at room temperature, followed by filtration using a syringe and an aqueous filter. For the preparation of the PbI2 precursor solution, 691.5 mg of PbI2 powder was dissolved in 1 mL of DMF/DMSO (900:100) and stirred overnight at 70 °C. To prepare the organic amine salt solution, an isopropyl alcohol (IPA) solution containing organic salts (with a mass ratio of FAI:MACl of 90 mg:15 mg) was stirred at 70 °C for 30 minutes. The preparation of the Spiro-OMeTAD HTL solution included 72.3 mg of Spiro-OMeTAD, 28.8 μL of 4-tertbutylpyridine, 17.5 μL of lithium-bis (trifluoromethanesulfonyl) imide (Li-TFSI) solution (520 mg Li-TFSI in 1 mL acetonitrile), and 1 mL of chlorobenzene. Cs2CO3 (0.2 g), ODE (10 mL), OA (0.7 mL) were loaded into a 50 mL flask and degassed for 1 h at 100 ℃ and then heated to 150 ℃ under N2 atmosphere until the Cs2CO3 was completely dissolved.

Quantum dots Preparation: CsPbBr3 QDs and CsPbI3 QDs were synthesized through a reported method with minor modifications [S1]. PbX2 (0.43 mmol) such as PbBr2 (0.157g) or PbI2 (0.2 g), ODE (10 mL), OA (1 mL) and OAm (1 mL) were loaded into a 50 mL flask and degassed for 1 h at 100 ℃ and then heated to 150 ℃ under N2 atmosphere to form a clear solution. The temperature was increased to 170 ℃, followed by the quick injection of 0.8 mL Cs-OA solution. 5 seconds after the injection, the reaction was stopped with an ice bath. The ethyl acetate was added to the crude solution (Ethyl acetate: crude solution=1:1 by volume) to precipitate QDs, then the mixture solution was centrifugation at 7000 rpm for 3 min. The collected CsPbX3 QDs were dispersed in toluene to form a solution with 15 mg/mL concentration.

Device Fabrication: The ITO glass substrates were initially cleaned with a detergent, followed by ultrasonic cleaning in deionized water, acetone, and isopropanol for 30 minutes each. The ITO glass was dried with nitrogen gas before undergoing a 5-minute plasma treatment. Subsequently, SnO2 was spin-coated onto the substrates at a speed of 3500 rpm to serve as the electron transport layer, followed by thermal annealing at 150°C for 30 minutes on a hot plate. After cooling to room temperature, the substrates were transferred to a nitrogen-filled glovebox. A 1.5M PbI2 solution (in anhydrous DMF: DMSO at a volume ratio of 9:1) was then spin-coated onto the SnO2 layer at 1700 rpm, annealed at 70°C for 1 minute, and allowed to cool for 10 minutes. Quantum dot solution, at a concentration of 3 mg/mL, was then spin-coated on the PbI2 layer, followed by a 70°C anneal for 1 minute. Afterwards, a FAI:MACl solution (90 mg:15 mg in 1 mL IPA) was spin-coated on the PbI2 layer at 1800 rpm for 30 seconds, after which the substrates were transferred to an air atmosphere glovebox (RH 30%-40%) for thermal annealing at 150°C for 10 minutes on a hot plate. Post-annealing, the substrates were cooled to room temperature in a nitrogen-filled glovebox. Next, a Spiro-OMeTAD solution was spin-coated onto the prepared perovskite film at 4000 rpm for 30 seconds. Lastly, a gold electrode approximately 80 nm thick was thermally evaporated under high vacuum through a mask.

Characterizations: The crystal structure and phases of the perovskite were characterized using a Bruker Advanced D8 X-ray diffractometer under Cu Kα (λ = 0.154 nm) radiation. The absorbance spectra of the perovskite film were obtained using a UV-Vis spectrophotometer (Agilent Cary 5000). Steady-state photoluminescence (PL) spectra were recorded on a Shimadzu RF-5301pc, while time-resolved photoluminescence spectra were acquired using a picosecond pulsed laser excitation with a 1 MHz repetition rate through a photoluminescence system (Fluo-Time 300). The morphology of the film was investigated using a scanning electron microscope (SEM; TESCAN MIRA3). The surface potential of the perovskite film was measured using an atomic force microscope (AFM; Asylum Research MFP-3D-Stand Alone). X-ray photoelectron spectroscopy (XPS) was performed on a Thermo K-Alpha+ spectrometer equipped with a monochromatic Al Kα X-ray source (1486.6 eV) operating at 100 W power. The samples were analyzed under vacuum (P < 10-8 mbar), calibrated through 150 eV (survey scan) or 50 eV (high-resolution scan) energy pass, with a binding energy of C 1s at 284.8 eV for calibration. Ultraviolet photoelectron spectroscopy (UPS, ESCALAB 250Xi, Thermo Fisher) measurements were carried out using a He Iα photon source (21.22 eV). Current-voltage (J-V) curves for fabricated devices were obtained by collecting data under forward and reverse scans with 30 mV intervals and a 10 ms delay time, under AM 1.5 G illumination (100 mW cm-2) using a source meter (Keysight B2901A) and a solar simulator (Enlitech SS-F5-3A). The external quantum efficiency (EQE) spectra were measured using an Enlitech QER-3011 quantum efficiency test system, calibrated for each wavelength's light intensity using a Si detector before measurement. The maximum power point (MPP) output was obtained from the maximum power point current density. Electrochemical impedance spectroscopy (EIS) tests were conducted using a Princeton Applied Research P4000+ electrochemical workstation in the frequency range from 100 Hz to 1 MHz, at a bias voltage of 1 V under dark conditions with an amplitude of 10 mV.

S2 Supplementary Figures and Tables

Fig. S1 Size distribution histograms of CsPbI3 and CsPbBr3 quantum dots

Fig. S2 (a-c) Grain size statistics for Control, Br-PVSK and I-PVSK perovskite films

Fig. S3 AFM topographical images of Control, Br-PVSK and I-PVSK perovskites films

Fig. S4 (a-c) Cross-sectional SEM images of PSC devices based on Control and  Br-PVSK, I-PVSK modified

Fig. S5 TEM morphology of (a, b) CsPbI3 and (c, d) CsPbBr3 QDs after IPA washing

Fig. S6 (a) The humidity stability of unencapsulated PSCs was evaluated in ambient air at approximately 85% relative humidity (RH) at room temperature. The devices were subjected to periodic testing under AM 1.5G illumination using a xenon arc lamp at a power density of 100 mW cm−2. (b) The thermal stability of unencapsulated PSCs was assessed under continuous heating at 85 °C in a nitrogen atmosphere. These devices were also periodic testing under AM 1.5G irradiation from a xenon arc lamp at 100 mW cm−2. (c) The stability of unencapsulated PSCs was examined during storage in ambient air at around 85% RH, coupled with heating at 85 °C. Periodic testing of these devices was conducted under AM 1.5G illumination from a xenon arc lamp at a power density of 100 mW cm−2

Fig. S7 UPS spectra of secondary electron cutoff and valence bands for Control, Br-PVSK and I-PVSK perovskite films, respectively

Fig. S8 (a) UV–vis absorption spectra of perovskite films on top of Control, Br-PVSK and I-PVSK. (b) Tauc’s plot calculated from the UV-Vis absorption spectra with equation (αhυ)2 = A(hυ-Eg), where α is the absorption coefficient, hυ is the photon energy, and Eg is the bandgap

Fig. S9 Perovskite energy level diagram constructed from UPS results, where Evac stands for vacuum energy level, CBM is conduction band minimum, Ef is fermi level of as-deposited perovskite film, Ei is fermi level of intrinsic perovskite film, and VBM is valence band maximum

Fig. S10 KPFM images of Control, Br-PVSK and I-PVSK perovskites films

Fig. S11 (a) Steady-state PL and (b) TRPL spectra of Glass/PVSK/ Spiro-OMeTAD, Glass/Br-PVSK/Spiro-OMeTAD and Glass/I-PVSK/Spiro-OMeTAD

Fig. S12 (a−c) Dark J−V curves representing electron-only devices fabricated by using control, Br-PVSK, and I-PVSK perovskite films

Table S1 TRPL parameters of the control, Br-PVSK and I-PVSK perovskite films

| Sample | A1 | τ1 [ns] | A2 | τ2 [ns] | τave [ns] |
| --- | --- | --- | --- | --- | --- |
| Control | 0.51 | 74.91 | 0.53 | 447.40 | 395.60 |
| Br-PVSK | 0.29 | 1346.10 | 1.72 | 267.35 | 759.90 |
| I-PVSK | 0.28 | 1388.40 | 0.79 | 265.90 | 994.50 |

Table S2 TRPL parameters of the Glass/PVSK/Spiro-OMeTAD, Glass/Br-PVSK/Spiro-OMeTAD and Glass/I-PVSK/Spiro-OMeTAD

| Sample | A1 | τ1 [ns] | A2 | τ2 [ns] | τave [ns] |
| --- | --- | --- | --- | --- | --- |
| Control | 0.85 | 43.20 | 0.45 | 324.80 | 271.30 |
| Br-PVSK | 0.36 | 55.50 | 0.63 | 205.10 | 201.20 |
| I-PVSK | 0.31 | 32.40 | 0.68 | 169.60 | 158.80 |

Table S3 Photovoltaic performance of the champion devices for the corresponding PSCs

| Sample | Scan direction | Voc [V] | Jsc [mA cm-2] | FF [%] | PCE [%] | Integrated Jsc [mA cm–2] |
| --- | --- | --- | --- | --- | --- | --- |
|  | Forward | 1.106 | 25.26 | 76.64 | 21.43 |  |
| Control | Reverse | 1.116 | 25.34 | 77.04 | 22.05 | 24.20 |
|  | Forward | 1.181 | 25.47 | 79.51 | 23.91 |  |
| Br-PVSK | Reverse | 1.184 | 25.55 | 79.70 | 24.11 | 24.51 |
|  | Forward | 1.194 | 25.38 | 81.42 | 24.67 |  |
| I-PVSK | Reverse | 1.196 | 25.38 | 81.55 | 24.75 | 24.34 |

Table S4 Conduction band minimum (CBM) and valence band maximum (VBM) of control, Br-PVSK and I-PVSK perovskite films

| Sample | VBM | CBM | Eg | WF |
| --- | --- | --- | --- | --- |
| Control | 5.85 | 4.29 | 1.56 | 4.57 |
| Br-PVSK | 5.79 | 4.23 | 1.56 | 4.54 |
| I-PVSK | 5.75 | 4.19 | 1.56 | 4.52 |

Supplementary Reference

[S1] L. Protesescu, S. Yakunin, M.I. Bodnarchuk, et al. Nanocrystals of cesium lead halide perovskites (CsPbX3, X = Cl, Br, and I): novel optoelectronic materials showing bright emission with wide color gamut. Nano Lett. 15(6), 3692-3696 (2015). https://doi.org/10.1021/nl5048779