Supporting Information for

Transformative Effect of Li Salt for Proactively Mitigating Interfacial Side Reactions in Sodium-Ion Batteries

Jooeun Byun 1,#, Joon Ha Chang 2,#, Chihyun Hwang 1,#, Chae Rim Lee 1, Miseung Kim 1, Jun Ho Song 1, Boseong Heo 3, Sunghun Choi 3, Jong Hyeok Han 4, Hee-Jae Jeon 5, Beom Tak Na 6,  Youngjin Kim 3,*, Ji-Sang Yu 1,*,  and Hyun-seung Kim 1,*

1 Advanced Batteries Research Center, Korea Electronics Technology Institute, 25, Saenari-ro, Seongnam 13509, Republic of Korea

2 Analysis and Assessment Research Group, Research Institute of Industrial Science and Technology, Cheongam-ro 67, Pohang 37673, Republic of Korea

3  Department of Battery Convergence Engineering, Kangwon National University1, Kangwon-daehakro, Chuncheon-si, Kangwon 24341, Republic of Korea

4 Department of Mechanical and Biomedical Engineering, Kangwon National University 1, Kangwon-daehakro, Chuncheon-si, Kangwon 24341, Republic of Korea

5 Department of Smart Health Science and Technology, Kangwon National University 1, Kangwon-daehakro, Chuncheon-si, Kangwon 24341, Republic of Korea

6 Research Institute of Intelligent Manufacturing & Materials Technology, Korea Institute of Industrial Technology, Gaetbeol-ro 156, Incheon, Republic of Korea

#Jooeun Byun, Joon Ha Chang, and Chihyun Hwang contributed equally to this work.

*Corresponding authors. E-mail: ykim@kangwon.ac.kr (Youngjin Kim); jisang@keti.re.kr (Ji-Sang Yu); hskim0113@keti.re.kr (Hyun-seung Kim)

Supplementary Figures and Table

Fig. S1 Raman spectra obtained from background and LiPF6-added electrolytes, respectively

Fig. S2 Linear sweep voltammogram obtained from Cu/Na cell with background and LiPF6-added electrolytes

Fig. S3 Ionic conductivities of background and LiPF6-added electrolytes

Fig. S4. Three-dimensionally reconstructed time-of-flight secondary ion-mass spectroscopy (ToF-SIMS) map obtained from the O3-type positive electrode cycled with the LiPF6-added electrolyte

Fig. S5 First cycle voltage profile of the O3-type positive electrode in a sodium half-cell

Fig. S6 (a) Cycleability and (b) Coulombic efficiency obtained from the O3 electrode-based half-cells with background and Li salt-added electrolytes

Fig. S7 (a) Cycleability and (b) Coulombic efficiency obtained from the hard carbon electrode-based half-cells with background and Li salt-added electrolytes

Fig. S8 Coulombic efficiency obtained from the hard carbon/O3-type electrode based pouch-cells with FEC-added and Li salt-added electrolytes, respectively

Fig. S9 C 1s X-ray photoelectron spectra obtained from the hard-carbon electrode after 400 cycles with the addition of the FEC and LiPF6 electrolytes

Fig. S10 Energy-dispersive spectroscopic results recorded from the cycled hard-carbon electrodes following the addition of the FEC and LiPF6 electrolytes

Fig. S11 Three-dimensionally reconstructed ToF-SIMS map of the hard-carbon electrode after formation following the addition of the LiPF6 and lithium difluoro(oxalato)borate (LiODFB) electrolytes

Fig. S12 Initial voltage profiles after the formation at pouch cells with the LiPF6 and LiODFB electrolytes

Fig. S13 (a) cycle performance obtained from background, FEC-added, and Li salt-added electrolytes, respectively, (b) HR-TEM and corresponding FFT images of cycled positive electrode, (c) SEM image of cycled negative electrode, (d) rate capability obtained from pouch cells with background and Li salt-added electrolytes

Table S1 The acheived capacity retention from recently reported literature and this work with hard carbon/O3 electrodes configuration

|  | Voltage Range / V | Cycle Number | Retention / % | Mass loading / mg cm-2 | C-rate / C | References |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 1.5-4.0 | 170 | 96 | 1.6 | 0.3 | Chemical Engineering Journal, 2024, 491, 151949 |
| 2 | 2.0-4.0 | 500 | 81 | 2.0 | 0.2 | Small, 2024, 2407425 |
| 3 | 1.5-4.0 | 16 | 80 | 4.3 | 0.2 | Electrochimica Acta, 2018, 281, 370 |
| 4 | 1.9-3.9 | 200 | 85 | 1.0 | 1.0 | Energy Storage Materials, 2025, 74, 103894 |
| 5 | 1.5-4.2 | 100 | 68 | N.A. | 1.0 | Journal of Alloys and Compounds, 2023, 968, 171808 |
| 6 | 1.0-4.0 | 200 | 77 | 1.0 | 1.0 | Journal of The Electrochemical Society, 2023, 170, 070518 |
| 7 | 1.2-4.0 | 400 | 92.7 | 15.0 | 1.0 | This Work |