Supporting Information for

Buried Interface Regulation with TbCl3 for Highly-Efficient All-Inorganic Perovskite/Silicon Tandem Solar Cells

Wenming Chai1, Weidong Zhu1*, He Xi1,3, Dazheng Chen1, Hang Dong1, Long Zhou1, Hailong You1, Jincheng Zhang1, Chunfu Zhang1*, Chunxiang Zhu2 and Yue Hao1

1State Key Laboratory of Wide-Bandgap Semiconductor Devices and Integrated Technology, School of Microelectronics, Xidian University, Xi'an 710071, P. R. China

2Department of Electrical and Computer Engineering, National University of Singapore, 10 Kent Ridge Crescent, 119260, Singapore

3Department of nanomaterials, University of Melbourne, Parkville Victoria, 3010, Australia

*Corresponding authors. E-mail: wdzhu@xidian.edu.cn (Weidong Zhu); cfzhang@xidian.edu.cn (Chunfu Zhang)

Supplementary Figures and Tables

Fig. S1 a C 1s, b Tb 4d, c Cl 2p, d Pb 4f, e Cs 3d, and f I 3d core-level XPS spectra of CsPbI3 films based on Me-4PACz with and without TbCl3 doping

Fig. S2 Cross-section SEM images of the CsPbI3 films based on Me-4PACz a without and b with TbCl3 doping

Fig. S3 AFM images of the CsPbI3 films based on Me-4PACz a without and b with TbCl3 doping

Fig. S4 Magnified (110) and (220) XRD peaks of CsPbI3 films prepared on Me-4PACz with and without TbCl3 doping

Fig. S5 PL spectra from the surface side of CsPbI3 films prepared on Me-4PACz with and without TbCl3 doping

Fig. S6 UPS spectra of Me-4PACz with and without TbCl3 doping

Fig. S7 Statistical a VOC, b JSC, c FF and d PCE for CsPbI3 PSCs prepared on Me-4PACz with 0.5, 1, 3, and 5 mg/mL TbCl3 doping

Fig. S8 Light J-V curves recorded under forward voltage scan from -0.1 to 1.3 V and reverse voltage scan from 1.3 to -0.1 V for the champion CsPbI3 PSC prepared without and with TbCl3-doped Me-4PACz

Fig. S9 Dark J-V curves of CsPbI3 PSCs based on Me-4PACz with and without TbCl3 doping

Fig. S10 Statistical a VOC and b FF for CsPbI3 PSCs prepared on Me-4PACz without and with TbCl3 doping

Fig. S11 PL spectral of CsPbI3 films prepared without and with TbCl3-doped Me-4PACz after storing for 5 days in ambient air

Fig. S12 J-V curves of CsPbI3 PSCs fabricated without and with TbCl3-doped Me-4PACz after storing for 5 days in ambient air

Fig. S13 a TPC and b TPV curves of CsPbI3 PSCs based on Me-4PACz with and without TbCl3 doping

Fig. S14 a Nyquist and b M-S plots of CsPbI3 PSCs based on Me-4PACz with and without TbCl3 doping

Table S1 The fitting parameters of TRPL spectra for CsPbI3 films on Me-4PACz with and without TbCl3 doping

|  | A1 | τ1 (ns) | A1 | τ2 (ns) | τave (ns) |
| --- | --- | --- | --- | --- | --- |
| w/o TbCl3 | 21.93 | 0.46 | 0.37 | 1.66 | 2.67 |
| w/ TbCl3 | 2.02 | 0.28 | 0.59 | 2.79 | 1.55 |

Table S2 Photovoltaic parameters of the optimized CsPbI3 PSCs based on Me-4PACz with and without TbCl3 doping

| Samples | VOC (V) | JSC (mA/cm2) | FF | PCE (%) |
| --- | --- | --- | --- | --- |
| w/o TbCl3 | 1.017 | 19.9 | 0.758 | 15.34 |
| w/ TbCl3 | 1.162 | 20.12 | 0.799 | 18.68 |

Table S3 Photovoltaic parameters of the semitransparent CsPbI3 PSC, the silicon solar cell before and after filtering, and the perovskite/silicon tandem device

| Samples | JSC (mA/cm2) | VOC (V) | FF | PCE (%) |
| --- | --- | --- | --- | --- |
| Si-Cell | 41.81 | 0.72 | 0.761 | 22.91 |
| Si-Filtered | 21.93 | 0.70 | 0.770 | 11.83 |
| Semitransparent PSCs | 19.75 | 1.11 | 0.802 | 17.57 |
| 4T TSCs |  |  |  | 29.40 |
| 2T TSCs | 18.56 | 1.75 | 0.783 | 25.44 |

Table S4 Performance comparisons of the tandem solar cells based on all-inorganic perovskite materials

| Device structure | All-inorganic materials | PCE (%) | Year | References |
| --- | --- | --- | --- | --- |
| all-perovskite TSC | CsPbI1.5Br1.5 | 18.07 | 2022 | [S1] |
| all-perovskite TSC | CsPbI2Br | 19.61 | 2023 | [S2] |
| Perovskite/organic TSC | CsPbI2Br | 17.24 | 2020 | [S3] |
| Perovskite/organic TSC | CsPbI2.1Br0.9 | 18.06 | 2021 | [S4] |
| Perovskite/organic TSC | CsPbI1.8Br1.2 | 21.04 | 2022 | [S5] |
| Perovskite/organic TSC | CsPbI2Br | 20.2 | 2022 | [S6] |
| Perovskite/organic TSC | CsPbI2Br | 21.4 | 2022 | [S7] |
| Perovskite/organic TSC | CsPbI2.2Br0.8 | 22.43 | 2022 | [S8] |
| Perovskite/organic TSC | CsPbI2Br | 23.21 | 2023 | [S9] |
| Perovskite/organic TSC | Cs0.99Rb0.01PbI2.2Br0.8 | 23.07 | 2024 | [S10] |
| Perovskite/organic TSC | CsPbI2.5Br0.5 | 23.24 | 2024 | [S11] |
| Perovskite/organic TSC | CsPbI2Br | 22.34 | 2023 | [S12] |
| Perovskite/silicon TSC | CsPbIxBr3-x | 22.95 | 2022 | [S13] |
| Perovskite/silicon TSC | CsPbI2.85Br0.15 | 25.31 | 2023 | [S14] |
| Perovskite/silicon TSC | CsPbI2.85Br0.15 | 27.27 | 2024 | [S15] |
| 2T Perovskite/silicon TSC | CsPbI3 | 25.44 | 2024 | This work |
| 4T Perovskite/silicon TSC | CsPbI3 | 29.40 | 2024 | This work |

Supplementary References

- Q. Sun, Z. Zhang, T. Zhang, Y. Feng, A. Gu et al. Integrated 4-terminal all-inorganic perovskite tandem solar cell with open-circuit voltage exceeding 2.1 V for water splitting. ACS Energy Lett. 7(12), 4215-4223 (2022). https://doi.org/10.1021/acsenergylett.2c02262

- Q. Wen, C. Duan, F. Zou, D. Luo, J. Li et al. All-inorganic CsPb1-xSnxI2Br perovskites mediated by dicyandiamide additive for efficient 4-terminal tandem solar cell. Chem. Engin. J. 452, 139697 (2023). https://doi.org/10.1016/j.cej.2022.139697

- K. Lang, Q. Guo, Z. He, Y. Bai, J. Yao et al. High performance tandem solar cells with inorganic perovskite and organic conjugated molecules to realize complementary absorption. J. Phys. Chem. Lett. 11(22), 9596-9604 (2020). https://doi.org/10.1021/acs.jpclett.0c02794

- X. Wu, Y. Liu, F. Qi, F. Lin, H. Fu et al. Improved stability and efficiency of perovskite/organic tandem solar cells with an all-inorganic perovskite layer. J. Mater. Chem. A 9(35), 19778-19787 (2021). https://doi.org/10.1039/D0TA12286F

- W. Chen, D. Li, X. Chen, H. Chen, S. Liu et al. Surface reconstruction for stable monolithic all‐inorganic perovskite/organic tandem solar cells with over 21% efficiency. Adv. Funct. Mater. 32(5), 2109321 (2022). https://doi.org/10.1002/adfm.202109321

- X. Gu, X. Lai, Y. Zhang, T. Wang, W. L. Tan et al. Organic solar cell with efficiency over 20% and VOC exceeding 2.1 V enabled by tandem with all‐inorganic perovskite and thermal annealing‐free process. Adv. Sci. 9(28), 2200445 (2022). https://doi.org/10.1002/advs.202200445

- Y. Ding, Q. Guo, Y. Geng, Z. Dai, Z. Wang et al. A low-cost hole transport layer enables CsPbI2Br single-junction and tandem perovskite solar cells with record efficiencies of 17.8% and 21.4%. Nano Today 46, 101586 (2022). https://doi.org/10.1016/j.nantod.2022.101586

- Q. Yao, Y. M. Xie, Y. Zhou, Q. Xue, X. Xu et al. Dual sub‐cells modification enables high‐efficiency n–i–p type monolithic perovskite/organic tandem solar cells. Adv. Funct. Mater. 33(8), 2212599 (2023). https://doi.org/10.1002/adfm.202212599

- S. Q. Sun, X. Xu, Q. Sun, Q. Yao, Y. Cai et al. All‐inorganic perovskite‐based monolithic perovskite/organic tandem solar cells with 23.21% efficiency by dual‐interface engineering. Adv. Energy Mater. 13(16), 2204347 (2023). https://doi.org/10.1002/aenm.202204347

- S. S. Mali, J. V. Patil, J. A. Steele, M. K. Nazeeruddin, J. H. Kim et al. All-inorganic halide perovskites for air-processed “n–i–p” monolithic perovskite/organic hybrid tandem solar cells exceeding 23% efficiency. Energy Environ. Sci. 17(3), 1046-1060 (2024). https://doi.org/10.1039/D3EE02763E

- Y. Li, Y. Yan, Y. Fu, W. Jiang, M. Liu et al. Highly durable inverted inorganic perovskite/organic tandem solar cells enabled by multifunctional additives. Angew. Chem. Int. Ed., e202412515 (2024). https://doi.org/10.1002/anie.202412515

- L. Liu, H. Xiao, K. Jin, Z. Xiao, X. Du et al. 4-Terminal inorganic perovskite/organic tandem solar cells offer 22% efficiency. Nano-Micro Lett. 15(1), 23 (2023). https://doi.org/10.1007/s40820-022-00995-2

- 13. S. Wang, P. Wang, B. Chen, R. Li, N. Ren et al. Suppressed recombination for monolithic inorganic perovskite/silicon tandem solar cells with an approximate efficiency of 23%. EScience 2(3), 339-346 (2022). https://doi.org/10.1016/j.esci.2022.04.001

- S. Wang, P. Wang, B. Shi, C. Sun, H. Sun et al. Inorganic perovskite surface reconfiguration for stable inverted solar cells with 20.38% efficiency and its application in tandem devices. Adv. Mater. 35(28), 2300581 (2023). https://doi.org/10.1002/adma.202300581

- S. Wang, H. Sun, P. Wang, X. Ge, Y. Li et al. Small molecule regulatory strategy for inorganic perovskite solar cells with 368 mV of VOC deficit and its application in tandem devices. Adv. Energy Mater., 2400151 (2024). https://doi.org/10.1002/aenm.202400151