Supporting Information for

Efficient Thermally-Evaporated Near-Infrared Perovskite Light-Emitting Diodes via Phase Regulation

Siwei He1,#, Lanxin Qin2,#, Zhengzheng Liu3,*, Jae-Wook Kang4, Jiajun Luo2,*, Juan Du1,*

1School of Physics and Optoelectronic Engineering, Hangzhou Institute for Advanced Study, University of Chinese Academy of Sciences, Hangzhou 310024, P. R. China.

2Wuhan National Laboratory for Optoelectronics (WNLO) and School of Optical and Electronic Information, Huazhong University of Science and Technology (HUST), 1037 Luoyu Road, Wuhan, Hubei 430074, P. R. China

3State Key Laboratory of High Field Laser Physics and CAS Center for Excellence in Ultra-Intense Laser Science, Shanghai Institute of Optics and Fine Mechanics, Chinese Academy of Sciences, Shanghai 201800, P. R. China

4Department of Flexible and Printable Electronics, LANL-JBNU Engineering Institute-Korea, Jeonbuk National University, Jeonju 54896, Republic of Korea.

#Siwei He and Lanxin Qin contributed equally to this work.

*Corresponding authors. E-mail: du@ucas.ac.cn (Juan Du); luojiajun@hust.edu.cn (Jiajun Luo); liuzhengzheng@siom.ac.cn (Zhengzheng Liu)

S1 Digital images of perovskite thin films

Fig. S1 Photographs of as-deposited (a) FAPbI3 via dual-source co-evaporation, and (b) FACsPbI3 via triple-source co-evaporation

S2 TRPL analysis

The PL lifetime decay curves of perovskite films were fitted using bi-exponential function through Equation S1:

I=nAnexp−tτnn=1,2,3…                    (S1)

The average PL lifetime (τavg) can be determined via Equation S2:

τavg=nAnτn2nAnτnn=1,2,3…                         (S2)

Table S1 PL decay lifetime of FAPbI3 and FACsPbI3 based on bi-exponential decay fitting of TRPL spectra

| Samples | A1 | τ1 (ns) | A2 | τ2 (ns) | τavg (ns) |
| --- | --- | --- | --- | --- | --- |
| FAPbI3 | 0.41 | 8.50 | 0.10 | 68.83 | 48.55 |
| FACsPbI3 | 1.90 | 4.84 | 0.18 | 80.37 | 51.02 |

S3 XPS analysis

Fig. S2	Overall XPS spectra of FAPbI3 and FACsPbI3 thin film

S4 UPS analysis

Fig. S3	UPS spectra of FAPbI3 and FACsPbI3 thin films

The valence band maximum (EVBM) of the perovskite films were calculated using Equation S3:

EVBM = hν - (Ecut-off  - Eonset)                      (S3)

where hν is the ultraviolet radiation energy (21.22 eV).

The Fermi levels of the perovskite films were calculated using Equation S4:

EFermi =hv - Ecut-off                      (S4)

The conduction band minimum (ECBM) of the perovskite films were calculated using Equation S5:

ECBM = EVBM - Eg                     (S5)

Table S2 Detailed band energy derived from UPS spectra for FAPbI3 and FACsPbI3 thin films

| Samples | Ecut-off [eV] | Eon-set [eV] | EVBM [eV] | EFermi [eV] | Eg [eV] | ECBM [eV] |
| --- | --- | --- | --- | --- | --- | --- |
| FAPbI3 | 17.11 | 1.58 | -5.69 | -4.11 | 1.60 | -4.09 |
| FACsPbI3 | 17.06 | 1.50 | -5.66 | -4.16 | 1.54 | -4.12 |

S5 Morphologies

Fig. S4 FE-SEM images of (a) FAPbI3 and (b) FACsPbI3. The crystal size distribution of (c) FAPbI3, and (d) FACsPbI3 deposited on PEDOT:PSS/TFB hole transport layer

S6 FIB images

Fig. S5 FIB images of the FAPbI3 and FACsPbI3 for the characterization of STEM

S7 Cross-sectional and EDS images

Fig. S6 Cross-sectional image and EDS spectra of (a) FAPbI3-based, and (b) FACsPbI3-based PeLEDs

S8 EQE and wavelength peak distribution

Fig. S7 EQE values (black, upper data) and wavelength peaks (yellow, lower data) for (a) FAPbI3 via dual-source co-evaporation, and (b) FACsPbI3 via triple-source co-evaporation. EQE-current density from the fourth row (denoted as #16-20) for (c) FAPbI3-based and (d) FACsPbI3-based devices

S9 SCLC analysis

Fig. S8 (a) Energy band diagram, and (b) current density-voltage curves for the hole-only devices based on FAPbI3 and FACsPbI3. (c) Energy band diagram, and (d) current density-voltage curves based on FAPbI3 and FACsPbI3

Table S3 Performance of the state-of-the-art NIR-PeLEDs

| Deposition method of perovskite | Perovskite | Device structure | EL (nm) | EQE (%) | Radiance (W sr-1 m-2) | Year | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Thermal evaporation | FACsPbI3 | ITO/PEDOT:PSS/ TFB/Pe/TPBi/LiF/Al | 770 | 10.25 | 2.64 | 2024 | This work |
|  | MAPbI3 | ITO/PEDOT:PSS/poly-TPD/Pe/PCBM/Ba/Ag | 765 | 0.04 | 0.084 | 2014 | [S1] |
|  | MAPbI3 | ITO/PEDOT:PSS/poly-TPD/Pe/PCBM/Ba/Ag | 765 | 0.06 | N.A. | 2015 | [S2] |
|  | MAPbI3 | ITO/MeO-TPD:F4TCNQ/MeO-TPD/Pe/Bphen/Bphen:Cs/Ag | 768 | 0.35 | 4.2 | 2016 | [S3] |
|  | MAPbI3 | ITO/ C60/Pe/ TaTm /Au | 760 | 1.92 | 4.1 | 2018 | [S4] |
| Solution-based process | MAPbI3-xClx | ITO/TiO2/Pe/F8/MoO3/Ag | 754 | 0.76 | 13.2 | 2014 | [S5] |
|  | FPMAI-MAPb0.6Sn0.4I3 | ITO/Poly-TPD/Pe/TPBi/LiF/Al | 917 | 5.0 | 2.7 | 2018 | [S6] |
|  | Cs0.17FA0.83PbI2.5Br0.5 | ITO/ZnO/PEIE/Pe/TFB/MoO3/Au | 800 | 17.4 | 965 | 2020 | [S7] |
|  | KI-MAPb0.8Sn0.2I3 | ITO/Poly-TPD/Pe/TPBi/LiF/Al | 868 | 9.6 | 0.025 | 2022 | [S8] |
|  | PEAI-FAPbI3 QDs | ITO/PEDOT:PSS/VB-FNPD/Pe/CN-T2T/LiF/Al | 772 | 15.4 | 128.1 | 2022 | [S9] |
|  | SFB10-FAPbI3 | ITO/ZnO/PEIE/Pe/TFB/MoOx/Au | 803 | 22.8 | 278.9 | 2022 | [S10] |
|  | Yb3+ :CsPb(Cl1-xBrx)3 QDs | ITO/PEDOT:PSS/Poly-TPD/PVK/Pe/TPBi/Liq/Al | 990 | 7.7 | NA | 2023 | [S11] |
|  | MSPE-FAPbI3 | ITO/ZnO/PEIE/Pe/Poly-TPD/MoOx/Au | 800 | 23.8 | > 3200 | 2023 | [S12] |
|  | Yb3+:CsPb(Cl1−xBrx)3 QDs | ITO/PEDOT:PSS/poly-TPD/PVK/Pe/PO-T2T/Liq/Al | 990 | 8.5 | 52.5 | 2024 | [S13] |
|  | CsSnI3 | ITO/PEDOT:PSS/Pe/TPBi/LiF/Al | 948 | 2.63 | 226 | 2024 | [S14] |

Supplementary References

[S1]	L. Gil-Escrig, G. Longo, A. Pertegás, C. Roldán-Carmona, A. Soriano et al, Efficient photovoltaic and electroluminescent perovskite devices. Chem. Comm. 51, 569–571 (2015). https://doi.org/10.1039/c4cc07518h

[S2]	L. Gil-Escrig, A. Miquel-Saempere, M. Sessolo, H.J. Bolink, Mixed iodide-bromide methylammonium lead perovskite-based diodes for light emission and photovoltaics. J. Phys. Chem. Lett. 6, 3743–3748 (2015). https://doi.org/10.1021/acs.jpclett.5b01716

[S3]	A. Genco, F. Mariano, S. Carallo, V.L.P. Guerra, S. Gambino et al, Fully vapor-deposited heterostructured light-emitting diode based on organo-metal halide perovskite. Adv. Electron Mater. 2, 1500325 (2016). https://doi.org/10.1002/aelm.201500325

[S4]	B. Dänekamp, N. Droseros, F. Palazon, M. Sessolo, N. Banerji et al, Efficient photo- and electroluminescence by trap states passivation in vacuum-deposited hybrid perovskite thin films. ACS Appl. Mater. Interfaces 10, 36187–36193 (2018). https://doi.org/10.1021/acsami.8b13100

[S5]	Z.K. Tan, R.S. Moghaddam, M.L. Lai, P. Docampo, R. Higler et al, Bright light-emitting diodes based on organometal halide perovskite. Nat. Nanotechnol. 9 687–692 (2014). https://doi.org/10.1038/nnano.2014.149

[S6]	W. Qiu, Z. Xiao, K. Roh, N.K. Noel, A. Shapiro et al, Mixed lead–tin halide perovskites for efficient and wavelength-tunable near-infrared light-emitting diodes. Adv. Mater. 31, 1806105 (2019). https://doi.org/10.1002/adma.201806105

[S7]	Y.H. Jia, S. Neutzner, Y. Zhou, M. Yang, J.M.F. Tapia et al, Role of excess FAI in formation of high-Efficiency FAPbI3-based light-emitting diodes, Adv. Funct. Mater. 30, 1906875 (2020). https://doi.org/10.1002/adfm.201906875

[S8]	H. Yu, W. Chen, Z. Fang, L. Ding, B. Cao et al, Alkalis-doping of mixed tin-lead perovskites for efficient near-infrared light-emitting diodes, Sci. Bull. (Beijing) 67, 54–60 (2022). https://doi.org/10.1016/j.scib.2021.07.021

[S9]	Z.L. Tseng, L.C. Chen, L.W. Chao, M.J. Tsai, D. Luo et al, Aggregation control, surface passivation, and optimization of device structure toward near-infrared perovskite quantum-dot light-emitting diodes with an EQE up to 15.4%, Adv. Mater. 34, 2109785 (2022). https://doi.org/10.1002/adma.202109785

[S10]	B. Guo, R. Lai, S. Jiang, L. Zhou, Z. Ren et al, Ultrastable near-infrared perovskite light-emitting diodes, Nat. Photonics 16, 637–643 (2022). https://doi.org/10.1038/s41566-022-01046-3

[S11]	Y.J. Yu, C. Zou, W.S. Shen, X. Zheng, Q.S. Tian et al, Efficient near-infrared electroluminescence from lanthanide-doped perovskite quantum cutters, Angew. Chem. Int. Ed. 62, 2302005 (2023). https://doi.org/10.1002/anie.202302005

[S12]	Y. Sun, L. Ge, L. Dai, C. Cho, J. Ferrer Orri et al, Bright and stable perovskite light-emitting diodes in the near-infrared range, Nature 615, 830–835 (2023). https://doi.org/10.1038/s41586-023-05792-4

[S13]	J.L. Pan, W.S. Shen, S.N. Li, Z. Da Zhang, F. Zhao et al, Polarity-mediated antisolvent control enables efficient lanthanide-based near-Infrared perovskite LEDs, Nano Lett. 24, 2765–2772 (2024). https://doi.org/10.1021/acs.nanolett.3c04586

[S14]	F. Yuan, G. Folpini, T. Liu, U. Singh, A. Treglia et al, Bright and stable near-infrared lead-free perovskite light-emitting diodes, Nat. Photonics 18, 170–176 (2024). https://doi.org/10.1038/s41566-023-01351-5