Supporting Information for

Mixed-Dimensional Nanowires/Nanosheet Heterojunction of GaSb/Bi2O2Se for Self-Powered Near-Infrared Photodetection and Photocommunication

Guangcan Wang1, Zixu Sa1, Zeqi Zang1, Pengsheng Li1, Mingxu Wang1, Bowen Yang1, Xiaoyue Wang1, Yanxue Yin1, and Zai-xing Yang1,*

1 School of Physics, State Key Laboratory of Crystal Materials, Shandong University, Jinan 250100, P. R. China

*Corresponding author. E-mail: zaixyang@sdu.edu.cn  (Zai-xing Yang)

Supplementary Figures and Tables

Fig. S1 I-V characteristics of the as-fabricated GaSb NW (a) and Bi2O2Se NS (b) photodetectors under the illumination of 1310 nm laser with various light intensities

Fig. S2 Responsivity of the NW, NS and NW/NS mixed-dimensional heterojunction photodetector under the different wavelengths with -3 V bias

Fig. S3 Photodetection behavior of NW/NS mixed-dimensional heterojunction photodetector. a I-V characteristics of the NW/NS mixed-dimensional heterojunction photodetector under the illumination of 520 nm laser with various light intensities. b I-V characteristics of the NW/NS mixed-dimensional heterojunction photodetector under the illumination of 1310 nm laser with various light intensities

Fig. S4 Photodetection behaviors of the NWs array/NS mixed-dimensional heterojunction. a Broad spectrum photodetection performance of the NWs array/NS mixed-dimensional heterojunction photodetector under -3V bias. b Response time of the NWs array/NS mixed-dimensional heterojunction photodetector under -3V bias. c I-V characterization of the NWs array/NS mixed-dimensional heterojunction photodetector in dark and light conditions

Table S1 Idark and response time comparison between this work and other photodetectors previously reported in the literatures

| Marerials | Response time (ms) | Idark (A) | References |
| --- | --- | --- | --- |
| GaSb | 11/16 | 4×10-7 | [49] |
| GaSb | 2/2 | 2×10-12 | [13] |
| GsSb | 4.5/212 | 3.5×10-7 | [48] |
| Bi2O2Se | 39/63 | 1×10-4 | [51] |
| Bi2O2Se | 6/20 | 1×10-9 | [50] |
| Bi2O2Se | 117/58 | 1×10-10 | [52] |
| Bi2O2Se NW/MoSe2 NS | 0.38/0.35 | 1×10-12 | [53] |
| Te NW/CdS NS | 35/45 | 1×10-8 | [54] |
| Te NW/MoSe2 NS | 100/100 | 4×10-12 | [56] |
| Se NW/InSe NS | 30/37 | 3.8×10-14 | [55] |

Notes. The references are in line with Figure 3g.