Supporting Information for

Chirality-Induced Suppression of Singlet Oxygen in Lithium–Oxygen Batteries with Extended Cycle Life

Kyunghee Chae,1 Youngbi Kim,2 Yookyeong Oh,1 Hosik Hahn,3 Jaehyun Son,4 Youngsin Kim,3 Hyuk-Joon Kim,3 Hyun Jeong Lee,1 Dohyub Jang,5 Jooho Moon,4,* Kisuk Kang,3,* Jeong Woo Han,3,* Filipe Marques Mota,6,* Dong Ha Kim1,7,8,9,10,*

1Department of Chemistry and Nanoscience, Ewha Womans University, 52 Ewhayeodae-gil, Seodaemun-gu, Seoul 03760, Republic of Korea

2Department of Chemical Engineering, Pohang University of Science and Technology (POSTECH), Pohang 37673, Republic of Korea

3Department of Materials Science and Engineering Seoul National University, 1 Gwanak-ro, Gwanak-gu, Seoul 08826, Republic of Korea

4Department of Materials Science and Engineering, Yonsei University, 50 Yonsei-ro Seodaemun-gu, Seoul 03722, Republic of Korea

5Chemical and Biological Integrative Research Center, Korea Institute of Science and Technology (KIST), 5 Hwarang-ro 14-gil, Seongbuk-gu, Seoul 02792, Republic of Korea

6Department of Chemistry, School of Natural Sciences, University of Lincoln, Brayford Pool, Lincoln LN6 7TS, United Kingdom

7College of Medicine, Ewha Womans University, 25, Magokdong-ro 2-gil, Gangseo-gu, Seoul 07804, Republic of Korea

8Gradutate Program in Innovative Biomaterials Convergence, 52 Ewhayeodae-gil, Seodaemun-gu, Ewha Womans University, Seoul 03760, Republic of Korea

9Basic Sciences Research Institute (Priority Research Institute), Ewha Womans University, Seoul 03760, Republic of Korea

10Nanobio • Energy Materials Center (National Research Facilities and Equipment Center), Ewha Womans University, Seoul 03760, Republic of Korea

*Corresponding authors. E-mail: jmoon@yonsei.ac.kr (Jooho Moon); matlgen1@snu.ac.kr (Kisuk Kang); jwhan98@snu.ac.kr (Jeong Woo Han); FMarquesMota@lincoln.ac.uk (Filipe Marques Mota); dhkim@ewha.ac.kr (Dong Ha Kim)

S1 Supplementary Method

S1. 1 Electrochemical linear sweep voltammetry

Linear sweep voltammetry (LSV) tests of Co3O4/CP electrodes were performed using typical three-electrode system with an electrochemical workstation (SP150) at room temperature. A graphite rod and Ag/AgCl were used as the counter and the reference electrodes, respectively. The described setup was used to investigate both OER and ORR profiles in 1 M KOH aqueous solution at a scan rate of 20 mV s-1, with as-prepared electrodes in each N2- and O2-saturated electrolyte.

S1.2 Acid-based titration

Inside the Ar-filled glove box, spent cathodes along with the soaked pieces of Celgard, microfiber separators, and stainless-steel meshes were directly placed into vials containing 5 mL of deionized water and gently shaken for a few minutes. A complete dissolution and reaction of present DC products with H2O were assumed as Li2O2 + 2H2O → H2O2 + 2LiOH. During the acid-base titration process to examine the formation of Li2O2, possible side reactions with atmospheric CO2 could lead to the formation of Li2CO3, potentially affecting the accuracy of the results. To minimize this effect, all titrations were conducted inside an Ar-filled glovebox to prevent CO2 exposure. The extracted solution was titrated immediately (within 5 minutes of Li2O2 extraction) using a freshly prepared 5 mM HCl aqueous solution as the titrant (LiOH + HCl = LiCl + H2O). Titration was performed dropwise under gentle stirring until the phenolphthalein indicator (20 μL, 1% in EtOH) changed color, indicating the neutralization of OH- species. To ensure reproducibility, at least three separate titrations were conducted for each sample, and the average Li2O2 yield was reported with standard deviation. Calibration was confirmed using a known LiOH standard (Fig. S9), and blank control titration were performed with fresh electrolyte-exposed separators and cathodes without cycling to confirm the absence of background alkalinity contributions.

S1.3 UV-vis analysis

UV-vis absorption spectra were recorded with a UV–Vis Varion 5000 spectrometer with a wavelength rate of 300-500 nm. TEGDME electrolytes containing 20 mM DMA were used as the original solution. After discharge and recharge for 1 hour at 0.08 mA cm-2, spent cathodes along with the soaked pieces of Celgard, microfiber separators, and stainless-steel meshes were diluted with TEGDME. Then, UV absorption spectra were recorded.

S2 Supplementary Figures and Tables

Fig. S1 SEM images of (a) rac-Co3O4 NS/ITO, (b) R-Co3O4 NS/ITO and (c) S-Co3O4 NS/ITO substrates

Fig. S2 SEM images of (a) bare carbon paper (CP), (b) Co3O4 NS/CP, (c) rac-Co3O4 NS/CP, and (d) R-Co3O4 NS/CP

Fig. S3 Dynamic light scanning (DLS) size distribution of (a) rac-Co3O4 NS, (b) R-Co3O4 NS, and (c) S-Co3O4 NS

Fig. S4 AFM height images of electrodeposited Co3O4 nanosheets on ITO substrates. (a) rac-Co3O4/CP and (b) R-Co3O4/CP

Fig. S5 XPS spectra of Co3O4 NS/CP, rac-Co3O4 NS/CP and R-Co3O4 NS/CP. All samples show deconvoluted Co2+ and Co3+ peaks along with their satellite features, confirming the typical mixed-valence nature of spinel Co3O4. The calculated Co2+/Co3+ ratios were 1.44 for Co3O4/CP, 1.46 for rac-Co3O4/CP, and 1.43 for R-Co3O4/CP, indicating consistent chemical states across samples

Fig. S6 CD spectra of (rac/R/S)-Co3O4 NS on an ITO substrate with (a) 1 mM, (b) 5 mM, and (c) 10 mM of (rac/R/S)-BINOL

Fig. S7 I-V curves of (a) rac-Co3O4/CP, (b) R-Co3O4/CP and (c) S-Co3O4/CP electrodes in the range of -3.0 to +3.0 V. The CoCr tip was magnetized along the north (gray) or south (green) orientation. The average I-V curve recorded over 30 scans at different points is shown. Spin polarization percentage (SP%) as a function of applied bias of (d) rac-Co3O4/CP, (e) R-Co3O4/CP and (f) S-Co3O4/CP electrodes

Fig. S8 (a) OER LSV curves of CP and (rac/R/S)-Co3O4/CP electrodes in the N2-saturated 1 M KOH electrolyte. (b) ORR LSV curves of CP and (rac/R/S)-Co3O4/CP electrodes in O2-saturated 1 M KOH electrolyte (subtracting the voltammograms in N2). Scan rate is 20 mV s-1

Fig. S9 Acid-base titration calibration curve with phenolphthalein indicator

To quantify the Li2O2 formed during the first discharge process, we conducted acid-base titration experiments following a 5-hour discharge at a current density of 0.8 mA cm–2, with a total capacity of 4 mAh/cm2. This titration process is based on the reaction of lithium peroxide (Li2O2) with water, which produces lithium hydroxide (LiOH), as shown in the reaction:

Li2O2 + 2H2O → H2O2 + 2LiOH

Here, the relationship between LiOH and Li2O2 follows a 2:1 molar ratio. The resulting LiOH can then be titrated using a standardized hydrochloric acid (HCl) solution, which reacts with LiOH to form lithium chloride (LiCl) and water.

For theoretical calculations, based on a 5-hour discharge at a capacity of 0.4 mAh cm–2 and an electrode surface area of 1.25668 cm2, the total discharge capacity is 0.5067 mAh (or 0.000507 Ah). This corresponds to 18.9 µmol of LiOH, given the two-electron transfer required for Li2O2 formation. Therefore, after 5 hours of discharge, the theoretical amount of Li2O2 produced should be 9.45 µmol, generating 18.9 µmol of LiOH in the titration process.

Fig. S10 Galvanostatic profiles of Li–O2 batteries with CP, Co3O4 NS/CP and R-Co3O4 NS/CP at 0.08 mA cm-2 for (a) 1st cycle, (b) 2nd cycle and (c) 5th cycle

Fig. S11 Cyclic voltammetry (CV) curves of (a) CP, (b) rac-Co3O4/CP, and (c) R-Co3O4/CP electrodes measured before and after 10 discharge/recharge galvanostatic cycles at a scan rate of 0.1 mV s-1 in the voltage range of 2.0-4.8 V vs. Li+/Li. The 10-cycle test was conducted at a current density of 0.08 mA cm-2 using a fixed charge/discharge time of 10 hours per cycle. (d) Overlaid CV profiles after cycling, demonstrating the superior catalytic stability of R-Co3O4/CP, which retains higher ORR and OER current densities compared to rac-Co3O4/CP and CP, indicating enhanced durability under prolonged cycling

Fig. S12 Schematic generation of 1O2 during discharge and charge processes

Fig. S13 UV-vis absorption spectrum of DMA in TEGDME with CP, Co3O4/CP and (rac/R)-Co3O4/CP electrodes after discharge (a) and recharge (b) for 1 hour at 0.08 mA cm-2

Fig. S14 Schematic diagram of operando PL cell design

Fig. S15 Excitation and emission spectra of 9,10-dimethylanthracene in 1.0 M LiTFSI in TEGDME. The emission was recorded from 400-600 nm with λex= 378nm

Fig. S16 Partial density of states (PDOS) for Co 3d orbitals in (a) rac-Co3O4 NS/CP and (b) R-Co3O4 NS/CP

Fig. S17 Partial density of states (PDOS) for O 2p orbitals in (a) rac-Co3O4 NS/CP and (b) R-Co3O4 NS/CP

Fig. S18 The computed geometries of bare, Li, LiO2*, Li2O2*, and 2Li2O2* at the rac-Co3O4 NS/CP cathode

Fig. S19 The computed geometries of bare, Li, LiO2*, Li2O2*, and 2Li2O2* at the R-Co3O4 NS/CP cathode

Table S1 Summary of ICP-OES results and relative standard deviation values (RSD, %)

| Sample name | Co 238.892 nm |  | Sample weight (g) |
| --- | --- | --- | --- |
|  | Conc. (wt%) | RSD |  |
| rac-Co3O4/CP | 5.274 | 1.579 | 0.0128 |
| R-Co3O4/CP | 5.006 | 2.190 | 0.0138 |
| S-Co3O4/CP | 6.149 | 0.797 | 0.0133 |