Supporting Information for

Moisture-Resistant Scalable Ambient-Air Crystallization of Perovskite Films via Self-Buffered Molecular Migration Strategy

Mei Yang1, Weidong Zhu1*, Laijun Liang1, Wenming Chai1, Xiaomeng Wu2*, Zeyang Ren1, Long Zhou3, Dazheng Chen1, He Xi3, Chunfu Zhang 1*, Jincheng Zhang1, Yue Hao1

1State Key Laboratory of Wide-Bandgap Semiconductor Devices and Integrated Technology, Xidian University, Xi'an 710071, P. R. China

2School of Electronic Engineering, Xi’an Shiyou University, Xi’an 710065, P. R. China

3School of Advanced Materials and Nanotechnology, Xidian University, Xi’an 710126, P. R. China

*Corresponding authors. E-mail: wdzhu@xidian.edu.cn (Weidong Zhu); xmwudz@xsyu.edu.cn (Xiaomeng Wu); cfzhang@xidian.edu.cn (Chunfu Zhang)

Supplementary Figures and Tables

Fig. S1 FTIR spectra of control and target intermediate-phase films after being exposed to ambient air for about 120 min

Fig. S2 a XRD patterns and b the magnified results in the range 2θ = 5°–10° for the control and target intermediate-phase films just exposure to ambient air (Conrol-0 min and Control-10 min) and exposed for 10 min (Target-0 min and Target-10 min)

Fig. S3 Statistical grain sizes of control and target perovskite films obtained with 0- and 15-min ambient-air exposure

Fig. S4 XRD patterns of the control perovskite films obtained with 0- and 15-min ambient-air loading and prepared in ambient air with RH of below 20%

Fig. S5 SEM images of a the perovskite film produced in glovebox (labeled as N2-preapred) and b the target perovskite film prepared with 0-min ambient-air exposure. c The corresponding XRD patterns

Fig. S6 a SEM image and b XRD pattern of perovskite film prepared by use of pure IPA solvent and with 0 min ambient-air exposure before annealing

Fig. S7 Statistical grain sizes for the target sample obtained with 15-min ambient-air exposure

Fig. S8 Tauc plots derived from the absorption spectra of the control and target perovskite films obtained with 0- and 15-min ambient exposure

Fig. S9 a Photographs and b core-level N 1s spectra of the delaminated control-0 min and target-15min films

Fig. S10 Re-plotted in-situ PL spectra for a control and b target intermediate-phase films exposed to ambient air with RH of 60-80%

Fig. S11 Statistical a Jscs, b FFs, and c Vocs for 20 individual control and target PSCs fabricated with 0- and 15-min ambient-air exposure

Fig. S12 Statistical RS PCEs for the control PSCs fabricated with 0- and 15-min ambient-air exposure. During the device fabrication process, the RH of ambient air was controlled to 30~40%

Fig. S13 Statistical RS PCEs for the PSCs fabricated in glovebox and with coating of BABr layer

Fig. S14 Thermal stability test results measured at ~85 ℃ and glovebox (H2O/O2 < 1ppm) for the control PSC (0-min ambient-air exposure) and target PSC (15-min ambient-air exposure)

Fig. S15 a SCLC analysis of hole-transport-only devices (ITO/NiOx/perovskite/Spiro-OMeTAD/Ag) based on the control film (0-min ambient-air exposure) and target film (15-min ambient-air exposure). b Cross-sectional SEM images of control film (0-min ambient-air exposure) and target film (15-min ambient-air exposure)

From Fig. S15(a), the trap-filled limit voltages (VTFLs) were determined to 1.50 and 1.34 V for control film (0-min ambient-air exposure) and target film (15-min ambient-air exposure), respectively. The trap density (Nt) can be correlated with the VTFL by following Nt=2VTFLεrε0/eL2, for which L is the thickness of perovskite film that can be determined from the cross-sectional SEM images in Fig. S15(b), ε0 stands for the vacuum permittivity (8.8542×10-14 F/m), εr represents the relative dielectric constant of perovskite film (32), and e is the elementary charge (1.602×10-19 C). In this manner, the trap densities were determined to 3.04×1016 and 2.55×1016 cm-3 for the control film (0-min ambient-air exposure) and target film (15-min ambient-air exposure), respectively.

Fig. S16 SEM images of the 1.53 eV-bandgap intermediate-phase films with the ambient-air exposure duration of 0, 5, 15, 30, and 60 min

Fig. S17 SEM images of the 1.77 eV-bandgap intermediate-phase films with the ambient-air exposure duration of 0, 5, 15, 30, and 60 min

Fig. S18 Statistical RS and FS PCEs for the target PSCs based on 1.53 eV-bandgap perovskite films

Fig. S19 Statistical RS and FS PCEs for the target PSCs based on 1.77 eV-bandgap perovskite films

Table S1 Photovoltaic performance parameters recorded under RS for best-performing control and target PSCs fabricated with 0- and 15-min ambient-air exposure

| Samples | Jsc (mA/cm2) | Voltage (V) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- |
| Control-0 min | 20.54 | 1.180 | 78.26 | 18.97 |
| Control-15 min | 19.31 | 1.176 | 79.09 | 17.96 |
| Target-0 min | 20.37 | 1.191 | 78.58 | 19.06 |
| Target-15 min | 20.96 | 1.231 | 82.16 | 21.20 |

Table S2 Photovoltaic performance parameters recorded under RS for the best-performing PSCs assembled with different shielding layers and 30-min ambient-air exposure

| Samples | Voc (V) | Jsc(mA/cm2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- |
| Target-30 min MACl | 1.222 | 21.43 | 80.97 | 21.20 |
| Target-30 min CF3PEACl | 1.200 | 21.47 | 82.06 | 21.14 |
| Target-30 min PEACl | 1.214 | 21.93 | 79.24 | 21.09 |
| Target-30 min CF3PEABr | 1.194 | 21.32 | 79.21 | 20.16 |
| Target-30 min OABr | 1.160 | 21.69 | 79.85 | 20.09 |

Table S3 Summary of the historical RS PCEs, Jscs, Vocs, and FFs of the n-i-p structured PSCs based on 1.68 eV-bandgap perovskite films prepared in N2-atomopshere and ambient air

| Preparation atmosphere | Voc (V) | Jsc (mA/cm2) | FF (%) | PCE (%) | Publication year | Refs |
| --- | --- | --- | --- | --- | --- | --- |
| Ambient air | 1.220 | 22.00 | 82.3 | 22.09 | 2025 | This work |
|  | 1.2 | 22.72 | 80.3 | 21.9 | 2024 | [S1] |
|  | 1.139 | 20.73 | 78.7 | 18.59 | 2024 | [S2] |
|  | 1.255 | 20.31 | 79.0 | 20.08 | 2023 | [S3] |
|  | 1.2 | 20.68 | 81.87 | 20.32 | 2022 | [S4] |
|  | 1.22 | 20.38 | 77.22 | 19.24 | 2021 | [S5] |
| N2 atmosphere | 1.22 | 21.27 | 79.2 | 20.55 | 2025 | [S6] |
|  | 1.282 | 22.43 | 81.2 | 23.35 | 2024 | [S7] |
|  | 1.212 | 22.52 | 83.13 | 22.69 | 2024 | [S8] |
|  | 1.214 | 20.49 | 82.49 | 20.34 | 2024 | [S9] |
|  | 1.249 | 20.31 | 81.25 | 20.61 | 2024 | [S10] |
|  | 1.21 | 21.8 | 77.3 | 20.4 | 2024 | [S11] |
|  | 1.25 | 21.85 | 77.66 | 21.12 | 2023 | [S12] |
|  | 1.17 | 21.81 | 81.90 | 20.90 | 2023 | [S13] |
|  | 1.22 | 20.6 | 76.9 | 19.3 | 2023 | [S14] |
|  | 1.256 | 20.43 | 78.71 | 20.2 | 2022 | [S15] |
|  | 1.233 | 20.5 | 71.6 | 18.1 | 2022 | [S16] |
|  | 1.195 | 19.95 | 78.2 | 18.64 | 2021 | [S17] |

Supplementary References

- T. Dong, L. Tan, Z. Li, J. Li, H. Li et al., Enhanced efficiency and intrinsic stability of wide-bandgap perovskite solar cells through dimethylamine-based cation engineering. Chem. 31(4), e202403527 (2025). https://doi.org/10.1002/chem.202403527

- T. Yang, D. Huang, Z. Wang, F. Li, J. Gong et al., Manipulating wide-band-gap perovskite compositions via Br sources for highly efficient perovskite/silicon tandem solar cells. ACS Appl. Energy Mater. 7(14), 5755–5764 (2024). https://doi.org/10.1021/acsaem.4c00822

- X. Zhang, X. Li, L. Tao, Z. Zhang, H. Ling et al., Precise control of crystallization and phase-transition with green anti-solvent in wide-bandgap perovskite solar cells with open-circuit voltage exceeding 1.25 V. Small 19(22), 2208289 (2023). https://doi.org/10.1002/smll.202208289

- X. Sun, Z. Shao, Z. Li, D. Liu, C. Gao et al., Highly efficient CsPbI3/Cs1-xDMAxPbI3 bulk heterojunction perovskite solar cell. Joule 6(4), 850–860 (2022). https://doi.org/10.1016/j.joule.2022.02.004

- B. Chen, P. Wang, R. Li, N. Ren, Y. Chen et al., Composite electron transport layer for efficient N-I-P type monolithic perovskite/silicon tandem solar cells with high open-circuit voltage. J. Energy Chem. 63, 461–467 (2021). https://doi.org/10.1016/j.jechem.2021.07.018

- X. Chen, Z. Yuan, S. Fan, X. Feng, X. Sun et al., Enhanced light transmittance of electron transport layer through bilayer SnO2 for high-performance semitransparent perovskite solar cells. ChemSusChem 18(11), e202402582 (2025). https://doi.org/10.1002/cssc.202402582

- Q. Ye, W. Hu, J. Zhu, Z. Cai, H. Zhang et al., Suppressing charge recombination in a methylammonium-free wide-bandgap perovskite film for high-performance and stable perovskite solar cells. Energy Environ. Sci. 17(16), 5866–5875 (2024). https://doi.org/10.1039/D4EE00666F

- D. Ding, Y. Yao, P. Hang, C. Kan, X. Lv et al., Visualizing the structure-property nexus of wide-bandgap perovskite solar cells under thermal stress. Adv. Sci. 11(29), 2401955 (2024). https://doi.org/10.1002/advs.202401955

- J. Shen, X. Ge, Q. Ge, N. Li, Y. Wang et al., Improvement of photovoltaic performance of perovskite solar cells by synergistic modulation of SnO2 and perovskite via interfacial modification. ACS Appl. Mater. Interfaces 16(19), 24748–24759 (2024). https://doi.org/10.1021/acsami.4c03595

- H. Yang, K. Wu, H. Guo, J. Wei, J. Guo et al., Crystallinity control and strain release in wide-bandgap perovskite film via seed-induced growth for efficient photovoltaics. ACS Appl. Mater. Interfaces 16(32), 42566–42576 (2024). https://doi.org/10.1021/acsami.4c08445

- S. Zhang, J. Wang, N. Kalasariya, P. Dally, C. Deger et al., Mitigating buried-interface energy losses through multifunctional ligands in n–i–p perovskite/silicon tandem solar cells. ACS Energy Lett. 9(9), 4633–4644 (2024). https://doi.org/10.1021/acsenergylett.4c01841

- Z. Li, X. Li, X. Feng, X. Chen, J. Chen et al., Strain control of mixed-halide wide-bandgap perovskites for highly efficient and stable solar cells. Sol. RRL 7(22), 2300615 (2023). https://doi.org/10.1002/solr.202300615

- X. Niu, N. Li, Z. Cui, L. Li, F. Pei et al., Anion confinement for homogeneous mixed halide perovskite film growth by electrospray. Adv. Mater. 35(45), 2305822 (2023). https://doi.org/10.1002/adma.202305822

- J. Zhao, A.S.R. Chesman, J. Yan, L.J. Sutherland, J. Jasieniak et al., Precursor engineering of lead acetate-based precursors for high-open-circuit voltage wide-bandgap perovskite solar cells. ACS Appl. Mater. Interfaces 15(15), 18800–18807 (2023). https://doi.org/10.1021/acsami.2c22179

- J. Tao, Z. Yu, X. Liu, J. Xue, J. Shen et al., A facile strategy to adjust SnO2/perovskite interfacial properties for high-efficiency perovskite solar cells. J. Mater. Chem. C 10(21), 8414–8421 (2022). https://doi.org/10.1039/D2TC00818A

- Z. Su, D. Xu, Q. Ma, K. Gao, C. Zhang et al., Atomic layer deposited ZnO–SnO2 electron transport bilayer for wide-bandgap perovskite solar cells. Sol. RRL 7(3), 2201026 (2023). https://doi.org/10.1002/solr.202201026

- X. Cui, P. Wang, B. Shi, Y. Zhao, X. Zhang, Insights into the effect of bromine-based organic salts on the efficiency and stability of wide bandgap perovskite. Nano Sel. 2(3), 615–623 (2021). https://doi.org/10.1002/nano.202000183