Supporting Information for

Gas Phase Construction of Compact Capping Layers for High-Performance Halide Perovskite X-Ray Detectors

Bin Zhang1, 2, †, Chuanyun Hao1, †, Shoufeng Zhang3, †, Bin Xue1, Xiangfan Xie1, Shengqiao Zeng1, Bin Yang1, Fang Xu1, Hui Li1, Xin’an Zhang1, Zhang Qu1, Kaihang Ye4, Guangda Niu5, 6, Wallace C. H. Choy7, Kezhou Fan8, Kam Sing Wong8, Lei Yan2, Xingzhu Wang2, *, Shuang Xiao1, *, Cangtao Zhou1

1 Shenzhen Key Laboratory of Ultraintense Laser and Advanced Material Technology, Center for Intense Laser Application Technology (iLaT) and College of Engineering Physics, Shenzhen Technology University, Shenzhen 518118, P. R. China

2 Engineering and Research Center for Integrated New Energy Photovoltaics & Energy Storage Systems of Hunan Province and School of Electrical Engineering, University of South China, Hengyang 421001, P. R. China

3 School of Electrical Engineering, Guangxi University of Science and Technology, Liuzhou 545006, P. R. China

4 Institute for Sustainable Transformation School of Chemical Engineering and Light Industry, Guangdong University of Technology, Guangzhou 510006, P. R. China

5 Research Institute of Huazhong University of Science and Technology in Shenzhen, Shenzhen 518052, P. R. China

6 Wuhan National Laboratory for Optoelectronics, Huazhong University of Science and Technology, Wuhan 430074, P. R. China

7 Department of Electrical and Electronic Engineering, The University of Hong Kong, Pokfulam Road, Hong Kong SAR, P. R. China

8 Department of Physics and William Mong Institute of Nano Science and Technology, The Hong Kong University of Science and Technology, Clear Water Bay, Kowloon, Hong Kong S.A.R., P. R. China

†Bin Zhang, Chuanyun Hao, and Shoufeng Zhang contributed equally to this work.

*Corresponding authors. E-mail: 2022000041@usc.edu.cn (Xingzhu Wang); xiaoshuang@sztu.edu.cn (Shuang Xiao)

DFT Calculations

The first-principles calculations were performed using the Vienna Ab initio Simulation Package (VASP, version5.4.4) [S1, S2] with standard projector augmented-wave (PAW) method and the exchange-correlation functional for generalized gradient approximation (GGA) in PBE format [S1]. The energy cut-off was set as 450 eV with energy convergence criterion of 10-5 eV and force converged accuracy of 0.01 eV/Å. A 233 k-points mesh was set in the Brillouin zone for all DFT calculations. The DFT-D3(Grimme 2006) [S2] was used to describe the vdW-interaction of organic-inorganic interfaces. The post-processing of the energy calculations was obtained by VASPKIT toolkit.

Supplementary Figures and Tables

Fig. S1 The photograph of the X-ray detector with lateral electrodes

Fig. S2 Schematic illustration of the X-ray response speed measurement

Scheme S1 The schematic structure of propylamine (PA) and 1,6-hexanediamine (HDA)

Fig. S3 Side-view scanning electron microscope (SEM) images of the MAPbBr3 single crystal with the (PA)2PbBr4 capping layers: (a) 130 nm (PA)2PbBr4 capping layer (PA 130) and (b) 460 nm (PA)2PbBr4 capping layer (PA 460). (PA)2PbBr4 capping layers are in red. SEM images of the MAPbBr3 single crystal with the (HDA)PbBr4 capping layers: (c) 230 nm (HDA)PbBr4 capping layer (HDA 230) and (d) 520 nm (HDA)PbBr4 capping layer (HDA 520). (HDA)PbBr4 capping layers are in green

Fig. S4 Sensitivity of devices with varying 2D perovskite layer thicknesses. (a) (PA)2PbBr4 capping devices: PA 130, PA 300, PA 460 denote 2D perovskite (PA)2PbBr4 thicknesses of 130 nm, 300 nm, and 460 nm, respectively. (b) (HDA)PbBr4 capping devices: HDA 230, HDA 450, HDA 520 correspond to 2D perovskite thicknesses of 230 nm, 450 nm, and 520 nm, respectively

Fig. S5 Elements molar ratios of Br/Pb alone the cross-section of (a) the (PA)2PbBr4 capping and (b) (HDA)PbBr4 capping samples

Fig. S6 Top-view atomic force microscopy (AFM) height images of (a) Ctrl, (b) (PA)2PbBr4 capping, and (c) (HDA)PbBr4 capping samples

Fig. S7 Taut plots of (a) Ctrl, (b) (PA)2PbBr4 capping, (c) (HDA)PbBr4 capping samples. The thicknesses of the two-dimensional perovskites (PA)2PbBr4 and (HDA)PbBr4 are both less than 500 nm. Compared with the several-millimeter-thick three-dimensional perovskite MAPbBr3, their influence on the UV-Vis spectroscopy test is basically negligible. Therefore, the displayed 2.13 eV bandgap corresponds to that of the three-dimensional perovskite MAPbBr3

Fig. S8 Steady-state photoluminescence of (PA)2PbBr4 capping and (HDA)PbBr4 capping samples

Fig. S9 Schematic band alignment of (a) the MAPbBr3-(PA)2PbBr4 heterojunction and (b) the MAPbBr3-(HDA)PbBr4 heterojunction, which show the energy levels of materials at equilibrium. The energy drop at interfaces are highlighted by red circles

Fig. S10 TRPL of heterostructures with varying 2D perovskite layer thicknesses. (a) (PA)₂PbBr₄ capping samples: PA 130, PA 300, PA 460 denote 2D perovskite (PA)₂PbBr₄ thicknesses of 130 nm, 300 nm, and 460 nm, respectively. (b) (HDA)PbBr₄ capping samples: HDA 230, HDA 450, HDA 520 correspond to 2D perovskite thicknesses of 230 nm, 450 nm, and 520 nm

Fig. S11 Space charge limited current (SCLC) of (a) Ctrl, (b) (PA)2PbBr4 capping, and (c) (HDA)PbBr4 capping samples

Fig. S12 The Time-Resolved Photocurrent Decay curves of (a) Ctrl, (b) (PA)2PbBr4 capping, and (c) (HDA)PbBr4 capping samples. The electric field for measurements was 267 V mm-1

Fig. S13 (a) The current-time (I-t) curve of the Ctrl device under X-ray dose rates ranging from 74.7 to 616.6 μGyair s-1. I-t curves of (b) the (PA)2PbBr4 capping and (c) the (HDA)PbBr4 capping devices under X-ray dose rates ranging from 1.3 to 10.7 μGyair s-1

Fig. S14 Sensitivity of Ctrl, (PA)2PbBr4 capping, and (HDA)PbBr4 capping samples under different electric fields. The dose rate of X-ray for measurements of the Ctrl sample was 5111.11 μGyair s-1. The dose rate of X-ray for measurements of the (PA)2PbBr4 capping and (HDA)PbBr4 capping samples was 86.11 μGyair s-1

Fig. S15 Relative X-ray absorption (blue curve) and mass attenuation coefficient (red curve) of MAPbBr3 in the 1 eV ~ 100 keV energy range. The relative X-ray absorption coefficient (𝜖) was directly obtained from μP by applying the relationship: 𝜖 = 1 – exp(–μP·ρd). By considering a photon energy Eph = 5.73 keV, which is the most probable energy in the case of a Cu-target X-ray tube, the mass attenuation coefficient is μP = 3.78 cm2 •g-1, corresponding to a relative X-ray absorption 𝜖 = 83.2% for a 1.5 mm-thick crystal. At the same photon energy (5.73 keV), the mass attenuation coefficient of dry air [5] is μ = 9.92 cm2 g-1. Finally, being the bandgap energy Eg = 2.13 eV, the estimated electron-hole pair creation energy is Ei = 2  2.13 + 1.43 = 5.69 eV.

By inserting all the numerical values into the St equation we obtain:

St=eμPρdμEi=16.5 μC·Gyair-1·cm-2

Fig. S16 The long-term dark current drift of (a) Ctrl, (b) (PA)2PbBr4 capping, and (c) (HDA)PbBr4 capping samples under an electric field of 267 V mm-1

Table S1 Performance comparison of perovskite-based X-ray detectors

| Materials | Electric field (V mm-1) | X-ray energy (kVp) | Sensitivity (μC·Gyair-1·cm-2) | LoD (μGyair s-1) | Response time (ms) | References |
| --- | --- | --- | --- | --- | --- | --- |
| MAPbBr3 | 0.1 | 50 | 80 | 0.5 | 0.73 | [S6] |
| MAPbBr3 | 2.67 | 40 | 7275 | 0.67 | / | [S7] |
| MAPbBr3 | 7.1 | 40 | 2181 | 0.48 | / | [S8] |
| FAPbI3 | 80 | 70 | 4.15 × 105 | 0.001 | 0.214 | [S9] |
| MA0.42FA0.58PbI3 | 71 | 22 | 1.16 × 106 | 0.037 | 20000 | [S10] |
| Cs0.05FA0.9MA0.05PbI3 | 200 | 59.3 | 1.5 × 104 | / | 0.235 | [S11] |
| CsPbI2Br | 125 | 50 | 1.48 × 105 | 0.28 | / | [S12] |
| CsPbBr3 | 21 | 50 | 5.57 × 104 | 0.215 | 92 | [S13] |
| (BDA)PbI4 | 310 | 40 | 242 | 0.43 | 7.3 | [S14] |
| 2D layered (NH4)3Bi2I9 | 10 | 50 | 8200 | 0.055 | 80 | [S15] |
| MA3Bi2I9 | 60 | 40 | 1947 | 0.083 | 23 | [S16] |
| MAPbBr3 - MAPbI3 | 80 | 40 | 3.98 × 105 | 0.012 | 1.5 | [S17] |
| MAPbI3 - (PEA)2MA3Pb4I13 | 33.3 | 70 | 1.95 × 104 | 0.48 | / | [S18] |
| MAPbBr3 -(PA)2PbBr4 | 267 | 60 | 2.22 × 104 | 0.13 | 0.240 | This work |
| MAPbBr3 -(HDA)PbBr4 | 267 | 60 | 1.79 × 104 | 0.56 | 0.269 | This work |

Supplementary References

- G. Kresse, J. Furthmüller, Efficiency of ab-initio total energy calculations for metals and semiconductors using a plane-wave basis set. Comput. Mater. Sci. 6(1), 15–50 (1996). https://doi.org/10.1016/0927-0256(96)00008-0

- G. Kresse, J. Furthmüller, Efficient iterative schemes for ab initio total-energy calculations using a plane-wave basis set. Phys. Rev. B 54(16), 11169–11186 (1996). https://doi.org/10.1103/physrevb.54.11169

- J. Perdew, K. Burke, M. Ernzerhof, Generalized gradient approximation made simple. Phys. Rev. Lett. 77(18), 3865–3868 (1996). https://doi.org/10.1103/PhysRevLett.77.3865

- S. Grimme, J. Antony, S. Ehrlich, H. Krieg, A consistent and accurate ab initio parametrization of density functional dispersion correction (DFT-D) for the 94 elements H-Pu. J. Chem. Phys. 132(15), 154104 (2010). https://doi.org/10.1063/1.3382344

- J. H. Hubbell, S. M. Seltzer, X-Ray Mass Attenuation Coefficients, NIST Standard Reference Database 126 (NISTIR 5632), accessed: October, 2023.
https://dx.doi.org/10.18434/T4D01F

- H. Wei, Y. Fang, P. Mulligan, W. Chuirazzi, H.-H. Fang et al., Sensitive X-ray detectors made of methylammonium lead tribromide perovskite single crystals. Nat. Photonics 10(5), 333–339 (2016). https://doi.org/10.1038/nphoton.2016.41

- D. Liu, L. Jiang, X. Jiang, X. Sun, G. Zhang et al., Interface-tension-assisted temperature-gradient crystallization of high-quality MAPbBr3 perovskite single crystals with low defect densities. ACS Appl. Mater. Interfaces 15(49), 57846–57855 (2023). https://doi.org/10.1021/acsami.3c13614

- Z. Zhu, W. Li, W. Deng, W. He, C. Yan et al., Controllable metastable growth of perovskite single crystals for highly sensitive X-ray detection. J. Mater. Chem. C 10(17), 6837–6845 (2022). https://doi.org/10.1039/D2TC00235C

- D. Chu, B. Jia, N. Liu, Y. Zhang, X. Li et al., Lattice engineering for stabilized black FAPbI3 perovskite single crystals for high-resolution X-ray imaging at the lowest dose. Sci. Adv. 9(35), eadh2255 (2023). https://doi.org/10.1126/sciadv.adh2255

- W.-G. Li, X.-D. Wang, Y.-H. Huang, D.-B. Kuang, Ultrasound-assisted crystallization enables large-area perovskite quasi-monocrystalline film for high-sensitive X-ray detection and imaging. Adv. Mater. 35(31), 2210878 (2023). https://doi.org/10.1002/adma.202210878

- Y. He, J. Song, M. Li, K. Sakhatskyi, W. Li et al., Perovskite computed tomography imager and three-dimensional reconstruction. Nat. Photon. 18(10), 1052–1058 (2024). https://doi.org/10.1038/s41566-024-01506-y

- W. Qian, X. Xu, J. Wang, Y. Xu, J. Chen et al., An aerosol-liquid-solid process for the general synthesis of halide perovskite thick films for direct-conversion X-ray detectors. Matter 4(3), 942–954 (2021). https://doi.org/10.1016/j.matt.2021.01.020

- W. Pan, B. Yang, G. Niu, K.-H. Xue, X. Du et al., Hot-pressed CsPbBr3 quasi-monocrystalline film for sensitive direct X-ray detection. Adv. Mater. 31(44), 1904405 (2019). https://doi.org/10.1002/adma.201904405

- Y. Shen, Y. Liu, H. Ye, Y. Zheng, Q. Wei et al., Centimeter-sized single crystal of two-dimensional halide perovskites incorporating straight-chain symmetric diammonium ion for X-ray detection. Angew. Chem. Int. Ed. 59(35), 14896–14902 (2020). https://doi.org/10.1002/anie.202004160

- R. Zhuang, X. Wang, W. Ma, Y. Wu, X. Chen et al., Highly sensitive X-ray detector made of layered perovskite-like (NH4)3Bi2I9 single crystal with anisotropic response. Nat. Photonics 13(9), 602–608 (2019). https://doi.org/10.1038/s41566-019-0466-7

- Y. Liu, Z. Xu, Z. Yang, Y. Zhang, J. Cui et al., Inch-size 0D-structured lead-free perovskite single crystals for highly sensitive stable X-ray imaging. Matter 3(1), 180–196 (2020). https://doi.org/10.1016/j.matt.2020.04.017

- X. Zhang, D. Chu, B. Jia, Z. Zhao, J. Pi et al., Heterointerface design of perovskite single crystals for high-performance X-ray imaging. Adv. Mater. 36(3), 2305513 (2024). https://doi.org/10.1002/adma.202305513

- X. Xu, W. Qian, J. Wang, J. Yang, J. Chen et al., Sequential growth of 2D/3D double-layer perovskite films with superior X-ray detection performance. Adv. Sci. 8(21), 2102730 (2021). https://doi.org/10.1002/advs.202102730