Supporting Information for

Ammonia Borane All-In-One Modification Strategy Enables High-Performance Perovskite Solar Cells

Jiaxin Ma1,2, Cong Shao1,2, Yirong Wang2,3, Guosheng Niu1,2, Kaiyi Yang1,2, Yao Zhao4, Fuyi Wang2,4, Zongxiu Nie2,4, and Jizheng Wang1,2*

1 Beijing National Laboratory for Molecular Sciences CAS Key Laboratory of Organic Solids, Institute of Chemistry, Chinese Academy of Sciences, Beijing 100190, P. R. China

2 School of Chemical Sciences, University of Chinese Academy of Sciences, Beijing 100049, P. R. China

3 CAS Key Laboratory of Engineering Plastics, Institute of Chemistry, Chinese Academy of Sciences, Beijing, P. R. China

4 Beijing National Laboratory for Molecular Sciences, National Centre for Mass Spectrometry in Beijing, CAS Key Laboratory of Analytical Chemistry for Living Biosystems, Chinese Academy of Sciences, Beijing, P. R. China

* Corresponding author. E-mail: jizheng@iccas.ac.cn (Jizheng Wang)

Supplementary Figures and Tables

NH3∙BH3+2H2O→NH4++BO2-+3H2

Fig. S1 The hydrolysis chemical equation of ammonium borane.

Fig. S2 O 1s XPS spectra of the SnO2 and SnO2/BNH6 films after oxygen plasma treatment

Fig. S3 J-V curves of the devices with no treatment or post treatment by oxygen plasma

Fig. S4 XRD spectra of the SnO2 and the SnO2/BNH6 films

Fig. S5 UPS spectra of the SnO2 and SnO2/BNH6 films

Fig. S6 LEIPS spectra of the SnO2 and SnO2/BNH6 films

Fig. S7 The transmittance spectra of the SnO2 and SnO2/BNH6 films

Fig. S8 UV-vis absorption spectra of the (a) SnO2 and (b) SnO2/BNH6 films, the insets are Tauc plots of corresponding films

Fig. S9 AFM images of the (a) SnO2 film and (b) SnO2/BNH6 film

Fig. S10 Contact angles of perovskite precursor solutions on the SnO2 and SnO2/BNH6 films

Fig. S11 Chemical reaction expression of I0 and I-

Fig. S12 Ion chromatography of the concentrations of I- at different times with and without BNH6

Fig. S13 Supercell constructed for DFT calculations, in which BNH6 molecules are adsorbed on the FAPbI3 (001) surface via (a) FAI and (b) PbI2 terminations, respectively

Fig. S14 The color change process of pristine PbI2 solution

Fig. S15 FTIR spectra of PbI2, BNH6, and PbI2 with BNH6 films

Fig. S16 Distribution histogram of crystal grain sizes of the perovskite films: (a) SnO2/PVK, (b) SnO2/BNH6/PVK, (c) SnO2/PVK/BNH6 and (d) SnO2/BNH6/PVK/BNH6

Fig. S17 AFM surface images of the perovskite films: (a) SnO2/PVK, (b) SnO2/BNH6/PVK, (c) SnO2/PVK/BNH6, and (d) SnO2/BNH6/PVK/BNH6

Fig. S18 2D-XRD images of the perovskite films: (a) SnO2/PVK, (b) SnO2/BNH6/PVK, (c) SnO2/PVK/BNH6, and (d) SnO2/BNH6/PVK/BNH6

Fig. S19 XRD images of the SnO2/PVK, SnO2/BNH6/PVK, SnO2/PVK/BNH6 and SnO2/BNH6/PVK/BNH6 films

Fig. S20 XPS spectra of the PVK and PVK/BNH6 films. (a) Pb 4f, (b) I 3d, (c) N 1s

Fig. S21 UPS spectra of the PVK and PVK/BNH6 films

Fig. S22 LEIPS spectra of the PVK and PVK/BNH6 films

Fig. S23 (a) UV-vis absorption spectra and (b) Tauc plots of the SnO2/PVK, SnO2/BNH6/PVK, SnO2/PVK/BNH6 and SnO2/BNH6/PVK/BNH6 films

Fig. S24 Urbach energy obtained from the (a) SnO2/PVK, (b) SnO2/BNH6/PVK, (c) SnO2/PVK/BNH6 and (d) SnO2/BNH6/PVK/BNH6 films

Fig. S25 Urbach energy calculated from the SnO2/PVK, SnO2/BNH6/PVK, SnO2/PVK/BNH6 and SnO2/BNH6/PVK/BNH6 films

Fig. S26 PL mapping of the (a) PVK, (b) BNH6/PVK, (c) PVK/BNH6 and (d) BNH6/PVK/BNH6 films

Fig. S27 Time-resolved transient absorption of the (a) PVK, (b) BNH6/PVK, (c) PVK/BNH6 and (d) BNH6/PVK/BNH6 films at different probe delay times

Fig. S28 The decay kinetics of the corresponding GSB peaks

Fig. S29 XRD spectra of the SnO2/PVK and SnO2/BNH6/PVK/BNH6 films after accelerated aging

Fig. S30 Optimal J-V curves of the PSCs measured in the reverse scan direction using different concentrations of BNH6. The BNH6 solution (0.5, 1.0, 2.0 and 3.0 mg/mL) coated at the buried and upper interface of perovskite was prepared by dissolving 0.5, 1.0, 2.0 and 3.0 mg BNH6 in 1 mL deionized water and 1 mL IPA, respectively. The other device preparation processes remain unchanged.

Fig. S31 Statistical device data based on 15 devices for (a) Jsc, (b) Voc and (c) FF

Fig. S32 Certification of PSC from Institute of Electrical Engineering Chinese Academy of Sciences

Fig. S33 Analysis of perovskite bandgap from the EQE spectrum by taking its derivative spectrum

Fig. S34 Dark I-V curves of (a) the electron-only devices and (b) the hole-only devices with and without BNH6

Fig. S35 Nyquist plots of the control and target devices (Inset: Equivalent circuit model)

Fig. S36 TPV of the control and target devices

Fig. S37 Mott-Schottky plots of the control and target devices

Fig. S38 Time evolution of XRD patterns of the (a) control and (b) target device under AM 1.5 G illumination with N2 atmosphere, (c) control and (d) target device under 65  3 °C heat with N2 atmosphere

Fig. S39 Long-term stability of the unencapsulated control and target devices stored under ambient air conditions (50~60% RH, 25 °C)

Fig. S40 (a) 1H NMR , (b) 11B NMR and (c) XRD spectra of fresh BNH6 and BNH6 under accelerated conditions for 7 days. The characteristic peaks of BNH6 remained essentially unchanged after aging, confirming its robust chemical stability and indicating that BNH6 would not compromise device performance

Fig. S41 (a) O 1s XPS and (b) the electrical conductivity spectra of the SnO2/BNH6  film under accelerated conditions for 7 days. No noticeable changes in the O 1s XPS characteristic peaks were observed after aging. And the electrical conductivity measurements of BNH6/SnO2 films before and after aging showed negligible variation, further verifying the robustness of the BNH6/SnO2 interface under accelerated conditions

Fig. S42 Contact angles of the control and target films

Table S1 Summary of photovoltaic performance of the effective interface modification strategies

| Additive | Configuration | PCE (%) | Certified PCE (%) | Reference |
| --- | --- | --- | --- | --- |
| C60-SAM | p-i-n | 17.3 | na | ACS Nano 12, 12701-12709 (2014) |
| C3-SAM | n-i-p | 15.67 | na | J. Am. Chem. Soc. 137, 2674-2679 (2015) |
| 2D PVSK | n-i-p | 20.64 | 19.77 | Nat. Commun. 9, 3021 (2018) |
| DPPP | n-i-p | 24.5 | na | Science 379, 690-694 (2023) |
| HP | n-i-p | 23.68 | na | Adv. Mater. 32, 2003990 (2020) |
| CPI | n-i-p/p-i-n | 24.3/26.0 | na | Science 384, 878-884 (2024) |
| CBz-PAI | n-i-p | 24.7 | na | Nat. Energy 8, 515-525 (2023) |
| 3TPYMB | p-i-n | 25.76 | na | Nat. Photon. 19, 28-35 (2025) |
| CPMAC | p-i-n | 26.1 | na | Science 288, 964-968 (2025) |
| TMPU/TMFS | n-i-p | 23.11 | na | Chem. Eng. J. 469, 143790 (2023) |
| AMP/ mF-PEAI and PDI | p-i-n | 25.35 | 24.87 | Adv. Energy Mater. 14, 2304486 (2024) |
| BNH6/BNH6 | n-i-p | 26.43 | 25.98 | This work |

Table S2 Best photovoltaic parameters of PSCs with no treatment or post treatment by oxygen plasma measured in reverse scan directions under standard AM 1.5 illumination (100 mW cm-2)

|  | Samples | Voc (V) | Jsc (mA cm-2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- | --- |
| No treatment | SnO2 | 1.171 | 25.53 | 78.08 | 23.34 |
|  | SnO2/BNH6 | 1.198 | 25.86 | 82.40 | 25.53 |
| Post treatment | SnO2 | 1.176 | 25.57 | 78.56 | 23.62 |
|  | SnO2/BNH6 | 1.198 | 25.96 | 82.42 | 25.63 |

Table S3 Parameters of the TRPL spectroscopy based on different samples

| Samples | A1 | τ1 (ns) | A2 | τ2 (ns) | τave (ns) |
| --- | --- | --- | --- | --- | --- |
| PVK | 158.92 | 147.28 | 748.22 | 1978.11 | 1949.61 |
| BNH6/PVK | 120.56 | 1196.47 | 750.33 | 3365.35 | 3248.15 |
| PVK/BNH6 | 161.68 | 621.38 | 1108.05 | 7010.56 | 6928.98 |
| BNH6/PVK/BNH6 | 163.98 | 1000.00 | 1119.16 | 9273.37 | 9144.68 |

Table S4 Best photovoltaic parameters of PSCs using different concentrations of BNH6 measured in reverse scan directions under standard AM 1.5 illumination (100 mW cm-2)

| SnO2/BNH6 | Concentration (mg mL-1) | VOC (V) | JSC (mA cm-2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- | --- |
|  | 0.5 | 1.196 | 25.93 | 81.16 | 25.18 |
|  | 1.0 | 1.198 | 25.96 | 82.42 | 25.63 |
|  | 2.0 | 1.181 | 25.47 | 80.45 | 24.20 |
|  | 3.0 | 1.174 | 25.21 | 80.80 | 23.92 |
| PVK/BNH6 | 0.5 | 1.197 | 25.90 | 80.67 | 25.00 |
|  | 1.0 | 1.203 | 25.91 | 83.51 | 26.03 |
|  | 2.0 | 1.185 | 25.16 | 81.13 | 24.19 |
|  | 3.0 | 1.185 | 25.05 | 80.77 | 23.98 |

Table S5 Photovoltaic parameters of control and target devices measured in reverse and forward scan directions under standard AM 1.5 illumination (100 mW cm-2)

|  | Scan Directions | VOC (V) | JSC (mA cm-2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- | --- |
| Control | RS | 1.176 | 25.57 | 78.56 | 23.62 |
|  | FS | 1.171 | 25.55 | 77.26 | 23.12 |
| Target | RS | 1.206 | 26.05 | 84.12 | 26.43 |
|  | FS | 1.201 | 25.99 | 83.67 | 26.12 |

Table S6 Parameters from SCLCs of the electron-only devices and of the hole-only devices

|  | SnO2/PVK | SnO2/BNH6/PVK | PVK/Spiro | PVK/BNH6/Spiro |
| --- | --- | --- | --- | --- |
| VTFL (V) | 0.227 | 0.129 | 0.136 | 0.119 |
| Trap density(cm-3) | 2.7910‧1015 | 1.5861‧1015 | 1.7705‧1015 | 1.2910‧1015 |

Trap densities were calculated using the VTFL from SCLC measurements, and the equation Ntraps=2ε0εrVTFL/(qL2), where the ε0 is the vacuum permittivity, εr (47) is the relative dielectric constant of FAPbI3, q is the elementary charge, and L (650 nm) is the thickness of the perovskite films, respectively.

Table S7 EIS fitting parameters of the control and target PSCs

| Device | Rs (Ω) | Rrec (Ω) |
| --- | --- | --- |
| Control | 33.28 | 1618 |
| Target | 29.65 | 5699 |