Supporting Information for

Dual-Gradient Impedance/Insulation Structured Polyimide Nonwoven Fabric for Multi-Band Compatible Stealth

Xinwei Tang1, Wei Hong1, Hongmiao Gao1, Shuangshuang Li1, Wei Li1, Kaixin Lai1, Mingzhen Xu2, Zaiyin Hu3, Yan Li4, Zicheng Wang1* and Tianxi Liu1*

1 The Key Laboratory of Synthetic and Biological Colloids, Ministry of Education, School of Chemical and Material Engineering, International Joint Research Laboratory for Nano Energy Composites, Jiangnan University, Wuxi, Jiangsu 214122, P. R. China

2 Yangtze Delta Region Institute (Huzhou), University of Electronic Science and Technology of China, Huzhou, Zhejiang 313001, P. R. China

3 Guizhou Aerospace Wujiang Electro-Mechanical Equipment Co., Ltd., No. 20-5, Dalian Road Aerospace Industrial Park, Huichuan District, Guizhou, Zunyi 563100, P. R. China

4 Jiangsu Ferrotec Semiconductor Technology Co., Ltd. Yancheng, Jiangsu 214000, P. R. China

*Corresponding author. E-mail: wangzc@jiangnan.edu.cn (Zicheng Wang); txliu@jiangnan.edu.cn (Tianxi Liu)

S1 Experimental Section

S1.1 Materials

Tris (hydroxymethyl) aminomethane (Tris, ≥99%), 3-Hydroxytyramine hydrochloride (DA, ≥99%), Dimethylaminoborane (DMAB, ≥97%), Chloroplatinic acid hexahydrate (H2PtCl6·6H2O, ≥99.9%), Lactic acid (≥90%) and Iron(III) Chloride Hexahydrate (FeCl3·6H2O, ≥99%) were purchased from Adamas Reagent Co., Ltd. Nickel (Ⅱ) sulfate hexahydrate (NiSO4·6H2O, ≥98.5%); Trisodium citrate dehydrate (≥99.5%), Hydrochloric acid (HCl, 36.0～38.0%) and Sodium hydroxide (NaOH, ≥96%) were purchased from Sinopharm Chemical Reagent Co., Ltd. 75 spray-glue was purchased from Minnesota Mining and Machinery Company. All other chemicals were used as received without further purification.

S1.2 Preparation of Fe3O4/Ni-loaded polyimide nonwoven fabrics

Firstly, a PI nonwoven fabric was prepared according to our previously reported method [26]. Subsequently, the nonwoven fabric was immersed in a 10 wt% NaOH solution for 3 min. Afterwards, it was sufficiently washed by Deionized (DI) water to remove residual NaOH. Then, the sample was placed in a 37 wt% solution of FeCl3·6H2O at 80 °C for 5 h. The treated nonwoven fabric was further washed by anhydrous ethanol, and then placed in an oven at 80 °C for 2h. Finally, the dried PI nonwoven fabric was thermal treated at 400 °C for 4 h under 12 vol% hydrogen-argon atmosphere. As a result, magnetic nanoparticle-loaded PI nonwoven fabric (PI@Fe3O4) was obtained, which can be named as PF.

Secondly, PF nonwoven fabric was placed in 10 mM Tris and 2 g L-1 DA solution, and reacted under magnetic stirring for 24 h. After the reaction, the nonwoven fabric was sufficiently washed by DI water. And then, it was further immersed in 0.5 g L-1 H2PtCl6 solution for 0.5 h. Afterwards, the nonwoven fabric was fully washed with DI water, and placed in a electroless nickel (Ni) plating solution for y min, which can be marked as PFNy.

As a control, a pure Ni-deposited PI (PNy) nonwoven fabric without Fe3O4 nanoparticles was similarly prepared by oxidative self-polymerization of DA, chloroplatinic acid activation, and electroless nickel plating processes. In detail, PI nonwoven fabric was placed in 10 mM Tris and 2 g L-1 DA solution, and reacted under magnetic stirring for 24 h. After the reaction, the nonwoven fabric was sufficiently washed by DI water. And then, it was further immersed in 0.5 g L-1 H2PtCl6 solution for 0.5 h. Afterwards, the nonwoven fabric was fully washed with DI water, and placed in a electroless Ni plating solution for y min. The obtained nonwoven fabric was labeled as PNy.

Electroless nickel plating process was carried out in a plating solution containing a 4:1 vol ratio of solution A and solution B. Solution A can be obtained by quantitatively preparing a solution mixture of NiSO4·6H2O (80 g L-1) and Trisodium citrate dehydrate (40 g L-1). Solution B was freshly prepared by dissolving 3 g L-1 DMAB and adjusting pH = 7 with ammonia.

S1.3 Fabrication of dual-gradient polyimide composite nonwoven fabrics

The dual-gradient polyimide nonwoven fabric was fabricated by combining with different PFNy and PNy nonwoven fabrics. Finally, the nonwoven fabrics were pasted by 75 spray-glue, which was denoted as PFNx-y-z.

S1.4 Characterization

The morphology of specimens was observed by a field emission scanning electron microscope (FE-SEM, Hitachi, S4800, Japan) at an accelerating voltage of 3 kV. Energy dispersive X-ray spectroscopy (EDS) analysis was also performed to analyze the surface composition of specimens. X-ray diffraction (XRD) patterns were characterized on a Bruker D2 X-ray diffractometer with a Cu Kα X-ray source (λ = 1.5418 Å). X-ray photoelectron spectroscopic (XPS) was conducted on an ESCA 2000 (VG Microtech, UK) by using a monochromic Al Kα X-ray source. Fourier transform infrared spectroscopy (FTIR) was performed using a Nicolet 6700 USA spectrophotometer. Thermal gravimetric analysis (TGA) was carried out using a TGA/DSC1/1100SF system under a N2 atmosphere at a heating rate of 10 °C/min. The stress-strain curves of samples were tested with an electronic universal testing machine (UTM2203, Shenzhen Suns Technology Stock Co. Ltd., China). Polyimide nonwoven fabrics were prepared by electrostatic spinning machine (ET-2535H, Beijing Ucalery Co.,Ltd., China). The thermal conductivity of nonwoven fabric was measured by using the transient plane source method on a hot disk instrument (TPS2500S, Hot Disk Inc., Sweden). Using Agilent E5234B vector network analyzer and waveguide method, the complex permittivity (εr=ε′-jε′′), permeability (μr=μ′-jμ′′) and scattering parameters (S11 and S21) of nonwoven fabrics were measured in the frequency of 8.2-12.4 GHz. Subsequently, the |Zin/Z0| of PFNy without metal-plate reflector and attenuation constant (α) was calculated by Eqs. S1, S2

zin/z0=1+S112-S2121-S112-S212                                                                                                           (S1)

α=2πfcμ''ε''-μ'ε'+μ''ε''-μ'ε'2+μ''ε'+μ'ε''2                                                               (S2)

, where f is the frequency, and c is the speed of light under vacuum conditions.

Meanwhile, EMI SE was measured on a vector network analyzer (Agilent E5234B) by using waveguide method in frequency range of 8.2-12.4 GHz. The corresponding EMI SE (SE or SET) and impedance matching performance (|Zin/Z0|) can be obtained by calculating the scattering parameters (S11 and S21) as follow Eqs. S3-S8.

R=|S11|2=|S22|2                                                                                                                     (S3)

T=|S21|2=|S12|2                                                                                                                      (S4)

A=1-R-T                                                                                                                                (S5)

SER=-10log1-R=-10log1-S112                                                                                    (S6)

SEA=-10logT1-R=-10log(S2121-S112)                                                                                        (S7)

SET=SER+SEA+SEM                                                                                                             (S8)

, when the SET exceeded 10 dB, SEM can be generally negligible.

The microwave absorption performance of samples can be described by the reflection loss (RL) values, and be calculated by Eqs. S9, 10:

Zin=Z0μrεrtanhj2πfdcεrμr                                                                                               (S9)

RL (dB)=20lgZin-Z0Zin+Z0                                                                                                           (S10)

, where Zin and Z0 represented the input impedance of sample and the impedance under vacuum conditions, respectively, and d is the thickness of sample.

Moreover, RL (dB) was also calculated by Eq. S11 to evaluate the ability of electromagnetic waves reflected from the surface of nonwoven fabrics.

RL=10logR=20log|S11|                                                                                                     (S11)

Furthermore, a self-made electromagnetic wave transmitter-receiver (10.5 GHz, 1W) was carried out to demonstrate EMI shielding and absorption performance of samples. Reflectivity of samples (200 mm*200 mm*5.3 mm) are also measured on vector network analyzers (Rohde & Schwarz, ZNA43. Ceyear, 3671G) by using arch method in 6-40 GHz. The nonwoven fabrics were further placed on a thermal stage of 200 oC (Shenzhen Jinglianghe Technology Co., Ltd.) to evaluate their high-temperature radar stealth performance. Meanwhile, the infrared thermal imager (FLUKE Ti400+, Fluke Corporation, USA) was applied to observed and recorded the changed in infrared radiation of samples.

S2 Supplementary Figures and Tables

Fig. S1 SEM images of PI nonwoven fabric

Fig. S2 FT-IR curves of PI, PF, PFN8, and PN80 nonwoven fabrics

Fig. S3 SEM image of NaOH-treated PI nonwoven fabric

Fig. S4 SEM image of PF nonwoven fabric

Fig. S5 EDS mapping images of PF nonwoven fabric

Fig. S6 High resolution XPS spectrum of Fe 2p for PF

Fig. S7 TGA curves of PI, PF, PFN5, PFN8, PFN12, and PN80 nonwoven fabrics

Fig. S8 SEM images of (a) PFN5, (b) PFN8, (c) PFN12 and (d) PN80

Fig. S9 EDS mapping images of (a) PFN5, (b) PFN8, (c) PFN12 and (d) PN80

Fig. S10 XRD patterns of PF and PFN8

Fig. S11 High resolution XPS spectra of Ni 2p for PN80

Fig. S12 Strain-Stress curves of PI, PF, PFN5, PFN8, PFN12, PN80, and PFN5-8-80

Fig. S13 (a) Real permeability (μ′) and (b) Imaginary permeability (μ′′) of PFN5, PFN8, and PFN12

Fig. S14 3D reflection loss of (a) PFN5, (b) PFN8, and (c) PFN12. 2D reflection loss of (d) PFN5, (e) PFN8, and (f) PFN12

Fig. S15 Electromagnetic parameters (ε′, ε′′, μ′, and μ′′) of PN80

Fig. S16 (a) Impedance matching (|Zin/Z0|) and (b) attenuation constant of PN80

Fig. S17 Simulation model of PFN5-8-80 in CST Studio Suite software

Fig. S18 Optical photograph of PFN80-8-5

Fig. S19 Optical photograph of PFN5-8-80

Fig. S20 The bonding force characteristic of PFN5-8-80 at 200 °C

Fig. S21 (a) SET and (b) Power Coefficients of PFN5-5, PFN5-8, and PFN8-8 with a thickness of 5 mm

Fig. S22 (a) SET, (b) SEA and SER of PFN5-8-80 at 6-40 GHz

Fig. S23 Impedance matching (|Zin/Z0|) of PFN5-8-80, PFN5-12-80, and PFN8-12-80

Fig. S24 (a) SET, (b) A, and (c) Reflection loss of PFN5-8-80, PFN5-12-80, and PFN8-12-80

Fig. S25 SET of PFN5-8-80 and PFN80-8-5

Fig. S26 (a) Power Coefficients and (b) Reflectivity of PFN5-8-80 and PFN80-8-5

Fig. S27 Photographs of 10.5 GHz electromagnetic demonstration devices

Fig. S28 3D RCS of PEC

Fig. S29 (a) RCS values of PEC, PFN5-8-80 and PFN5-8-80+PEC. (b) RCS reduction of PFN5-8-80 and PFN5-8-80+PEC in comparison with PEC

The RCS reduction value under different degree and frequency is caiculated by the following equation:

(1) RCS reduction (PFN5-8-80) = RCS (PEC) - RCS (PFN5-8-80)

(2) RCS reduction (PFN5-8-80+PEC) = RCS (PEC) - RCS (PFN5-8-80+PEC)

Fig. S30 Power loss density of PFN5, PFN8, and PN80 at 12 GHz

Fig. S31 Power loss density of PFN5-8-80 at 9, 10, 11, and 12 GHz

Fig. S32 The infrared emissivity of PFN5

Fig. S33 Photography of infrared stealth testing for PFN5-8-80 on a thermal stage

Fig. S34 Infrared image of PFN5-8-80 at a thermal stage of 200 °C for 24 h

Table S1 Comparison for radar stealh performances of recently reported materials

| Samples | Density (g cm-3) | Thickness (mm) | RLmin (dB) | EABmax (GHz) | Refs. |
| --- | --- | --- | --- | --- | --- |
| Hf/epoxy-L(OBN)f/epoxy | / | 5.6 | -19.4 | 9.8 | [44] |
| PI/CB | 0.27 | 25 | -44.8 | 16 | [45] |
| PI/GN/Fe3O4/SiO2 | 0.40 | 15 | -25.5 | 22.4 | [46] |
| NiCoFe@C |  | 2.0 | -31 | 11 | [47] |
| CNT@ZIS/CNF | 0.04 | 2.7 | -13 | 3.4 | [48] |
| CB/CIP |  | 8.6 | ~ -32 | 14.3 | [49] |
| ACDMS | / | 25 | -37.9 | 35.9 | [50] |
| SiC-BN@CNT | / | 15 | ~ -37 | 34.62 | [51] |
| 3D resistance film | / | 11 | -15.9 | 22.3 | [52] |
| CuHT-FCIP-EP | 0.89 | 9.3 | -51 | 38 | [53] |
| PFN5-8-80 | 0.15 | 5.3 | -23.87 | 22.1 | This work |

Movie S1 Demonstration of electromagnetic interference shielding and electromagnetic absorption capability of PFN5-8-80 at 10.5 GHz.

Movie S2 Demonstration of electromagnetic interference shielding and electromagnetic reflection capability of PFN80-8-5 at 10.5 GHz.

Movie S3 Demonstration of Real-Time Reflection loss of PFN5-8-80 at 8.2 GHz.

Movie S4 Demonstration of Real-Time Reflection loss of PFN80-8-5 at 8.2 GHz.

Movie S5 Demonstration of Real-Time Reflection loss of PFN5-8-80 and PFN80-8-5 at 8.2 GHz.