Supporting Information for

Nanoreactor-Structured Defective MoS2: Suppressing Intercalation-Induced Phase Transitions and Enhancing Reversibility for Potassium-Ion Batteries

Chunrong Ma1, Cyrus Koroni2, Jiacheng Hu2, Ji Qian3, Guangshuai Han4*, and Hui Xiong2*

1 School of Mechanical and Electrical Engineering, Qingdao University, Qingdao 266071, P. R. China

2 Micron School of Materials Science and Engineering, Boise State University, Boise, ID 83725, United States

3 Shandong Key Laboratory of Advanced Chemical Energy Storage and Intelligent Safety, Advanced Technology Research Institute, Beijing Institute of Technology, Jinan 250300, P. R. China

4 School of Automotive Studies, Tongji University, Shanghai 201804, P. R. China

*Corresponding authors. E-mail: 17666026@tongji.edu.cn (Guangshuai Han); clairexiong@boisestate.edu (Hui Xiong)

Supplementary Figures and Tables

Fig. S1 TEM image of pure MoS2

Fig. S2 HRTEM image of MoS2@NC

Fig. S3 Elemental mapping images of MoSSe@NC composite

Fig. S4 XPS of MoSSe@NC composite

Fig. S5 XPS spectrum of a) C1s and b) N1s in the MoSSe@NC composite

Fig. S6 Raman spectra of CNT and MoSSe@NC

Fig. S7 TGA profiles of MoSSe@NC

Fig. S8 N₂ adsorption–desorption isotherm

Table S1 Comparison of initial Coulombic efficiency with MoS2-based anode materials

| Materials | Charge/discharge capacity (mAh g-1) | Current density (mA g-1) | ICE | References |
| --- | --- | --- | --- | --- |
| MoSSe@NC | 466 / 576 | 200 | 70% | Our work |
| the C-p-MoS2/C | 666 / 963 | 50 | 69% | Adv. Funct. Mater. 2023, 33, 2207 |
| 1T’’’MoS2 | 130 / 240 | 40 | 49% | Adv. Funct. Mater. 2023, 33, 23065 |
| DWHNS Sn/MoS2@C, | 445 / 903 | 100 | 49.2% | ACS Nano 2021, 15, 14125−1413 |
| the MoS2-on-NC | 304 / 760 | 200 | 40% | Adv. Mater. 2020, 32, 20009 |
| TiNb2O6@MoS2/C | 592 / 1180 | 100 | 51% | J. Mater. Chem. A, 2019, 7, 5760–5768 |

Table S2 Comparison of the electrochemical performance of the MoSSe@NC electrode with state-of-the-art MoS₂-based anodes reported in the literature

| Materials | Rate/Capcity (A g-1/mAh g-1) | Cycling performance | References |
| --- | --- | --- | --- |
| MoSSe@NC | 10 / 176 | 1000 cycles at 3A g-1 92% capacity retention | Our work |
| 1T/2H-MoS2/NCNHP | 2 / 302 | 500 cycles at 1A g-1 70% capacity retention | Small 2020,16, 2004178 |
| 1T’’’ MoS2 | 1 / 75 | 1400 cycles at 1A g-1 95% capacity retention | Adv. Funct. Mater.2023, 33,2306550 |
| MoSSe | 5 / 275 | 1000 cycles at 2A g-1 75% capacity retention | ACS Nano 2019, 13, 11843-11852 |
| Fe9S10@MoS2@C | 5 / 95 | 50 cycles at 2A g-1 80% capacity retention | Energy Storage Materials 24 (2020) 208–219 |
| MoS1.5Se0.5-NC | 5 / 210 | 490 cycles at 5A g-1 70% capacity retention | Adv. Energy Mater. 2020, 10, 1904162 |
| CTMG | 5 / 186 | 380 cycles at1A g-1 65% capacity retention | Adv. Funct. Mater. 2020, 30, 2001484 |
| MoS2/C | 1 / 175 | 300 cycles at1A g-1 55% capacity retention | J. Mater. Chem. A, 2019, 7, 5760–5768 |

Fig. S9 SAED patterns of MoSSe@NC: (a) before cycling and (b) after 500 cycles

Fig. S10 (a) The charge-discharge profiles and (b) Cycling performance at 0.5 A g-1 of full cell

The diffusion coefficient can be expressed as the following equation:

DK+=4πmBVMMBA2∆EsτdEτ/d(τ)2 (τ≪L2/DK+)     (S1)

In this equation, τ(s) is the constant current flux time, mB (g) is the active mass of the electrode, VM (cm3 mol−1) is the molar volume of the electrode, MB (g mol-1) is the molecular weight, A (cm2) is the surface area of the electrode, L (cm) is the thickness of the electrode, ES (V) is the total change in cell voltage during a single step and Eτ (V) is the voltage change in the steady state during a single step.

If E versus τ shows a linear behavior during the current pulse, the equation can be transformed into:

DK+=4πmBVMMBA2∆Es∆Et2  (τ≪L2/DK+)          (S2)

Fig. S11 GITT profiles of MoSSe@NC and MoS2@NC composite

Fig. S12 EIS spectra of MoS₂@NC and MoSSe@NC

Fig. S13 The capacitive contribution in the total charge storage at 0.2 mV s-1

Computational Method

Calculations were conducted by the Gaussian and the Vienna Ab initio Simulation Package (VASP). Projector-augmented-wave (PAW) potentials were used to consider the electron-ion interactions, whereas the electron exchange-correlation interactions were treated using the Perdew-Burke-Ernzerhof (PBE) exchange correlation functional in the scheme of generalized gradient approximation (GGA). For the substrate, a vacuum space of 15 Å placed between adjacent layers to avoid periodic interactions. All the atomic positions and lattice vectors fully optimized using a conjugate gradient algorithm to obtain the unstrained configuration. The Brillouin zone integration employed a gamma-centred 3 × 3 × 1 Monkhorst-Pack mesh of k points. The electron wavefunctions were expanded in a plane wave basis with kinetic energy cutoff of 500 eV. Atomic relaxation performed until the change in total energy was less than 1×10-5 eV, and maximum forces were smaller than 0.02 eV/Å.

Fig. S14 the Strucutre of MoS2@NC and MoSSe@NC

Fig. S15 The structural diffusion paths of K on MoSSe@NC and MoS₂@NC