Supporting Information for

Vertical Interfacial Engineering in Two-Step-Processed Perovskite Films Enabled by Dual Interface Modification for High-Efficiency p-i-n Solar Cells

Wenhao Zhou1#, Heng Liu2,3#, Haiyan Li4#, Weihai Zhang1,2,* Hui Li1, Xia Zhou1, Rouxi Chen5, Wenjun Zhang1, Tingting Shi4,*, Antonio Abate1*, and Hsing-Lin Wang2*

1 School of New Energy, Ningbo University of Technology, Ningbo, 315211, P. R. China

2 Department of Materials Science and Engineering, Southern University of Science and Technology, Shenzhen, 518055, P. R. China

3 Institute of Materials, Henan Academy of Sciences, Zhengzhou, 450046, P. R. China

4 Siyuan Laboratory, Guangzhou Key Laboratory of Vacuum Coating Technologies and New Energy Materials, Department of Physics, Jinan University, Guangzhou, 510632, P. R. China

5 School of Innovation and Entrepreneurship, Southern University of Science and Technology, Shenzhen, 518055, P. R. China

#Wenhao Zhou, Heng Liu, and Haiyan Li contributed equally to this work.

*Corresponding authors. E-mail: zhangwh@nbut.edu.cn (Weihai Zhang); ttshi@jnu.edu.cn (Tingting Shi); antonio.abate@unina.it (Antonio Abate); wangxl3@sustech.edu.cn (Hsing-Lin Wang)

Supplementary Figures and Tables

Fig. S1 a Schematic structure of the regular n-i-p and inverted p-i-n devices. b J-V curves of the TSP n-i-p and p-i-n devices

Fig. S2 Exfoliation process of the perovskite film

Note: The detailed exfoliation process as follows: 1) The as-deposited perovskite films were encapsulated by dispensing a drop of UV-curable adhesive and then covered with a clean glass. 2) After encapsulating the sample, it was exposed to 365 nm UV light for 10 minutes to cure the UV-curable adhesive. 3) The ITO substrate was then gently peeled off to expose the bottom surface of the perovskite film for investigation.

Fig. S3 XPS C 1s and Pb 4f core spectra of the top and bottom sides of the TSP film

Fig. S4 Depth-profiled a I 3d and b Pb 4f core spectra of the TSP film with varying etching time

Note: The I/Pb ratio of the TSP perovskite film with different etching time can be estimated according to the equation: NI∕NPb=AI∕SI∕APb∕SPb, where AI and APb represent the I 3d and Pb 4f peak areas, respectively, and SI (5.337) and SPb (6.968) denote the sensitivity factors for I and Pb. The detailed parameteres are summarized in Table S1.

Fig. S5 19F NMR spectra of pure Sn(OTF)2 and Sn(OTF)2+PbI2 samples in deuterated DMSO-d6 solution

Note: The characteristic resonance signal of F in pure Sn(OTF)2 reveals upshift of resonance peak for the Sn(OTF)2+PbI2 sample, verifying the interaction between -CF3 groups and PbI2.

Fig. S6 a, b XRD patterns and c, d SEM images of PbI2 films deposited on bare NiOx (control) and NiOx/Sn(OTF)2 (Sn(OTF)2) substrates

Note: The inset photos suggest that the control-PbI2 films exhibit a significantly faster color transition from semitransparent yellow to deep yellow compared to the Sn(OTF)2-PbI2 films. This visual observation directly suggests that the control-PbI2 films undergo crystallization at a higher rate than the Sn(OTF)2-PbI2 films. Consistently, the corresponding XRD results reveal that under identical experimental conditions, the control-PbI2 films display substantially stronger diffraction intensities relative to the Sn(OTF)2-PbI2 films, confirming the faster crystallization rate of the control-PbI2 films. The SEM results suggest that the Sn(OTF)2-PbI2 film demonstrates a more mesoporous morphology than that of the control-PbI2 film, indicating that Sn(OTF)2 interlayer interact with PbI2, thus retarding its crystallization. This more mesoporous PbI2 film is beneficial for ammonium salt penetration, facilitating perovskite crystallization.

Fig. S7 Cross-sectional SEM image of the device

Note: According to the scale bar, the thickness of the perovskite film is approximately 700 nm.

Fig. S8 J-V curves obtained from reverse (Voc to Jsc) and forward (Jsc to Voc) scans for the a control, b Sn(OTF)2, and c Sn(OTF)2+PEA devices. d EQE spectra and e stabilized power outputs of the champion devices based on the control, Sn(OTF)2, and Sn(OTF)2+PEA films

Note: Hysteresis studies based on H-index: HI=PCEreverse-PCEforwardPCEreverse, where PCEreverse and PCEforward are power conversion efficiency of devices for reverse and forward scan, respectively, reveal that Sn(OTF)2+PEA device delivers the smallest HI value (1.9%) compared to the control (9.3%) and Sn(OTF)2 (4.7%) devices, which is mainly attributed to a more favorable charge extraction environment within the Sn(OTF)2+PEA device.

Fig. S9 Models and adsorption energies of SO3-NiOx(Ni), CF3-NiOx(Ni), SO3-FAPbI3(Pb), and CF3-FAPbI3(Pb), respectively

Fig. S10 SEM and AFM images of the bare NiOx and NiOx/Sn(OTF)2 films. The scale bar is 1 μm. Statistical RMS values for different films. A total of 5 different random positions (5 × 5 μm2 per position) for each sample were counted

Note: The Sn(OTF)2 modification does not alter the morphology of NiOx films. While, a reduction in RMS roughness from 5.29 ± 0.34 nm (bare NiOx) to 4.76 ± 0.18 nm (NiOx/Sn(OTF)2) can be observed.

Fig. S11 Optical transmission spectra of the bare NiOx and NiOx/Sn(OTF)2 films

Fig. S12 In-situ PL spectra of control and Sn(OTF)2 perovskite films as a function of different annealing time

Fig. S13 GIXRD spectra of the control and Sn(OTF)2 films acquired from the bottom surface

Fig. S14 Depth-profiled Pb 4f core spectra of the Sn(OTF)2 film with varying etching time

Note: It can be seen that after 330 seconds of etching, the Pb 4f peak disappeared, indicating complete etching through the perovskite film. By combining the thickness (700 nm) measured via cross-sectional SEM with the etching duration, the etching rate was calculated to be 2.1 nm/s.

Fig. S15 UV-vis absorption spectra and Urbach energy of different perovskite film

Note: The Urbach energy was calculated from the UV-Vis absorption spectra with equation lnα=lnα0+hvEu, where α0 is a constant, α is the absorption coefficient, hυ is the photon energy, and Eu is the Urbach energy. A smaller Eu is highly desirable for semiconductor devices, indicative of highly crystallized film with less impurities.

Fig. S16 AFM images of different perovskite films

Note: The RMS values of the control, Sn(OTF)2 and Sn(OTF)2+PEA films are 39.9, 37.2, and 33.7 nm, respectively. The Sn(OTF)2+PEA film exhibits the smallest surface roughness, which is critical for achieving high device performance.

Fig. S17 Tauc’s plots of the FAPbI3 and FASn0.1Pb0.9I3 perovskite films

Note: The Tauc’s plots were derived from the UV-Vis absorption spectra with equation αhν2=Ahυ-Eg, where α is the absorption coefficient, hυ is the photon energy, and Eg is the bandgap of the perovskite film. Accordingly, the bandgaps of the FAPbI3 and FASn0.1Pb0.9I3 perovskites were determined to be 1.55 and 1.45 eV, respectively.

Fig. S18 Energy level alignment plots of the a control, b Sn(OTF)2, and c Sn(OTF)2+PEA films

Fig. S19 Jsc response under different light intensities

Note: The Sn(OTF)2+PEA device delivers a most ideal α value of 0.957 compared to the control (0.911) and Sn(OTF)2 (0.946) devices, demonstrating improved charge carrier extraction efficiency.

Fig. S20 The contact angle of control, Sn(OTF)2, and Sn(OTF)2+PEA films

Note: It can be seen that the Sn(OTF)2+PEA film exhibits a contact angle of 91.4°, much larger than that of control (67.4°) and Sn(OTF)2 (69°) films. The results suggest that after F-PEA post-treatment, the resulting Sn(OTF)2+PEA film demonstrates a more hydrophobic surface, which is essential for the enhancement of long term stability of the resulting device.

Fig. S21 Sn 3d5/2 XPS core spectra derived from the bottom surface of the perovskite film as a function of ambient exposure time

Note: It can be seen that after 168 h exposure, the Sn4+/Sn2+ ratio only increased slightly from 14.1 to 21.0%. This slow oxidation rate indicates the Pb-Sn interlayer has strong ambient resilience. The mild increase aligns with the gradual degradation of unencapsulated perovskite films, which is unavoidable in ambient conditions but well-controlled here.

Fig. S22 J-V curves and corresponding photovoltaic parameters of the unencapsulated PSCs a function of ambient exposure time

Note: It can be seen that after 168 h exposure, the PCE of the device decreased slightly from 25.21%to 24.7%. The minor efficiency loss was primarily attributed to a small drop in FF (from 81.9% to 80.8%), not JSC or VOC. This confirms the interlayer’s energy level alignment function (critical for JSC and VOC) remains intact, and the decay stems from trivial bulk perovskite degradation, not interlayer failure.

Table S1 I/Pb ratio of the TSP perovskite film with different etching time

| Etching time (s) | AI | APb | SI | SPb | I/Pb ratio |
| --- | --- | --- | --- | --- | --- |
| 0 | 1616816 | 824578 | 5.337 | 6.968 | 2.56 |
| 30 | 1624230 | 818762 | 5.337 | 6.968 | 2.59 |
| 60 | 1643074 | 812574 | 5.337 | 6.968 | 2.64 |
| 90 | 1678798 | 808763 | 5.337 | 6.968 | 2.71 |
| 120 | 1712927 | 801578 | 5.337 | 6.968 | 2.79 |
| 150 | 1728758 | 797538 | 5.337 | 6.968 | 2.83 |

Table S2 Photovoltaic parameters of champion PSCs based on different perovskite films

| Device | Scan direction | Voltage (V) | Current density (mA cm-2) | FF (%) | PCE (%) | HI (%) |
| --- | --- | --- | --- | --- | --- | --- |
| control | Forward | 1.06 | 23.9 | 73.1 | 18.6 | 9.3 |
|  | Reverse | 1.11 | 24.4 | 75.7 | 20.5 |  |
| Sn(OTF)2 | Forward | 1.14 | 25.4 | 77.5 | 22.5 | 4.7 |
|  | Reverse | 1.14 | 25.2 | 81.8 | 23.6 |  |
| Sn(OTF)2+PEA | Forward | 1.18 | 26 | 81.5 | 25.1 | 1.9 |
|  | Reverse | 1.18 | 26.1 | 82.8 | 25.6 |  |

Table S3 Conductivity of bare NiOx and NiOx/Sn(OTF)2 films

| Sample | Thickness (nm) | Area (cm2) | slope | Conductivity (S·cm-1) |
| --- | --- | --- | --- | --- |
| NiOx | 40 | 0.04 | 0.2 | 210-5 |
| NiOx/Sn(OTF)2 | 40 | 0.04 | 0.26 | 2.610-5 |

Note: The conductivity of the films were calculated according to the equation: σ=D/(SR), where σ is the conductivity, D is the film thickness, S is the effective area, and R is the resistance. Based on the I-V curve, R can be extracted as 1/slope.

Table S4 UPS parameters of the bare NiOx and NiOx/Sn(OTF)2 films

| Sample | Ecutoff (eV) | Eonset (eV) | VBM (eV) | EF (eV) |
| --- | --- | --- | --- | --- |
| NiOx | 16.60 | 0.71 | 5.33 | 4.62 |
| NiOx/Sn(OTF)2 | 16.43 | 0.68 | 5.47 | 4.79 |

Table S5 Fitted TRPL parameters of the different perovskite films

| Perovskite | A1 | τ1 (ns) | A2 | τ2 (ns) | τave (ns) |
| --- | --- | --- | --- | --- | --- |
| control | 0.406 | 181.45 | 0.473 | 386.8 | 327.9 |
| Sn(OTF)2 | 0.59 | 240.5 | 0.256 | 792.4 | 565.2 |
| Sn(OTF)2+PEA | 0.696 | 337.13 | 0.225 | 1140 | 756.6 |

Note: The fitting biexponential decay function was y=y0+A1exp-tτ1+A2exp-tτ2.

Table S6 UPS parameters of the control perovskite film with different etching depths

| Depth [nm] | Ecutoff (eV) | Eonset (eV) | VBM (eV) | Eg (eV) | CBM (eV) | EF (eV) |
| --- | --- | --- | --- | --- | --- | --- |
| 700 | 16.4 | 1.02 | -5.84 | 1.55 | -4.29 | 4.82 |
| 600 | 16.43 | 0.99 | -5.78 | 1.55 | -4.23 | 4.79 |
| 500 | 16.46 | 0.95 | -5.71 | 1.55 | -4.16 | 4.76 |
| 400 | 16.46 | 0.88 | -5.64 | 1.55 | -4.09 | 4.76 |
| 300 | 16.45 | 0.82 | -5.59 | 1.55 | -4.04 | 4.77 |
| 200 | 16.47 | 0.77 | -5.52 | 1.55 | -3.97 | 4.75 |
| 100 | 16.5 | 0.76 | -5.48 | 1.55 | -3.93 | 4.72 |
| 0 | 16.53 | 0.73 | -5.42 | 1.55 | -3.87 | 4.69 |

Table S7 UPS parameters of the Sn(OTF)2 perovskite film with different etching depths

| Depth [nm] | Ecutoff (eV) | Eonset (eV) | VBM (eV) | Eg (eV) | CBM (eV) | EF (eV) |
| --- | --- | --- | --- | --- | --- | --- |
| 700 | 16.45 | 0.77 | -5.54 | 1.45 | -4.09 | 4.77 |
| 600 | 16.43 | 0.81 | -5.6 | 1.55 | -4.05 | 4.79 |
| 500 | 16.42 | 0.84 | -5.64 | 1.55 | -4.09 | 4.8 |
| 400 | 16.41 | 0.86 | -5.67 | 1.55 | -4.12 | 4.81 |
| 300 | 16.41 | 0.85 | -5.66 | 1.55 | -4.11 | 4.81 |
| 200 | 16.4 | 0.84 | -5.66 | 1.55 | -4.11 | 4.82 |
| 100 | 16.41 | 0.81 | -5.62 | 1.55 | -4.07 | 4.81 |
| 0 | 16.4 | 0.76 | -5.58 | 1.55 | -4.03 | 4.82 |

Table S8 UPS parameters of the Sn(OTF)2+PEA perovskite film with different etching depths

| Depth [nm] | Ecutoff (eV) | Eonset (eV) | VBM (eV) | Eg (eV) | CBM (eV) | EF (eV) |
| --- | --- | --- | --- | --- | --- | --- |
| 700 | 16.47 | 0.78 | -5.53 | 1.45 | -4.08 | 4.75 |
| 600 | 16.42 | 0.81 | -5.61 | 1.55 | -4.06 | 4.80 |
| 500 | 16.42 | 0.85 | -5.65 | 1.55 | -4.10 | 4.80 |
| 400 | 16.41 | 0.86 | -5.67 | 1.55 | -4.12 | 4.81 |
| 300 | 16.41 | 0.87 | -5.68 | 1.55 | -4.13 | 4.81 |
| 200 | 16.4 | 0.88 | -5.70 | 1.55 | -4.15 | 4.82 |
| 100 | 16.39 | 0.91 | -5.74 | 1.55 | -4.19 | 4.83 |
| 0 | 16.38 | 0.95 | -5.79 | 1.55 | -4.24 | 4.84 |

Table S9 SCLC parameters for different perovskite films

| Perovskite | Dielectric factor | Vacuum permittivity (F m-1) | Thickness (nm) | Elementary charge | VTFL (V) | Trap density (cm-3) |
| --- | --- | --- | --- | --- | --- | --- |
| control | 48 | 8.85×10-12 | 700 | 1.6×10-19 | 0.64 | 6.91×1015 |
| Sn(OTF)2 | 48 | 8.85×10-12 | 700 | 1.6×10-19 | 0.47 | 5.07×1015 |
| Sn(OTF)2+PEA | 48 | 8.85×10-12 | 700 | 1.6×10-19 | 0.39 | 4.21×1015 |

Note: The trap density of the perovskite films can be calculated through the following equation:

Nt=2VTFLεrε0eL2                    (S1)

where εr is the relative dielectric constant of perovskite, which is approximately 48, ε0 is the vacuum permittivity, e is the elementary charge, and L is the thickness of the perovskite film, which is approximately 700 nm. Accordingly, the defect density was determined to be 6.91×1015, 5.07×1015, and 4.21×1015 cm-3 for the control, Sn(OTF)2, and Sn(OTF)2+PEA films, respectively.