Supporting Information for

Electrically Insulating Rigid Multi-Channel Electrolyte Container for Customizable Electron Transfer in Zn-Halogen Batteries

Yifan Zhou1,#, Yicai Pan2,#, Yongqiang Yang3,*, Taghreed F. Altamimi4, Yunpeng Zhong5, Dalal A. Alshammari6, Zeinhom M. El-Bahy7, Shuquan Liang1, Jiang Zhou1, and Xinxin Cao1,*,

1 School of Materials Science and Engineering, Key Laboratory of Electronic Packaging and Advanced Functional Materials of Hunan Province, Central South University, Changsha 410083, P. R. China

2 Department of Materials Science and Engineering & Center of Super-Diamond and Advanced Films (COSDAF), City University of Hong Kong, Hong Kong SAR 999077, P. R. China

3 Department of Applied Biology and Chemical Technology, The Hong Kong Polytechnic University, Hong Kong SAR 999077, P. R. China

4 Department of Physics, College of Science, University of Hail, P.O. Box, 2440, Hail, Saudi Arabia

5 Christopher Ingold Laboratory, Department of Chemistry, University College London, London, WC1H0AJ, U.K.

6 Department of Chemistry, College of Science, University of Hafr Al Batin, Hafr Al Batin P.O. Box 39524, Saudi Arabia

7 Department of Chemistry, Faculty of Science, Al-Azhar University, Nasr City 11884, Cairo, Egypt

# Yifan Zhou and Yicai Pan contributed equally to this work.

* Corresponding authors. E-mail: yong-qiang.yang@polyu.edu.hk (Yongqiang Yang); caoxinxin@csu.edu.cn (Xinxin Cao)

Supplementary Figures and Tables

Fig. S1 Single-chain molecular structure of α-PVDF, β-PVDF, and PVDF-hfp

In the TGTG' conformation of the α-phase, the dipole moments along the molecular chains partially cancel each other, resulting in relatively low overall polarization, lower dielectric constant and reduced polarization strength. In contrast, the fully trans TTTT conformation of the β-phase allows for effective superposition of dipole moments along the chain direction, leading to higher overall polarization and an increased dielectric constant.

Fig. S2 XPS spectra of PVDF-hfp, SiO2 and SP: (a) full spectrum, (b) O 1s and Si 2p spectra

Fig. S3 FT-IR spectra of SiO2, PVDF-hfp, SP, LE and SPE, respectively

Fig. S4 Raman spectra of SiO2, PVDF-hfp, SP, Zn(CF3SO3)2, LE and SPE, respectively

Fig. S5 3D snapshots of (a) LE and (b) SPE obtained from MD simulation

Fig. S6 TG curves of (a) SiO2, PVDF-hfp, SP powder, SP, SPE, respectively, and (b) SPE prepared with different soaking times

TG analysis was conducted under nitrogen at a heating rate of 10°C min−1. SiO2 exhibits excellent thermal stability, while PVDF-hfp begins decomposing at 400°C. The as-prepared SP powder shows an initial mass loss of 32.4% owing to the evaporation of residual NMP, a phenomenon absent in the fully dried SP disc, indicating its effective removal (Fig. S6a). To explore the electrolyte absorption kinetics, a more detailed analysis was performed on SPE discs with different soaking times (Fig. S6b). The weight loss curves before 450°C can be divided into two distinct stages: the loss of loosely bound “physical water” (below ~300°C) and the loss of more tightly bound “structural water” (300~450 °C). As results, the “physical water” content increases steadily, from 17.5% at 1 hour to 22.1% at 2 hours, before plateauing at 23.0% overnight. These are attributed to a fast adsorption within the macroporous volume, followed by a slower internal diffusion-filling process. On the other hand, the “structural water” content was only around 2% after both 1 and 2 hours but increased significantly to 7.2% after soaking overnight. This indicates that its formation rate is considerably slower. Therefore, to establish stable interactions between the LE components and the SP framework and to allow for the complete formation of ion solvation sheaths, a longer soaking time is evidently required.

Fig. S7 SEM and TEM images of (a) SiO2, (b) PVDF-hfp; (c) SEM and TEM images with EDS elemental mappings of SP surface

Fig. S8 Cross-sectional SEM images of SP: (a) initial edge, (b) cutting edge

Fig. S9 Surface and cross-sectional SEM images with EDS elemental mappings of the SPE after heat treatment

Fig. S10 Nitrogen adsorption-desorption isotherms and corresponding pore size distribution curve of (a) SiO2, (b) PVDF-hfp, (c) SP, and (d) SPE

Fig. S10a, S10b: Type I adsorption-desorption isotherm.

At the lower relative pressures, the amount adsorbed increases rapidly until saturation is reached, indicating clear micropore characteristics.

Fig. S10c, S10d: Type IV adsorption-desorption isotherm.

As relative pressure increases, the amount adsorbed gradually rises, with a hysteresis phenomenon occurring as the relative pressure approaches 1, which is typical of mesoporous materials.

Fig. S11 Pore size distributions of (a) SP and (b) SPE obtained from mercury intrusion porosimetry

Fig. S12 Load-displacement curves of SP and SPE obtained from nanoindentation

Based on the above depth-load curves, the hardness (G Pa) of the samples can be calculated by the following formula:

H=PmaxA

where Pmax is the maximum load (the peak load during the indentation process, μN), and A is the contact area (nm2) between the indenter tip and sample.

The elastic modulus (G Pa) is determined via the Oliver-Pharr method [S1], with the formula:

Esample=1-νsample2Er-1-νtip2Etip-1

where νsample and νtip are the Poisson’s ratios of sample and indenter tip, respectively. Etip is the elastic module of the indenter tip and Er is the reduced modulus, which was calculated with the formula:

Er=π2⋅SA

where S is the unloading stiffness (μN nm−1). The calculation results are summarized in Table S2.

Fig. S13 Thickness measurements of SP and SPE

Fig. S14 Frequency-dependent dielectric properties of SiO2 and SP

Fig. S15 EIS plots with stainless steel/stainless steel cells and calculated ionic conductivity of SPE and LE

The ionic conductivity (σ) of electrolytes was evaluated via EIS using stainless steel/stainless steel cells, which was calculated using the formula:

σ= lRA

where l is the thickness (cm) of the electrolyte, A is the reaction area (cm2) between electrolyte and electrodes, R is the bulk resistance (Ω) extracted from the high-frequency intercept of the Nyquist plot on the real axis.

Fig. S16 Chronoamperometry curves with a polarization voltage of 10 mV, corresponding EIS plots before and after the polarization in Zn/Zn cells and calculated Zn2+ transference number (t) of (a) LE and (b) SPE

The Zn2+ transference number (tZn2+) was determined via chronoamperometry (CA) coupled with EIS in Zn/Zn symmetric cells. A polarization voltage (∆V) of 10 mV was applied, and corresponding current relaxation (I0→Is) and interfacial resistance evolution (Ri0→Ris) were monitored. The tZn2+was calculated using the Bruce-Vincent formula [S2]:

tZn2+=Is ∆V - I0Ri0I0 ∆V - IsRis

The calculation results are summarized in Table S3.

Fig. S17 In-situ differential electrochemical mass spectrometry (DEMS) on the Zn/Zn symmetric cells at 1 mA cm−2@0.5 mAh cm−2 with (a) SPE and (b) LE

Fig. S18 CE plots at 0.5 mA cm−2@0.25 mAh cm−2 in additional Zn/Cu cells with SPE, with the bottom panels showing the corresponded avg. CE with calculated standard deviation

Fig. S19 Voltage curves for Zn/Cu cells with LE and SPE at Zn plating/stripping conditions of (a) 0.5 mA cm−2@0.25 mAh cm−2, and (b) 1 mA cm−2@5 mAh cm−2

Fig. S20 Voltage curves at 10 mA cm−2@5 mAh cm−2 for Zn/Zn cells with SPE and LE

Fig. S21 (a) SEM images after plating for different cycles and (b) corresponding EDS mappings in the 100th cycle of Zn electrode in Zn/Zn cells with SPE at 0.5mA cm−2@0.25 mAh cm−2

Fig. S22 (a) SEM images after plating for different cycles and (b) corresponding EDS mappings in the 100th cycle of Zn electrode in Zn/Zn cells with LE at 0.5mA cm−2@0.25 mAh cm−2

Fig. S23 In-situ optical microscope snapshots of Zn plating in (a) LE and (b) SPE

Fig. S24 XRD patterns of Zn electrode after plating for different cycles in Zn/Zn cells with (a) SPE and (b) LE

Fig. S25 (a) Cycling performance and (b) corresponding voltage curve of Zn-halogen coin cell in voltage range of 0.8 to 1.8 V with SPE without potassium chloride and potassium iodide addition

Fig. S26 (a) CV curves at 0.1 to 1.0 mV s−1, (b) corresponding log(current) vs. log (scan rate) plots of redox peaks and (c) calculated capacitive-controlled contributions of Zn-halogen cell in the voltage range of 0.8 to 1.9 V with SPE

According to Dunn’s research [S3, S4], the relationship between current (i) and scan rate (v) in CV curves can be described by the following equations:

i = avb

log(i) = b × log(v) + log(a)

where a, b are adjustable parameters, Specifically, a b-value of 0.5 indicates a fully diffusion-controlled process, while a b-value of 1 represents an entirely capacitive-controlled process. The b-value can be directly determined from the slope of the log(i) vs. log(v) plots.

Furthermore, the contributions from pseudocapacitive and diffusion-controlled processes can be quantified by the following equations [S5, S6]:

i = k1v + k2v1/2

i/v1/2 = k1v1/2 + k2

where k1 denotes capacitive contribution, and k2 corresponds to diffusion-controlled contribution. By calculating these parameters (k1 and k2), relative fractions of capacitive and diffusion-limited currents can be clearly distinguished.

Fig. S27 Voltage curves for Zn-halogen coin cells in the voltage range of 0.6 to 1.8 V with SPE at (a) 3 mA cm−2 and (b) 10 mA cm−2

Fig. S28 (a) Cycling performance of Zn-halogen coin cell in the voltage range of 0.6 to 1.8 V with SPE at 20 mA cm−2; (b) Cycling performances of additional coin cells, with the bottom panels showing the corresponded avg. CE with calculated standard deviation

Fig. S29 Voltage curves for Zn-halogen pouch cells (3×3 cm2) in the voltage range of 0.8 to 1.8 V: (a) SPE and (b) LE with carbon fiber cloth current collector at 4 mA cm−2; (c) SPE with carbon felt current collector at 2 mA cm−2

Fig. S30 In-situ DEMS on the Zn-halogen coin cell in the voltage range of 0.8 to 2.1 V at 3 mA cm−2 with (a) SPE and (b) LE

Fig. S31 Voltage curves and optical images of the battery components after cycling of Zn-halogen coin cells in the voltage range of 0.8 to 2.1 V with (a) LE and (b) SPE at 1 mA cm−2

Fig. S32 Cycling performances of additional Zn-halogen coin cells in the voltage range of 0.8 to 2.1 V with SPE at 10 mA cm−2, with the bottom panels showing the corresponded avg. CE with calculated standard deviation

Fig. S33 Voltage curves of Zn-halogen coin cells in the voltage range of 0.8 to 2.1 V with SPE at (a) 3 mA cm−2 and (b) 10 mA cm−2

Fig. S34 Comparisons of areal capacity, coulombic efficiency and lifespan in other metal-halogen coin cells

Fig. S35 Galvanostatic intermittent titration technique (GITT) voltage curves of Zn-halogen coin cells in the voltage range of 0.8 to 1.8 V with SPE and LE at 3 mA cm−2

The GITT was performed in coin cells with a current pulse duration of 300 s and a relaxation time of 600 s. The diffusion coefficient (D) can be calculated according to the following equation [S7]:

D = 4L2πτ∆Es∆Et2

where t and 𝜏 represent the durations of current pulse (s) and relaxation period (s), respectively; L is the diffusion length of charge carrier, equal to the electrode thickness; ∆Es is the steady-state voltage change (V) induced by current pulse, and ∆Et is the voltage variation (V) during the constant current pulse after subtracting the voltage change following relaxation.

Fig. S36 Ex-situ EIS spectra of double-electron transfer Zn-halogen coin cells with SPE and LE

Fig. S37 Ex-situ XPS spectra of cathodes in the different cycling states in double-electron transfer Zn-halogen cells with SPE: (a) Full spectra; (b) C 1s region

Fig. S38 SEM images for different cycles and corresponding EDS mappings in the 100th cycle of Zn anode in double-electron transfer Zn-halogen coin cells with (a) LE and (b) SPE, respectively

Table S1 Hydrogen bond statistics derived from the solvation boxes of SP and SPE

| Sample | Types of H-bonds | Lengths (Å) |  |  |  | Numbers |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Min. | Max. | Md. | Avg. |  |
| LE | H2O−CF3SO3− | 1.37505 | 2.49994 | 2.13763 | 2.09969 | 5509 (54%) |
|  | H2O−H2O | 1.35916 | 2.49983 | 1.98025 | 1.99027 | 4747 (46%) |
| SPE | H2O−CF3SO3− | 1.34828 | 2.49916 | 1.80388 | 1.87974 | 3291 (36%) |
|  | H2O−H2O | 1.43786 | 2.49916 | 1.85446 | 1.90428 | 1651 (18%) |
|  | H2O−SiO2 | 1.43786 | 2.49916 | 2.01224 | 2.02149 | 2548 (27%) |
|  | H2O−PVDF-hfp | 1.43786 | 2.49916 | 1.87967 | 1.92704 | 1764 (19%) |

Table S2 Hardness and elastic modulus of SP and SPE derived from nanoindentation

| Sample | No. | Pmax (μN) | A (nm2) | S (μN mm−1) | E (GPa) | H (GPa) |
| --- | --- | --- | --- | --- | --- | --- |
| SP | 1 | 1996.75 | 8576600.71 | 10.70 | 3.238109 | 0.232814 |
|  | 2 | 1996.87 | 6814426.37 | 9.77 | 3.315582 | 0.293036 |
|  | 3 | 1996.89 | 8120832.23 | 11.20 | 3.481248 | 0.245898 |
|  | 4 | 1996.71 | 8995816.70 | 10.32 | 3.047446 | 0.221960 |
|  | 5 | 1996.99 | 7832634.02 | 11.04 | 3.495007 | 0.254957 |
| SPE | 1 | 1996.76 | 7905203.69 | 9.84 | 3.101648 | 0.252588 |
|  | 2 | 1996.87 | 6934619.92 | 8.57 | 2.881734 | 0.287957 |
|  | 3 | 1996.83 | 9188505.38 | 9.45 | 2.762539 | 0.217318 |
|  | 4 | 1996.89 | 9225901.08 | 9.44 | 2.753576 | 0.216444 |
|  | 5 | 1996.94 | 9821988.13 | 10.29 | 2.910396 | 0.203313 |

Table S3. Calculations of Zn2+ transference numbers (t) for LE and SPE

| Sample | I0 (mA) | Is (mA) | Ri0 (Ω) | Ris (Ω) | t(Zn2+) |
| --- | --- | --- | --- | --- | --- |
| LE | 0.432 | 0.068 | 88.65 | 126.50 | 0.70142 |
| SPE | 0.440 | 0.099 | 73.86 | 127.60 | 0.57912 |

Table S4 Comparisons of areal capacity, discharge mid-voltage and capacity in other metal-halogen pouch cells

| Label | Type | Electrochemical performance |  |  |  | Refs. |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Capacity (mAh) | Areal capacity (mAh cm−2) | Current density (mA cm−2) | Mid-voltage (V) |  |
| AC//3 M Zn(CF3SO3)2 + 2 M KCl+0.5 M KI in SPE | I−/I0/I+ | 107 | 11.9 | 2 | 1.3 | This work |
| I2@EI-ZrP//HCP | I−/I0 | 10 | 1.11 |  | 1.2 | [S8] |
| PC@Fe2N-I2//2 M ZnSO4 | I−/I0 | 14.2 | 0.75 | 1.85 | 1.07 | [S9] |
| I2@CNT//PAH-PCH/CP | I−/I0 | 20 | 2.22 |  | 1.15 | [S10] |
| I2@Fe SAC-MNC//2 M ZnSO4 + 0.04 M I3− | I−/I0 | 36.88 |  |  | 1.21 | [S11] |
| CNT@MPC12-I−//1 M ZnSO4 | I−/I0 | 51.3 | 1.71 | 5 | 1.18 | [S12] |
| I2@Ti-C//2 M ZnSO4 + 5 mM TDFND | I−/I0 | 68 | 2.6 | 4 | 1.08 | [S13] |
| I2@PC//2 M ZnSO4 + PG | I−/I0 | 78.5 |  |  | 1.15 | [S14] |
| I2@AC//2 M ZnSO4//Zn-CCS | I−/I0 | 140 | 4.39 | 4 | 0.98 | [S15] |
| NH4V4O10+PAC//3 M Zn(CF3SO3)2 + 0.5 M KI in EG/H2O | I−/I0 | 2.17 | 0.241 | 1.5 | 1.08 | [S16] |
| I2@AC//0.5 M ZnSO4 + 0.5 M Li2SO4 | I−/I0 | 12.9 | 0.516 | 0.806 | 1.15 | [S17] |
| CC-I2//3 m ZnSO4 + 3.5 m LiBr + 0.1 m LiNO3 | I−/I0/I+ | 0.799 | 2.22 | 1.5 | 1.4 | [S18] |
| I2@C//ZTEs | I−/I0/I+ | 10 | 0.25 |  | 1.3 | [S19] |
| PTCDI//I2 + saturated KCl | I−/I0/I+ | 2.72 | 0.057 | 80 | 1.25 | [S20] |
| I2@PAC//19 m ZnCl2 + 19 m LiCl + 8 m ACN | I−/I0/I+ | 2.436 | 3.1 | 0.8 | 1.4 | [S21] |
| I2@PAC//2 M ZnCl2 + PEG | I−/I0/I+ | 67.2 | 4.2 | 4 | 1.3 | [S22] |
| I2@AC//BAVBr | I−/I0/I+ | 19.8 | 1.65 | 3 | 1.25 | [S23] |
| IBr@CF//2 M ZnSO4 | I−/I0/I+, Br−/Br0 | 110 | 3.67 | 8.33 | 1.5 | [S24] |
| I2@AC//30 m ZnCl2 | I−/I0/I+, Cl−/Cl0 | 124.7 | 1.56 | 2.5 | 1.48 | [S25] |

Table S5 Comparisons in mass transfer capacities and interfacial reaction stability with PVDF-hfp gels, Janus separators, quasi-solid electrolytes used interphase-engineering approaches for Zn-based batteries

i) PVDF-hfp gels

| Material | σ (mS cm−1) | t (Zn2+) | ESW (V) |
| --- | --- | --- | --- |
| Zn(TFSI)2+0.1EC+ 0.9PEGDME+PVDF-hfp | 0.47 | − | >3 |
| Zn(Tf)2+ PVDF-hfp solid polymer | 0.0244 | 0.983 | 3.45 |

continuation of the previous table

| CE (%) in half-cell | Lifespan (h) in half-cell | Lifespan (h) in Zn-Zn cell | Full cell | Lifespan | Refs. |
| --- | --- | --- | --- | --- | --- |
| − | − | − | − | − | [S26] |
| − | − | 100 (0.05@0.05) | − | − | [S27] |

ii) Janus separators

| Material | σ (mS cm−1) | t (Zn2+) | ESW (V) |
| --- | --- | --- | --- |
| 3D VG on glass fiber separator | − | − | − |
| Graphene and sulfonic cellulose on glass fiber | 2.45×10−5 | 0.826 | − |
| Bacterial cellulose (BC)//AgNWs-BC | 3.83 | − | − |
| Dowex//Fe-SCNT-GF | 14.6 | 0.629 | − |
| PAZPM hydrogel | 17.0 | − | − |

continuation of the previous table

| CE (%) in half-cell | Lifespan (h) in half-cell | Lifespan (h) in Zn-Zn cell | Full cell | Lifespan | Ref. |
| --- | --- | --- | --- | --- | --- |
| − | − | 600 (10@1) | Zn−V2O5 | 5000 (5 A g−1) | [S28] |
| 99.6 | 1780 (1@1) | 1400 (10@10) | Zn−CNT-MnO2 | 1900 (1) | [S29] |
| 98.1 | >800 (1@1) | 600 (10@1) | Zn−K0.27Mn2·0.54H2O | 700 (3) | [S30] |
| 99.5 | 1000 (2@1) | 2500 (1@1) | Zn−I2-AC | 30000 (5) | [S31] |
| − | − | 3600 (0.5@0.25) | Zn−(NH4)2V10O25·8H2O | 1000 (5) | [S32] |

iii) Quasi-solid electrolytes used interphase-engineering approaches

| Material | σ (mS cm−1) | t (Zn2+) | ESW (V) |
| --- | --- | --- | --- |
| ZnSO4-PEG400 hydrogel | − | − | − |
| ZnAc2-PVA416 hydrogel | 49.8 | 0.517 | − |
| ZnAc2-PVA hydrogel | 16.5 | − | − |
| Zn(OTf)2 in cellulose gel | 38.6 | 0.73 | − |
| ZnSO4 in CS- and PASP-gels | 5.51 | − | − |
| CarraChi gel | 5.3 | 0.52 | − |
| CD-PEO/PAM hydrogel | 22.4 | 0.923 | − |
| PAM-Hbimcp-Zn hydrogel | 38.2 | − | − |
| PAAm/DMSO/Zn(Otf)2 hydrogel | − | − | − |

continuation of the previous table

| CE (%) in half-cell | Lifespan (h) in half-cell | Lifespan (h) in Zn-Zn cell | Full cell | Lifespan | Refs. |
| --- | --- | --- | --- | --- | --- |
| 99.96 | 200 (12@1) | >1500 (18@18) | Zn−MnO2 | 200 (0.07 A g−1) | [S33] |
| − | − | >4 (0.5@0.1) | Zn−PANI | 5000 (2) | [S34] |
| − | − | 1450 (0.5@0.5) | Zn−ZnHCF | 700 (0.2 A cm−2) | [S35] |
| 99.4 | 400 (5@1) | 2000 (0.5@0.5) | Zn−PANC/CC | 2000 (2) | [S36] |
| 99.6 | >800 (10@5) | 2200 (10@10) | Zn−MnO2 | 5000 (5) | [S37] |
| 99.5 | 120 (5@1) | 4000 (10@35) | Zn−ZnxV2O5 (0.9 Ah) | 200 (0.2) | [S38] |
| − | − | 180 (1@1) | Zn−La-V2O5 | 3500 (5) | [S39] |
| − | − | 500 (1@1) | Zn−V2O5 | 1000 (2) | [S40] |
| 99.5 | 1300 (2@4) | 1350 (2@4) | Zn−Zn3V2O8 | 3000 (1) | [S41] |

Supplementary References

- Measurement of thin film mechanical properties using nanoindentation. MRS Bull. 17(7), 28–33 (1992). https://doi.org/10.1557/S0883769400041634

- P.G. Bruce, J. Evans, C.A. Vincent, Conductivity and transference number measurements on polymer electrolytes. Solid State Ion. 28, 918–922 (1988). https://doi.org/10.1016/0167-2738(88)90304-9

- V. Augustyn, J. Come, M.A. Lowe, J.W. Kim, P.-L. Taberna et al., High-rate electrochemical energy storage through Li+ intercalation pseudocapacitance. Nat. Mater. 12(6), 518–522 (2013). https://doi.org/10.1038/nmat3601

- V. Augustyn, P. Simon, B. Dunn, Pseudocapacitive oxide materials for high-rate electrochemical energy storage. Energy Environ. Sci. 7(5), 1597 (2014). https://doi.org/10.1039/c3ee44164d

- T. Brezesinski, J. Wang, S.H. Tolbert, B. Dunn, Ordered mesoporous alpha-MoO3 with Iso-oriented nanocrystalline walls for thin-film pseudocapacitors. Nat. Mater. 9(2), 146–151 (2010). https://doi.org/10.1038/nmat2612

- D. Chao, C. Zhu, P. Yang, X. Xia, J. Liu et al., Array of nanosheets render ultrafast and high-capacity Na-ion storage by tunable pseudocapacitance. Nat. Commun. 7, 12122 (2016). https://doi.org/10.1038/ncomms12122

- W. Weppner, R.A. Huggins, Determination of the kinetic parameters of mixed-conducting electrodes and application to the system Li3Sb. J. Electrochem. Soc. 124(10), 1569–1578 (1977). https://doi.org/10.1149/1.2133112

- J. Wu, J.-L. Yang, B. Zhang, H.J. Fan, Immobilizing polyiodides with expanded Zn2+ channels for high-rate practical zinc-iodine battery. Adv. Energy Mater. 14(3), 2302738 (2024). https://doi.org/10.1002/aenm.202302738

- Q. Chen, S. Chen, J. Ma, S. Ding, J. Zhang, Synergic anchoring of Fe2N nanoclusters on porous carbon to enhance reversible conversion of iodine for high-temperature zinc-iodine battery. Nano Energy 117, 108897 (2023). https://doi.org/10.1016/j.nanoen.2023.108897

- J.-L. Yang, Z. Yu, J. Wu, J. Li, L. Chen et al., Hetero-polyionic hydrogels enable dendrites-free aqueous Zn-I(2) batteries with fast kinetics. Adv. Mater. 35(44), e2306531 (2023). https://doi.org/10.1002/adma.202306531

- X. Yang, H. Fan, F. Hu, S. Chen, K. Yan et al., Aqueous zinc batteries with ultra-fast redox kinetics and high iodine utilization enabled by iron single atom catalysts. Nanomicro Lett. 15(1), 126 (2023). https://doi.org/10.1007/s40820-023-01093-7

- J. He, H. Hong, S. Hu, X. Zhao, G. Qu et al., Chemisorption effect enables high-loading zinc-iodine batteries. Nano Energy 119, 109096 (2024). https://doi.org/10.1016/j.nanoen.2023.109096

- T. Li, S. Hu, C. Wang, D. Wang, M. Xu et al., Engineering fluorine-rich double protective layer on Zn anode for highly reversible aqueous zinc-ion batteries. Angew. Chem. Int. Ed. 62(51), e202314883 (2023). https://doi.org/10.1002/anie.202314883

- J. Hao, L. Yuan, Y. Zhu, X. Bai, C. Ye et al., Low-cost and non-flammable eutectic electrolytes for advanced Zn-I(2) batteries. Angew. Chem. Int. Ed. 62(39), e202310284 (2023). https://doi.org/10.1002/anie.202310284

- Z. Hu, X. Wang, W. Du, Z. Zhang, Y. Tang et al., Crowding effect-induced zinc-enriched/water-lean polymer interfacial layer toward practical Zn-iodine batteries. ACS Nano 17(22), 23207–23219 (2023). https://doi.org/10.1021/acsnano.3c10081

- Y. Yang, S. Guo, Y. Pan, B. Lu, S. Liang et al., Dual mechanism of ion (de)intercalation and iodine redox towards advanced zinc batteries. Energy Environ. Sci. 16(5), 2358–2367 (2023). https://doi.org/10.1039/D3EE00501A

- K. Wang, H. Li, Z. Xu, Y. Liu, M. Ge et al., An iodine-chemisorption binder for high-loading and shuttle-free Zn–iodine batteries. Adv. Energy Mater. 14(17), 2304110 (2024). https://doi.org/10.1002/aenm.202304110

- S. Lv, T. Fang, Z. Ding, Y. Wang, H. Jiang et al., A high-performance quasi-solid-state aqueous zinc-dual halogen battery. ACS Nano 16(12), 20389–20399 (2022). https://doi.org/10.1021/acsnano.2c06362

- W. Li, H. Xu, H. Zhang, F. Wei, T. Zhang et al., Designing ternary hydrated eutectic electrolyte capable of four-electron conversion for advanced Zn–I2 full batteries. Energy Environ. Sci. 16(10), 4502–4510 (2023). https://doi.org/10.1039/d3ee01567j

- Z. Zhang, Y. Zhu, M. Yu, Y. Jiao, Y. Huang, Development of long lifespan high-energy aqueous organic||iodine rechargeable batteries. Nat. Commun. 13(1), 6489 (2022). https://doi.org/10.1038/s41467-022-34303-8

- Y. Zou, T. Liu, Q. Du, Y. Li, H. Yi et al., A four-electron Zn-I2 aqueous battery enabled by reversible I-/I2/I+ conversion. Nat. Commun. 12(1), 170 (2021). https://doi.org/10.1038/s41467-020-20331-9

- T. Liu, C. Lei, H. Wang, J. Li, P. Jiang et al., Aqueous electrolyte with weak hydrogen bonds for four-electron zinc-iodine battery operates in a wide temperature range. Adv. Mater. 36(32), e2405473 (2024). https://doi.org/10.1002/adma.202405473

- Y. Liu, L. Zhang, L. Liu, Q. Ma, R. Wang et al., All-climate energy-dense cascade aqueous Zn-I2 batteries enabled by a polycationic hydrogel electrolyte. Adv. Mater. 2415979 (2025). https://doi.org/10.1002/adma.202415979

- S. Chen, Y. Ying, S. Wang, L. Ma, H. Huang et al., Solid interhalogen compounds with effective Br0 fixing for stable high-energy zinc batteries. Angew. Chem. Int. Ed. 62(19), e202301467 (2023). https://doi.org/10.1002/anie.202301467

- G. Liang, B. Liang, A. Chen, J. Zhu, Q. Li et al., Development of rechargeable high-energy hybrid zinc-iodine aqueous batteries exploiting reversible chlorine-based redox reaction. Nat. Commun. 14(1), 1856 (2023). https://doi.org/10.1038/s41467-023-37565-y

- H. Ye, J.J. Xu, Zinc ion conducting polymer electrolytes based on oligomeric polyether/PVDF-HFP blends. J. Power Sources 165(2), 500–508 (2007). https://doi.org/10.1016/j.jpowsour.2006.10.042

- J. Liu, Z. Khanam, R. Muchakayala, S. Song, Fabrication and characterization of Zn-ion-conducting solid polymer electrolyte films based on PVdF-HFP/Zn(Tf)2 complex system. J. Mater. Sci. Mater. Electron. 31(8), 6160–6173 (2020). https://doi.org/10.1007/s10854-020-03169-1

- C. Li, Z. Sun, T. Yang, L. Yu, N. Wei et al., Directly grown vertical graphene carpets as Janus separators toward stabilized Zn metal anodes. Adv. Mater. 32(33), e2003425 (2020). https://doi.org/10.1002/adma.202003425

- X. Zhang, J. Li, K. Qi, Y. Yang, D. Liu et al., An ion-sieving Janus separator toward planar electrodeposition for deeply rechargeable Zn-metal anodes. Adv. Mater. 34(38), 2205175 (2022). https://doi.org/10.1002/adma.202205175

- Z. Zheng, S. Guo, M. Yan, Y. Luo, F. Cao, A functional Janus Ag nanowires/bacterial cellulose separator for high-performance dendrite-free zinc anode under harsh conditions. Adv. Mater. 35(47), 2304667 (2023). https://doi.org/10.1002/adma.202304667

- Y. Kang, G. Chen, H. Hua, M. Zhang, J. Yang et al., A Janus separator based on cation exchange resin and Fe nanoparticles-decorated single-wall carbon nanotubes with triply synergistic effects for high-areal capacity Zn−I2 batteries. Angew. Chem. Int. Ed. 62(22), e202300418 (2023). https://doi.org/10.1002/anie.202300418

- K. Zhu, X. Niu, W. Xie, H. Yang, W. Jiang et al., An integrated Janus hydrogel with different hydrophilicities and gradient pore structures for high-performance zinc-ion batteries. Energy Environ. Sci. 17(12), 4126–4136 (2024). https://doi.org/10.1039/D4EE01018C

- S. Jin, Y. Deng, P. Chen, S. Hong, R. Garcia-Mendez et al., Solid-adsorbed polymer-electrolyte interphases for stabilizing metal anodes in aqueous Zn and non-aqueous Li batteries. Angew. Chem. Int. Ed. 62(18), e202300823 (2023). https://doi.org/10.1002/anie.202300823

- Y. Yan, S. Duan, B. Liu, S. Wu, Y. Alsaid et al., Tough hydrogel electrolytes for anti-freezing zinc-ion batteries. Adv. Mater. 35(18), e2211673 (2023). https://doi.org/10.1002/adma.202211673

- C. Li, W. Wang, J. Luo, W. Zhuang, J. Zhou et al., High-fluidity/high-strength dual-layer gel electrolytes enable ultra-flexible and dendrite-free fiber-shaped aqueous zinc metal battery. Adv. Mater. 36(21), e2313772 (2024). https://doi.org/10.1002/adma.202313772

- H. Zhang, X. Gan, Y. Yan, J. Zhou, A sustainable dual cross-linked cellulose hydrogel electrolyte for high-performance zinc-metal batteries. Nanomicro Lett. 16(1), 106 (2024). https://doi.org/10.1007/s40820-024-01329-0

- H. Lu, J. Hu, X. Wei, K. Zhang, X. Xiao et al., A recyclable biomass electrolyte towards green zinc-ion batteries. Nat. Commun. 14(1), 4435 (2023). https://doi.org/10.1038/s41467-023-40178-0

- F. Wang, J. Zhang, H. Lu, H. Zhu, Z. Chen et al., Production of gas-releasing electrolyte-replenishing Ah-scale zinc metal pouch cells with aqueous gel electrolyte. Nat. Commun. 14(1), 4211 (2023). https://doi.org/10.1038/s41467-023-39877-5

- H. Xia, G. Xu, X. Cao, C. Miao, H. Zhang et al., Single-ion-conducting hydrogel electrolytes based on slide-ring pseudo-polyrotaxane for ultralong-cycling flexible zinc-ion batteries. Adv. Mater. 35(36), 2301996 (2023). https://doi.org/10.1002/adma.202301996

- Z.-J. Chen, T.-Y. Shen, M.-H. Zhang, X. Xiao, H.-Q. Wang et al., Tough, anti-fatigue, self-adhesive, and anti-freezing hydrogel electrolytes for dendrite-free flexible zinc ion batteries and strain sensors. Adv. Funct. Mater. 34(26), 2314864 (2024). https://doi.org/10.1002/adfm.202314864

- H. Lu, J. Hu, L. Wang, J. Li, X. Ma et al., Multi-component crosslinked hydrogel electrolyte toward dendrite-free aqueous Zn ion batteries with high temperature adaptability. Adv. Funct. Mater. 32(19), 2112540 (2022). https://doi.org/10.1002/adfm.202112540