Supporting Information for

Regulation Engineering of Alkali Metal Interlayer Pillar in P2-type Cathode for Ultra-high Rate and Long-term Cycling Sodium-Ion Batteries

Xu Wang1, Zixiang Yang1, Yujia Cai1, Heng Ma2, Jinglei Xu2, Rabia Khatoon3, Zhizhen Ye1, Dashuai Wang4, *, Muhammad Tariq Sajjad3, *, Jianguo Lu1, *

1State Key Laboratory of Silicon and Advanced Semiconductor Materials, School of Materials Science and Engineering, Zhejiang University, Hangzhou 310058, P. R. China

2Zhejiang HuaDian Electric Equipment Testing and Research Institute Co., Ltd., Hangzhou, 311100, P. R. China

3London South Bank University,103 Borough Road, London, SE1 0AA, England

4Institute of Zhejiang University-Quzhou, Quzhou 324000, P. R. China

*Corresponding authors. E-mail: dswang@zju.edu.cn (Dashuai Wang); sajjadt@lsbu.ac.uk  (Muhammad Tariq Sajjad); lujianguo@zju.edu.cn (Jianguo Lu)

Supplementary Figures

Fig. S1 The long-term cycle performance comparison of Y0.03, Y0.05, and Y0.07 cathodes at an ultra-high rate of 20 C

To determine the optimal doping concentration of Y, a series of samples with varying Y gradient content were synthesized during the preliminary experimental stage. These included Na0.67Y0.03Ni0.2Cu0.1Mn0.67O2 (denoted as Y0.03), Na0.67Y0.05Ni0.18Cu0.1Mn0.67O2 (denoted as Y0.05), and Na0.67Y0.07Ni0.16Cu0.1Mn0.67O2 (denoted as Y0.07). As shown in Fig. S1, the Y0.05 sample exhibited the best capacity retention after 1000 cycles at a high current density. This result was used as the basis for subsequent experimental designs.

Fig. S2 XRD patterns of the four materials

Fig. S3 Rietveld refinement patterns of (a) NYNMO, (b) NNCMO, (c) NNC0.15MO, and (d) NCNYMO (putting Cu at the AM layer and the Y at the transition metal layer)

Fig. S4 SEM image of (a) NNMO, (b) NNCMO, and (c) NYNMO

Fig. S5 SAED pattern collected from [001] axis

Fig. S6 Crystal structure viewed from [210] axis (the red spheres, white spheres, violet spheres, and dark yellow spheres represent O ions, metal ions (Ni, Mn, Cu), Y ions, and Na ions, respectively)

Fig. S7 The first five cycles CVs of (a) NYNCMO, (b) NNCMO, (c) NYNMO and (d) NNMO at a scanning speed of 0.2 mV s-1

Fig. S8 Charge and discharge curves of NNMO electrode materials at different rates

Fig. S9 The comparison of cycling performances of NNMO and NYNCMO at (a) 1 C and (b) 5 C

Fig. S10 The cycling performances of NYNCMO at an ultra-high rate of 50 C

Fig. S11 Structural characterizations of electrode after deep cycling: SEM image after cycling 100 cycles at 1 C of (a) NNMO, (b) NNCMO, (c) NYNMO and (d) NYNCMO

Fig. S12 Multisweep CVs of (a) NNMO, (b) NYNMO and (c) NNCMO at various scan rates and (d-f) the corresponding cycling response of different peaks of NNMO, NYNMO and NNCMO, respectively

Fig. S13 Wavelet transform (WT) contour plots of Mn in NYNCMO-pristine, charge to 4.3 V, and discharge to 2.0 V

Fig. S14 Ex-situ X-ray photoelectron spectroscopy (XPS) of Mn high-resolution spectra analysis at different states of NYNCMO (a) Pristine; (b) Charge-4.3 V; (c) Discharge-2.0 V

Fig. S15 Ex-situ X-ray photoelectron spectroscopy (XPS) of Ni high-resolution spectra analysis at different states of NYNCMO (a) Pristine; (b) Charge-4.3 V; (c) Discharge-2.0 V

Fig. S16 Ex-situ X-ray photoelectron spectroscopy (XPS) of O high-resolution spectra analysis at different states of NYNCMO (a) Pristine; (b) Charge-4.3 V; (c) Discharge-2.0 V

Fig. S17 Ex-situ X-ray photoelectron spectroscopy (XPS) of Cu high-resolution spectra analysis at different states of NYNCMO (a) Pristine; (b) Charge-4.3 V; (c) Discharge-2.0 V

Fig. S18 Ex-situ X-ray photoelectron spectroscopy (XPS) of Y high-resolution spectra analysis at different states of NYNCMO (a) Pristine; (b) Charge-4.3 V; (c) Discharge-2.0 V

Fig. S19 Diagram of selected 8 Na sites adjacent to Y for the calculation of bond length

Fig. S20 Comparison of total energy between P2 phase and O2 phase with and without Y

Fig. S21 Specific mean square displacement performance of Na ions in (a) NNMO, (b) NNCMO, (c) NYNMO, and (d) NYNCMO

Fig. S22 Schematic diagram of Na+ diffusion trajectories in (a) NNMO and (b) NYNCMO

Fig. S23 Schematic diagram of interlayer spacing variation between NNMO and NYNCMO

Supplementary Tables

Table S1 Inductively coupled plasma optical emission spectrometry (ICP-OES) of NYNCMO

|  | Na | Y | Ni | Cu | Mn |
| --- | --- | --- | --- | --- | --- |
| NYNCMO | 0.63 | 0.04 | 0.18 | 0.10 | 0.68 |

Table S2 Crystallographic parameters of NYNCMO obtained from XRD Rietveld refinement

| Space group | P63/mmc |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| atom | site | x | y | z | Occ. |
| Naf | 2b | 0 | 0 | 0.25 | 0.33 |
| Nae | 2d | 0.3333 | 0.6667 | 0.25 | 0.33 |
| Y | 2d | 0.3333 | 0.6667 | 0.25 | 0.05 |
| Ni | 2a | 0 | 0 | 0 | 0.18 |
| Cu | 2a | 0 | 0 | 0 | 0.1 |
| Mn | 2a | 0 | 0 | 0 | 0.67 |
| O | 4f | 0.3333 | 0.6667 | 0.0945 | 1.0 |
| a=2.8933 Å | c=11.1586 Å | V=80.899 Å3 | Rw=5.769% | Gof=2.18 |  |

Table S3 Crystallographic parameters of NYNMO obtained from XRD Rietveld refinement

| Space group | P63/mmc |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| atom | site | x | y | z | Occ. |
| Naf | 2b | 0 | 0 | 0.25 | 0.33 |
| Nae | 2d | 0.3333 | 0.6667 | 0.25 | 0.33 |
| Ni | 2a | 0 | 0 | 0 | 0.28 |
| Mn | 2a | 0 | 0 | 0 | 0.67 |
| Y | 2a | 0 | 0 | 0 | 0.05 |
| O | 4f | 0.3333 | 0.6667 | 0.0945 | 1.0 |
| a=2.8854 Å | c=11.1651 Å | V=80.501 Å3 | Rw=5.897% | Gof=2.20 |  |

Table S4 Crystallographic parameters of NNC0.1MO obtained from XRD Rietveld refinement

| Space group | P63/mmc |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| atom | site | x | y | z | Occ. |
| Naf | 2b | 0 | 0 | 0.25 | 0.2820 |
| Nae | 2d | 0.3333 | 0.6667 | 0.25 | 0.3880 |
| Ni | 2a | 0 | 0 | 0 | 0.23 |
| Cu | 2a | 0 | 0 | 0 | 0.10 |
| Mn | 2a | 0 | 0 | 0 | 0.67 |
| O | 4f | 0.3333 | 0.6667 | 0.0945 | 1.0 |
| a=2.8867 Å | c=11.1907 Å | V=80.759 Å3 | Rw=6.888% | Gof=2.56 |  |

Table S5 Crystallographic parameters of NNC0.15MO obtained from XRD Rietveld refinement

| Space group | P63/mmc |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| atom | site | x | y | z | Occ. |
| Naf | 2b | 0 | 0 | 0.25 | 0.3729 |
| Nae | 2d | 0.3333 | 0.6667 | 0.25 | 0.3419 |
| Ni | 2a | 0 | 0 | 0 | 0.18 |
| Cu | 2a | 0 | 0 | 0 | 0.15 |
| Mn | 2a | 0 | 0 | 0 | 0.67 |
| O | 4f | 0.3333 | 0.6667 | 0.0945 | 1.0 |
| a=2.8882 Å | c=11.1909 Å | V=80.843 Å3 | Rw=5.233% | Gof=2.70 |  |

Table S6 The agreement factors variation after putting Cu ion at the Na sites

| Space group | P63/mmc |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| atom | site | x | y | z | Occ. |
| Naf | 2b | 0 | 0 | 0.25 | 0.33 |
| Nae | 2d | 0.3333 | 0.6667 | 0.25 | 0.33 |
| Cu1 | 2a | 0 | 0 | 0 | 0.05 |
| Ni | 2a | 0 | 0 | 0 | 0.18 |
| Mn | 2a | 0 | 0 | 0 | 0.67 |
| Cu2 | 2a | 0 | 0 | 0 | 0.05 |
| Y | 2a | 0 | 0 | 0 | 0.05 |
| O | 4f | 0.3333 | 0.6667 | 0.0945 | 1.0 |
| a=2.8753 Å | c=11.0984 Å | V=79.462 Å3 | Rw=6.875% | Gof=2.82 |  |

Table S7 Crystallographic parameters of NNMO obtained from XRD Rietveld refinement

| Space group | P63/mmc |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| atom | site | x | y | z | Occ. |
| Naf | 2b | 0 | 0 | 0.25 | 0.33 |
| Nae | 2d | 0.3333 | 0.6667 | 0.25 | 0.33 |
| Ni | 2a | 0 | 0 | 0 | 0.28 |
| Mn | 2a | 0 | 0 | 0 | 0.67 |
| O | 4f | 0.3333 | 0.6667 | 0.0945 | 1.0 |
| a=2.8713 Å | c=11.1090 Å | V=79.317 Å3 | Rw=4.988% | Gof=2.10 |  |

Table S8 Comparison of electrochemical properties between NYNCMO and other reported values in half battery

| Samples | Max Current rate (A g-1)(Rate) | Max cycle numbers |  | Retention(%) |
| --- | --- | --- | --- | --- |
| P2-Na7/9Li1/9Ni2/9Mn5/9Ti1/9O2 | 1.5 (10 C) | 200 | 88 |  |
| Na0.67Ni0.28Zn0.05Mn0.62Ti0.05O1.95F0.05 | 1.7 (10 C) | 1000 | 86 |  |
| Na0.67Ni0.23Mg0.1Mn0.65Sn0.02O2 | 1 | 500 (0.5 A g-1) | 80 |  |
| P2-Na0.8Cu0.22Li0.08Mn0.67O2 | 6.5 (50 C) | 500 (0.65 A g-1) | 86.5 |  |
| Na0.67Mn0.6Ni0.2Cu0.1Co0.1O2 | 2 (20 C) | 500 (1 A g-1) | 82.07 |  |
| Na0.72Li0.24Mn0.76O2 | 2 (10 C) | 300 (1 A g-1) | 84.28 |  |
| Na0.67Ni0.23Mg0.05Cu0.05Mn0.67O2 | 1.7 (10 C) | 2000 | 83.4 |  |
| Na0.9[Ni0.3Mn0.55Cu0.1Ti0.05]O2 | 0.75 | 600 (0.3 A g-1 ) | 83.4 |  |
| Na0.6Mn0.93Fe0.04Mg0.03O2 | 3 (10 C) | 1000 (1 A g-1) | 72.5 |  |
| Na2/3Ni1/6Mn2/3Cu1/9Mg1/18O2 | 3.6 (30 C) | 500 (1 A g-1) | 84.2 |  |
| This Work | 3.0 (20 C) | 1600 | 71.7 |  |
|  | 7.5 (50 C) | 1000 | 76 |  |
|  | 1.5 (10 C) | 3000 | 65 |  |

Table S9 Comparison of EIS fitting results of four materials

|  | NNMO | NYNMO | NNCMO | NYNCMO |
| --- | --- | --- | --- | --- |
| Rs/Ω | 4.046 | 5.584 | 7.606 | 4.001 |
| Rct/Ω | 784.7 | 342.2 | 526 | 222.8 |

Table S10 The diffusion coefficient in X, Y, Z direction and total of the four materials

| Diffusion Coefficient | X direction (cm2/s) | Y direction (cm2/s) | Z direction (cm2/s) | Average (cm2/s) |
| --- | --- | --- | --- | --- |
| NNMO | 0.7447×10-5 | 0.9563×10-5 | 0.1122×10-7 | 0.5674×10-5 |
| NYNMO | 0.9805×10-6 | 0.2905×10-5 | 0.3244×10-7 | 0.1306×10-5 |
| NNCMO | 0.6708×10-5 | 0.5618×10-5 | 0.1615×10-7 | 0.4114×10-5 |
| NYNCMO | 0.1012×10-4 | 0.2531×10-4 | 0.2299×10-7 | 0.1182×10-4 |

Table S11 The ionic mobility in X, Y, Z direction and total of the four materials

| Ionic Mobility | X direction (cm2/s/V) | Y direction (cm2/s/V) | Z direction (cm2/s/V) | Average (cm2/s/V) |
| --- | --- | --- | --- | --- |
| NNMO | 0.1235×10-3 | 0.1585×10-3 | 0.1860×10-6 | 0.9406×10-4 |
| NYNMO | 0.1625×10-4 | 0.4815×10-4 | 0.5378×10-6 | 0.2165×10-4 |
| NNCMO | 0.1112×10-3 | 0.9313×10-4 | 0.2677×10-6 | 0.6820×10-4 |
| NYNCMO | 0.1678×10-3 | 0.4196×10-3 | 0.3182×10-6 | 0.1959×10-3 |