Nano-Micro Letters

Supporting Information for
Flexible High-Aspect-Ratio COF Nanofibers: Defect-Engineered Synthesis, Superelastic Aerogels, and Uranium Extraction Applications
Binbin Fan1, Jianyong Yu2, Xueli Wang2 *, Yang Si2 *, Peixin Tang2 *

1 College of Textiles, Donghua University, Shanghai 201620, P. R. China
2 Innovation Center for Textile Science and Technology, Donghua University, Shanghai 201620, P. R. China

*Corresponding authors. E-mail: wxl@dhu.edu.cn (Xueli Wang); yangsi@dhu.edu.cn (Yang Si); pxtang@dhu.edu.cn (Peixin Tang)
S1 Supplementary Methods
Materials. Uranyl nitrate hexahydrate (99%, MACKLIN), bacterial cellulose nanofibers dispersion (BCN, 0.8 wt%, Qihong, Guilin, Guangxi, China), sodium hydroxide (96%, Collins), hydrochloric acid (CP, SCR), uranium standard solution (Beijing Century Oko Biotechnology Co., Ltd., China), cupric chloride anhydrous (CuCl2, 98%, Adamas-bata), zinc nitrate hexahydrate (Zn(NO3)2·6H2O, AR, SCR), iron (III) nitrate nonahydrate (Fe(NO3)3·9H2O, 98.5%, MACKLIN), nickel (II) acetate tetrahydrate (Ni(OCOCH3)2·4H2O, 99%, Infinity Scientific), ammonium metavanadate (NH4VO3, 99%, MERYER), cobaltous nitrate hexahydrate (Co(NO3)2·6H2O, 99%, RHAWN), lead(II) nitrate (Pb(NO3)2, 99%, AR, SCR). All chemicals are directly used as received. 
Characterizations. Attenuated total reflection spectroscopy (ATR) was acquired by a Nicolet TM iS50 spectrometer (Thermo Fisher Scientific). The transmittance mode was used, and the data were collected in the wavenumbers of 400~4000 cm-1 with a resolution of 2 cm-1. 13C SSNMR was acquired from a Bruker AVANCE NEO 400M (German) spectrometer utilizing TMS (0 ppm) as a reference, and the spectra were processed using the MestReNova software. Atomic force microscopy (AFM) was performed on Bruker Dimension Icon (German), and all the original data were processed using the NanoScope Analysis 3.00 software. Thermogravimetric analysis (TGA) was performed on a TGA2 (Mettler-Toledo) instrument. Firstly, the sample (~5 mg) was heated to 100oC and held for 1 min to remove any free water. Then, the system was cooled to room temperature under N2 atmosphere and reheated to 700 oC with a heating rate and N2 flow rate of 20oC min-1 and 50 mL min-1, respectively. The samples were coated with a thin layer of gold before scanning electron microscope (SEM) monitoring. The SEM images of the materials were captured on an SU8010 (Hitachi, Japan). Transmission electron microscope (TEM, JEM-2100F) was operated at a voltage of 200 kV. X-ray diffraction (XRD) was acquired by SmartLab SE (Rigaku, Japan). The sample was scanned at a scanning rate of 3o min-1 from 3o to 80o with a test target of cuprum. N2 sorption isotherm was obtained from a physisorption system of BSD-660 (Beishide Instrument-S&T. (Beijing) Co., Ltd.) at 77 K. The samples were degassed at 100ºC for 5h before testing. The BET surface areas were acquired based on BET theory. The pore volumes were obtained according to the Barrett-Joyner-Halenda (BJH) model. An ultraviolet-visible spectrophotometer (UV-Vis) of UV3600 (SHIMADZU, Japan) was used to collect the adsorption spectra of materials in the wavelengths of 200~1000 nm. All the light sources are standard (Halogen Tungsten Lamp (Model 64604), Deuterium lamp (Model L6380)) and the lights are in their working life-span (<2000 h). Inductively coupled plasma emission spectrometer-atomic emission spectrometer (ICP-OES) was performed on Prodigy Plus (Teledyne Leeman Labs, USA).
Fabrication of COF-A. BCNs and COF particles were homogenized under ultrasonication for 10 min. Then, the suspension of BCN/COF particle was shaped into nanofibrous aerogels (COF-As) via liquid N2 freezing and lyophilization. Citric acid (CA) was used as the crosslinking agent for enhancing the structural stability of aerogels. By heating the aerogels under 160oC for 30 min, esterification reactions occurred between CA and BCNs, thus inhibiting the re-dispersion of BCNs in water during practical applications. Given the combined interaction of hydrogen bonding and ester bond crosslinking, COF-A with 90.91wt% COF loading was fabricated.
Compression Tests of CNF-A. The compression tests were performed on an Exceed Model E42 (MTS Systems Co., Shanghai, China) with a constant compression rate of 60.00 mm min-1. The samples for compression tests were in a cylinder shape with a diameter of 2 cm and a height of 2.5 cm. The compression cycle test was performed for 500 cycles in distilled water at a maximum strain of 50%.
Adsorption of CNF-A. The U adsorption performance was first conducted by dissolving a specific amount of uranyl nitrate (UO2(NO3)2) in distilled water (initial concentration=128 ppm, pH=4). In each specific adsorption test, 25 mg of the adsorbent was added to 200 mL of U-spiked distilled water. Then, the reaction systems were irradiated by visible light (405 nm, 300 mW cm-2) in a crosslinking box (UVGO, China). The distance between sample and lamps was controlled as 8.0 cm. Adsorption selectivity examination was performed in metal ion-spiked distilled water. UO22+ and competitive metal ions (V5+, Fe3+, Zn2+, Cu2+, Ni2+, Pb2+, Co2+), whose concentrations are 100 times higher than their actual concentration in natural seawater, were dissolved in distilled water. Then, 100 mg of CNF-A adsorbent was added to the mixture solution (1.0 L) to perform the competitive adsorption assay. After 24 h of the adsorption under visible light irradiation, the CNF-A was taken out and then dried at 60℃ under a vacuum for 12 h. Additionally, the U adsorption performance in natural seawater (5.0 L) was conducted using 5 mg of CNF-A adsorbent. The natural seawater was collected from Laoshan (Qingdao, China). After 24 h of the adsorption under visible light irradiation, the CNF-A adsorbent was taken out and then dried at 60℃ under vacuum for 12 h. The mass content of the adsorbed metal ions in CNF-A was analyzed by ICP-OES after microwave digestion.
Computational Simulations. Calculations including ground state structure optimization and frequency calculations based on density functional theory (DFT) were performed with Gaussian 09 at unrestricted DFT-B3LYP/6-31G(d,p), nosymm level of theory under gas phase (i.e., no solvent system model was applied). No imaginary frequency was found in the frequency calculation results, indicating all the optimized geometries are at their minimal energy states. The optimized geometries of the interested compounds and composites were obtained and viewed by GaussView 5.0.
S2 Supplementary Figures
[image: image1.png]DAAQ

™

CNF




Fig. S1 Synthesis reaction and chemical structure of CNF synthesized by DAAQ and TP
[image: image2.png]



Fig. S2 AFM image of an individual CNF
[image: image3.png]Intensity (a.u.)

T T T T T
4000 3500 3000 2500 2000 1500

0

C=0 (1618 cm™)

lf c-N (1252 cm™)

T T
1000 500

Wavenumber (cm™)

—TP

T T T T T T
50 100 150 200 250 300 350 400 450 500 550 600 650 70|
Temperature (°C)

N
w-f\/\yvﬂnlj"v.«m‘

. J
W

zj\

Yoo
e

§ou

~ L W«'»\ A r("\m,»“ﬂM‘UﬂW\*"\A o

20 230 230 210 200 150 130 170 180 150 140 130 130 o 100 o 80 70 61 S 40 3 20 10

Chamical shift (pom)

499.58 °C

TP
DAAQ
CNF

445.05°C

234.70°C Y
] I

T
50 1

00 150 200 250 300 350 400 450 500 550 600 650 700

Temperature (°C)





Fig. S3 a ATR-FTIR spectra of TP, DAAQ and CNF. b 13C SSNMR of CNF. The inserted photograph shows the optical image of CNFs. c The TGA and d DTG curves of TP, DAAQ, and CNF
[image: image4.png]



Fig. S4 SEM images of the CNF synthesized at different time points
[image: image5.png]80

40

30
Reaction time (h)

(%) Ayuneyshan

20 (degree)

(‘n-e) Ajisuajuj





Fig. S5 a XRD spectra, and b calculated crystallinity of the CNF synthesized at different time points
[image: image6.png],

d)

g)

‘“\

M/BA =5/0

M/BA =1/1

M/BA =0/5

DAAQ

DAAQ

DAAQ

50um

50um

50pum

e)
F

M/BA =4/1

=

M/BA =2/3

DAAQ

DAAQ

50pum

M/BA =3/2
e/

3

f). .

M/BA =1/4

O
>
>
e

A < . sy
[ 4
50pum
I
DAAQ o
3
L]
V.
50pum
—




Fig. S6 a-g Microscope photos of DAAQ in different M/BA systems under ultrasonication for 30 min and stirring 60 min. h The DAAQ particle sizes and i HSP data of DAAQ in different M/BA systems
[image: image7.png]Concentration (mM)

] : i\

°] — .
8 - .ii
-
6 ‘k —m—CNF
5] —o—TP
4 —A—DAAQ

1 @

3_

] A
2- f -

- - e

i o
0ol m 4

(IJ 1I0 2I0 3IO l 4I0 . 5IO GIO l 7I0

Reaction time (h)

.

k,: 0.09 mM" h”!

m CNF
e TP
A DAAQ

ky: -0.15 mM™ h!

ky: -0.23 mM! h*!

2 4 6 8 10 12
Reaction time (h)





Fig. S7 a Correlation between the concentration changes of TP, DAAQ, and CNFs in the synthesis system and reaction time. b Second-order kinetics of TP and DAAQ consumption and CNF formation
[image: image8.png]100% Acetic acid “12M"Acetic acid

f)

—— 12M Acetic acid

—— 6M Acetic acid

Intensity (a.u.)

—— 3M Acetic acid

—— 1M Acetic acid

6
26 (degree)





Fig. S8 a-e SEM images and f XRD spectra of the CNF synthesized with different concentrations of catalyst
[image: image9.png]M/BA =4/1

o

5pm

M/BA=1/1 |

—— MiBA=SI0

MiBA=4/1

MWBA=32

mBA=1/1

——WBA=23

6 7
26 {degree)





Fig. S9 a-g SEM images and h XRD spectra of the CNF synthesized in different solvent systems
[image: image10.png]A~

[——100% Acetic acid M/BA=5/0

—— 12M Acetic acid —— M/BA=411

—— 6M Acetic acid

—3M Acetic acid —— M/BA=1/1

Intensity (a.u.)

Intensity (a.u.)

— 1M Acetic acid — M/BA=213

—— M/BA=1/4
€=0 (1618 cm")

c=0 (1618 cm) | i/ e (1252 cm) i if N (12520m") c

T T T T L T T T T T T T T T T T T T T T T
4000 3500 3000 2500 2000 1500 1000 500 3500 3000 2500 2000 1500 1000 500) 4000 3500 3000 2500 2000 1500 1000 500

0 (1613 ¢ (1252 cm

Wavenumber (cm™) Wavenumber (cm™) Wavenumber (cm™)





Fig. S10 The ATR spectra of CNFs synthesized a at different time points, b with different concentrations of catalysts, and c in different solvent systems
[image: image11.png]aH
8H
10H
12H
——24H
———48H
——72H

—72H i
1750218 °C
m_/\/_v_
50034 °C
?mq\’\/—
!_~a98.66°0

—12H i
|_~ar00°c

425.49°C

50 100 150 200 250 300 350 400 450 500 550 600 650 700

Temperature (°C)

100% Acetic acid
12M Acetic acid
6M Acatic acid
3M Acatic acld
1M Acetic acid

50 100 150 200 250 300 350 400 450 500 550 600 650 700)

Temperature (°C)

[—— 1M Acetic acid

|——3M Acetic acid

500.34 °C|

—6M Acetic acid

|—— 12M Acetic acid
498.66 °C

[—— 100% Acetic acid
497.90°C

T T T T T T T T T T
50 100 150 200 250 300 350 400 450 500 550 600 650 700
Temperature (°C)

DTG

T T T T T T T T T T T
50 100 150 200 250 300 350 400 450 500 550 600 650 700

Temperature (°C)

i
|—— M/BA=0/5 1
B,
34713 < ll 291.94°C
[ mBA=1/4 R B
380.43°C N\, i
7 495.30°C

[—— M/BA=2/3 415.26 °C i
S 499.58°C
——M/BA=312 " i
- 416.94°C 3

|—— m/BA=4/1

425.49°C

[— miBA=510 415.26°C

T T T T T T T T T T T T
50 100 150 200 250 300 350 400 450 500 550 600 650 700

Temperature (°C)

T T T T T T T T T T T T
50 100 150 200 250 300 350 400 450 500 550 600 650 700

Temperature (°C)





Fig. S11 The TGA and DTG curves of CNFs synthesized a, b at different time points, c, d with different concentrations of catalysts, and e, f in different solvent systems
[image: image12.png]Intensity (a.u.)

(100)

Experimental
—— AB Stacking

(110) (220) —— AA stacking





Fig. S12 Experimental and simulated XRD spectra of the CNF
[image: image13.png]AG=-970.68 kJ mol™ AG=-44.67 kJ mol!

R e
HQ
s . - . .
AG=118.84 kJ mol! e o'\' AG=-39.40 kJ mol!
. . f‘\ .

.
. .

Q.O . - °o\ N

.
.




Fig. S13 Reversed Schiff based reaction triggered by BA
[image: image14.png]N I . . . .
( AG=-970.68 kJ mol'! O \‘ AG=-6.94 kJ mol™*
. . .
. .
. . .

AG= 85.98 kJ mol* AG= -24.59 kJ mol !

e % . .

e .

. e
O . .
. B
O . . . N

.




Fig. S14 Reversed Schiff based reaction triggered by MA
[image: image15.png].

\7/CH3

. e . s .
AG=-970.68 kJ mol! AG=-9.58 kJ mol”
R . .
e
e e N .
. . . .
AG=89.07 kJ mol” AG=-40.97 kJ mol”
R R
. e

s .
N .
-

I

.




Fig. S15 Reversed Schiff based reaction triggered by IPA
[image: image16.png]AG= -12.14 kJ mol!
.

O AG=-970.68 kJ mol !
e N

AG=78.22 kJ mol! AG= -38.52 kJ mol!
. % e ’

.

.




Fig. S16 Reversed Schiff based reaction triggered by CA
[image: image17.png]



Fig. S17 TEM image of CNF with misaligned overlapping COF grains
[image: image18.png]Crystalline





Fig. S18 HR-TEM images CNF containing grains with different orientations and crystalline/amorphous distinct regions
[image: image19.png]DMT Modulus (GPa)

Average Elastic Modulus
4.90 £ 0.75 GPa

o -

50

T T T
100 150 200
Distance (nm)

T T
250 300




Fig. S19 The distribution of elastic modulus along three different spots in an individual CNF
[image: image20.png]



Fig. S20 FEA simulation of the extension side of the CNF under dynamic bending
[image: image21.png]



Fig. S21 a The optical image of CNF-M with good flexibility. B-c SEM images of the cross-section of CNF-M and the binding points between CNFs caused by photoinduced crosslinking
[image: image22.png]d)

AN
S S
N





Fig. S22 Photographs of the large-size CNF-As in size of a, b 140 mm×15 mm (D×H), and c, d 55 mm×60 mm (D×H)
[image: image23.png]Binding point

1 um





Fig. S23 The photograph and SEM image of the cross-section of the laminated CNF-A under different magnifications. The binding point between CNFs is attributed to the photoinduced chemical crosslinking
[image: image24.png]Binding point

1 pm




Fig. S24 The photograph and SEM images of the cross-section of the isotropic CNF-A under different magnifications. The binding point between CNFs is attributed to the photoinduced chemical crosslinking
[image: image25.png]N
.
o

Crosslinking Pathway:
.




Fig. S25 The photoinduced chemical crosslinking reaction of CNFs [S1]
[image: image26.png]Q

N’

Compressive stress (KPa)

g
o

g
=)
1

-
(3,
1

-
o
1

[
[5,]
I

g
o
1

Compressive strain (%)

60

b) 3.0 1

Compressive stress (KPa)
- - N N
) o o 2
1 1 1 1

e
o
1

o
o
Il

XX
J
X
X
- 5 10 30 60

Irradiation time (min)

3min

5minw

'~10min

30min %Omin





Fig. S26 a The stress-strain curves (ε=50%) b maximum stress at ε=50%, and c the photographs of CNF-As after compression in a dry condition with different irradiation times during photo-crosslinking. The original height of the CNF-As were 20 mm. √ indicates that CNF-A maintains structural integrity after compression. X denotes the formation of minor cracks or presence of slight deformation after compression. XX refers to the formation of large cracks or presence of sever deformation after compression.
[image: image27.png]N Py IS -

Compressive stress (KPa)

05 1.0 20
Concentration of MSB (%)





Fig. S27 Compression stress of CNF-As with different MSB concentrations. The irradiation time was set as 10 min. √ indicates that CNF-A maintains structural integrity after compression. X denotes the formation of minor cracks or presence of slight deformation after compression. XX refers to the formation of large cracks or presence of sever deformation after compression.
[image: image28.png]a) b)
300 pm 300 pm
) d)
LT 300 pm
€)

300 pum





Fig. S28 SEM and ImageJ converted images of CNF-As with different MSB concentrations: a 0%, b 0.5%, c 1.0%, d 2.0%, and e 3.0%. Irradiation time=10 min. No big difference in porosity of CNF-As was noticed when varying the MSB concentration from 0~3.0%. Considering the crosslinking efficiency and economy, 1.0% of MSB was set as the optimal condition
[image: image29.png]a)

Gl

e)





Fig. S29 SEM and ImageJ converted images of CNF-As with different irradiation times during photo-crosslinking: a 0 min, b 3 min, c 5 min, d 10 min, e 30 min, and f 60 min. MSB concentration=1.0%. Slightly decrease in porosity of CNF-As by ~2% was noticed when varying the irradiation time from 0~60 min. Irradiation time of 10 min achieved the optimal relationship between mechanical properties and porosity.
[image: image30.png]



Fig. S30 The photographs of CNF-A, which can be folded and recovered without forming any cracks
[image: image31.png]Dry CNF-A





Fig. S31 Photographs of CNF-A a in a dry phase and b-h structural stability in water with different immersion durations. I UV-vis spectra of CNF-A suspension, and the solution after immersion for 180 days. The CNF suspension presented a broad adsorption at 250-600 nm, while no such adsorption was found in the solution after CNF-A immersion for 180 days.
[image: image32.png]Compressive stress (KPa)

0
~

Compressive stress (KPa)

Sample 1

T T T T
1000 2000 3000 4000
Time (s)

T T T
5000 6000 7000

-
=)
1

]
1

o
1

IS
1

N
1

Sample 3

T T T T
1000 2000 3000 4000
Time (s)

T T T
5000 6000 7000

=3
~
-
=)

L

Compressive stress (KPa)

o
~—

Compressive stress (KPa)

Sample 2

0

T T T T T
1000 2000 3000 4000 5000
Time (s)

T T
6000 7000

a2 o
® © o =
1 1 1

~
1

o
1

54

-

H

Sample 1

Sample 2

Sample 3

Average





Fig. S32 a-c Stress-time compression curves of different CNF-A samples for 500 cycles in water. D Averaged compressive stresses of CNF-As
[image: image33.png]Adsorbed Capacity (cm?/g) STP

8

8

s 2
3 2 8

N
3

°

— COF-P

—e— CNF
—*—CNF-A —A— COF-

T o a e A S

Joiiis
'f
;

o

—o-a-g-94-47 39:9:3‘9‘. ]
_aﬁ»“""*—::::*/





Fig. S33 The N2 sorption isotherms of different materials at 77 K. CNF and CNF-A both exhibited a type I/II character with sharp adsorption at lower (P/P0 < 0.1) and higher (P/P0 > 0.9) partial pressures, indicating the presence of micropores and mesopores in their structures. The presence of hysteresis loop also described specific adsorption behavior of a mesoporous material.
[image: image34.png]



Fig. S34 The SEM images of a-c longitudinal-section and d-f cross-section of COF-A. The inserted photographs display the optical image of COF-A
[image: image35.png])

dV/dD/(cm?/g/nm)

0.007 4

0.006

0.005 4

0.004 4

0.003 4

0.002 4

0.001 4

0.000

_»206nm
L ]

—=— COF-P

O
IS

Diameter (nm)

dv/dD/(cm?/g/nm)

e o o
[=J =3 =3
B 2] <«
1 ! !

0.02

0.00

—=—CNF
—e—CNF-A

T
8 16
Diameter (nm)





Fig. S35 The pore size distribution of different materials
[image: image36.png])

Potential vs. NHE

1.2
09
06

&

0.0
03
06
09
12
15
18
24

HOMO
e 0,-0,
L U0,21U0,
Eg=1.94 eV
Lumo
________________ OHIOH





Fig. S36 Schematic illustration of the mechanism of photocatalytic reduction of UO22+ to UO2 by CNF-A
The photoexcitation of the benzophenone moiety in the CNFs is essential to the reduction of U(VI) to U(IV). The benzophenone moiety exhibits strong absorption in the ultraviolet (UV) to visible light range due to its conjugated π-system and carbonyl group. According to reported literature [S2, S3, S39], electrons occupying the HOMO orbital, which is the n electrons in the carbonyl group of benzophenone, are promoted into the antibonding π* orbitals (LUMO) in the conjugated benzophenone ring. When excited-state electrons return from the LUMO orbital to the HOMO (i.e., the excited state of CNF returns to its ground state), they can be captured by surrounding U(VI) ions because of the energy matching between the HOMO/LUMO levels of CNFs and the redox potential of UO22+/UO2. This process realizes the reduction reaction of U(VI) to U(IV) by the benzophenone group in CNFs.
[image: image37.png]900
) b)
. 800
@ >
o o
E 20 2o
2 2 600
H 8
8 150 2 500
g g
8 8
5 g
g B30
s s
i 3
-2 Z200
2 > 100
o

Light Dark

Different condition




Fig. S37 a The adsorption amount of CNF-A from U-spiked distilled water (initial concentration=32 ppm) with different Ph. B Adsorption amount of U from U-spiked distilled water under visible light irradiation and dark incubation (initial concentration=128 ppm)
[image: image38.png]— 1000 -

{ —=—coFp
| —e—coF-a

650

__ 600

COF-P
COF-A

3 3 "o 550
g’soo-
"2 450
>
‘S 400
2 350
< ]
© 300
[ J
.O 250 -
) -
£ 200 -
8 J
45 150
< 100 -
D 4

CNF
CNF-A

4 > o n

k,: 68.39mg g’ h"

k;: 51.58 mg g h™!

U Adsorption capacity (mg g'1

k,: 37.94mg g’ h" ;
k.:29.16 mgg” h™

(] 10 20 30 40 50 60 70 80 0 1 2 3 4
Exposure time (h) Exposure time (h)





Fig. S38 a U absorption amounts versus time of different materials. b Initial adsorption rate of different materials
[image: image39.png]v v [ Fe [ zn [ cu B Ni @ Py [ co

10
©

3% & 5 32
(,.6 Bu) axeydn suoi [e3oly

CNF CNF-A
Different adsorbent materials

COF-A

COF-P




Fig. S39 Adsorption amount of competitive metal ions in distilled water by different materials under visible light irradiation for 24 h
[image: image40.png]3.88-fold

Cu Ni
Metal ions

Zn

@





Fig. S40 Adsorption amount of U and competitive metal ions by CNF-A in natural seawater after 15 days
[image: image41.png]600
50

0

H

=
>
£
g
S
g
4
g
5
M
§
B
5
b
2
s

2

3 )
Cyele number

@




Fig. S41 U adsorption amount (initial concentration=128 ppm) and elution efficiency in six successive adsorption-desorption cycles under visible light irradiation by CNF-As
S3 Supplementary Tables
Table S1 Size characteristics of previously reported fiber-shaped COFs
	Labels
	Materials
	Length (nm)
	L/D ratio
	Refs.

	1
	CPPs
	515
	5.72
	[S4]

	2
	TPT-DAHQ COF
	7400
	7.40
	[S5]

	3
	TfBD
	5000
	62.50
	[S6]

	4
	MF-COF-1
	2500
	35.71
	[S7]

	5
	TAPB-BTCA 12C
	20000
	66.70
	[S8]

	6
	N3-COF100
	2000
	40.00
	[S9]

	7
	COF-300
	10000
	2.00
	[S10]

	8
	COF-300
	20000
	1.54
	[S10]

	9
	COF-300
	60000
	3.00
	[S10]

	10
	LZU-79
	100000
	12.50
	[S10]

	11
	LZU-111
	50000
	1.00
	[S10]

	/
	CNF
	22670
	103.05
	This work


Table S2 The HSP values and the product yields of CNF obtained from different solvent systems
	Solvent system (v/v)
	δD
	δP
	δH
	HSP distance to DAAQ
	HSP distance to TP
	HSP distance to COF
	Yield

	M/BA 5/0
	18.00
	0.60
	0.60
	19.95
	26.01
	22.91
	48.60%

	M/BA 4/1
	18.08
	1.74
	3.22
	17.58
	23.43
	20.41
	72.11%

	M/BA 3/2
	18.16
	2.88
	5.84
	15.38
	20.92
	18.02
	85.92%

	M/BA 1/1
	18.20
	3.45
	7.15
	14.37
	19.70
	16.88
	94.11%

	M/BA 2/3
	18.24
	4.02
	8.46
	13.44
	18.51
	15.79
	89.51%

	M/BA 1/4
	18.32
	5.16
	11.08
	11.87
	16.25
	13.79
	82.53%

	M/BA 0/5
	18.40
	6.30
	13.70
	10.84
	14.22
	12.14
	57.75%

	M/MA 3/2
	16.68
	5.28
	9.28
	14.32
	20.27
	16.68
	82.45%

	M/IPA 2/3
	16.68
	3.90
	10.08
	15.09
	20.65
	17.24
	86.15%

	M/CA 2/3
	18.66
	3.84
	8.04
	13.28
	20.80
	16.58
	76.27%


Table S3 ΔG for each step of the alcohol-triggered reverse Schiff base reaction
	Alcohols
	Step 1 
(kJ mol-1)
	Step 2 
(kJ mol-1)
	Step 3 
(kJ mol-1)
	Step 4 
(kJ mol-1)

	BA
	-940.68
	-44.67
	118.84
	-39.40

	MA
	-940.68
	-6.94
	85.98
	-24.60

	IPA
	-940.68
	-9.58
	89.07
	-40.97

	CA
	-940.68
	-12.14
	78.22
	-38.52


Table S4 Elastic modulus of natural and synthetic fibers

	Fibers
	Elastic modulus (GPa)
	Refs.

	CNF
	3.50~5.50
	This work

	Cotton
	5.00~12.00
	[S11]

	Wool
	3.20~4.50
	[S12]

	Silk
	8.90~17.40
	[S13]

	PET
	1.07~2.50
	[S14]

	Nylon
	1.30~1.70
	[S15]

	PAN nanofiber
	1.10~3.50
	[S16]

	PTFE nanofiber
	0.17~1.42
	[S17]

	PP fiber
	14.70~19.00
	[S18]


Table S5 The original data of U adsorption amount by COF-P, COF-A, CNF, and CNF-A under visible light irradiation for 24 h
	Materials
	U Adsorption capacity (mg g-1)
(Initial conc.=128 ppm)
	Average value (mg g-1)
	SE

	COF-P
	45.02
	50.60
	71.18
	55.60
	13.78

	COF-A
	78.96
	68.05
	88.49
	78.50
	10.23

	CNF
	496.05
	471.17
	483.52
	483.58
	12.44

	CNF-A
	919.09
	930.47
	909.96
	920.12
	6.55

	
	919.97
	923.05
	915.88
	
	

	
	921.54
	926.68
	917.04
	
	

	
	912.33
	915.47
	929.96
	
	


Table S6 Performances of reported materials for UES

	Labels
	Materials
	U Adsorption 
capacity
(mg g-1)
	Initial
concentration
(ppm)
	Solution system
	Refs.

	a
	MITpBD
	800.20
	150
	U-spiked seawater
	[S19]

	b
	UiO-66-3C4N
	654.99
	128 
	U-spiked simulated seawater
	[S20]

	c
	Ti3C2-AO-PA
	108.50
	100
	U-spiked deionized water
	[S21]

	d
	PAF-170-AO
	702.00
	85 
	U-spiked simulated seawater
	[S22]

	e
	SA-DNA
	189.50
	60 
	U-spiked simulated seawater
	[S23]

	f
	COF-R5
	253.70
	50 
	U-spiked seawater
	[S24]

	g
	CMCS/P(AO-co-AM-Cu)
	962.40
	32 
	U-spiked seawater
	[S25]

	h
	PAO/Alg NF
	803.77
	32 
	U-spiked seawater
	[S26]

	i
	AO-PIM-1
	345.94
	32 
	U-spiked water
	[S27]

	j
	DNA-UEH
	16.15
	16
	U-spiked simulated seawater
	[S28]

	k
	PPH-OP
	139.47
	16 
	U-spiked simulated seawater
	[S29]

	l
	TPM
	933.32
	450 
	U-spiked deionized water
	[S30]

	m
	g-C3N4/GO
	322.00
	80 
	U-spiked deionized water
	[S31]

	n
	PAO@MXene
	639.98
	60 
	U-spiked deionized water
	[S32]

	o
	CPP
	541.20
	35 
	U-spiked filtered natural seawater
	[S33]

	p
	Anti-GO-BPG-GLACS
	599.00
	32 
	U-spiked water
	[S34]

	q
	TTh-COF-AO
	682.10
	20 
	U-spiked seawater
	[S35]

	r
	PGM-1
	443.20
	20 
	U-spiked deionized water
	[S36]

	s
	COF-4P
	449.30
	20 
	U-spiked seawater
	[S37]

	t
	COF 2-Ru-AO
	382.00
	19
	U-spiked seawater
	[S38]

	u
	MOF/BPQD
	472.90
	16 
	U-spiked simulated seawater
	[S39]

	v
	Zr/Ti-MOF-25
	438.80
	16 
	U-spiked simulated seawater
	[S40]

	w
	LB-COF
	320.00
	8 
	U-spiked water
	[S41]

	/
	CNF-A
	920.12
	128 
	U-spiked deionized water
	This work


Table S7 The original data of adsorption amount of competitive metal ions under visible light irradiation for 24 h
	Metal ions
	Initial concentration (ppb)
	Adsorption amount (mg g-1)
	SE
	Kd
(×104 mL g-1)

	U
	330
	30.36
	0.62
	4.530

	V
	200
	13.12
	0.60
	0.015

	Fe
	300
	6.89
	0.35
	0.003

	Zn
	400
	2.39
	0.14
	0.001

	Cu
	60
	0.55
	0.05
	0.004

	Ni
	100
	0.45
	0.06
	0.001

	Pb
	3
	0.34
	0.04
	0.283

	Co
	5
	0.18
	0.04
	0.005


Note: Kd is the selective coefficient calculated based on the equation Kd=(Cadsorbent)/(Csolution).
Table S8 The original data of U adsorption amount and elution efficiency in a 6 successive adsorption-desorption cycles under visible light irradiation
	Cycle number
	U adsorption capacity (mg g-1)
(Initial conc.=128 ppm)
	Average (mg g-1)
	SE

	1
	900.40
	922.03
	934.66
	919.03
	17.33

	2
	882.71
	915.09
	904.85
	900.88
	16.55

	3
	901.01
	891.89
	867.14
	886.68
	17.53

	4
	826.93
	860.54
	839.11
	842.19
	17.02

	5
	843.98
	830.28
	810.58
	828.28
	16.79

	6
	819.56
	829.41
	797.71
	815.56
	16.22

	Cycle number
	U elution efficiency (%)
	Average (%)
	SE

	1
	103.17
	95.57
	99.93
	99.56
	3.81

	2
	95.7
	99.56
	101.68
	98.98
	3.03

	3
	97.01
	102.59
	92.93
	97.51
	4.85

	4
	88.86
	92.61
	98.33
	93.27
	4.77

	5
	90.02
	94.41
	85.63
	90.02
	4.39

	6
	83.1
	92.16
	87.36
	87.54
	4.53


Table S9 The comprehensive performances of COF-based aerogels used for UES
	Aerogels
	U Adsorption 
capacity (mg g-1)
	Kd 
(×104 mL g-1）
	COF content (%)
	SBET (m2 g-1)
	U adsorption rate (%)
	Refs.

	CNF-A
	920.12
	4.53
	100.00
	396.15
	89.83
	This work

	TpTHA/CNF
	177.90
	1.90
	34.00
	28.15
	74.13
	S42

	BCCOF-SO3NH4
	883.44
	7.00
	42.60
	70.77
	86.42
	S43

	BHMS3
	402.30
	0.02
	23.08
	634.00
	11.50
	S44

	PCA10.0
	361.40
	0.45
	90.91
	188.27
	61.61
	S45


Note: Kd is the selective coefficient calculated based on the equation Kd=(Cadsorbent)/(Csolution).

Supplementary References
[S1] J. Zou, A. O. Sbodio, B. Blanco-Ulate, L. Wang, G. Sun, Novel Robust, Reusable, Microbial-Resistant, and Compostable Protein-Based Cooling Media. Adv. Funct. Mater. 32(26), 2201347 (2022). https://doi.org/10.1002/adfm.202201347 
[S2] Z. Zhang, Y. Si, G. Sun, Photoactivities of Vitamin K Derivatives and Potential Applications as Daylight-Activated Antimicrobial Agents. ACS Sustain. Chem. Eng. 7(22), 18493-18504 (2019). https://doi.org/10.1021/acssuschemeng.9b04449 
[S3] Y. Si, Z. Zhang, W. Wu, Q. Fu, K. Huang et al., Daylight-driven rechargeable antibacterial and antiviral nanofibrous membranes for bioprotective applications, Sci. Adv. 4(3), eaar5931 (2018). https://doi.org/10.1126/sciadv.aar5931 
[S4] A. Halder, S. Kandambeth, B. P. Biswal, G. Kaur, N. C. Roy et al., Decoding the Morphological Diversity in Two Dimensional Crystalline Porous Polymers by Core Planarity Modulation. Angew. Chem. Int. Ed. 55(27), 7806-7810 (2016). https://doi.org/10.1002/anie.201600087 
[S5] A. F. M. El-Mahdy, Y. Hung, T. H. Mansoure, H. Yu, T. Chen et al., A Hollow Microtubular Triazine- and Benzobisoxazole-Based Covalent Organic Framework Presenting Sponge-Like Shells that Functions as a High-Performance Supercapacitor. Chem. Asian J. 14(9), 1429-1435 (2019). https://doi.org/10.1002/asia.201900296 
[S6] W. Kong, W. Jia, R. Wang, Y. Gong, C. Wang et al., Amorphous-to-crystalline transformation toward controllable synthesis of fibrous covalent organic frameworks enabling promotion of proton transport. Chem. Commun. 55(1), 75-78 (2019). https://doi.org/10.1039/c8cc08590k 
[S7] D. Rodríguez-San-Miguel, A. Abrishamkar, J. A. R. Navarro, R. Rodriguez-Trujillo, D. B. Amabilino et al., Crystalline fibres of a covalent organic framework through bottom-up microfluidic synthesis. Chem. Commun. 52(59), 9212-9215 (2016). https://doi.org/10.1039/c6cc04013f 
[S8] S. Wang, Z. Zhang, H. Zhang, A. G. Rajan, N. Xu et al., Reversible Polycondensation-Termination Growth of Covalent-Organic-Framework Spheres, Fibers, and Films. Matter 1(6), 1592-1605 (2019). https://doi.org/10.1016/j.matt.2019.08.019 
[S9] X. Ma, K. R. Meihaus, Y. Yang, Y. Zheng, F. Cui et al., Photocatalytic Extraction of Uranium from Seawater Using Covalent Organic Framework Nanowires. J. Am. Chem. Soc. 146(33), 23566-23573 (2024). https://doi.org/10.1021/jacs.4c07699 
[S10] T. Ma, E. A. Kapustin, S. X. Yin, L. Liang, Z. Zhou et al., Single-crystal x-ray diffraction structures of covalent organic frameworks. Science 361(6397), 48-52 (2018). https://doi.org/10.1126/science.aat7679 
[S11] W. E. Morton, J. W. S. Hearle, Fibre length. Phys. Prop. Text. Fibres 1, 134-162 (2008). https://doi.org/10.1533/9781845694425.134 
[S12] Y. Elmogahzy, R. Farag, 7-Tensile properties of cotton fibers: Importance, research, and limitations. Tens. Prop Cot. Fibers 1, 223-273 (2018). https://doi.org/10.1016/B978-0-08-101272-7.00007-9 
[S13] L. Lu, X. Liu, Y. Sun, S. Wang, J. Liu et al., Silk-Fabric Reinforced Silk for Artificial Bones. Adv. Mater. 36(23), 230874 (2024). https://doi.org/10.1002/adma.202308748 
[S14] B. A. Alshammari, M. Hossain, A. M. Alenad, A. G. Alharbi, B. M. Alotaibi, Experimental and Theoretical Analysis of Mechanical Properties of Graphite/Polyethylene Terephthalate Nanocomposites. Polymers 14(9), 1718 (2022). https://doi.org/10.3390/polym14091718 
[S15] I. C. Yeh, B. C. Rinderspacher, J. W. Andzelm, L. T. Cureton, J. La Scala, Computational study of thermal and mechanical properties of nylons and bio-based furan polyamides. Polymer 55(1), 166-174 (2014). https://doi.org/10.1016/j.polymer.2013.11.009 
[S16] D. Sawai, Y. Fujii, T. Kanamoto, Development of oriented morphology and tensile properties upon superdawing of solution-spun fibers of ultra-high molecular weight poly(acrylonitrile). Polymer 47(12), 4445-4453 (2006). https://doi.org/10.1016/j.polymer.2006.03.067 
[S17] Y. L. Yu, X. Q. Xu, C. D. Lu, T. H. Zhang, Y. Ma, Investigation on the microstructural and mechanical properties of a Polytetrafluoroethylene thin film by radio frequency magnetron sputtering. Thin Solid Films 712, 138302 (2020). https://doi.org/10.1016/j.tsf.2020.138302 
[S18] D. Gregor-Svetec, F. Sluga, High modulus polypropylene fibers. I. Mechanical properties. J. Appl. Polym. Sci. 98(1), 1-8 (2005). https://doi.org/10.1002/app.21990 
[S19] W. Zhang, M. Wu, Y. Xin, H. Liu, F. Li et al., Comparative analysis of seawater uranium extraction materials: Toward the development of bio-based and biomimetic materials. Coord. Chem. Rev. 534, 216589 (2025). https://doi.org/10.1016/j.ccr.2025.216589 
[S20] Y. Yuan, S. Feng, L. Feng, Q. Yu, T. Liu et al., A Bio-inspired Nano-pocket Spatial Structure for Targeting Uranyl Capture. Angew. Chem. Int. Ed. 59(11), 4262-4268 (2020). https://doi.org/10.1002/anie.201916450 
[S21] D. Zhang, L. Liu, B. Zhao, X. Wang, H. Pang et al., Highly efficient extraction of uranium from seawater by polyamide and amidoxime co-functionalized MXene. Environ. Pollut. 317, 120826 (2023). https://doi.org/10.1016/j.envpol.2022.120826 
[S22] Z. Li, Q. Meng, Y. Yang, X. Zou, Y. Yuan et al., Constructing amidoxime-modified porous adsorbents with open architecture for costeffective and efficient uranium extraction. Chem. Sci. 11(18), 4747-4752 (2020). https://doi.org/10.1039/d0sc00249f 
[S23] W. Zhang, Y. Xin, Y. Fa, F. Li, Y. Liu et al., SA-DNA hydrogel microspheres for Ultra-Selective uranyl (VI) extraction from seawater. Chem. Eng. J. 495, 153690 (2024). https://doi.org/10.1016/j.cej.2024.153690 
[S24] Y. Xie, Y. Wu, X. Liu, M. Hao, Z. Chen et al., Rational design of cooperative chelating sites on covalent organic frameworks for highly selective uranium extraction from seawater. Cell Reports Phys. Sci. 4(1), 101220 (2023). https://doi.org/10.1016/j.xcrp.2022.101220 
[S25] Y. Zhang, Y. Wang, Z. Dong, Y. Wang, Y. Liu et al., Boosting uranium extraction from Seawater by micro-redox reactors anchored in a seaweed-like adsorbent. Nat. Commun. 15, 9124 (2024). https://doi.org/10.1038/s41467-024-53366-3 
[S26] X. Xu, Y. Yue, D. Cai, J. Song, C. Han et al., Aqueous Solution Blow Spinning of Seawater-Stable Polyamidoxime Nanofibers from Water-Soluble Precursor for Uranium Extraction from Seawater. Small Methods 4(12), 2000558 (2020). https://doi.org/10.1002/smtd.202000558 
[S27] L. Yang, H. Xiao, Y. Qian, X. Zhao, X. Kong et al., Bioinspired hierarchical porous membrane for efficient uranium extraction from seawater. Nat. Sustain. 5, 71-80 (2022). https://doi.org/10.1038/s41893-021-00792-6 
[S28] Y. Yuan, T. Liu, J. Xiao, Q. Yu, L. Feng et al., DNA nano-pocket for ultra-selective uranyl extraction from seawater. Nat. Commun. 11, 5708 (2020). https://doi.org/10.1038/s41467-020-19419-z 
[S29] Y. Yuan, Q. Yu, M. Cao, L. Feng, S. Feng et al., Selective extraction of uranium from seawater with biofouling-resistant polymeric peptide. Nat. Sustain. 4, 708 (2021). https://doi.org/10.1038/s41893-021-00709-3 
[S30] B. Zhang, X. Shan, J. Yu, H. Zhang, K. Tawfik Alali et al., Facile synthesis of TiO2-PAN photocatalytic membrane with excellent photocatalytic performance for uranium extraction from seawater. Sep. Purif. Technol. 328, 125026 (2024). https://doi.org/10.1016/j.seppur.2023.125026 
[S31] Y. Liao, B. Yuan, D. Zhang, J. Zhang, X. Wang et al., Fabrication of Heterostructured Metal Oxide/TiO2 Nanotube Arrays Prepared via Thermal Decomposition and Crystallization. Inorg. Chem. 57(16), 10249-10256 (2018). https://doi.org/10.1021/acs.inorgchem.8b01483 
[S32] M. Fu, C. Huang, L. Ma, Y. Yao, J. Chen et al., Solar enhanced uranium extraction from seawater with the efficient strategy of MXene loaded nano-porous polyamidoxime membrane. Sep. Purif. Technol. 332, 125803 (2024). https://doi.org/10.1016/j.seppur.2023.125803 
[S33] W. R. Cui, C. R. Zhang, R. P. Liang, J. D. Qiu, Covalent organic framework hydrogels for synergistic seawater desalination and uranium Extraction. J. Mater. Chem. A 9(45), 25611-25620 (2021). https://doi.org/10.1039/d1ta06732j 
[S34] T. Li, X. Lin, Z. Zhang, L. Yang, Y. Qian et al., Photothermal-Enhanced Uranium Extraction from Seawater: A Biomass Solar Thermal Collector with 3D Ion-Transport Networks. Adv. Funct. Mater. 33(19), 2212819 (2023). https://doi.org/10.1002/adfm.202212819 
[S35] F. Yu, C. Li, W. Li, Z. Yu, Z. Xu et al., Π-Skeleton Tailoring of Olefin-Linked Covalent Organic Frameworks Achieving Low Exciton Binding Energy for Photo-Enhanced Uranium Extraction from Seawater. Adv. Funct. Mater. 34(1), 2307230 (2024). https://doi.org/10.1002/adfm.202307230 
[S36] Z. Liu, K. Feng, X. Zhang, L. Fu, J. Ren et al., Enhanced uranium extraction using a nanostructured photothermal hydrogel membrane. Chem. Eng. J. 498, 155423 (2024). https://doi.org/10.1016/j.cej.2024.155423 
[S37] H. Yang, M. Hao, Y. Xie, X. Liu, Y. Liu et al., Tuning Local Charge Distribution in Multicomponent Covalent Organic Frameworks for Dramatically Enhanced Photocatalytic Uranium Extraction. Angew. Chem. Int. Ed. 62(30), e202303129 (2023). https://doi.org/10.1002/anie.202303129 
[S38] M. Hao, Y. Xie, X. Liu, Z. Chen, H. Yang et al., Modulating Uranium Extraction Performance of Multivariate Covalent Organic Frameworks through Donor-Acceptor Linkers and Amidoxime Nanotraps. JACS Au 3(1), 239-251 (2023). https://doi.org/10.1021/jacsau.2c00614 
[S39] M. Chen, T. Liu, X. Zhang, R. Zhang, S. Tang et al., Photoinduced Enhancement of Uranium Extraction from Seawater by MOF/Black Phosphorus Quantum Dots Heterojunction Anchored on Cellulose Nanofiber Aerogel. Adv. Funct. Mater. 31(22), 2100106 (2021). https://doi.org/10.1002/adfm.202100106 
[S40] T. Liu, S. Tang, T. Wei, M. Chen, Z. Xie et al., Defect-engineered metal-organic framework with enhanced photoreduction activity toward uranium extraction from seawater. Cell Reports Phys. Sci. 3(5), 100892 (2022). https://doi.org/10.1016/j.xcrp.2022.100892 
[S41] Y. Zhao, S. Li, G. Fu, H. Yang, S. Li et al., Construction of Layer-Blocked Covalent Organic Framework Heterogenous Films via Surface-Initiated Polycondensations with Strongly Enhanced Photocatalytic Properties. ACS Cent. Sci. 10(4), 775-781 (2024). https://doi.org/10.1021/acscentsci.3c01195 
[S42] M. Li, B. Qing, H. Luo, W. Gao, Q. Shou et al., Recyclable covalent organic frameworks/cellulose aerogels for efficient uranium adsorption. Int. J. Biol. Macromol. 282, 137156 (2024). https://doi.org/10.1016/j.ijbiomac.2024.137156 
[S43] M. Li, L. Sun, W. Gao, B. Qing, H. Yao et al., In-situ bioprocessing of bacterial cellulose aerogel with covalent organic frameworks for enhanced uranium extraction. Sep. Purif. Technol. 355, 129654 (2025). https://doi.org/10.1016/j.seppur.2024.129654 
[S44] W. Cui, C. Zhang, R. Liang, J. Liu, J. Qiu, Covalent Organic Framework Sponges for Efficient Solar Desalination and Selective Uranium Recovery. ACS Appl. Mater. Interfaces 13(27), 31561-31568 (2021). https://doi.org/10.1021/acsami.1c04419 
[S45] B. Fan, Y. Si, J. Yu, X. Wang, P. Tang, Multi-Interfacial Interaction Engineered Underwater Superelastic Covalent Organic Framework Aerogels for Photoinduced Uranium Extraction. Chem. Eng. J. 498, 155756 (2024). https://doi.org/10.1016/j.cej.2024.155756 
S2/S32

