Supporting Information for

Heterolayered Carbonized MXene/Polyimide Aerogel for Multi-Spectrum Compatible Protection with Low Reflection

Shan Zhang1,2, †, Chen-Ming Liang1,2, †, Lu Zhou1,2, †, Juntao Wu1,2, *, Martin C. Koo 1,2, Zongxin Wu2, Yun-Tian Chen1,2 and Guang-Sheng Wang1,2, *

1 State Key Laboratory of Bioinspired Interfacial Materials Science, Bioinspired Science Innovation Center, Hangzhou International Innovation Institute, Beihang University, Hangzhou 311115, P. R. China

2School of Chemistry, Beihang University, Beijing 100191, P. R. China

†Shan Zhang, Chen-Ming Liang, and Lu Zhou contributed equally to this work.

*Corresponding authors. E-mail: wjt@buaa.edu.cn (Juntao Wu); wanggsh@buaa.edu.cn (Guang-Sheng Wang)

Supplementary Figures and Tables

Fig. S1 (a) XRD patterns of Ti3AlC2 MAX powders and Ti3C2Tx MXene film (b) TEM image of Ti3C2Tx MXene flakes (c) AFM image and (d) height profiles of the Ti3C2Tx MXene flakes

Fig. S2 The synthesis process of poly(amic acid) (PAA) and poly(amic acid) ammonium salt (PAS)

Fig. S3 Schematic diagram of self-made freeze-drying mold

Fig. S4 Schematic diagram of the process for preparing three-layer heterolayered structures by stepwise freezing

Fig. S5 The MXene/PI aerogel was prepared by stepwise freezing. The first layer of ice crystals grew from bottom to top in liquid nitrogen. The second layer of ice crystals grew randomly in the refrigerator. The third layer of ice crystals grew horizontally along the left copper plate

Fig. S6 (a) Front view and (b) top view photos of the C-MXene/PI aerogel supporting a 500 g weight

Fig. S7 The cross-sectional SEM images of the radial sections of the three layers

Fig. S8 Photos of the mechanical torsion test for the C-MXene/PI aerogel

Fig. S9 The lattice fringes of the TiC (111) plane

Fig. S10 (a) XPS survey spectra and (b) High-resolution XPS spectra of Ti 2p for MXene, MP and CMP

Fig. S11 (a) The cross-section SEM images of heterolayered CMP aerogel. (b) Photo of the heterolayered CMP aerogel measured with a ruler

Fig. S12 EMI SET, SER, and SEA of the (a) vertical structure MXene/PI aerogel, (b) disordered structure MXene/PI aerogel and (c) horizontal structure MXene/PI aerogel. (d) Coefficients of vertical, disordered and horizontal structure MXene/PI aerogel

Fig. S13 EMI SET, SER, and SEA of the (a) vertical structure C-MXene/PI aerogel, (b) disordered structure C-MXene/PI aerogel and (c) horizontal structure C-MXene/PI aerogel. (d) Coefficients of vertical, disordered and horizontal structure C-MXene/PI aerogel

Fig. S14 EMI SE of MP with different structures

Fig. S15 The electrical conductivities of the vertical, disordered and horizontal structural layers of MP and CMP

Fig. S16 (a) EMI SE of CMP after exposure at 40-50% humidity and different temperatures for varying durations. (b) EMI SE of CMP after exposure at 80-90% humidity and different temperatures for varying durations. (c) XRD patterns of the pristine CMP sample and after 10 days of exposure in a damp-heat environment

Fig. S17 EMI SET, SER, and SEA of the (a) MP-T, (b) MP-B and (c) MP-BG. (d) Coefficients of MP-T, MP-B and MP-BG

Fig. S18 The electric field (EF) distribution maps of (a) CMP-T, (b) CMP-B and (c) CMP-BG

Fig. S19 The electrical energy density (EED) distribution maps of (a) CMP-T, (b) CMP-B and (c) CMP-BG

Fig. S20 The enlarged error bar illustration in Fig. 2j

Fig. S21 Comparison of SSE and density with those of previously reported EMI shielding materials

Fig. S22 The schematic diagram of (a) transmission mode and (b) reflection mode for THz time-domain spectral test

Fig. S23 The THz time-domain spectroscopy of CMP for transmission mode

Fig. S24 SET of CMP with different structures in a frequency range of 0.2-1.6 THz

Fig. S25 SER of different structural CMP aerogels in a frequency range of 0.2-1.6 THz

Fig. S26 Schematic diagram of heating the sample on the heating platform

Fig. S27 The infrared emissivity of different structured CMP in the 2-16 μm

Table S1 The thickness of CMP aerogels with different structures

| Sample | Aggregate thickness (cm) | Vertical layer thickness (cm) | Disordered layer thickness (cm) | Horizontal layer thickness (cm) |
| --- | --- | --- | --- | --- |
| Vertical CMP aerogel | 1.00 | 1.00 | 0 | 0 |
| Disordered CMP aerogel | 1.00 | 0 | 1.00 | 0 |
| Horizontal CMP aerogel | 1.00 | 0 | 0 | 1.00 |
| Heterolayered CMP aerogel | 1.00 | 0.33 | 0.33 | 0.33 |

Table S2 SET, SEA and SER average value of CMP-T, CMP-B and CMP-BG

| Material type | EMI SET | EMI SEA | EMI SER |
| --- | --- | --- | --- |
| CMP-T | 91.4 | 85.4 | 6.0 |
| CMP-B | 91.3 | 88.9 | 2.4 |
| CMP-BG | 91.0 | 88.8 | 2.2 |

Table S3 Comparison of EMI SE and R Coefficient with those of previously reported EMI shielding materials

| Material type | EMI SE (dB) | R | Refs. |
| --- | --- | --- | --- |
| CoNi/MXene/nanocellulose | 35.1 | 0.72 | [S1] |
|  | 21.2 | 0.75 |  |
| CNF/MXene/FeCo | 58.0 | 0.51 | [S2] |
| Fe3O4/CNT/PU&MXene | 60.0 | 0.38 | [S3] |
| TCTCF | 85.0 | 0.42 | [S4] |
| AgNWs/Fe3O4@NC | 50.0 | 0.45 | [S5] |
| CNT@MXene | 23.4 | 0.37 | [S6] |
| Cellulose/biochar | 72.4 | 0.58 | [S7] |
| Carbon black/graphene/nickel polyimide | 44.0 | 0.29 | [S8] |
| HWLS/PAN/ZIF-67 | 25.2 | 0.43 | [S9] |
| C-MXene/PI | 91.0 | 0.40 | This work |

Table S4 Comparison of SSE and density with those of previously reported EMI shielding materials

| Material type | Density (mg/cm3) | EMI SE (dB) | SSE (dB•cm2/g) | Refs. |
| --- | --- | --- | --- | --- |
| Graphene/PDMS | 60.0 | 20.0 | 333.3 | [S10] |
| Ti3C2Tx/RGO | 30.0 | 56.4 | 1880.0 | [S11] |
| Graphene foam | 60.0 | 25.2 | 420.0 | [S12] |
| PI/ rGO | 76.0 | 28.8 | 378.9 | [S13] |
| IGA | 18.0 | 83.0 | 4611.1 | [S14] |
| Reduced graphene aerogel | 5.5 | 30.5 | 6777.8 | [S15] |
| CNF/rGO | 5.8 | 33.0 | 5689.7 | [S16] |
| MXene (Ti3C2Tx)/ANFs | 82.0 | 56.8 | 692.7 | [S17] |
| MXene/CMC | 35.0 | 52.2 | 1490.0 | [S18] |
| rGO/MXene | 29.0 | 83.3 | 2872.4 | [S9] |
| PLLA-MWCNT | 30.0 | 23.0 | 766.7 | [S20] |
| O-PI/CNT | 28.5 | 46.5 | 1631.6 | [S21] |
| ANF/GN | 40.0 | 31.6 | 788.8 | [S22] |
| OSG/BNNR | 45.8 | 70.9 | 1548.0 | [S23] |
| PU@PDA@Ag | 32.0 | 84.0 | 2625.0 | [S24] |
| Polyurethane/Silver Nanowire | 45.0 | 48.6 | 1080.0 | [S25] |
| Cu Nanowire @Graphene | 7.5 | 25.4 | 3386.7 | [S26] |
| Polyimide/graphene aerogels | 25.0 | 48.3 | 1931.0 | [S27] |
| AgNW/MXene | 16.6 | 52.5 | 3162.7 | [S28] |
| PSA/AgNWs | 12.3 | 44.0 | 3580.5 | [S29] |
| CMP-T | 12.0 | 91.4 | 7616.7 | This work |
| CMP-B | 12.0 | 91.3 | 7680.3 | This work |
| CMP-BG | 12.0 | 91.0 | 7583.3 | This work |

Table S5 The EMI SE, R and thermal conductivity of five batches of independent experiments for heterolayered CMP aerogels

| Sample | EMI SE in X band (dB) | R in X band | EMI SE in THz band (dB) | R in THz band | Thermal conductivity (W/(m•K)) |
| --- | --- | --- | --- | --- | --- |
| 1 | 91.0 | 0.40 | 66.2 | 0.33 | 0.383 |
| 2 | 91.3 | 0.40 | 68.0 | 0.35 | 0.386 |
| 3 | 90.5 | 0.39 | 63.7 | 0.32 | 0.377 |
| 4 | 90.7 | 0.40 | 64.4 | 0.34 | 0.380 |
| 5 | 91.5 | 0.41 | 68.7 | 0.31 | 0.389 |

Table S6 The R, t and σ of CMP-T, CMP-B and CMP-BG aerogels.

| Sample | Vertical layer |  |  | Disordered layer |  |  |  | Horizontal layer |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | R | t | σ | R | t | σ |  | R | t | σ |
| CMP-T | 8.9 | 0.33 | 0.34 | 8.9 | 0.33 | 0.34 |  | 8.9 | 0.33 | 0.34 |
| CMP-B | 8.9 | 0.33 | 0.34 | 8.9 | 0.33 | 0.34 |  | 8.9 | 0.33 | 0.34 |
| CMP-BG | 30.3 | 0.33 | 0.10 | 8.9 | 0.33 |  | 0.34 | 5.3 | 0.33 | 0.57 |

Table S7 The electromagnetic wave incidence direction and electrical conductivity of CMP-T, CMP-B and CMP-BG aerogels.

| Sample | The incident direction of EW | Vertical layer conductivity (S/cm) |  | Disordered layer conductivity (S/cm) | Horizontal layer conductivity (S/cm) |
| --- | --- | --- | --- | --- | --- |
| CMP-T | From the horizontal layer |  | 0.34 | 0.34 | 0.34 |
| CMP-B | From the vertical layer |  | 0.34 | 0.34 | 0.34 |
| CMP-BG | From the vertical layer |  | 0.10 | 0.34 | 0.57 |

Supplementary References

- T. Mai, L. Chen, Q. Liu, Z.-H. Guo, M.-G. Ma, Zeolitic imidazolate frameworks derived magnetic nanocage/MXene/nanocellulose bilayer aerogels for low reflection electromagnetic interference shielding and light-to-heat conversion. Adv. Funct. Mater. 35(13), 2417947 (2025). https://doi.org/10.1002/adfm.202417947

- M. Ma, W. Tao, X. Liao, S. Chen, Y. Shi et al., Cellulose nanofiber/MXene/FeCo composites with gradient structure for highly absorbed electromagnetic interference shielding. Chem. Eng. J. 452, 139471 (2023). https://doi.org/10.1016/j.cej.2022.139471

- J. Zhang, L. Zeng, X. Liu, D. Zhang, A. Gao et al., Lattice-filler dual-gradient and hierarchical porous architectures customized by multiple-nozzle 3D printing towards excellent absorption-dominant electromagnetic interference shielding. Compos. Sci. Technol. 262, 111058 (2025). https://doi.org/10.1016/j.compscitech.2025.111058

- L. Wang, J. Men, W. Ren, Z. Yang, Y. Gao et al., Low-reflection electromagnetic interference shielding composite foams with asymmetric structure towards infrared camouflage and response switching. J. Colloid Interface Sci. 697, 137941 (2025). https://doi.org/10.1016/j.jcis.2025.137941

- M. Sun, Z. Wang, J. Xiao, X. Tian, X. Ma et al., AgNWs/Fe3O4@NC conductive network hierarchical assembly to prepare flexible EMI shielding textile. Small 20(14), 2304622 (2024). https://doi.org/10.1002/smll.202304622

- W. Feng, L. Zou, C. Lan, S. E, X. Pu, Core-sheath CNT@MXene fibers toward absorption-dominated electromagnetic interference shielding fabrics. Adv. Fiber Mater. 6(5), 1657–1668 (2024). https://doi.org/10.1007/s42765-024-00452-2

- S. Li, Y. Du, H. Ye, J. Wu, Y. Wang et al., All-natural self-bonded biocomposite providing superior electromagnetic interference shield performance with effective absorption. Adv. Funct. Mater. 34(41), 2406282 (2024). https://doi.org/10.1002/adfm.202406282

- Y. Wang, Y. Zhong, J. Kang, B. Zhang, Z. Ma et al., Multifunctional rigid polyimide foams with outstanding EMI shielding and wave absorption via densification strategy. J. Mater. Sci. Technol. 227, 155–163 (2025). https://doi.org/10.1016/j.jmst.2024.12.021

- D. Gao, S. Guo, Y. Zhou, B. Lyu, X. Li et al., Absorption-dominant, low-reflection multifunctional electromagnetic shielding material derived from hydrolysate of waste leather scraps. ACS Appl. Mater. Interfaces 14(33), 38077–38089 (2022). https://doi.org/10.1021/acsami.2c10787

- Z. Chen, C. Xu, C. Ma, W. Ren, H.-M. Cheng, Lightweight and flexible graphene foam composites for high-performance electromagnetic interference shielding. Adv. Mater. 25(9), 1296–1300 (2013). https://doi.org/10.1002/adma.201204196

- S. Zhao, H.-B. Zhang, J.-Q. Luo, Q.-W. Wang, B. Xu et al., Highly electrically conductive three-dimensional Ti3C2Tx MXene/reduced graphene oxide hybrid aerogels with excellent electromagnetic interference shielding performances. ACS Nano 12(11), 11193–11202 (2018). http://doi.org/10.1021/acsnano.8b05739

- B. Shen, Y. Li, D. Yi, W. Zhai, X. Wei et al., Microcellular graphene foam for improved broadband electromagnetic interference shielding. Carbon 102, 154–160 (2016). https://doi.org/10.1016/j.carbon.2016.02.040

- 13 Z. Yu, T. Dai, S. Yuan, H. Zou, P. Liu, Electromagnetic interference shielding performance of anisotropic polyimide/graphene composite aerogels. ACS Appl. Mater. Interfaces 12(27), 30990–31001 (2020). https://doi.org/10.1021/acsami.0c07122

- J. Liu, Y. Liu, H.-B. Zhang, Y. Dai, Z. Liu et al., Superelastic and multifunctional graphene-based aerogels by interfacial reinforcement with graphitized carbon at high temperatures. Carbon 132, 95–103 (2018). https://doi.org/10.1016/j.carbon.2018.02.026

- S. Bi, L. Zhang, C. Mu, M. Liu, X. Hu, Electromagnetic interference shielding properties and mechanisms of chemically reduced graphene aerogels. Appl. Surf. Sci. 412, 529–536 (2017). https://doi.org/10.1016/j.apsusc.2017.03.293

- M. Li, F. Han, S. Jiang, M. Zhang, Q. Xu et al., Lightweight cellulose nanofibril/reduced graphene oxide aerogels with unidirectional pores for efficient electromagnetic interference shielding. Adv. Mater. Interfaces 8(24), 2101437 (2021). https://doi.org/10.1002/admi.202101437

- Z. Lu, F. Jia, L. Zhuo, D. Ning, K. Gao et al., Micro-porous MXene/Aramid nanofibers hybrid aerogel with reversible compression and efficient EMI shielding performance. Compos. Part B Eng. 217, 108853 (2021). https://doi.org/10.1016/j.compositesb.2021.108853

- Y. Cheng, W. Zhu, X. Lu, C. Wang, Lightweight and flexible MXene/carboxymethyl cellulose aerogel for electromagnetic shielding, energy harvest and self-powered sensing. Nano Energy 98, 107229 (2022). https://doi.org/10.1016/j.nanoen.2022.107229

- X. Zheng, J. Tang, P. Wang, Z. Wang, L. Zou et al., Interfused core-shell heterogeneous graphene/MXene fiber aerogel for high-performance and durable electromagnetic interference shielding. J. Colloid Interface Sci. 628, 994–1003 (2022). https://doi.org/10.1016/j.jcis.2022.08.019

- T. Kuang, L. Chang, F. Chen, Y. Sheng, D. Fu et al., Facile preparation of lightweight high-strength biodegradable polymer/multi-walled carbon nanotubes nanocomposite foams for electromagnetic interference shielding. Carbon 105, 305–313 (2016). https://doi.org/10.1016/j.carbon.2016.04.052

- S. Liu, Q. Xu, Y. Bai, X. Wang, X. Liu et al., Toward strong X-band-electromagnetic-wave-absorbing materials: polyimide/carbon nanotube composite aerogel with radial needle-like porous structure. J. Mater. Chem. A 10(47), 25140–25147 (2022). http://doi.org/10.1039/d2ta05845f

- N. Luo, Y.-Y. Zhang, H. Zhang, T.-L. Liu, Y. Wang et al., Electromagnetic interference shielding performance of lightweight aramid nanofiber/graphene composite aerogels. J. Mater. Chem. A 12(17), 10359–10368 (2024). http://doi.org/10.1039/d3ta07473k

- L. Feng, P. Wei, Q. Song, J. Zhang, Q. Fu et al., Superelastic, highly conductive, superhydrophobic, and powerful electromagnetic shielding hybrid aerogels built from orthogonal graphene and boron nitride nanoribbons. ACS Nano 16(10), 17049–17061 (2022). https://doi.org/10.1021/acsnano.2c07187

- C. Liang, Y. Liu, Y. Ruan, H. Qiu, P. Song et al., Multifunctional sponges with flexible motion sensing and outstanding thermal insulation for superior electromagnetic interference shielding. Compos. Part A Appl. Sci. Manuf. 139, 106143 (2020). https://doi.org/10.1016/j.compositesa.2020.106143

- Z. Zeng, M. Chen, Y. Pei, S.I. Seyed Shahabadi, B. Che et al., Ultralight and flexible polyurethane/silver nanowire nanocomposites with unidirectional pores for highly effective electromagnetic shielding. ACS Appl. Mater. Interfaces 9(37), 32211–32219 (2017). http://doi.org/10.1021/acsami.7b07643

- S. Wu, M. Zou, Z. Li, D. Chen, H. Zhang et al., Robust and stable Cu Nanowire@Graphene core–shell aerogels for ultraeffective electromagnetic interference shielding. Small 14(23), 1800634 (2018). https://doi.org/10.1002/smll.201800634

- Y. Zhao, H. Chen, S. Qiao, Z. Wang, J. Yan, Hierarchically porous polyimide/graphene aerogels with superior compressibility and electromagnetic interference shielding performance. J. Mater. Chem. A 13(28), 22613–22620 (2025). http://doi.org/10.1039/d5ta02068a

- C. Weng, G. Wang, Z. Dai, Y. Pei, L. Liu et al., Buckled AgNW/MXene hybrid hierarchical sponges for high-performance electromagnetic interference shielding. Nanoscale 11(47), 22804–22812 (2019). https://doi.org/10.1039/c9nr07988b

- J. Wang, Q. Zhang, S. Zhang, R. Liu, Y. Zhang et al., Multifunctional Polysulfonamide/AgNWs aerogel for electromagnetic interference shielding. Compos. Commun. 56, 102346 (2025). https://doi.org/10.1016/j.coco.2025.102346