Supporting Information for

Wafer-Level Self-Assembly and Interface Passivation Patterning Technology for Nanomaterial-Compatible 3D MEMS Sensing Chips

Zheng Zhang1, Yanlin Zhang1, Yuanyuan Luo2, Guoliang Lv1, Jianglin Yin1, Pengwei Tan1, and Guotao Duan1, 3, *

1School of Integrated Circuits, Huazhong University of Science and Technology, Wuhan 430074, P. R. China

2Key Laboratory of Materials Physics, Institute of Solid State Physics, HFIPS, Chinese Academy of Sciences, Hefei 230031, P. R. China

3Wuhan National Laboratory for Optoelectronics, Huazhong University of Science and Technology, Wuhan 430074, P. R. China

*Corresponding author. E-mail: duangt@hust.edu.cn (Guotao Duan)

Supplementary Figures and Tables

- Schematic diagrams illustrating the expected effects and current challenges in nanomaterials film transfer. Challenges include improve transfer efficiency, thickness uniformity and accurately pattern transfer

- Operation process of the self-assembly equipment. a Container is adjusted horizontally by the bottom leveling device. b Target wafer is placed in the container. c DI water is added to submerge the entire wafer, with the liquid level 1 cm above the wafer surface. d Automatic syringe is assembled. e Automatic syringe is activated to inject suspension, and the films gradually form on the water surface as shown in Fig. 2c. f Liquid level controlling device is turned on to decrease the liquid level. g Self-assembly monolayer films are transferred onto the wafer surface as the liquid level decreases

- Schematic diagrams of the “film first, cantilever later” wafer-level process flow. Following the IDE deposition step as shown in Fig. 1, the subsequent steps are: (V) The film pattern are defined by lithography. (VI) Self-assembly is performed to form the sensing film. (VII) Unwanted film areas are removed by a lift-off process. (VIII) Cantilever stucture is released via TMAH wet etching

- Self-assembly films prepared on photoresist layers of varying thickness. a SEM images showing the film seperation status. b Thicknesses of photoresist under different spin rates

- Photograph of the self-assembly monolayer SnO2 films before wet etching, deposited on a SiO2 substrate

Fig. S6 a-b Photographs and optical microscope images of SnO2 films on Si3N4 substrates before etching and after different etching durations. c-e Enlarged optical images highlighting surface changes corresponding to each etching time

Fig. S7 Raman spectra of the etched SnO2 films on Si3N4 substrates. For the 300-min sample, three spectra represent measurements at distinct positions marked by white dots in Fig. S9e. The spectra of P3 shows the absence of the classic SnO2 peak

Fig. S8 Adsorption energy (ΔEads) calculation results for amorphous SiO2/Si and crystalline HfO2/SiO2/Si structure model. a From left to right is the model of amorphous SiO2/Si structure with single-side interface H passivation, ΔEads of Si site toward OH species, ΔEads of Si site toward H2O molecule, and ΔEads of O site toward H2O molecule. b From left to right is the model of crystalline HfO2/SiO2/Si structure with single-side interface H passivation, ΔEads of Hf site toward OH species, ΔEads of Hf site toward H2O molecule, and ΔEads of O site toward H2O molecule

Fig. S9 Photograph of the self-assembly monolayer SnO2 films before wet etching, deposited on a HfO2 substrate

Fig. S10 Optical microscope images of SnO2 film on Ti/Pt electrodes underwent 800 °C annealing. a Both SnO2 and metal films are intact before annealing. b Curvature and detachment occurred in the metal film, leading to the breakage of the SnO2 film

Fig. S11 SEM images of various SnO2 film patterns. a The regular shapes are suitable for individual MEMS gas sensors. b The irregular shapes can be utilized for MEMS gas sensor arrays structure or more complex sensors structure

Fig. S12 Simulation models and results of MEMS hotplates. a 3D geometry of MEMS hotplate. b Electric field distribution of the heater. c-d Thermal distribution and isotherm explanation of MEMS hotplate. e-f 3D geometry and electric field distribution of array-type MEMS hotplates

Fig. S13 a-b Infrared images of the fabricated MEMS micro hotplate. c Thermal distribution of conventional rectangular range of interest. d Thermal distribution of isothermal-defined range of interest

Fig. S14 a Comparison of photographs and optical microscope images of In2O3 films on HfO2 substrates before and after etching. b Comparison of XRD patterns, both showing the characteristic peaks of In2O3

Fig. S15 Comparison of SEM-EDS images of In2O3 nanosphere films on HfO2 substrates. a Before TMAH etching. b After TMAH etching. The In2O3 nanospheres film retains intact

Fig. S16 a Comparison of photographs and optical microscope images of ZnO films on HfO2 substrates before and after etching. b Comparison of XRD patterns, indicating the characteristic peaks of ZnO are absent in the after-etching sample. c Comparison of SEM images, highlighting the detachment caused by the etching effect

Fig. S17 Schematic of the complete wafer-level manufacturing process flow for MEMS gas sensing chips. (i) A SiO2/Si3N4/SiO2 supporting film is prepared on the Si wafer. (ii) Ti/Pt electrodes are deposited to form the microheaters. (iii) A SiO2 insulating layer is deposited. (iv) A HfO2 passivation layer is deposited on the central sensing area of the insulating layer. (v) Bonding pads and etching windows are exposed. (vi) Ti/Pt testing electrodes are prepared. (vii) The self-assembly gas sensing film is transferred aligned with HfO2. (viii) The suspended cantilever is released by TMAH wet etching, resulting in the final MEMS gas sensing chips

Fig. S18 Response comparison of Pd/SnO2 sensing chips operating at different temperatures

Fig. S19 Linear fitting curves of the responses of a monolayer Pd/SnO2 sensor responses to H2 concentrations ranging from 1 to 500 ppm at 300 °C

Fig. S20 Response time of a monolayer Pd/SnO2 sensor towards 20 ppm H2 at 300 °C

Fig. S21 Response variation of 25 monolayer Pd/SnO2 sensors randomly selected from five different regions of the wafer, with statistical distribution illustrated by box plots

Fig. S22 a Response of monolayer SnO2 sensors towards 20 ppm H2. b Response of trilayer Pd/SnO2 sensors towards 20 ppm H2

Table S1 Comparison of fabrication capabilities and H2 sensing performance of MEMS micro hotplate sensors with different film-deposition methods

| Sensing materials | Film-deposition methods | Fabrication scale | Film pattern morphology | Concentration Range (ppm) | Response | Response time (s) | Temperature (°C) | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Au-Pd dual-metal modified In2O3 | Dropped by pipette | Single device | Naturally formed | 0.05 ~ 100 | 8.35 (10 ppm) | 5.0 (10 ppm) | 245.2 | [S1] |
| (FeCoNi)100−xOx | Dropped by needle | Single device | Naturally formed | 200 ~ 1000 | 8.60 (200 ppm) | \ | 150.0 | [S2] |
| SnO2 | Dropped by pipette | Single device | Naturally formed | 0.1 ~ 20 | 2.21 (6 ppm) | 7.0 (6 ppm) | 250.0 | [S3] |
| Pd NPs/SnO2 film | Mask-assistant sputtering and ALD | Wafer level (Silicon) | Rectangle | 0.5 ~ 500 | 1.52 (20 ppm) | 115.4 (20 ppm) | 150.0 | [S4] |
| Pd/SnO2 nanospheres | Lithography-based self-assembly | Wafer level (Silicon) | Customizable | 1 ~ 500 | 1.92* (20 ppm) | 19.7 (20 ppm) | 300.0 | This work |

* Sensitivity to different H2 concentrations at 300 °C: 1.32 (5 ppm), 1.50 (10 ppm), 1.92 (20 ppm), and 4.92 (200 ppm). Sensitivity to 20 ppm H2 at different temperatures: 1.00 (100 °C), 1.10 (150 °C), 1.34 (200 °C), 1.53 (250 °C), 1.92 (300 °C), 1.46 (350 °C)

Supplementary References

- Z. Yang, Q. Rong, W. Zhang, X. Fan, M. Shao et al., A ZnO packaged MEMS hydrogen sensor for reliable sibo breath analysis with anti-H2S interference. Chem Eng J (Lausanne). 522, 167331 (2025). https://doi.org/10.1016/j.cej.2025.167331

- W. Yan, Y. Liu, Y. Bai, Y. Chen, H. Zhou et al., Intelligent MEMS sensor based on an oxidized medium-entropy alloy (FeCoNi) for H2 and co recognition. ACS Appl Mater Interfaces. 16(37), 49474-49483 (2024). https://doi.org/10.1021/acsami.4c07782

- N. Luo, C. Wang, D. Zhang, M. Guo, X. Wang et al., Ultralow detection limit MEMS hydrogen sensor based on SnO2 with oxygen vacancies. Sens Actuators B Chem. 354, 130982 (2022). https://doi.org/10.1016/j.snb.2021.130982

- Z. Zhang, L. Luo, Y. Zhang, G. Lv, Y. Luo et al., Wafer-level manufacturing of MEMS H2 sensing chips based on Pd nanoparticles modified SnO2 film patterns. Adv Sci. 10(26), 2302614 (2023). https://doi.org/10.1002/advs.202302614W

ss