Supporting Information for

# Efficient and Pure I-III-VI AIGS Quantum Dot-based Light-Emitting Diodes via Ligand-Reshaped Surface State

Leimeng Xu1, Jianpeng Zhao1, Jindi Wang1, Jisong Yao1, Shalong Wang1, Zhi Wu1, Jizhong Song1*

1Key Laboratory of Materials Physics of Ministry of Education, Laboratory of Zhongyuan Light, School of Physics, Zhengzhou University, Daxue Road 75, Zhengzhou 450051, P. R.   China

*Corresponding author. E-mail: songjizhong@zzu.edu.cn (Jizhong Song)

S1 Method of density functional theory simulations

DFT calculations [S1, S2] were performed using the Vienna ab initio simulation package (VASP). The generalized gradient approximation (GGA) in the form of Perdew-Burke-Ernzerhof (PBE) [S3] was adopted as the exchange correlation functional. The energy cutoff of 450 eV and the k-point meshes of 1×1×1 were proposed to carry out geometry optimization and electronic structure calculation. During the geometry optimization, the entire system is considered to have successfully converged until the convergence thresholds of maximum force and energy were smaller than 0.05 eV/A and 1.0×10-5 eV/atom, respectively. The vacuum slab was set as 15Å to avoid interactions between neighboring structures.

S2 Supplementary Figures and Tables

Fig. S1 PL spectra of AIGS QDs before and after GS coating

Fig. S2 The molecular structure of DSA

Fig. S3 Schematic diagram of VS and VGa on GS surface and their corresponding vacancy formation energy

Fig. S4 1H and 13C NMR spectra of DSA and LR QDs

Fig. S5 Electron paramagnetic resonance (EPR) spectra of QDs and LR QDs

Fig. S6 (a) TEM image, (b) Size distribution histogram, (c) HRTEM image of AIGS QDs before GS coating. (d-h) energy dispersive spectroscopy elemental maps of Ag/In/Ga/S of AIGS QDs before GS coating

Fig. S7 Energy dispersive spectroscopy elemental maps of Ag/In/Ga/S of control AIGS QDs, the scale bar is 5 nm

Fig. S8 PLQY spectra of (a) control QDs and (b) LR QDs

Fig. S9 AFM image and roughness of (a) control QD film and (b) LR QD film

Fig. S10 The fs-TA spectra of (a) control QDs and (b) LR QDs

Fig. S11 (a) The PL attenuation curves of colloidal QDs at atmosphere for one month. PL attenuation of QD film (b) under 365 nm UV light irradiation and (c) heating at 80 °C

Fig. S12 (a) C-V curve of ITO/QDs/Al tested at 700 KHz. (b) AFM line scanning of QD film

The relative dielectric constant (ε) of AIGS/GS QDs are tested using a flat capacitor with the structure of ITO/QDs/Al, and calculated its relative dielectric constant using the formula . C denotes the maximum capacitance achieved under stable conditions (Fig. S12a); d represents the thickness of the tested sample, which was determined to be approximately 140 nm via AFM measurement (Fig. S12b); A represents the effective electrode area (6 mm2), ε0 represents the vacuum dielectric constant (8.8510-12 F/m). Ultimately, the dielectric constant of the QDs, as experimentally determined, was approximately 9.3.

Fig. S13 EL spectra of (a) control QLEDs and (b) LR QLEDs tested from 2.4 V to 6 V

Fig. S14 The CIE chromaticity coordinates of (a) control and (b) LR QLEDs

Fig. S15 The operational lifetime of QLEDs tested at initial luminance of 100 cd/m2

Table S1 The atomic ratio of elemental from ICP characterization

|  | QDs | LR QDs |
| --- | --- | --- |
| Ag | 2.5 | 2.6 |
| In | 0.6 | 0.7 |
| Ga | 1.6 | 1.8 |
| S | 4.1 | 4.5 |
| ratio | 1:0.24:0.64:1.64 | 1:0.26:0.69:1.73 |

Table S2 Summary of TR-PL decay fitting parameters for control and LR QDs

|  | τ1 (ns) | α1 | τ2 (ns) | α2 | τ3 (ns) | α3 | τave (ns) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| LR QDs | 18.9 | 17.5% | 67.5 | 65.2% | 273.8 | 17.3% | 94.6 |
| QDs | 12.2 | 31% | 64.6 | 43.2% | 289.3 | 25.8% | 106 |

Table S3 Summary of GSB fitting parameters for control and LR QDs

|  | τ1 (ps) | α1 | τ2 (ps) | α2 | τ3 (ps) | α3 | τave (ps) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| LR QDs | 2.47 | 0.02% | 5099.2 | 99.18% | 308.8 | 0.8% | 94.6 |
| QDs | 1.67 | 0.18% | 64 | 3.16% | 2229.5 | 96.66% | 106 |

Table S4 Performance summary of reported AIGS QLEDs

| Time | Material | PL (nm) | FWHM (nm) | PLQY (%) | EQE (%) | Luminance (cd/m2) | References |
| --- | --- | --- | --- | --- | --- | --- | --- |
| This work | AIGS@GS | 531 | 31 | 89 | 8.4 | 1219 |  |
| 2024 | AIGS@GS | 524 | 30 | 53 | 5.4 | >1000 | Adv. Phys. Res., 2024, 3, 240042 |
| 2024 | AIGS@AGS | 532 | 36 | 45 | 0.75 | 2747 | J. Mater. Chem. C, 2024, 12, 6528 |
| 2024 | AIGS@AGS | 532 | 33 | 45 | 0.26 | 1518 | Chinese J. Lumin., 2024, 45, 1849 |
| 2024 | AIGZS | 482, 532, 620 | 49, 38, 44 |  | 0.53, 0.13, 0.03 | 405, 184, 196 | Nano Lett., 2024, 24, 9683 |
| 2024 | AIGS@ZS | 553 | 44.6 | 16 | 0.1 |  | Chem. Commun., 2024, 5731 |
| 2023 | AIGS@GS | 531 | 32 | 32.0 | 1.10 | 175 | ACS Appl. Mater. Interfaces., 2023, 15, 8336 |
| 2023 | ZAIGS@IS | 628 | 78 | 86.2 | 5.32 | 218.1 | ACS Appl. Mater. Interfaces., 2023, 15, 50254 |
| 2022 | AGZS | 470 | 48 | 16.7 | 0.40 | 123.1 | J. Phys. Chem. Lett., 2022, 13, 11857 |
| 2020 | AIS@ZS | 666 | 122 | 72.0 | 1.25 | 1120 | J. Phys. Commun., 2020, 4, 045016 |
| 2020 | AIS@GS | 560 | 45 | 70.0 | 0.54 | 120.5 | Appl. Phys. Lett., 2020, 117, 091101 |

Supplementary References

- P. Hohenberg, W. Kohn, Inhomogeneous electron gas. Phys. Rev. 136(3B), B864 (1964). https://doi.org/10.1103/PhysRev.136.B864

- W. Kohn, L.J. Sham, Self-consistent equations including exchange and correlation effects. Phys. Rev. 140(4A), A1133 (1965). https://doi.org/10.1103/PhysRev.140.A1133

- J.P. Perdew, K. Burke, M. Ernzerhof, Generalized gradient approximation made simple. Phys. Rev. Lett. 77(18), 3865 (1996). https://doi.org/10.1103/PhysRevLett.77.3865