Supporting Information for

Spin Regulation of Fe Single Site Induced by Adjacent Mg Site Achieving Excellent Oxygen Reduction Catalysis

Yuan Shi1, Ziyi Zhang1, Lei Bai1, Dingding Li1, Jingbo Shi1, Zongye Yue1,2, Tianyu Yuan3, Jinbo Bai4, Jintao Bai1, Kunyue Leng1, *, Xiaolin Li2, *, Xuejing Wang5, *, Yunteng Qu1, *

1 Collaborative Center on Photoelectric Technology and Nano Functional Materials, Institute of Photonics and Photon-Technology, Northwest University, Xi’an 710069, P. R. China

2 Institute of Intelligent Manufacturing Technology, Shenzhen Polytechnic University, Shenzhen 518055, P. R. China

3 Institute for Advanced Study, Chengdu University, Chengdu 610106, P. R. China

4 Université Paris-Saclay, CentraleSupélec, ENS Paris-Saclay, CNRS, LMPS-Laboratoire de Mécanique Paris-Saclay, 8-10 rue Joliot-Curie, 91190 Gif-sur-Yvette, France

5 School of Life Sciences, Northwestern Polytechnical University, 1 Dongxiang Road, Xi’an 710069, P. R. China

*Corresponding authors. E-mail: lengky@nwu.edu.cn (Kunyue Leng); wangxuejing@nwpu.edu.cn (Xuejing Wang); yuntengqu@nwu.edu.cn (Yunteng Qu)

S1 Electrochemical measurement

Linear sweep voltammetry (LSV) was performed at a scan rate of 5 mV/s in the region between 0.2 and 1.1 V (vs. RHE). LSV curves at various rotating speed from 400 to 2500 rpm was carried out to estimate the electron transfer number (n). The electron transfer number (n) was determined by the Koutecky-Levich (K-L) equation:

|  | 1J=1JL+1Jk=1Bω1/2+1Jk | (S1) |
| --- | --- | --- |
|  | B=0.62nFCoD2/3v-1/6 | (S2) |
|  | Jk=nFkCo | (S3) |

Where J is the measured current density, Jk and JL are the kinetic and diffusion-limiting current densities. ω is the angular velocity of the disk, n represents the electron transfer number, F is the Faraday constant (96485 C mol-1), Co is the saturated O2 concentration (1.2×10-6 mol cm-3), D is the diffusion coefficient of O2 (1.9×10-5 cm2 s-1), ν is the kinetic viscosity (0.01 cm2 s-1) and k is the electron transfer rate constant.

Tafel slopes were calculated by the Tafel equation based on LSV data:

|  | η=b log ( J )+ɑ | (S4) |
| --- | --- | --- |

Rotating ring-disc electrode (RRDE) is recognized as a high effective method to calculate the number of electron transferred and yield of hydrogen peroxide.

|  | H2O2%=200Jr/NJd+Jr/N | (S5) |
| --- | --- | --- |
|  | n=4×JdJd+Jr/N | (S6) |

where Jd is the disk current, Jr is the ring current, and N is the H2O2 collection coefficient at the ring (0.37).

The mass activity (MA) of the catalyst was calculated using the following equation:

|  | MA=JCcat | (S7) |
| --- | --- | --- |

where J is the measured current density under a potential (V vs. RHE) and Ccat is the quality per unit area of the catalyst (0.4 mg·cm-2 for RDE and RRDE in this work).

The electrochemically active surface area (ECSA) can be calculated according to the equations given below based on CV data:

|  | Cdl=QU=(dQ/dt)(dU/dt)=Jr | (S8) |
| --- | --- | --- |
|  | ECSA=CdlCs | (S9) |
|  | SA=MAECSA | (S10) |

Where Q is the quantity of electric charge per unit area, U is the voltage, J is the current density and r is the scan rate, so the double-layer capacitance (Cdl) is the slope of J~r. Cs is the specific capacitance value for a flat standard with 1 cm2 of real surface area. The general value for Cs is between 20 μF·cm-2 and 60 μF·cm-2. Here, Cs is the average value (40 μF·cm-2). SA denotes the intrinsic catalytic capability (turnover frequency, TOF) of catalysts per unit exposed area.

The current density (J) values in this paper were recorded as the ratios of the measured current values to the geometric area of RDE. All LSV curves were carried out with iR compensation.

The accelerated stability was examined by LSV experiments before and after 5000 continuous cycling voltammograms with a scan rate 5 mV/s. Tolerance test to methanol was performed by the i-t chronoamperometric responses at 0.7 V (vs. RHE) by methanol injection into the O2-saturated 0.1 M HClO4 electrolyte at the time of 300 s.

S2 In situ Raman spectra measurements

Raman spectra were recorded with a confocal microprobe Raman system (HORIBA FRANCE SAS LABRAM HR EVO). A 50× long working distance (8 mm) objective was used. The wavelength of the excitation laser was 532 nm from an Ar ion laser (the power was about 13 mW). The electrolyte is O2-saturated 0.1 M KOH solution and 0.1 M HClO4 solution. Each Raman spectrum shown here is acquired after 5 s of reaction in i-t mode.

S3 In situ ATR-FTIR spectra measurements

In situ ATR-FTIR was performed on a Thermo NICOLET iS50 FT-IR spectrometer equipped with a VeeMax III (PIKE technologies) accessory. The electrochemical test was conducted in a custom-made three-electrode electrochemical single cell. A Pt wire and a saturated Ag/AgCl were used as the counter and reference electrodes, respectively. The electrolyte is O2-saturated 0.1 M KOH solution and 0.1 M HClO4 solution. Each IR spectrum shown here is acquired after 5 s of reaction in i-t mode.

S4 Hydrogen-Oxygen fuel cell measurements

Membrane: DuPont NC700; gas diffusion layer: SGL, 28BC. The MEA with an active area 5 cm2 was prepared through a spraying method without hot pressing. Catalyst loading: Sample #1, 4.0 mg cm-2 (total) nonprecious catalysts in cathode and 0.1 mgPt·cm-2 Pt/C (20 wt% Pt/C, Alfa Aesar) in anode; Sample #2, 0.2 mg·cm-2 Pt/C (20 wt% Pt/C, Alfa Aesar) in cathode and 0.1 mgPt·cm-2 Pt/C (20 wt % Pt/C, Alfa Aesar) in anode. Single cell performance: Fuel cell performance of the obtained MEA was performed on a multi-range fuel cell test system (850e, Scribner Associates Inc.) with a back pressure of 1.5 bar. The cell temperature was 353 K. The H2 and O2 flow rates were both 300 ccm at 100% relative humility (RH) for polarization curve measurement.

S5 Zinc-Air Battery assembly and test

An aqueous Zn-air battery was assembled with homemade electrochemical cell frameworks. On the air electrode, the catalyst ink was uniformly coated onto carbon fiber paper at an effective size of 1.0 × 1.0 cm2 and then dried at room temperature. The catalyst loading per area was 0.20 mg·cm-2 unless otherwise stated. A polished Zn plate was used as the anode with the same effective size. The electrolyte was composed of 6 mol·L-1 KOH and 0.2 mol·L-1 zinc acetate. The battery performance measurements were carried out under a constant current charging-discharging process by a Neware CT-4008-5V50 mA-164 laboratory instrument at room temperature. FeMg-N-C or Pt/C was used as air cathode and a zinc plate as the anode. The specific capacity of the Zn-air batteries was calculated by the following equation:

|  | specific capacity = I* tmzn | (S11) |
| --- | --- | --- |

where I is the measured current density, t is the service hours, and mzn is the mass of consumed zinc.

S6 Calculation of rate constants for ORR by Damjanovic modeling

The RRDE voltammetric equations were derived by Damjanovic to calculate the rate constants (k1, k2 and k3) of the ORR model shown in Scheme 1 and expressed as follows:

Scheme S1 Damjanovic model of ORR

|  | IdIr =1+2k1 /k2N + 2(1+k1 /k2)NZ2 k3ω-1/2 | (S12) |
| --- | --- | --- |
|  | IdlIdl- Id=1+ k1+ k2Z1 ω-1/2 | (S13) |

Where Z1=0.2DO22/3v-1/6and Z2=0.2DH2O22/3v-1/6; Id is the disk current; Ir is the ring current; Idl is the disk limiting current; ω is the rotational speed of electrode; N is the collection efficiency; DH2O2and DO2are the respective diffusion coefficients of H2O2 and O2; and v is the kinematic viscosity of the solution used. By combining the intercepts and slopes of both Id /Ir vs. ω-1/2and Idl /(Idl-Id) vs. ω-1/2 plots, the step rate constants can be expressed by following equations:

|  | k1= S2Z1I1N-1I1N+1 | (S14) |
| --- | --- | --- |
|  | k2 = 2Z1S2I1N+1 | (S15) |
|  | k3 = NZ2S1I1N+1 | (S16) |

where I1 and S1 are respectively the intercept and slope of the plot of Id /Ir vs. ω-1/2, and S2 is the slope of the plot of Idl /(Idl-Id) vs. ω-1/2.

S7 Calculation of the g-value

For paramagnetic centers with specific structures, the gyromagnetic ratio (g) serves as a fixed intrinsic parameter, also known as a fingerprint. When a single electron meets the resonance condition:

|  | ∆E=hv=geμBB0 | (S17) |
| --- | --- | --- |

Where h is Planck's constant, v is microwave frequency, μB is Bohr magneton, and B0 is magnetic field.

For the g-value of a specific sample, the conversion is as follows:

|  | g = 714.4773506 *ν(GHz)B(G) | (S18) |
| --- | --- | --- |

Where v is the actual microwave frequency during testing (in GHz), and B represents the magnetic field at the position where the g-factor needs to be calculated (in G).

S8 Calculation of the number of unpaired electrons

The number of unpaired 3d electrons (n) of Fe center is evaluated from the effective magnetic moment (μeff) according to the following equation:

|  | μeff = n*(n+2)μB | (S19) |
| --- | --- | --- |

where μB is the Bohr magneton.

The μeff can be obtained using the following equation:

|  | μeff = 8CμB | (S20) |
| --- | --- | --- |

where C is the Curie constant and the slope of the χ-1–T curve

|  | χ = C/(T-θ) | (S21) |
| --- | --- | --- |

Susceptibility (χ) can be obtained derived from the following equation:

|  | χ = M/H | (S22) |
| --- | --- | --- |

S9 Computational details

The four elementary steps of oxygen reduction in acidic solution are as follows:

|  | *+O2+H++ e- → *OOH | (23) |
| --- | --- | --- |
|  | *OOH+H++ e- → *O+H2O | (S24) |
|  | *O+H++ e- → *OH | (S25) |
|  | *OH+H++ e- → *+ H2O | (S26) |

where * represents the preferable adsorption site for intermediates.

The four elementary steps of oxygen reduction in alkaline solution are as follows:

|  | *+ O2+ H2O+e- → *OOH+OH- |  |  | (S27) |
| --- | --- | --- | --- | --- |
|  |  | *OOH+e- → *O+OH- | (S28) |  |
|  |  | *O+H2O+e- → *OH+OH- | (S29) |  |
|  |  | *OH+e- → *+ OH- | (S30) |  |

where * represents the preferable adsorption site for intermediates.

For each step, the reaction free energy is calculated by:

|  | ∆G = ∆E + ∆ZPE - T∆S | (S31) |
| --- | --- | --- |

where ΔE is the total energy difference between reactants and products of reactions, ΔZPE is the zero-point energy correction, and ΔS is the vibrational entropy change at finite temperature T.

Supplementary Figures

Fig. S1 XRD patterns of FeMg-ZIF-8, Fe-ZIF-8 and related samples

Fig. S2 The SEM and TEM images of ZIF-8 (a, b)

Fig. S3 The SEM and TEM images of FeMg-ZIF-8 (a, b)

Fig. S4 Aberration-corrected HAADF-STEM images of FeMg-N-C and the corresponding statistical distribution of single atom and dual atoms

Fig. S5 The 3D atomic resolution map and intensity profiles on site 1 of a typical Fe-Mg diatomic site.

Fig. S6 The SEM and TEM images of Fe-N-C (a, b)

Fig. S7 The SEM and TEM image of NC (a, b)

Fig. S8 HAADF images and corresponding EDS element mapping of Fe-N-C

Fig. S9 HAADF images and corresponding EDS element mapping of Mg-N-C

Fig. S10 High resolution spectra of the C 1s XPS peak of (a) FeMg-N-C, (b) Fe-N-C, (c) Mg-N-C and (d) NC samples

Fig. S11 High resolution spectra of the N 1s XPS peak of (a) Fe-N-C, (b) Mg-N-C and (c) NC samples

Fig. S12 Raman spectra of the FeMg-N-C, Fe-N-C, Mg-N-C and NC catalysts

Fig. S13 (a) Mg K-edge FT EXAFS spectra of FeMg-N-C and Mg-Pc. (b) Fitting results at R space

Fig. S14 Mass activity at a voltage of 0.8 and 0.9 V vs. RHE for FeMg-N-C, Fe-N-C, Mg-N-C, NC and Pt/C in alkaline solutions

Fig. S15 Nyquist plots of the FeMg-N-C catalyst and control samples in O2-saturated 0.1 M KOH solution

Fig. S16 CV curves of FeMg-N-C , Fe-N-C , Mg-N-C, and NC in the potential range of 1.0~1.1 V vs. RHE with the scan rate increasing from 10 to 50mV s-1 in N2-saturated 0.1 M KOH

Fig. S17 Corresponding electrochemical double-layer capacitance (Cdl) in N2-saturated 0.1 M KOH

Fig. S18 N2 adsorption desorption isotherm and pore size distributions of the FeMg-N-C (a, b), Fe-N-C (c, d), NC (e, f) catalysts

Fig. S19 (a) LSV curves at different rotating rates, and (b) Koutecky-Levich (K-L) plots of the FeMg-N-C catalyst in O2-saturated 0.1 M KOH solution

Fig. S20 Electron transfer number (n) and peroxide yield derived from ring-disk voltammograms (H2O2%) of the FeMg-N-C, Fe-N-C, Mg-N-C, NC and commercial Pt/C catalysts in O2-saturated 0.1 M KOH solution

Fig. S21 (a, b) TEM images, (c) Fe K-edge XANES spectra, (d) Fe K-edge FE EXAFS spectra, and (e) XRD patterns of FeMg-N-C after long-term test in alkaline solutions

Fig. S22 Aberration-corrected HAADF-STEM image and EDS elemental mapping of FeMg-N-C after stability testing in alkaline medium

Fig. S23 (a) C 1s, (b) N 1s, (c) Fe 2p and (d) Mg 1s XPS spectra of FeMg-N-C after stability testing in alkaline medium

Fig. S24 I-t chronoamperometric responses of the FeMg-N-C, and commercial Pt/C catalysts in O2-saturated 0.1 M KOH solution

Fig. S25 Tolerance to methanol of FeMg-N-C compared with 20% Pt/C at 0.70 V. Methanol is injected into the O2-saturated 0.1 M KOH electrolyte at the time of 300 s

Fig. S26 The zinc-air battery (ZAB) system used in this work

Fig. S27 Constant current discharge curves at 10 mA cm-2 of the liquid alkaline Zn-air batteries with air cathodes of the FeMg-N-C,Fe-N-C and Pt/C+RuO2 catalysts

Fig. S28 Mass activity at a voltage of 0.8 V and 0.9 V vs. RHE for FeMg-N-C, Fe-N-C, Mg-N-C, NC and Pt/C in acidic solutions

Fig. S29 Nyquist plots of the FeMg-N-C catalyst and control samples in O2-saturated 0.1 M HClO4 solution

Fig. S30 CV curves of FeMg-N-C , Fe-N-C , Mg-N-C, and NC in the potential range of 1.0~1.1 V vs. RHE with the scan rate increasing from 10 to 50 mV s-1 in N2-saturated 0.1 M HClO4

Fig. S31 Corresponding electrochemical double-layer capacitance (Cdl) in N2-saturated 0.1 M HClO4

Fig. S32 (a) LSV curves at different rotating rates, and (b) Koutecky-Levich (K-L) plots of the FeMg-N-C catalyst in O2-saturated 0.1 M HClO4 solution

Fig. S33 Electron transfer number (n) and peroxide yield derived from ring-disk voltammograms (H2O2%) of the FeMg-N-C,Fe-N-C,Mg-N-C,NC and commercial Pt/C catalysts in O2-saturated 0.1 M HClO4 solution

Fig. S34 I-t chronoamperometric responses of the FeMg-N-C, and commercial Pt/C catalysts in the acidic media

Fig. S35 (a, b) TEM images, (c) Fe K-edge XANES spectra, (d) Fe K-edge FE EXAFS spectra, and (e) XRD patterns of FeMg-N-C after long-term test in acidic solutions

Fig. S36 Aberration-corrected HAADF-STEM image and EDS elemental mapping of FeMg-N-C after stability testing in acidic medium

Fig. S37 (a) C 1s, (b) N 1s, (c) Fe 2p and (d) Mg 1s XPS spectra of FeMg-N-C after stability testing in acidic medium

Fig. S38 Tolerance to methanol of FeMg-N-C compared with 20% Pt/C at 0.70 V. Methanol is injected into the O2-saturated 0.1 M HClO4 electrolyte at the time of 300 s

Fig. S39 Comparison of H2-air fuel cell performance at begin-of-life (BOL) of FeMg-N-C and Fe-N-C cathode under 150 kPaabs of air pressure and flow rates of 700/1,700 s.c.c.m.

Fig. S40 The long-term stability of the H2-Air PEMFC tested at a constant voltage of 0.6 V

Fig. S41 XRD spectra of FeMg-N-C catalyst at different temperatures

Fig. S42 (a-c) CV curves of FeMg-N-C at the potential range of 1.0~1.1 V vs. RHE with the scan rate increasing from 10 to 50mV s-1, d) Corresponding electrochemical double-layer capacitance (Cdl) in N2-saturated 0.1 M KOH

Fig. S43 (a-c) CV curves of FeMg-N-C at the potential range of 1.0~1.1 V vs. RHE with the scan rate increasing from 10 to 50mV s-1, d) Corresponding electrochemical double-layer capacitance (Cdl) in N2-saturated 0.1 M HClO4

Fig. S44 ORR polarization curves of FeMg-N-C catalysts pyrolyzed at different temperatures in O2‑saturated 0.1 M KOH. Scan rate: 5 mV s-1; rotation rate: 1600 rpm

Fig. S45 ORR polarization curves of FeMg-N-C catalysts pyrolyzed at different temperatures in O2‑saturated 0.1 M HClO4. Scan rate: 5 mV s-1; rotation rate: 1600 rpm

Fig. S46 ORR polarization curves of FeMg-N-C catalysts with different Fe:Mg molar ratios in O2‑saturated 0.1 M KOH. Scan rate: 5 mV s-1; rotation rate: 1600 rpm

Fig. S47 ORR polarization curves of FeMg-N-C catalysts with different Fe:Mg molar ratios in O2‑saturated 0.1 M HClO4. Scan rate: 5 mV s-1; rotation rate: 1600 rpm

Fig. S48 ORR polarization curves of FeCa-N-C, FeNa-N-C, FeLi-N-C and Fe-N-C catalysts in O2‑saturated 0.1 M KOH. Scan rate: 5 mV s-1; rotation rate: 1600 rpm

Fig. S49 ORR polarization curves of FeCa-N-C, FeNa-N-C, FeLi-N-C and Fe-N-C catalysts in O2-saturated 0.1 M HClO4. Scan rate: 5 mV s-1; rotation rate: 1600 rpm

Fig. S50 ORR polarization curves of Co-N-C and MgCo-N-C catalysts in O2-saturated 0.1 M KOH. Scan rate: 5 mV s-1; rotation rate: 1600 rpm

Fig. S51 ORR polarization curves of Co-N-C and MgCo-N-C catalysts in O2-saturated 0.1 M HClO4. Scan rate: 5 mV s-1; rotation rate: 1600 rpm

Fig. S52 Digital photograph of electrochemistry operando Raman device used in this work

Fig. S53 FT-IR spectra of various samples generated during the prepared process in 0.1 M KOH

Fig. S54 FT-IR spectra of various samples generated during the prepared process in 0.1 M HClO4

Fig. S55 The curve of O2-TPD of NC

Fig. S56 EPR spectra at 77 K of the FeMg-N-C catalyst and control samples

Fig. S57 Magnetic hysteresis loops of catalysts at room temperature of Mg-N-C and NC

Fig. S58 Temperature-dependent magnetic susceptibility (𝜒-1-T) curves of Mg-N-C and NC

Fig. S59 Formation energy data calculated for different models and structural models of FeMg-N6, Fe-N4/Mg-N4-1 and Fe-N4/Mg-N4-2

Fig. S60 Partial density of States for (a) Fe-N4 and (b) FeMg-N6 moieties

Fig. S61 The total COHP for Fe-N4

Fig. S62 Optimized Fe/Mg dual-site atomic structures for the main adsorption intermediates in FeMg-N-C

Fig. S63 Optimized atomic structures for the main adsorption intermediates in Fe-N-C

Fig. S64 Diagram of ORR catalytic mechanism

Supplementary Tables

Table S1 ICP-OES results for metal contents in the obtained FeMg-N-C and the references

| Sample | Fe (wt%) | Mg (wt%) |
| --- | --- | --- |
| FeMg-N-C | 1.25 | 0.61 |
| Fe-N-C | 1.23 | / |

Table S2 EXAFS fitting parameters at the Fe K-edge and Mg K-edge

| Sample | Shell | Na | R (Å) b | σ2 (Å2·10-3) c | ΔE0 (eV) d | R-Factor |
| --- | --- | --- | --- | --- | --- | --- |
| FeMg-N-C | Fe-N | 3.8±0.2 | 2.00±0.03 | 5.8±3.5 | -1.2±0.2 | 0.031 |
| Fe -N-C | Fe-N | 3.9±0.2 | 1.99±0.02 | 4.7±3.5 | -1.3±0.2 | 0.042 |
| FeMg-N-C | Mg-N | 3.9±0.2 | 1.91±0.03 | 3.8±2.5 | -1.1±0.2 | 0.033 |
| Mg-Pc | Mg-N | 4±0.1 | 1.93±0.02 | 4.1±2.5 | -1.2±0.2 | 0.036 |

a N: coordination numbers; b R: bond distance; c σ2: Debye-Waller factors; d ΔE0: the inner potential correction.

Table S3 BET surface area and the pore size distribution results of NC, Fe-N-C, and FeMg-N-C samples

| Sample Name | BET(m2g-1) | Pore Volume (cm3g-1) |
| --- | --- | --- |
| NC | 964.5 | 0.433 |
| Fe-N-C | 932.6 | 0.888 |
| Fe Mg-N-C | 944.0 | 0.501 |

Table S4 ICP-MS analysis of electrolytes after 25-hour chronoamperometry tests over FeMg-N-C catalyst

| Electrolyte | K content (wt%) | Fe Content (wt%) | Mg Content (wt%) |
| --- | --- | --- | --- |
| 0.1 M KOH | 0.40 | Not detected | Not detected |
| 0.1 M HClO4 | -- | Not detected | Not detected |

Table S5 Comparison of ORR performance in alkaline media of FeMg-N-C with reported representative non-precious electrocatalysts

| Catalyst | Eonset (V vs. RHE) | E1/2 (V vs. RHE) | Tafel slop (mV decade-1) | Electrolyte | Reference |
| --- | --- | --- | --- | --- | --- |
| FeMg-N-C | 1.192 | 1.004 | 44 | 0.1 M KOH | This work |
| Fe1/d-CN | 1.05 | 0.950 | 54 | 0.1 M KOH | [S1] |
| Cu-Se DAs | 1.12 | 0.905 | 30.6 | 0.1 M KOH | [S2] |
| FeNb/c-SNC | - | 0.922 | 52 | 0.1 M KOH | [S3] |
| Mg-N-C | 1.03 | 0.91 | 62 | 0.1 M KOH | [S4] |
| FeSA/AC@HNC | 0.99 | 0.90 | 55 | 0.1 M KOH | [S5] |
| Fe-Sn-N/C | 1.1 | 0.92 | 69 | 0.1 M KOH | [S6] |
| Fe,Zn-N-C | - | 0.90 | 67 | 0.1 M KOH | [S7] |
| FeAl-RNC | - | 0.92 | 65.8 | 0.1 M KOH | [S8] |
| Fe1/NCP | 1.1 | 0.95 | 56.9 | 0.1 M KOH | [S9] |
| FeCo-NC-1100 | - | 0.877 | 69.06 | 0.1 M KOH | [S10] |
| NiFe-N-C | - | 0.87 | 33 | 0.1 M KOH | [S11] |
| PtFe-DAC | 1.04 | 0.935 | 67.9 | 0.1 M KOH | [S12] |
| FeI-N-CR | 1.025 | 0.915 | 52.9 | 0.1 M KOH | [S13] |
| FeMn/N-C | - | 0.928 | 97 | 0.1 M KOH | [S14] |
| Fe SAs-HP | 1.06 | 0.94 | - | 0.1 M KOH | [S15] |
| Sr/FeNC-2 | - | 0.85 | 83 | 0.1 M KOH | [S16] |
| Fe SAs/N-C | 1.02 | 0.91 | 68 | 0.1 M KOH | [S17] |
| Zn/Fe-N-C | 1.9 | 0.90 | - | 0.1 M KOH | [S18] |

Table S6 Comparison of ORR performance in acidic media of FeMg-N-C ith reported representative non-precious electrocatalysts

| Catalyst | Eonset (V vs. RHE) | E1/2 (V vs. RHE) | Tafel slop (mV decade-1) | Electrolyte | Reference |
| --- | --- | --- | --- | --- | --- |
| FeMg-N-C | 1.053 | 0.881 | 55 | 0.1 M HClO4 | This work |
| FeSA/AC@HNC | 0.88 | 0.78 | 66 | 0.5 M H2SO4 | [S5] |
| Fe,Zn-N-C | - | 0.79 | 84 | 0.5 M H2SO4 | [S7] |
| FeAl-RNC | - | 0.83 | 128.8 | 0.5 M H2SO4 | [S8]. |
| FeMn/N-C | - | 0.804 | 79 | 0.1 M HClO4 | [S14] |
| Fe SAs-HP | 0.90 | 0.78 | - | 0.1 M HClO4 | [S15] |
| Fe SAs/N-C | 0.95 | 0.798 | 66 | 0.1 M HClO4 | [S17] |
| Zn/Fe-N-C | 0.95 | 0.81 | - | 0.1 M HClO4 | [S18] |
| (Fe,Co)/N-C | 1.06 | 0.863 | 66 | 0.1 M HClO4 | [S19] |

Table S7 The performance comparison Zn-air batteries

| Catalyst | Peak power density (mW cm-2) | Specific capacity@10 mA cm-2 (mA h g Zn-1 ) | Reference |
| --- | --- | --- | --- |
| FeMg-N-C | 530.1 | 802.4 | This work |
| Fe1/d-CN | 144 | 770 | [S1] |
| Cu-Se DAs | 206.5 | 809.3 | [S2] |
| FeNb/c-SNC | 314.3 | - | [S3] |
| FeSA/AC@HNC | 171.5 | 811.8 | [S5] |
| Fe,Zn-N-C | 211.7 | 856.6 | [S7] |
| Fe1/NCP | 263.8 | 713.1 | [S9] |
| FeCo-NC-1100 | 372 | - | [S10] |
| NiFe-N-C | 153 | 818 | [S11] |
| PtFe-DAC | 192 | 780 | [S12] |
| FeI-N-CR | 197.9 | - | [S13] |
| FeMn/N-C | 160.8 | - | [S14] |
| Fe SAs-HP | 254.2 | - | [S15] |
| Fe SAs/N-C | 225 | 636 | [S17] |

Table S8 Performance comparison of H2-O2 fuel cell employing non-precious metal catalyst as the cathode

| Catalyst | Cathode catalyst Loading (mg cm-2) | Test condition | Current density (mA cm-2) @ 0.9 V | Peak power density (W cm-2) | Reference |
| --- | --- | --- | --- | --- | --- |
| FeMg-N-C | 4 | 150 kPa, 100% RH, 353 K | 45.1 | 1.06 | This work |
| Fe SAs/N-C | 2 | 200 kPa, 100% RH, 353 K | - | 0.75 | [S17] |
| (Fe,Co)/N-C | 0.77 | 200 kPa, 100% RH, 353 K | - | 0.98 | [S19] |
| Fe-N-C-FG | 4.5 | 150 kPa, 75% RH, 353 K | 50.8 | - | [S20] |
| Fe-AC | 5 | 100 kPa, 100% RH, 353 K | 44.2 | - | [S21] |
| OP-Fe-NC | 4 | 200 kPa, 100% RH, 353 K | 29 | 0.937 | [S22] |
| Co4/Fe1@NC | 3 | 150 kPa, 100% RH, 353 K | 33.4 | 0.84 | [S23] |
| sur-FeN4-HPC | 4 | 100 kPa, 100% RH, 353 K | 24.2 | 0.79 | [S24] |
| Fe-N-C-Phen-PANI | 5 | 200 kPa, 100% RH, 353 K | - | 1.06 | [S30] |
| Fe2-Z8-C | 2.8 | 250/200 kPa, 100% RH, 353 K | - | 1.141/1.110 | [S31] |
| Fe/N/C(4mlm) | 3 | 100/200 kPa, 100% RH, 353 K | - | 1.12/1.33 | [S33] |
| Fe-HMT@Z8 | 2.8 | 150 kPa, 100% RH, 353 K | 28 | 1.355 | [S34] |
| Fe/N/C-Recry | 3 | 200 kPa, 100% RH, 353 K | 62 | 1.36 | [S35] |
| Feg-NC/Phen | 4.41 | 200 kPa, 100% RH, 353 K | 46 | 1.53 | [S36] |
| Fe-NCBrCl | 3.5 | 250 kPa, 100% RH, 353 K | 54 | 1.86 | [S37] |

Table S9 Performance comparison of H2-air fuel cell employing non-precious metal catalyst as the cathode

| Catalyst | Cathode catalyst Loading (mg cm-2) | Test condition | Current density (mA cm-2) @ 0.8 V | Peak power density (W cm-2) | Stability Performance | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| FeMg-N-C | 4 | 150 kPa，100% RH, 353 K | 120.0 | 609.92 | 150 h / 50% @0.6V | This work |
| Fe SAs/N-C | 2 | 200 kPa，100% RH, 353 K | - | 350 | - | [S17] |
| (Fe,Co)/N-C | 0.77 | 200 kPa，100% RH, 353 K | - | 505 | 100 h / - | [S19] |
| Fe-N-C-FG | 4.5 | 150 kPa，100% RH, 353 K | 191.0 | 501 | 200 h / 43% @0.67V | [S20] |
| Fe-AC | 5 | 100 kPa，100% RH, 353 K | 151.0 | 601 | 200 h / 20% @0.67V | [S21] |
| 1.5Fe-ZIF | 4 | 100 kPa，100% RH, 353 K | 76 | 360 | 118 h / 50% @0.7V | [S25] |
| ZIF-NC-0.5Fe-700 | 3.5 | 150 kPa，100% RH, 353 K | 78 | 320 | - | [S26] |
| FeNx/Gp | 4 | 200 kPa，100% RH, 353 K | 70 | 430 | 100 h / 37.5% @0.4V | [S27] |
| FeCl2-/NC-1000 | 4 | 100 kPa，100% RH, 353 K | 37 | 280 | - | [S28] |
| Fe-N-C-Phen-PANI | 5 | 200 kPa，100% RH, 353 K | - | 380 | - | [S30] |
| TPI@Z8(SiO2)-650-C | 2 | 100 kPa，100% RH, 353 K | 105 | 420 | 120 h / 62% @0.5V | [S32] |
| Fe/N/C(4mlm) | 3 | 100/200 kPa，100% RH, 353 K | - | 467/538 | - | [S33] |
| Fe/N/C-Recry | 3 | 200 kPa，100% RH, 353 K | - | 650 | - | [S35] |
| Feg-NC/Phen | 4.41 | 100 kPa，100% RH, 353 K | - | 710 | 25 h / 15% @0.6V | [S36] |
| Fe-NCBrCl | 3.5 | 250 kPa，100% RH, 353 K | 259 | 880 | - | [S37] |

Table S10 The ICOP of Fe 2p -O 2p for FeMg-N-C and Fe-N-C

|  | FeMg-N-C | Fe-N-C |
| --- | --- | --- |
| Spin-up | -1.00 | -1.17 |
| Spin-down | -1.62 | -1.74 |

Supplementary References

- C. Li, Y. Zhang, M. Yuan, Y. Liu, H. Lan et al., A pH-universal ORR catalyst with S heteroatom doping single-atom iron sites derived from a 2D flake-like MOF for superior flexible quasi-solid-state rechargeable Zn-air battery. Chem. Eng. J. 471, 144515 (2023). https://doi.org/10.1016/j.cej.2023.144515

- Z. Sun, H. Zhang, L. Cao, X. Liu, D. Wu et al., Understanding synergistic catalysis on Cu-Se dual atom sites via operando x-ray absorption spectroscopy in oxygen reduction reaction. Angew. Chem. Int. Ed. 62, e202217719 (2023). https://doi.org/10.1002/anie.202217719

- R. Sui, B. Liu, C. Chen, X. Tan, C. He et al., Constructing asymmetric Fe-Nb diatomic sites to enhance ORR activity and durability. J. Am. Chem. Soc. 146, 26442-26453 (2024). https://doi.org/10.1021/jacs.4c09642

- S. Liu, Z. Li, C. Wang, W. Tao, M. Huang et al., Turning main-group element magnesium into a highly active electrocatalyst for oxygen reduction reaction. Nat. Commun. 11, 938 (2020). https://doi.org/10.1038/s41467-020-14565-w

- H. Zhang, H.-C. Chen, S. Feizpoor, L. Li, X. Zhang et al., Tailoring oxygen reduction reaction kinetics of Fe-N-C catalyst via spin manipulation for efficient zinc-air batteries. Adv. Mater. 36, 2400523 (2024). https://doi.org/10.1002/adma.202400523

- V. Krishnamoorthy, P. Sabhapathy, P. Raghunath, C.-Y. Huang, A. Sabbah et al., Synergistic electronic interaction of nitrogen coordinated fe-sn double-atom sites: an efficient electrocatalyst for oxygen reduction reaction. Small Methods 8, 2301674 (2024). https://doi.org/10.1002/smtd.202301674

- L. Wang, Z. Mei, Q. An, X. Sheng, Q. Jing et al., Modulating the electronic spin state of atomically dispersed iron sites by adjacent zinc atoms for enhanced spin-dependent oxygen electrocatalysis. Chem Catal. 3, 100758 (2023). https://doi.org/10.1016/j.checat.2023.100758

- Y. Liu, J. Li, Z. Lv, H. Fan, F. Dong et al., Efficient proton-exchange membrane fuel cell performance of atomic Fe sites via p-d hybridization with Al dopants. J. Am. Chem. Soc. 146, 12636-12644 (2024). https://doi.org/10.1021/jacs.4c01598

- S. Ji, Y. Mou, H. Liu, X. Lu, Y. Zhang et al., Manipulating the electronic properties of an fe single atom catalyst via secondary coordination sphere engineering to provide enhanced oxygen electrocatalytic activity in zinc-air batteries. Adv. Mater. 36, 2410121 (2024). https://doi.org/10.1002/adma.202410121

- Y. He, X. Yang, Y. Li, L. Liu, S. Guo et al., Atomically dispersed Fe-Co dual metal sites as bifunctional oxygen electrocatalysts for rechargeable and flexible Zn-air batteries. ACS Catal. 12, 1216-1227 (2022). https://doi.org/10.1021/acscatal.1c04550

- H. Meng, B. Wu, D. Zhang, X. Zhu, S. Luo et al., Optimizing electronic synergy of atomically dispersed dual-metal Ni-N4 and Fe-N4 sites with adjacent Fe nanoclusters for high-efficiency oxygen electrocatalysis. Energy Environ. Sci. 17, 704-716 (2024). https://doi.org/10.1039/d3ee03383j

- Z. Zhang, Y. Dai, P. Guo, B. Liu, Y. Xia et al., Noncovalent Assembly Strategy for Efficient Synthesis of Dual-Atom Catalysts. Adv. Funct. Mater. 34, 2407128 (2024). https://doi.org/10.1002/adfm.202407128

- M. Du, B. Chu, Q. Wang, C. Li, Y. Lu et al., Dual Fe/I Single-Atom Electrocatalyst for High-Performance Oxygen Reduction and Wide-Temperature Quasi-Solid-State Zn-Air Batteries. Adv. Mater. 36, 2412978 (2024). https://doi.org/10.1002/adma.202412978

- G. Yang, J. Zhu, P. Yuan, Y. Hu, G. Qu et al., Regulating Fe-spin state by atomically dispersed Mn-N in Fe-NC catalysts with high oxygen reduction activity. Nat. Commun. 12, 1734 (2021). https://doi.org/10.1038/s41467-021-21919-5

- P. Zhang, H.-C. Chen, H. Zhu, K. Chen, T. Li et al., Inter-site structural heterogeneity induction of single atom Fe catalysts for robust oxygen reduction. Nat. Commun. 15, 2062 (2024). https://doi.org/10.1038/s41467-024-46389-3

- W. Li, J. Jiang, Z. Huang, Z. Wang, W. Zhou et al., Strontium doped Fe-based porous carbon for highly efficient electrocatalytic ORR and MOR reactions. J. Colloid Interface Sci. 659, 799-810 (2024). https://doi.org/10.1016/j.jcis.2024.01.042

- Z. Yang, Y. Wang, M. Zhu, Z. Li, W. Chen et al., Boosting Oxygen Reduction Catalysis with Fe-N4 Sites Decorated Porous Carbons toward Fuel Cells. ACS Catal. 9, 2158-2163 (2019). https://doi.org/10.1021/acscatal.8b04381

- F. Xiao, G.-L. Xu, C.-J. Sun, M. Xu, W. Wen et al., Nitrogen-coordinated single iron atom catalysts derived from metal organic frameworks for oxygen reduction reaction. Nano Energy 61, 60-68 (2019). https://doi.org/10.1016/j.nanoen.2019.04.033

- J. Wang, Z. Huang, W. Liu, C. Chang, H. Tang et al., Design of N-Coordinated Dual-Metal Sites: A Stable and Active Pt-Free Catalyst for Acidic Oxygen Reduction Reaction. J. Am. Chem. Soc. 139, 17281-17284 (2017). https://doi.org/10.1021/jacs.7b10385

- Y. Zeng, C. Li, B. Li, J. Liang, M. J. Zachman et al., Tuning the thermal activation atmosphere breaks the activity-stability trade-off of Fe-N-C oxygen reduction fuel cell catalysts. Nat. Catal. 6, 1215-1227 (2023). https://doi.org/10.1038/s41929-023-01062-8

- S. Liu, C. Li, M. J. Zachman, Y. Zeng, H. Yu et al., Atomically dispersed iron sites with a nitrogen-carbon coating as highly active and durable oxygen reduction catalysts for fuel cells. Nat. Energy 7, 652-663 (2022). https://doi.org/10.1038/s41560-022-01062-1

- J. Li, W. Xia, X. Xu, D. Jiang, Z.-X. Cai et al., Selective etching of metal-organic frameworks for open porous structures: mass-efficient catalysts with enhanced oxygen reduction reaction for fuel cells. J. Am. Chem. Soc. 145, 27262-27272 (2023). https://doi.org/10.1021/jacs.3c05544

- A. Han, W. Sun, X. Wan, D. Cai, X. Wang et al., Construction of Co4 Atomic Clusters to Enable Fe-N4 Motifs with Highly Active and Durable Oxygen Reduction Performance. Angew. Chem. Int. Ed. 62, e202303185 (2023). https://doi.org/10.1002/anie.202303185

- G. Chen, Y. An, S. Liu, F. Sun, H. Qi et al., Highly accessible and dense surface single metal FeN4 active sites for promoting the oxygen reduction reaction. Energy Environ. Sci. 15, 2619-2628 (2022). https://doi.org/10.1039/d2ee00542e

- H. Zhang, H. T. Chung, D. A. Cullen, S. Wagner, U. I. Kramm et al., High-performance fuel cell cathodes exclusively containing atomically dispersed iron active sites. Energy Environ. Sci. 12, 2548-2558 (2022). https://doi.org/10.1039/C9EE00877B

- J. Li, H. Zhang, W. Samarakoon, W. Shan, D. A. Cullen et al., Thermally Driven Structure and Performance Evolution of Atomically Dispersed FeN4 Sites for Oxygen Reduction. Angew. Chem. Int. Ed. 58, 18971-18980 (2019). https://doi.org/10.1002/anie.201909312

- X. Fu, N. Li, B. Ren, G. Jiang, Y. Liu et al., Tailoring FeN4 Sites with Edge Enrichment for Boosted Oxygen Reduction Performance in Proton Exchange Membrane Fuel Cell. Adv. Energy Mater. 9, 1803737 (2019). https://doi.org/10.1002/aenm.201803737

- J. Li, L. Jiao, E. Wegener, L. L. Richard, E. Liu et al., Evolution Pathway from Iron Compounds to Fe1(II)-N4 Sites through Gas-Phase Iron during Pyrolysis. J. Am. Chem. Soc. 142, 1417-1423 (2020). https://doi.org/10.1021/jacs.9b11197

- Y. Li, X. Liu, L. Zheng, J. Shang, X. Wan et al., Preparation of Fe-N-C catalysts with FeNx (x= 1, 3, 4) active sites and comparison of their activities for the oxygen reduction reaction and performances in proton exchange membrane fuel cells. J. Mater. Chem. A 7, 26147-26153 (2019). https://doi.org/10.1039/C9TA08532G

- X. Fu, P. Zamani, J.-Y. Choi, F. M. Hassan, G. Jiang et al., In situ polymer graphenization ingrained with nanoporosity in a nitrogenous electrocatalyst boosting the performance of polymer-electrolyte-membrane fuel cells. Adv. Mater. 29, 1604456 (2017). https://doi.org/10.1002/adma.201604456

- Q. Liu, X. Liu, L. Zheng, J. Shui, The Solid-Phase Synthesis of an Fe-N-C Electrocatalyst for High-Power Proton-Exchange Membrane Fuel Cells. Angew. Chem. Int. Ed. 57, 1204-1208 (2018). https://doi.org/10.1002/anie.201709597

- X. Wan, X. Liu, Y. Li, R. Yu, L. Zheng et al., Fe-N-C electrocatalyst with dense active sites and efficient mass transport for high-performance proton exchange membrane fuel cells. Nat. Catal. 2, 259 (2019). https://doi.org/10.1038/s41929-019-0237-3

- Y. Li, P. Zhang, L. Wan, Y. Zheng, X. Qu et al., A general carboxylate-assisted approach to boost the ORR performance of ZIF-derived Fe/N/C catalysts for proton exchange membrane fuel cells. Adv. Funct. Mater. 31, 2009645 (2021). https://doi.org/10.1002/adfm.202009645

- W. Li, X. Wan, X. Guo, Q. Liu, Y. Wang et al., Large 3D network of concave Fe-NC nanoparticles by nano-welding for high-power fuel cells. Sci. China Chem. 68, 2081-2087 (2025). https://doi.org/10.1007/s11426-024-2397-6

- Y. Wu, M. Yuan, X. Li, R. Ding, X. Duan et al., Assistance of rearrangement of active sites in Fe/N/C catalyst for harvesting ultra-high power density PEMFCs. Appl. Catal. B-Environ. 312, 121365 (2022). https://doi.org/10.1016/j.apcatb.2022.121365

- S.-H. Yin, S.-L. Yang, G. Li, G. Li, B.-W. Zhang et al., Seizing gaseous Fe2+ to densify O2-accessible Fe-N4 sites for high-performance proton exchange membrane fuel cells Energy Environ. Sci. 15, 3033-3040 (2022). https://doi.org/10.1039/D2EE00061J

- S. Yin, L. Chen, J. Yang, X. Cheng, H. Zeng et al., A Fe-NC electrocatalyst boosted by trace bromide ions with high performance in proton exchange membrane fuel cells. Nat. Commun. 15, 7489 (2024). https://doi.org/10.1038/s41467-024-51858-w

- Y. Zeng, C. Li, B. Li, J. Liang, M. J. Zachman et al., Tuning the thermal activation atmosphere breaks the activity-stability trade-off of Fe-N-C oxygen reduction fuel cell catalysts. Nat. Catal. 6, 1215-1227 (2023). https://doi.org/10.1038/s41929-023-01062-8