Supporting Information for

Diamine-Mediated Synergistic Engineering of Orientation and Interfacial Field of 3D/1D Heterojunctions for Efficient Perovskite Photovoltaics

Yaobin Li1#, Yunxuan Cao1#, Yu Zou1,2*, Wenjin Yu4, Zhenhuang Su5, Zhuoer Cai6, Yueli Liu1, Qinyun Liu1, Hantao Wang1, Lefan Gong1, Yucheng Ye1, Rong Tang1, Yunan Gao1, Felix Thomas Eickemeyer4, Bo Qu1*, Lixin Xiao1,3*, Zhijian Chen1*

1State Key Laboratory for Artificial Microstructures and Mesoscopic Physics, School of Physics, Peking University, Beijing 100871, P. R. China

2Future Photovoltaics Research Center, Global Institute of Future Technology (GIFT), Shanghai Jiao Tong University, Shanghai 200240, P. R. China

3AI for Science (AI4S)-Preferred Program, Peking University Shenzhen Graduate School, Shenzhen 518055, P. R. China

4Laboratory of Photonics and Interfaces, Institute of Chemical Sciences and Engineering, École Polytechnique Fédérale de Lausanne (EPFL), Lausanne, Switzerland

5Shanghai Synchrotron Radiation Facility (SSRF), Shanghai Advanced Research Institute, Chinese Academy of Sciences, Shanghai 201204, P. R. China

6School of Chemistry and Chemical Engineering, Southeast University, Nanjing 211189, P. R. China

#Yaobin Li and Yunxuan Cao contributed equally to this work.

*Corresponding authors. E-mail: yu.zou@sjtu.edu.cn (Yu Zou); bqu@pku.edu.cn (Bo Qu); lxxiao@pku.edu.cn (Lixin Xiao); zjchen@pku.edu.cn (Zhijian Chen)

Supplementary Figures and Tables

Fig. S1 Chemical Structures of PDAI2 (a) and 4APyCl (b)

Fig. S2 Gaussian electrostatic potential of 4APy+

Fig. S3 XRD of PbI2, PDAI2, PDAI2:PbI2 mixture and 4APyCl:PbI2 mixture

Fig. S4 XRD patterns of 3D/PDAI2 with different concentration of PDAI2

Fig. S5 XRD of PbI2, 4APyCl, 4APyCl:PbI2 mixture

Fig. S6 XRD of PbI2, 4APyI, 4APyI:PbI2 mixture

Fig. S7 SEM images of perovskites with different post-treatments

Fig. S8 AFM images of perovskite films with different post-treatments

Fig. S9 Grain size distribution and average grain size of perovskite films with different post-treatments

Fig. S10 Crystal structure of 2D perovskite 4APyPbI4

Note S1 During the crystal synthesis, HI further protonates the nitrogen atom on the pyridine ring of 4APy+, converting it into 4APy2+, which then reacts with PbI2 to form the DJ-type 2D perovskite 4APyPbI4. In contrast, DMF does not protonate 4APy+ during the synthesis process, resulting in the formation of slender 1D perovskite crystals, (4APy)2PbI4. The single-crystal XRD results of (4APy)2PbI4 are consistent with the GIWAXS data of the 3D/4APyCl sample (Fig. 2e).

Fig. S11 The photoelectric properties of the 1D perovskite (4APy)2PbI4

Fig. S12 Tauc plot of perovskites with different post-treatment

Fig. S13 The stability of 1D perovskite (4APy)2PbI4 in air

Fig. S14 UPS results of perovskite films with different post-treatments

Fig. S15 Energy band structure diagram with a unified vacuum energy level

Fig. S16 EC-EF value of perovskite films with different post-treatments

Fig. S17 Cross-sectional SEM image of device of Figure 5a

Fig. S18 Reverse and forward J-V scan of champion PSCs with 4 structures of Figure 5b

Fig. S19 EQE curve of PSC with 3D/PDAI2/1D heterojunction of Figure 5b (Integral JSC is 24.00 mA cm-2)

Fig. S20 Stabilized power output of PSC with 3D/PDAI2/1D heterojunction of Figure 5b

Fig. S21 Box plots of a VOC, b JSC, c FF and d PCE of PSCs with different PDAI2 concentrations

Fig. S22 Box plots of a VOC, b JSC, c FF and d PCE of PSCs with different 4APyCl concentration

## Table S1. Crystal data and structure refinement for (4APy)2PbI4 single crystal.

| Compound | (4APy)2PbI4 |
| --- | --- |
| Empirical formula | C12H16I4N6Pb |
| Formula weight | 959.10 |
| Temperature [K] | 226(7) |
| Crystal system | monoclinic |
| Space group (number) | P21/n (14) |
| a [Å] | 4.0389(7) |
| b [Å] | 10.4245(19) |
| c [Å] | 21.865(4) |
| α [°] | 90 |
| β [°] | 94.015(17) |
| γ [°] | 90 |
| Volume [Å3] | 918.3(3) |
| Z | 2 |
| F(000) | 848 |

Table S2 Atomic coordinates and Ueq [Å2] for (4APy)2PbI4 single crystal

| Atom | x | y | z | Ueq |
| --- | --- | --- | --- | --- |
| Pb1 | 0.500000 | 1.000000 | 0.500000 | 0.0300(10) |
| I2 | 0.0374(16) | 0.9918(4) | 0.5961(3) | 0.1249(17) |
| I1 | 0.5432(15) | 0.7285(6) | 0.49780(19) | 0.151(2) |
| C5 | 1.1212(16) | 0.6685(3) | 0.35225(18) | 0.026(3) |
| H5 | 1.123896 | 0.690961 | 0.393917 | 0.032 |
| N3 | 1.1839(19) | 0.7370(3) | 0.24835(12) | 0.032(3) |
| N2 | 0.8233(18) | 0.4796(10) | 0.42806(16) | 0.031(4) |
| H2A | 0.785914 | 0.421111 | 0.455121 | 0.037 |
| H2B | 0.785077 | 0.559884 | 0.435819 | 0.037 |
| C3 | 0.959(2) | 0.5257(4) | 0.26737(9) | 0.029(4) |
| H3 | 0.869556 | 0.448107 | 0.251653 | 0.035 |
| C6 | 1.230(2) | 0.7533(5) | 0.30844(10) | 0.033(4) |
| H6 | 1.343917 | 0.827365 | 0.322620 | 0.039 |
| C1 | 0.9341(15) | 0.4476(2) | 0.37704(13) | 0.031(4) |
| C4 | 1.0481(16) | 0.6234(3) | 0.2295(2) | 0.033(4) |
| H4 | 1.012000 | 0.610388 | 0.186976 | 0.039 |
| C2 | 1.0075(19) | 0.5480(3) | 0.33106(10) | 0.030(3) |
| N1 | 0.999(3) | 0.3286(3) | 0.3612(4) | 0.025(4) |
| H1A | 0.967095 | 0.265788 | 0.386323 | 0.030 |
| H1B | 1.074728 | 0.312874 | 0.325647 | 0.030 |

Ueq is defined as 1/3 of the trace of the orthogonalized Uij tensor.

Table S3 Fitting parameters of the TRPL spectra for the PVK films with different surface treatment

| Sample | τavg (ns) | τ1 (ns) | A1 (%) |  | τ2 (ns) | A2 (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 3D | 783.96 | 97.99 | 19.89 | 804.70 |  | 80.11 |
| 3D/1D | 2901.55 | 130.01 | 9.70 | 2914.83 |  | 90.30 |
| 3D/PDAI2/1D | 3301.49 | 191.26 | 4.83 | 3310.60 |  | 95.17 |

Note S2

TRPL decay curves are fitted by bi-exponential function:

ft=A1exp-t/τ1+A2exp-t/τ2

where τ1 and τ2 represent the lifetimes of charge carriers in distinct relaxation pathways, A1 and A2 are corresponding decay amplitudes. The average carrier lifetime τavg are calculated by function:

τavg=(A1τ12+A2τ22)/(A1τ1+A2τ2)

Table S4 Photovoltaic parameters of Champion PSCs with 4 structures of Figure 5b

| Structure | Scan | Voc (V) | Jsc (mA·cm-2) | FF (%) | PCE (%) | HI |
| --- | --- | --- | --- | --- | --- | --- |
| 3D | R | 1.102 | 24.3 | 82.9 | 22.2 | 0.05 |
|  | F | 1.100 | 23.9 | 79.9 | 21.0 |  |
| 3D/PDAI2 | R | 1.156 | 25.2 | 81.2 | 23.6 | 0.03 |
|  | F | 1.141 | 24.7 | 81.3 | 22.9 |  |
| 3D/1D | R | 1.115 | 25.3 | 84.0 | 23.7 | 0.03 |
|  | F | 1.116 | 25.0 | 82.4 | 23.0 |  |
| 3D/PDAI2/1D | R | 1.167 | 25.0 | 83.3 | 24.3 | 0.02 |
|  | F | 1.154 | 24.7 | 83.5 | 23.8 |  |

R represents Reverse scan, and F represents Forward scan.

Table S5 Photovoltaic parameters PSCs of Figure 5f

| Structure | Scan | Voc (V) | Jsc (mA·cm-2) | FF (%) | PCE (%) | HI |
| --- | --- | --- | --- | --- | --- | --- |
| 3D/PDAI2/1D | R | 1.170 | 26.0 | 84.9 | 25.8 | 0.01 |
|  | F | 1.170 | 25.9 | 84.4 | 25.6 |  |

R represents Reverse scan, and F represents Forward scan.

Table S6 Summary of recently reported PSCs containing 3D/1D heterojunction (PCE>20%)

| 1D ligand | Device (Bulk/Interface) | PCE (%) | Refs. |
| --- | --- | --- | --- |
| DEAECl | n-i-p (Bulk) | 22.90 | [S1] |
| HABr | n-i-p(Bulk) | 21.20 | [S2] |
| TPI | p-i-n(Bulk) | 22.90 | [S3] |
| EMIMTFA | n-i-p(Bulk) | 22.14 | [S4] |
| TA-NI | n-i-p(Interface) | 23.84 | [S5] |
| Me3SI | n-i-p(Bulk) | 22.07 | [S6] |
| CBAH | n-i-p(Interface) | 21.95 | [S7] |
| p-PBAI2 | n-i-p(Interface) | 23.84 | [S8] |
| BnI | p-i-n(Bulk) | 21.17 | [S9] |
| Phen | n-i-p(Interface) | 23.30 | [S10] |
| BPy | n-i-p(Bulk) | 21.18 | [S11] |
| PAI | n-i-p(Interface) | 21.19 | [S12] |
| PyI | n-i-p(Interface) | 23.10 | [S13] |
| HDI | p-i-n(Interface) | 25.30 | [S14] |
| TBAAc | n-i-p(Interface) | 20.10 | [S15] |
| PyBr | n-i-p(Interface) | 23.74 | [S16] |
| TMA-TFSI | n-i-p(Interface) | 23.15 | [S17] |
| MTIm | p-i-n(Both) | 23.80 | [S18] |
| Benzimidazolium | n-i-p(Interface) | 24.43 | [S19] |
| CPMIMCl | n-i-p(Interface) | 24.13 | [S20] |
| PFACl | n-i-p(Interface) | 24.90 | [S21] |
| SMORCl | p-i-n(Interface) | 25.60 | [S22] |
| DMIMBF4 | n-i-p(Interface) | 24.75 | [S23] |
| 2ADPCl | n-i-p(Interface) | 24.55 | [S24] |
| C6I | n-i-p(Interface) | 23.11 | [S25] |
| BzMIMI | p-i-n(Interface) | 24.09 | [S26] |
| ABTI | p-i-n(Bulk) | 23.27 | [S27] |
| 4APyCl | p-i-n(Interface) | 25.80 | This work |

“Bulk/Interface” denotes the location where the 3D/1D heterojunction exists.

Supplementary References

- T. Kong, H. Xie, Y. Zhang, J. Song, Y. Li et al., Perovskitoid-templated Formation of a 1D@3D perovskite structure toward highly efficient and stable perovskite solar cells. Adv. Energy Mater. 11(34), 2101018 (2021). https://doi.org/10.1002/aenm.202101018

- S. Yu, H. Liu, S. Wang, H. Zhu, X. Dong et al., Hydrazinium cation mixed FAPbI3- based perovskite with 1D/3D hybrid dimension structure for efficient and stable solar cells. Chem. Eng. J. 403, 125724 (2021). https://doi.org/10.1016/j.cej.2020.125724

- H. Jiao, Z. Ni, Z. Shi, C. Fei, Y. Liu et al., Perovskite grain wrapping by converting interfaces and grain boundaries into robust and water-insoluble low-dimensional perovskites. Sci. Adv. 8(48), eabq4524 (2022). https://doi.org/10.1126/sciadv.abq4524

- N. Wei, Y. Chen, X. Wang, Y. Miao, Z. Qin et al., Multi-level passivation of MAPbI3 perovskite for efficient and stable photovoltaics. Adv. Funct. Mater. 32(16), 2108944 (2022). https://doi.org/10.1002/adfm.202108944

- Z. Chen, Q. Cheng, H. Chen, Y. Wu, J. Ding et al., Perovskite grain-boundary manipulation using room-temperature dynamic self-healing “ligaments” for developing highly stable flexible perovskite solar cells with 23.8% efficiency. Adv. Mater. 35(18), 2300513 (2023). https://doi.org/10.1002/adma.202300513

- C. Ge, J.-F. Lu, M. Singh, A. Ng, W. Yu et al., Mixed dimensional perovskites heterostructure for highly efficient and stable perovskite solar cells. Sol. RRL 6(4), 2100879 (2022). https://doi.org/10.1002/solr.202100879

- J. Wang, L. Liu, S. Chen, L. Qi, M. Zhao et al., Growth of 1D nanorod perovskite for surface passivation in FAPbI3 perovskite solar cells. Small 18(3), 2104100 (2022). https://doi.org/10.1002/smll.202104100

- J. Chen, Y. Yang, H. Dong, J. Li, X. Zhu et al., Highly efficient and stable perovskite solar cells enabled by low-dimensional perovskitoids. Sci. Adv. 8(4), eabk2722 (2022). https://doi.org/10.1126/sciadv.abk2722

- Y. Zhan, F. Yang, W. Chen, H. Chen, Y. Shen et al., Elastic lattice and excess charge carrier manipulation in 1D–3D perovskite solar cells for exceptionally long-term operational stability. Adv. Mater. 33(48), 2105170 (2021). https://doi.org/10.1002/adma.202105170

- Q. Chen, K. Deng, Y. Shen, L. Li, Stable one dimensional (1D)/three dimensional (3D) perovskite solar cell with an efficiency exceeding 23%. InfoMat 4(5), e12303 (2022). https://doi.org/10.1002/inf2.12303

- P. Liu, Y. Xian, W. Yuan, Y. Long, K. Liu et al., Lattice-matching structurally-stable 1D@3D perovskites toward highly efficient and stable solar cells. Adv. Energy Mater. 10(17), 1903654 (2020). https://doi.org/10.1002/aenm.201903654

- N. Yang, C. Zhu, Y. Chen, H. Zai, C. Wang et al., An in situ cross-linked 1D/3D perovskite heterostructure improves the stability of hybrid perovskite solar cells for over 3000 h operation. Energy Environ. Sci. 13(11), 4344–4352 (2020). https://doi.org/10.1039/D0EE01736A

- H.B. Lee, A. Mohamed, N. Kumar, N.H. Zain Karimy, V.V. Satale et al., Low-cost, scalable fabrication of multi-dimensional perovskite solar cells and modules assisted by mechanical scribing. Small Methods 9(1), 2400850 (2025). https://doi.org/10.1002/smtd.202400850

- Y. Zhao, Y.-C. Ye, X.-M. Chen, J.-G. Wang, L.-J. Zhang et al., Surface impurity healing by the formation of 1D/3D perovskite heterojunctions for inverted perovskite solar cells. ACS Sustainable Chem. Eng. 13(32), 13148–13156 (2025). https://doi.org/10.1021/acssuschemeng.5c06468

- A. Mei, X. Peng, X. Li, G. Zhang, S. Lin et al., Anions regulation of 1D perovskite intrusion-behavior for efficient and stable perovskite solar cells. ACS Appl. Mater. Interfaces 16(24), 31209–31217 (2024). https://doi.org/10.1021/acsami.4c06087

- J. Cha, C. Beom Lee, S. Min Park, D. Baek, S. Kim et al., Lattice-matched in-situ-formed 1D perovskite phase in Multi-dimensional solar cells achieving high phase stability and favorable energy landscape. Chem. Eng. J. 484, 149280 (2024). https://doi.org/10.1016/j.cej.2024.149280

- S.-K. Jung, K. Park, J.-H. Lee, S.-G. Choi, J.S. Choi et al., Exploiting an interfacial reaction in perovskite solar cells: quaternary alkylammonium ionic salt dopants for spiro-OMeTAD. Adv. Energy Mater. 15(2), 2402144 (2025). https://doi.org/10.1002/aenm.202402144

- C. Zhou, F. Wang, X. Ai, Y. Liu, Y. Han et al., Dual interfacial modification with 1D perovskite for self-assembled monolayer based inverted perovskite solar cells. Nano Energy 128, 109811 (2024). https://doi.org/10.1016/j.nanoen.2024.109811

- R. Chen, H. Shen, Q. Chang, Z. Tang, S. Nie et al., Conformal imidazolium 1D perovskite capping layer stabilized 3D perovskite films for efficient solar modules. Adv. Sci. 9(36), 2204017 (2022). https://doi.org/10.1002/advs.202204017

- F. Wang, D. Duan, K. Zhou, Y.Z.B. Xue, X. Liang et al., Ionic liquid engineering enabled in-plane orientated 1D perovskite nanorods for efficient mixed-dimensional perovskite photovoltaics. InfoMat 5(8), e12459 (2023). https://doi.org/10.1002/inf2.12459

- F. Ye, T. Tian, J. Su, R. Jiang, J. Li et al., Tailoring low-dimensional perovskites passivation for efficient two-step-processed FAPbI3 solar cells and modules. Adv. Energy Mater. 14(4), 2302775 (2024). https://doi.org/10.1002/aenm.202302775

- S. Li, H. Gu, A. Zhu, J. Guo, C. Xi et al., Anion-cation synergistic regulation of low-dimensional perovskite passivation layer for perovskite solar cells. Adv. Mater. 37(28), 2500988 (2025). https://doi.org/10.1002/adma.202500988

- F. Wang, K. Zhou, C. Zhou, X. Liang, T. Wang et al., Ionic liquid-induced 1D perovskite: exploring 1D perovskite structure to 1D/3D heterojunction-based photovoltaics. Adv. Energy Mater. 14(23), 2400021 (2024). https://doi.org/10.1002/aenm.202400021

- X. Zhou, X. Liang, F. Wang, H. Sun, Q. Zhu et al., Pyridine substitution strategy for one-dimensional perovskite: Toward efficient and stable mixed-dimensional photovoltaics. Chem. Eng. J. 493, 152539 (2024). https://doi.org/10.1016/j.cej.2024.152539

- Y. Hu, L. Gao, H. Su, X. Du, N. Yuan et al., Amino acid-based low-dimensional management for enhanced perovskite solar cells. Sol. RRL 6(7), 2200168 (2022). https://doi.org/10.1002/solr.202200168

- D. Wang, J. Chen, P. Zhu, Y. Qiao, H. Hu et al., Binary microcrystal additives enabled antisolvent-free perovskite solar cells with high efficiency and stability. Adv. Energy Mater. 13(7), 2203649 (2023). https://doi.org/10.1002/aenm.202203649

- Y. Zhang, C. Li, E. Bi, T. Wang, P. Zhang et al., Efficient inverted perovskite solar cells with a low-dimensional halide/perovskite heterostructure. Adv. Energy Mater. 12(48), 2202191 (2022). https://doi.org/10.1002/aenm.202202191