Supporting Information for

Synergistic sp-C/sp-N Anchoring of Metal Single Atoms on Graphdiyne for Enhanced Microwave Absorption

Yihao Fan 1, 2, Haichuan Cheng 1, Pengyu Deng 1, Jianfeng Wu 1, 2,※ , Baoliang Zhang 1, 3, ※

1 School of Chemistry and Chemical Engineering, Northwestern Polytechnical University, Xi’an710072, People’s Republic of China

2 Xi’an Key Laboratory of Functional Organic Porous Materials, Northwestern Polytechnical University, Xi’an 710129, People’s Republic of China

3 Shaanxi Engineering and Research Center for Functional Polymers on Adsorption and Separation, Sunresins New Materials Co. Ltd., Xi’an 710072, People’s Republic of China

※Corresponding authors. E-mail: jfwu@nwpu.edu.cn (Jianfeng Wu); blzhang@nwpu.edu.cn (Baoliang Zhang)

S1 Experimental Section

S1.1 Microwave absorption test

The electromagnetic parameters of the powder samples were measured by a vector network analyzer (ZNLE18, Rohde & Schwarz) using the coaxial method. The samples were mixed with paraffin wax, and then coaxial rings with an inner diameter of 3.04 mm and an outer diameter of 7 mm were machined with a mold. The filler content of all the samples was 24%.

Reflection loss (RL) is an important evaluation index of electromagnetic wave absorption performance. According to the transmission line theory, RL can be calculated by Eqs. S1 and S2:

|  | Z=ZinZO=μrεr tanhj2πfdcμrεr | (S1) |
| --- | --- | --- |

|  | RLdB=20 log10Zin-Z0Zin+Z0 | (S2) |
| --- | --- | --- |

According to Debye's theory, the imaginary part of the complex permittivity (ε'') can be divided into conduction loss (εC'') and polarisation loss (εP'') by means of Eqs. S3 and S4:

|  | ε''=ωτ(εs-ε∞)1+ω2τ2+σωε0=εp''+εC'' | (S3) |
| --- | --- | --- |
|  | εC''=αωε0 | (S4) |

The attenuation constant (α) was calculated by Eqs. S5:

|  | α=μ''ε''-ε'μ'+(μ''ε''-ε'μ')2+(μ''ε''+ε'μ')2 | (S5) |
| --- | --- | --- |

S1.2 CST simulation

Radar cross section (RCS) was simulated using CST Studio Suite 2022. Four models were simulated. In the radar cross-section simulation, the model consists of an upper absorbing layer and a lower perfect electrical conductor (PEC) layer with thicknesses of 2.0 mm and 1.0 mm, respectively. In addition, the square model was designed with a side length of 200 mm. A linearly polarized plane wave was defined as the excitation port, with the microwave propagating in the negative direction along the Y-axis and the direction of the magnetic field along the Z-axis. Open boundary conditions were used in this direction. The radar RCS of the simulated sample was represented by the following Eq. S6:

|  | σ(dBm2 )=10log4πSλ2EsEi2 | (S6) |
| --- | --- | --- |

Where S is the area of the simulated plate, λ is the length of the incident microwave, Es is the electric field strength of the transmitted wave, and Ei is the electric field strength of the received wave.

S1.3 DFT calculation

All the DFT calculations were conducted based on the Vienna Ab initio Simulation Package (VASP). The exchange-correlation potential was described by the Perdew−Burke−Ernzerhof (PBE) generalized gradient approach (GGA). The electron-ion interactions were accounted by the projector augmented wave (PAW). All DFT calculations were performed with a cut-off energy of 400 eV, and the 3×3×1 Gamma centered Monkhorst-Pack grids k-points were selected to sample the Brillouin zone integration. The energy and force convergence criteria of the self-consistent iteration were set to 10-4 eV and 0.02 eV Å-1, respectively. DFT-D3 method was used to describe van der Waals (vdW) interactions.

S2 Supplementary Figures and Tables

Fig. S1 SEM figure of Cu2O/GDY

Fig. S2 a Nitrogen adsorption-desorption isotherms and b pore size distribution curves

Fig. S3 FTIR curves of GDY and Fe-N-GDY

Fig. S4 Raman spectra of Cu2O/GDY

Fig. S5 Double Cs-corrected image of Fe-GDY

Fig. S6 a HAADF-STEM image and b lattice analysis of Fe NPs/Fe-N-GDY

Fig. S7 Electrical conductivity measurement via the four-probe method

Fig. S8 a Real part ε' and b imaginary part ε'' of complex permittivity

Fig. S9 3D RL-frequency plots of the series of microwave absorbers: a Fe-N-GDY, b GDY-900, c N-GDY, d Fe NPs/Fe-N-GDY, e Fe-GDY

Fig. S10 Plots of reflection losses and λ/4 with frequency of a GDY-900, b Fe-N-GDY and c Fe-G

Fig. S11 ε'-ε'' curves of a GDY-900, b Fe-N-GDY and c Fe-GDY

Fig. S12 |Zin/Z0| two-dimensional contour maps of a Fe-N-GDY, b GDY-900, c N-GDY, d Fe NPs/Fe-N-GDY, e Fe-GDY

Fig. S13 a ε''C, b ε''P, and c ɑ of the samples

Fig. S14 |Zin/Z0| two-dimensional contour maps of a Cr-N-GDY, b Mn-N-GDY, c Co-N-GDY, d Ni-N-GDY, e Cu-N-GDY, and f Zn-N-GDY

Fig. S15 Cole-Cole plots of a Cr-N-GDY, b Mn-N-GDY, c Co-N-GDY, d Ni-N-GDY, e Cu-N-GDY, and f Zn-N-GDY

Fig. S16 3D RCS reflection signals of each sample at 4 GHz, 8GHz and 12GHz

Table S1 The elemental contents determined by ICP-MS

| Samples | Fe-GDY | Fe-N-GDY | Fe NPs/Fe-N-GDY |
| --- | --- | --- | --- |
| Fe wt% | 1.2 | 1.6 | 5.4 |

Table S2 Curvefit parameters for Fe K-edge EXAFS for Fe-N-GDY

| Path | C.N. | R (Å) | σ2 (Å2) | ΔE0 (eV) | R factor |
| --- | --- | --- | --- | --- | --- |
| Fe-N | 2 | 1.92±0.04 | 0.012±0.003 | -6.0±2.6 | 0.019 |
| Fe-C | 2 | 2.03±0.04 |  |  |  |

C. N. is the coordination number; R is interatomic distance; σ2 is Debye-Waller factor (the Mean Square Relative Displacement (MSRD)); ΔE0 is inner potential correction. R factor is used to value the goodness of the fitting. Data ranges:2.5≤k≤14 Å,1.0≤R≤3.0 Å. The number of variables is 4.

Table S3 ID/IG of the related samples

| Samples | Fe-N-GDY | Fe NPs/Fe-N-GDY | Fe-GDY | N-GDY | GDY-900 |
| --- | --- | --- | --- | --- | --- |
| ID/IG | 0.88 | 0.95 | 0.90 | 0.81 | 0.84 |