Supporting Information for

Electronic Blockade of Shunting Pathways via Dual Insulator Contacts for High-Efficiency Wide-Bandgap Perovskite Indoor Photovoltaics

Quanxi Liu1, 2, Yousheng Wang1, * Qiaoyan Ma1, Jianzha Zheng1, 4, Yinghui Peng1, Liwei Wang1, Zeyu Chen1, Tianhao Du1, Daxin Xiao1, Jiandong Fan1, *, Yoon-Bong Hahn5 and Yaohua Mai1, 3, *

1 Institute of New Energy Technology, College of Physics & Optoelectronic Engineering, Jinan University, Guangzhou 510632, P. R. China

2 Department of Electronic Engineering, College of Information Science and Technology, Jinan University, Guangzhou 510632, P. R. China

3 Guangdong Mellow Energy Co., Ltd, Zhuhai 519000, P. R. China

4 Institute of Applied Physics and Materials Engineering, University of Macau, Macao 999078, P. R. China

5 School of Semiconductor and Chemical Engineering, Solar Energy Research Center, Jeonbuk National University, 567 Baekjedaero, Deokjin-gu, Jeonju-si, Jeollabuk-do, 54896 Republic of Korea

*Corresponding authors. E-mail: wangys0120@jnu.edu.cn (Yousheng Wang); jdfan@jnu.edu.cn (Jiandong Fan); yaohuamai@jnu.edu.cn (Yaohua Mai)

Supplementary Figures and Tables

Fig. S1 Current density-voltage (J-V) characteristics obtained at two working distances (WDA = 37.5 cm and WDB = 18.4 cm) from light-emitting diode (1,000 lx, 288.4 µW cm-2, 2,950 K)

Table S1 Photovoltaic parameters of WBG-PIPVs under light-emitting diode (1,000 lx, 288.4 µW cm-2, 2,950 K) illumination at two working distances (WDA = 37.5 cm and WDB = 18.4 cm). The angular effects were assessed by comparing indoor performance at two different distances of 37.5 cm (A) and 18.4 cm (B) under the same illuminance (1,000 lx), which confirmed a deviation (ε) of less than 5% (ε = PCEB-PCEAPCEB= (42.72-41.73)/42.72≤2.32%).

| Distance | Scan direction | PCE(i) (%) | Voc (V) | Jsc (μA/cm2) | FF (%) | Pout (μW cm-2) |
| --- | --- | --- | --- | --- | --- | --- |
| 18.4 cm | RS | 42.72 | 1.0745 | 138.37 | 82.86 | 123.20 |
|  | FS | 41.93 | 1.061 | 138.34 | 82.39 | 120.93 |
| 37.5 cm | RS | 41.73 | 1.0745 | 136.44 | 82.10 | 120.37 |
|  | FS | 41.00 | 1.061 | 136.52 | 81.63 | 118.24 |

Fig. S2 Contact angles of the perovskite precursor on a hybrid ultrathin layer with different contents of PMMA: a without PMMA, b-d ratio of mp-Al2O3 to PMMA of 5:1, 3:1 and 2:1

Fig. S3 SEM surface images of mp-Al2O3-PMMA hybrid ultrathin layer: a mp-Al2O3 and b mp-Al2O3-PMMA

Table S2 Photovoltaic parameters of WBG-PIPVs under light-emitting diode (1,000 lx, 288.4 µW cm-2, 2,950 K) illumination for the optimal four types of cells

| Devices | Scan direction | PCE(i) (%) | Voc (V) | Jsc (μA/cm2) | FF (%) | Pout (μW cm-2) |
| --- | --- | --- | --- | --- | --- | --- |
| Con | Rs | 39.06 | 1.018 | 137.11 | 80.70 | 112.64 |
|  | Fs | 36.34 | 1.005 | 136.99 | 76.12 | 104.80 |
| GIC | Rs | 42.02 | 1.064 | 137.43 | 82.88 | 121.19 |
|  | Fs | 41.33 | 1.057 | 137.36 | 82.09 | 119.19 |
| BIC | Rs | 41.75 | 1.028 | 138.00 | 84.87 | 120.40 |
|  | Fs | 40.66 | 1.016 | 138.01 | 83.63 | 117.27 |
| DIC | Rs | 44.36 | 1.091 | 138.72 | 83.97 | 127.94 |
|  | Fs | 43.51 | 1.082 | 137.82 | 83.37 | 125.47 |

Fig. S4 J-V performance of both reverse and forward scan under LED illumination (1,000 lx, 288.4 µW cm-2, 2,950 K) for different contents of PMMA in EA antisolvent

Table S3 Photovoltaic parameters of WBG-PIPVs under light-emitting diode (1,000 lx, 288.4 µW cm-2, 2,950 K) illumination for different contents of PMMA in EA antisolvent

| Contents of PMMA | Scan direction | PCE(i) (%) | Voc (V) | Jsc (μA/cm2) | FF (%) | Pout (μW cm-2) |
| --- | --- | --- | --- | --- | --- | --- |
| 0.05 | Rs | 40.27 | 1.028 | 138.11 | 81.80 | 116.14 |
|  | Fs | 39.81 | 1.028 | 138.04 | 80.89 | 114.79 |
| 0.1 | Rs | 40.63 | 1.040 | 137.34 | 82.03 | 117.17 |
|  | Fs | 39.83 | 1.028 | 137.56 | 81.22 | 114.86 |
| 0.2 | Rs | 42.60 | 1.064 | 137.56 | 83.93 | 122.85 |
|  | Fs | 41.80 | 1.052 | 137.72 | 83.20 | 120.55 |
| 0.3 | Rs | 36.28 | 0.968 | 138.38 | 78.11 | 104.63 |
|  | Fs | 34.58 | 0.944 | 138.60 | 76.22 | 99.73 |

Fig. S5 Performance statistics of reverse and forward scan in WBG-PIPVs (15~20 cells) measured under LED illumination (1,000 lx, 288.4 µW cm-2, 2950 K) for different contents of PMMA in EA solvent: a i-PCE, b Voc and c FF

Fig. S6 J-V performance of both reverse and forward scan under LED illumination (1,000 lx, 288.4 µW cm-2, 2,950 K) for different ratios of mp-Al2O3 to PMMA as a hybrid ultrathin layer

Table S4 Photovoltaic parameters of WBG-PIPVs under light-emitting diode (1,000 lx, 288.4 µW cm-2, 2,950 K) illumination for different ratios of mp-Al2O3 to PMMA as a hybrid ultrathin layer

| Ratio of mp-Al2O3 to PMMA | Scan direction | PCE(i) (%) | Voc (V) | Jsc (μA/cm2) | FF (%) | Pout (μW cm-2) |
| --- | --- | --- | --- | --- | --- | --- |
| 3：1 | Rs | 39.04 | 1.028 | 138.08 | 79.32 | 112.60 |
|  | Fs | 36.93 | 1.016 | 138.22 | 75.84 | 106.51 |
| 5：1 | Rs | 41.75 | 1.028 | 138.00 | 84.87 | 120.40 |
|  | Fs | 40.67 | 1.016 | 138.03 | 83.63 | 117.28 |
| 7：1 | Rs | 40.82 | 1.016 | 138.78 | 83.49 | 117.77 |
|  | Fs | 39.37 | 1.004 | 138.96 | 81.39 | 113.56 |
| 9：1 | Rs | 41.15 | 1.028 | 138.54 | 83.32 | 118.67 |
|  | Fs | 39.73 | 1.016 | 138.66 | 81.31 | 114.56 |

Fig. S7 Performance statistics of reverse and forward scan in WBG-PIPVs (15~20 cells) measured under LED illumination (1,000 lx, 288.4 µW cm-2, 2,950 K) for different ratios of mp-Al2O3 to PMMA as a hybrid ultrathin layer: a i-PCE, b Voc and c FF

Table S5 Summarized photovoltaic parameters of control devices under light-emitting diode (1,000 lx, 288.4 µW cm-2, 2,950 K) illumination

| # | PCE(i) (%) | Voc (V) | Jsc (μA/cm2) | FF (%) | Pout (μW cm-2) |
| --- | --- | --- | --- | --- | --- |
| 1 | 36.63 | 1.010 | 135.22 | 77.34 | 105.62 |
| 2 | 36.88 | 1.018 | 132.54 | 78.83 | 106.36 |
| 3 | 37.86 | 1.010 | 138.48 | 78.07 | 109.19 |
| 4 | 38.51 | 1.012 | 135.71 | 80.85 | 111.04 |
| 5 | 38.17 | 1.001 | 137.17 | 80.16 | 110.07 |
| 6 | 36.67 | 1.018 | 136.09 | 76.33 | 105.77 |
| 7 | 38.05 | 1.005 | 136.50 | 80.00 | 109.74 |
| 8 | 37.86 | 1.004 | 137.04 | 79.36 | 109.19 |
| 9 | 34.55 | 0.944 | 137.07 | 77.00 | 99.64 |
| 10 | 36.19 | 0.980 | 134.80 | 79.00 | 104.36 |
| 11 | 36.91 | 0.956 | 137.49 | 80.97 | 106.43 |
| 12 | 38.58 | 1.016 | 135.23 | 80.97 | 111.25 |
| 13 | 35.74 | 0.992 | 131.50 | 79.00 | 103.06 |
| 14 | 39.06 | 1.016 | 136.76 | 81.07 | 112.65 |
| 15 | 38.28 | 1.018 | 135.24 | 80.20 | 110.41 |
| Ave. | 37.33 | 1.00 | 135.78 | 79.28 | 107.65 |

Table S6 Summarized photovoltaic parameters of GIC-based WBG-PIPVs under light-emitting diode (1,000 lx, 288.4 µW cm-2, 2,950 K) illumination

| # | PCE(i) (%) | Voc (V) | Jsc (μA/cm2) | FF (%) | Pout (μW cm-2) |
| --- | --- | --- | --- | --- | --- |
| 1 | 40.48 | 1.028 | 138.29 | 82.12 | 116.74 |
| 2 | 38.83 | 1.035 | 134.32 | 80.54 | 111.97 |
| 3 | 38.69 | 1.018 | 134.33 | 81.59 | 111.57 |
| 4 | 37.91 | 1.015 | 134.62 | 80.01 | 109.33 |
| 5 | 39.32 | 1.055 | 133.70 | 80.38 | 113.38 |
| 6 | 37.57 | 1.015 | 131.81 | 80.99 | 108.35 |
| 7 | 38.14 | 1.018 | 133.97 | 80.65 | 109.99 |
| 8 | 40.77 | 1.028 | 138.40 | 82.64 | 117.57 |
| 9 | 42.03 | 1.064 | 137.43 | 82.88 | 121.19 |
| 10 | 39.89 | 1.031 | 138.73 | 80.44 | 115.05 |
| 11 | 40.55 | 1.028 | 139.67 | 81.44 | 116.93 |
| 12 | 39.33 | 1.018 | 137.54 | 81.01 | 113.42 |
| 13 | 40.09 | 1.045 | 140.01 | 79.01 | 115.62 |
| 14 | 41.26 | 1.055 | 136.16 | 82.84 | 118.99 |
| 15 | 40.41 | 1.040 | 138.57 | 80.86 | 116.53 |
| Ave. | 39.71 | 1.033 | 136.57 | 81.22 | 114.50 |

Table S7 Summarized photovoltaic parameters of BIC-based WBG-PIPVs under light-emitting diode (1,000 lx, 288.4 µW cm-2, 2,950 K) illumination

| # | PCE(i) (%) | Voc (V) | Jsc (μA/cm2) | FF (%) | Pout (μW cm-2) |
| --- | --- | --- | --- | --- | --- |
| 1 | 39.75 | 0.980 | 138.31 | 84.57 | 114.63 |
| 2 | 40.15 | 1.016 | 137.93 | 82.63 | 115.79 |
| 3 | 41.05 | 1.016 | 138.92 | 83.88 | 118.38 |
| 4 | 40.22 | 1.016 | 138.23 | 82.00 | 116.00 |
| 5 | 39.47 | 1.004 | 135.04 | 83.96 | 113.84 |
| 6 | 41.22 | 1.014 | 139.54 | 84.02 | 118.88 |
| 7 | 39.51 | 1.018 | 132.72 | 84.32 | 113.93 |
| 8 | 41.06 | 1.018 | 137.76 | 84.43 | 118.41 |
| 9 | 39.19 | 1.016 | 135.96 | 81.82 | 113.02 |
| 10 | 40.29 | 1.020 | 136.12 | 83.68 | 116.18 |
| 11 | 40.03 | 1.016 | 134.74 | 84.34 | 115.46 |
| 12 | 40.81 | 1.004 | 138.66 | 84.54 | 117.70 |
| 13 | 40.62 | 1.024 | 136.81 | 83.62 | 117.15 |
| 14 | 41.36 | 1.016 | 138.73 | 84.62 | 119.27 |
| 15 | 39.43 | 0.992 | 138.44 | 82.79 | 113.70 |
| 16 | 41.75 | 1.028 | 138.00 | 84.87 | 120.40 |
| 17 | 39.51 | 0.992 | 138.58 | 82.28 | 113.93 |
| 18 | 40.66 | 1.004 | 138.30 | 84.45 | 117.27 |
| 19 | 40.28 | 1.016 | 139.41 | 82.02 | 116.17 |
| 20 | 40.93 | 1.016 | 138.83 | 83.71 | 118.08 |
| Ave. | 40.45 | 1.011 | 137.57 | 83.63 | 116.64 |

Table S8 Summarized photovoltaic parameters of DIC-based WBG-PIPVs under light-emitting diode (1,000 lx, 288.4 µW cm-2, 2,950 K) illumination

| # | PCE(i) (%) | Voc (V) | Jsc (μA/cm2) | FF (%) | Pout (μW cm-2) |
| --- | --- | --- | --- | --- | --- |
| 1 | 43.48 | 1.064 | 139.48 | 84.50 | 125.40 |
| 2 | 42.64 | 1.057 | 137.82 | 84.41 | 122.96 |
| 3 | 41.48 | 1.057 | 136.42 | 82.96 | 119.63 |
| 4 | 42.46 | 1.057 | 137.79 | 84.07 | 122.44 |
| 5 | 41.27 | 1.057 | 136.87 | 82.28 | 119.03 |
| 6 | 42.42 | 1.070 | 136.74 | 83.62 | 122.34 |
| 7 | 41.27 | 1.057 | 135.30 | 83.22 | 119.01 |
| 8 | 41.99 | 1.070 | 135.57 | 83.48 | 121.10 |
| 9 | 43.10 | 1.083 | 138.09 | 83.11 | 124.29 |
| 10 | 43.49 | 1.083 | 138.43 | 83.66 | 125.42 |
| 11 | 42.93 | 1.076 | 137.30 | 83.79 | 123.79 |
| 12 | 41.02 | 1.057 | 136.07 | 82.24 | 118.28 |
| 13 | 43.12 | 1.070 | 139.06 | 83.57 | 124.35 |
| 14 | 44.36 | 1.091 | 138.72 | 83.97 | 127.94 |
| 15 | 43.51 | 1.082 | 137.82 | 83.37 | 125.47 |
| 16 | 43.71 | 1.083 | 138.17 | 84.24 | 126.06 |
| 17 | 43.74 | 1.083 | 138.72 | 83.96 | 126.14 |
| 18 | 42.58 | 1.070 | 137.82 | 83.27 | 122.80 |
| 19 | 43.59 | 1.083 | 137.69 | 84.30 | 125.71 |
| 20 | 43.15 | 1.076 | 138.09 | 83.75 | 124.44 |
| Ave. | 42.93 | 1.068 | 137.57 | 83.83 | 123.81 |

Fig. S8 Steady-state power output (SPO) curves of the champion DIC device at the maximum power point (MPP) Voc of 0.944 V under LED illumination (1,000 lx, 288.4 µW/cm2, 2,950 K) for 1200 s

Fig. S9 EQE spectra and the integrated current density for the control and DIC champion devices under 1,000 lx illumination

Fig. S10 Integrated current density from EQE spectra of DIC champion devices under (a) 600 lx, (b) 400 lx and (c) 200 lx illumination, respectively

Fig. S11 J-V curves and corresponding photovoltaic parameters incorporated reverse and forward scans of the DIC-device under 50 lx illumination

Table S9 Reported efficiencies of PIPVs under low irradiances (~600 lx) illumination conditions (LED)

| Perovskite compositions | Eg (eV) | Illumination conditions | Active/aperture area (cm2) | Voc (V) | FF (%) | PCE(i) (%) | Pout (μW cm-2) | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (FAPbI3)0.97(MAPbBr3)0.03 | 1.59 | 500 lx, 170 μW cm-2, 2,700 K | 0.08 | 0.92 | 79.01 | 35.55 | N/A | [S1] |
|  |  | 200 lx, 71 μW cm-2, 2,700 K (DYSON, CD05) |  | 0.89 | 72.44 | 34.77 | N/A |  |
| FAPbI3 | 1.52 | 531 lx, 167 μW cm-2, 2,956 K | 0.07 | 0.89 | 79.7 | 30.56 | 51.0 | [S2] |
|  |  | 212 lx, 83 μW cm-2, 2,956 K |  | 0.84 | 80.3 | 30.65 | 20.5 |  |
|  |  | 106 lx, 42 μW cm-2, 2,956 K (N/A) |  | 0.83 | 80.7 | 29.89 | 9.98 |  |
| Cs0.17FA0.83PbI1.8Br1.2 | 1.77 | 600 lx, 181 μW cm-2, 3,000 K | 0.09 | 1.01 | 80.46 | 32.93 | 59.66 | [S3] |
|  |  | 400 lx, 121 μW cm-2, 3,000 K |  | 0.99 | 79.08 | 31.96 | 38.60 |  |
|  |  | 200 lx, 61 μW cm-2, 3,000 K (WLED) |  | 0.98 | 78.75 | 32.68 | 19.73 |  |
| CsPbI3 | 1.69 | 522 lx, 168 μW cm-2, 2,956 K | 0.09 | 0.91 | 78 | 32.54 | 54.34 | [S4] |
|  |  | 106 lx, 33.84 μW cm-2, 2,956 K (N/A) |  | 0.83 | 74 | 29.45 | 9.82 |  |
| FA0.85MA0.15PbI3 | 1.54 | 500 lx, 138 μW cm-2, 3,000 K | 0.09 | 0.93 | 80.92 | 39.31 | N/A | [S5] |
|  |  | 200 lx, 56 μW cm-2, 3,000 K |  | 0.90 | 74.59 | 38.31 |  |  |
|  |  | 500 lx, 138 μW cm-2, 3,000 K | 1 | 0.94 | 80.16 | 39.13 |  |  |
|  |  | 200 lx, 56 μW cm-2, 3,000 K |  | 0.90 | 79.86 | 36.84 |  |  |
|  |  | 500 lx, 138 μW cm-2, 3,000 K | 2.56 | 0.94 | 79.32 | 39.44 |  |  |
|  |  | 200 lx, 56 μW cm-2, 3,000 K (N/A) |  | 0.90 | 74.59 | 36.84 |  |  |
| Cs0.05FA0.70MA0.25PbI2.25Br0.75 | 1.71 | 600 lx, 181 μW cm-2, 3,000 K | 0.09 | 1.03 | 80 | 41.09 | 74.43 | [S6] |
|  |  | 400 lx, 121 μW cm-2, 3,000 K |  | 1.02 | 79.62 | 40.31 | 48.69 |  |
|  |  | 200 lx, 60 μW cm-2, 3,000 K (WLED) |  | 0.98 | 79.37 | 37.48 | 22.64 |  |
| N/A | 1.52 | 500 lx, 138 μW cm-2, 3,000 K | 0.07 | 0.94 | 80.91 | 39.03 | N/A | [S7] |
|  |  | 200 lx, 56 μW cm-2, 3,000 K (DYSON, CD05) |  | 0.89 | 75.84 | 35.54 | N/A |  |
| Cs0.05(FA0.75MA0.25)0.95Pb(I0.75Br0.25)3 | 1.67 | 500 lx, 147 μW cm-2, 3,000 K | 0.07 | 1.05 | 82.10 | 39.53 | 56 | [S8] |
|  |  | 200 lx, 55 μW cm-2, 3,000 K (N/A) |  | 1.01 | 81.57 | 38.55 | 21 |  |
| Cs0.05(FA0.95MA0.05)0.95Pb(I0.95Br0.05)3 | 1.55 | 500 lx, 157 μW cm-2, 3,000 K | N/A | 0.99 | 83.17 | 41.16 | N/A | [S9] |
|  |  | 200 lx, 65 μW cm-2, 3,000 K |  | 0.95 | 82.94 | 38.43 | N/A |  |
| Cs0.05FA0.70MA0.25PbI2.25Br0.75 | 1.71 | 600 lx, 172.7 μW cm-2, 2,950 K | 0.09 | 1.06 | 84.52 | 43.08 | 74.41 | This work |
|  |  | 400 lx, 115.3 μW cm-2, 2,950 K |  | 1.05 | 82.97 | 40.24 | 46.40 |  |
|  |  | 200 lx, 57.77 μW cm-2, 2,950 K (WLED) |  | 1.02 | 82.83 | 40.94 | 23.65 |  |

Fig. S12 Time-dependent photographs of WBG-perovskite crystallization for different contents of PMMA in EA antisolvent by recording videos

Fig. S13 Photographs of surface structure of WBG-perovskite films incorporated PMMA. a Without PMMA, b 0.05 mg/mL, c 0.2 mg/mL and d 1 mg/mL

Fig. S14 (a-c) SEM images of surface morphologies and (d-f) corresponding crystalline grain size distribution histograms of the control, BIC- and DIC-WBG-perovskite films, and (g) cross-sectional SEM image of BIC-WBG-perovskite film

Fig. S15 XRD patterns of control- (ITO/NiOx/PTAA/mp-Al2O3/WBG-perovskite), BIC- (ITO/NiOx/PTAA/mp-Al2O3-PMMA/WBG-perovskite) and DIC-perovskite films (ITO/NiOx/PTAA/mp-Al2O3-PMMA/WBG-perovskite-PMMA)

Fig. S16 Water contact angles of the WBG-perovskite films incorporated different contents of PMMA: a without PMMA, b 0.2 mg/mL, c 0.5 mg/mL and d 1 mg/mL.

Fig. S17 PL mapping images for control (ITO/NiOx/PTAA/Al2O3/WBG-perovskite) and DIC-based WBG-perovskite films (ITO/NiOx/PTAA/Al2O3-PMMA/WBG-perovskite-PMMA)

Fig. S18 Steady-state PL and PLQY with an excitation of 532 nm for control (ITO/NiOx/PTAA/Al2O3/WBG-perovskite) and DIC-based WBG-perovskite films (ITO/NiOx/PTAA/Al2O3-PMMA/WBG-perovskite-PMMA)

Fig. S19 The electrical conductivity characteristics. a Dark J-V curves, b the dJ/dV with the fit used to determine Rsh, c the dV/dJ with the fit used to determine Rs for control and DIC-based devices

Fig. S20 EIS Nyquist plots measured by the electrochemical impedance spectra (EIS) of the control- and DIC-devices under dark conditions with an bias voltage of 1.1 V

Table S10 Impedance parameters of control and DIC-devices obtained from fitting EIS data

| Device | Rs (Ω) | R1 (Ω) | C1 (×10-8 F cm-2 sn-1) | R2 (Ω) | C2 (×10-5 F cm-2 sn-1) |
| --- | --- | --- | --- | --- | --- |
| Con | 15.08 | 2496 | 1.286 | 148.91 | 23.768 |
| DIC | 11.50 | 4413 | 1.087 | 1424 | 3.116 |

Fig. S21 ToF-SIMS depth profile for ITO/HTL/PMMA-Al2O3/PMMA-PVK at 0-800 s

Supplementary References

- X. He, J. Chen, X. Ren, L. Zhang, Y. Liu et al., 40.1% record low-light solar-cell efficiency by holistic trap-passivation using micrometer-thick perovskite film. Adv. Mater. 33(27), 2100770 (2021). https://doi.org/10.1002/adma.202100770

- C.-H. Chen, Z.-H. Su, Y.-H. Lou, Y.-J. Yu, K.-L. Wang et al., Full-dimensional grain boundary stress release for flexible perovskite indoor photovoltaics. Adv. Mater. 34(16), e2200320 (2022). https://doi.org/10.1002/adma.202200320

- C. Zhang, M. He, S. Wu, Y. Gao, M. Ma et al., Occlusal architecture of the buried interface enables record-efficiency flexible perovskite photovoltaic modules with enhanced in-plane bending mechanical endurance. Adv. Funct. Mater. 34(19), 2313910 (2024). https://doi.org/10.1002/adfm.202313910

- K.-L. Wang, H. Lu, M. Li, C.-H. Chen, B.Z. Ding- et al., Ion-dipole interaction enabling highly efficient CsPbI(3) perovskite indoor photovoltaics. Adv. Mater. 35(31), e2210106 (2023). https://doi.org/10.1002/adma.202210106

- Y. Li, T. Nie, X. Ren, Y. Wu, J. Zhang et al., In situ formation of 2D perovskite seeding for record-efficiency indoor perovskite photovoltaic devices. Adv. Mater. 36(1), e2306870 (2024). https://doi.org/10.1002/adma.202306870

- Q. Ma, Y. Wang, L. Liu, P. Yang, W. He et al., One-step dual-additive passivated wide-bandgap perovskites to realize 44.72%-efficient indoor photovoltaics. Energy Environ. Sci. 17(5), 1637–1644 (2024). https://doi.org/10.1039/d3ee04022d

- C. Liu, T. Yang, W. Cai, Y. Wang, X. Chen et al., Flexible indoor perovskite solar cells by in situ bottom-up crystallization modulation and interfacial passivation. Adv. Mater. 36(24), e2311562 (2024). https://doi.org/10.1002/adma.202311562

- C.-H. Chen, X.-Y. He, R.-H. Qin, K.-L. Wang, L. Huang et al., Reliable perovskite indoor photovoltaics for self-powered devices. Natl. Sci. Rev. 12(8), nwaf242 (2025). https://doi.org/10.1093/nsr/nwaf242

- J. Jin, Z. Zhu, Y. Ming, Y. Zhou, J. Shang et al., Spontaneous bifacial capping of perovskite film for efficient and mechanically stable flexible solar cell. Nat. Commun. 16(1), 90 (2025). https://doi.org/10.1038/s41467-024-55652-6