Nano-Micro Letters

Supporting Information for
Anion-Diluent Decoupled Solvation Chemistry in Ionic Liquid-Based Localized High-Concentration Electrolytes Toward High-Voltage Lithium Metal Batteries
Guangye Wu1,2+, Haifeng Tu2,3+, Zhicheng Wang4,5*, Yiwen Gao1,2, Peng Ding2,3, Yi Yang6, Lingwang Liu2,3, Suwan Lu2,3, Farwa Mushtaq2,3, Guochao Sun2,3, Hexiang Chen2,3, Haiyang Zhang2,3, Jiangyan Xue2,3, Jingjing Xu6, Hong Li4,5, and Xiaodong Wu2,3,4*

1School of Materials Science and Engineering, Shanghai University, Shanghai 200444, P. R. China
2i-lab, Suzhou Institute of Nano-Tech and Nano-Bionics, Chinese Academy of Sciences, Suzhou, Jiangsu 215123, P. R. China
3School of Nano-Tech and Nano-Bionics, University of Science and Technology of China, Hefei, Anhui 230026, P. R. China

4Tianmu Lake Institute of Advanced Energy Storage Technologies Co., Ltd., Liyang 213300, P. R. China
5Beijing Advanced Innovation Center for Materials Genome Engineering Key Laboratory for Renewable Energy, Beijing Key Laboratory for New Energy Materials and Devices, Institute of Physics, Chinese Academy of Sciences, Beijing 100190, P. R. China
6College of Material Science and Engineering, Hohai University, Changzhou, Jiangsu 213022, P. R. China
+Guangye Wu and Haifeng Tu contributed equally to this work.
*Corresponding authors. E-mail: zc_wang2023@163.com (Zhicheng Wang); xdwu2011@sinano.ac.cn (Xiaodong Wu) 

[image: image1.png]b 0.08 0.050

0.07 L2
0.030
0.06
0.020
~ 005 0.010
=2
E 004 0.000
¥
o0 -0.010
-0.020
0.02
-0.030
R 0,040
0.00 -0.050
w T M e = 9 = & @ ¥ wn
S & & © § & & © & S o
S S 3 3 3 S S S S S S
sign(L)r (a.u.)
c p >0 sign(4,)p decreases p ~0 sign(%,)pincreases p >0
2<0 " =0 Y 14>0
p>0 J U U\ J
“=---== —~ Y Y
bond with prominent attractive van der Waals ~ prominent repulsive interaction
nonnegligible weak interaction interaction (steric effect in ring and cage...)

covalency (H-bond, halogen-bond ...),
and purely ionic bond



Supplementary Figures and Tables
[image: image20.png]



Fig. S1 (a) Reference labels for atoms in the intermolecular contact matrix of TFE and FSI- anion. (b) Scatter map between RDG and sign(I2)r of the grid points used to Fig. 1c. (c) Commonly used color scale in non-covalent interaction (NCI) map and common interpretation of various color ranges.

[image: image2.png]a.u.

012

009

0.06

003

0.00

TFEE-FSI”

Fezn
[ 2H
[~ 0ZH

B ]

F8IH
FLH
FoLd
Fsid
[vid
Feld
Fzio
[0
oo
[ 69
84
Fud
Fod
Fsd

N s

[-€0
F2o
FLo

031 o

030

029

028

F27

526 4

N25 4

$24

F23

0.050

0.040

0.030

0.020

0.010
0.000

-0.010

-0.020

=0.030

-0.040

-0.050

0.08

0.07

0.06

0.05

0.04

(ne) 3p

@
<
=3

0.02

0.01

0.00

00
00
€00
200
00 3
g
000 &
5
100- 3
00~
£0°0-
P00~
S0'0-




Fig. S2 (a) Reference labels for atoms in the intermolecular contact matrix of TFEE and FSI- anion. (b) Intermolecular contact matrix and interaction energy gradient isosurfaces of TFEE-FSI- obtained by the RDG (reduced density gradient) method. (c) corresponding scatter plot between RDG and sign(I2)r.
[image: image3.png]TFEE+Pyr, FSI

TFEE+Pyr,FSI

H Chemical shift (ppm)

TFEE |
I
. TFEE
[
' AX,
TFE+Pyr,,FSI i
A e TFE+Pyr oFSl
I
JL
I
TFE | TFE
T T T T T T T T T !
6 5 4 3 2 1 0 65 6.0 55

H Chemical shift (ppm)




Fig. S3 (a, b) The ¹H NMR spectra of the pure diluent and the diluent after being mixed with the ionic liquid. 
[image: image4.png]



Fig. S4 Molecular dynamics (MD) simulation snapshot of (a) TFE-LHCE and (b) TFEE-LHCE. 
[image: image5.png]g

50

404

30

204

101

TFE-LHCE
= - - Li*-O(FSI)
—— - - Li*-F (TFE)

first solvation
radius

20

F15

50

TFEE-LHCE

— - - LiO(FsI)

e - - Li*-F (TFEE)
404

first solvation
30 4 radius
204
104 [t
0 -
0

20

15




Fig. S5 (a) RDF and CN of Li+-O (FSI-) and Li+-F (TFE) obtained from MD simulations in TFE-LHCE. (b) RDF and CN of Li+-O (FSI-) and Li+-F (TFEE) obtained from MD simulations in TFEE-LHCE. 

[image: image6.png]1E-4




Fig. S6 Wide-angle X-ray scattering (WAXS) test result of an empty glass capillary. 
[image: image7.png]Q)

N
3]

Conductivity (mS/cm)

N
o

-
(9]

-
o

o
&

o
o

TFE-LHCE

TFEE-LHCE

pH

8.5

8.0

TFE-LHCE

TFEE-LHCE




Fig. S7 (a) Ionic conductivities and (b) pH value of TFE-LHCE and TFEE-LHCE were tested by using an Mettler Toledo S400.
[image: image8.png]035 —— TFEE-LHCE
0.25
J— —
T ey stte " Stesa st
. £ 030
I
£ £
g g
So20 5 025
© 3}
020
0.15 T T T T T T T
0 500 1000 1500 2000 2500 3000 3500 4000 0 500 1000 1500 2000 2500 3000 3500 4000

Time (s) Time (s)




Fig. S8 (a, b) The lithium-ion transference numbers of the two electrolytes were determined via direct current polarization combined with alternating current impedance using Li||Li symmetric cells. 
[image: image9.emf]LiFSI-Pyr

13

FSI

TFE-LHCE

TFEE-LHCE

0

20

40

60

80

100

120

Viscosity (Pa·s)


Fig. S9 The viscosities of the LiFSI-Pyr13FSI electrolyte, TFE-LHCE electrolyte, and TFEE-LHCE electrolyte. 

[image: image10.png]b R Bk R B R Rl mh |

1E-7 1E-50.001 0.1 10
1(S)

> E
Charge 2 Discharge

w
<




Fig. S10 Relaxation Time Distribution (DRT) derived from in-situ electrochemical impedance spectroscopy (EIS) of Li||TFEE-LHCE||NCM811 cells after formation cycles at a 4.3 V cutoff voltage.

[image: image11.emf]1E-7

1E-5

0.001

0.1

10

?(t)

t(s)

t

SEI

t

CT

TFEE-LHCE

1E-7

1E-5

0.001

0.1

10

?(t)

t(s)

TFE-LHCE

t

SEI

t

CT

a

b


Fig. S11 DRT analysis derived from in-situ EIS of (a) Li|TFE-LHCE|Li and (b) Li|TFEE-LHCE|Li cells after formation cycles. 

[image: image12.png]Voltage (V)

1.0 JTFELHCE
| 2nd
1} ——100th
08 ——200th
\ 300th
06 400th
600th
04l
0.2-
004 T
02— . . . .
0 200 400 600 800

Capacity (mAh)

1000

Voltage (V)

TFEE-LHCE

0 200 400 600

Capacity (mAh/g)

800

1000




Fig. S12 Li plating/stripping voltage profiles in Li||Cu cells with (a) TFE-LHCE and (b) TFEE-LHCE.
[image: image13.png]—— TFE-LHCE
= TFEE-LHCE

0 200 400 600 800 1000 1200
Time (h)




Fig. S13 Cycling performance of the Li||Li cell at 0.1 mA cm-2 and 0.1 mAh cm-2.

[image: image14.png]Sputtering time (s)

120

100

80

60

40

20

Counts b

6400

800.0

525 530 535
Bingding energy (eV)

540

Sputtering time (s)

120

100

@
o
L

D
o
L

Counts
7620

1160

525 530 535
Bingding energy (eV)

540




Fig. S14 XPS O1s contour plots of lithium metal after 50 cycles with (a) TFE-LHCE and (b) TFEE-LHCE electrolytes. 
[image: image15.png]TFE-LHCE j TFEE-LHCE

10pm | 10um





Fig. S15 Top-view SEM morphologies of lithium metal after cycling in (a) Li||TFE-LHCE||Li and (b) Li||TFEE-LHCE||Li.
[image: image16.png]



Fig. S16 Top-view SEM morphologies of (a) pristine NCM811 cathode and after 200 cycles with (b) TFE-LHCE and (c) TFEE-LHCE.
[image: image17.png]a

<)

>

(]
o)

]

4.6 JTFE-LHCE
444
42
40
1st
38 ——50th
——100th

361 200th
34-
32
30-
284— r r r r r

0 50 100 150 200 250 300

Specific Capacity (mAh/g™)

b

<)

(]
o)

4.6 4
4.4 4

3.8 4

TFEE-LHCE

1st
——50th
———100th

50 100 150 200 250 300
Specific Capacity (mAh/g™)




Fig. S17 Charge/discharge voltage profiles of (a) Li||TFE-LHCE||NCM811 and (b) Li||TFEE-LHCE||NCM811 coin cell under 3.0-4.3 V at 0.5 C. 
[image: image18.emf]0

5

10

15

20

25

0

50

100

150

200

250

 TFE-LHCE

 TFEE-LHCE

Cycle number

Specific capacity (mAh/g)

0.3C

0.5C

1C

1.3C

1.5C

0.5C


Fig. S18 The rate capability of the Li||NCM811 batteries with different electrolytes. 
[image: image19.png]Voltage (V)

w
'

4.4 ]TFE-LHCE

«
-]

«
o

3.0

Pouch cell

2.8
0.0 0.5 1.0 1.5 2.0

Specific Capacity (mAh/g™)

25





Fig. S19 Charge/discharge voltage profiles of 2.6 Ah Li||TFE-LHCE||Ni83 pouch cell under 3.0-4.3 V at 0.1 C.
S2/S9

