Supplementary Information for

Hetero-Solvent Microenvironment for Selective CO2 to Ethanol Electrolysis via Interfacial Water Control

Dohun Kim1, Suyun Lee1, Seeun Jung2, Jaemin Kim3, Junsic Cho2, Dong Ki Lee4,5, Seoin Back6,7,8*, Chang Hyuck Choi2*, and Chanyeon Kim1*

1 Department of Energy Science and Engineering, Daegu Gyeongbuk Institute of Science & Technology (DGIST), Daegu 42988, Republic of Korea

2 Department of Chemistry, Pohang University of Science and Technology (POSTECH), Pohang 37673, Republic of Korea

3 Department of Chemical and Biomolecular Engineering, Sogang University, Seoul 04107, Republic of Korea

4 Clean Energy Research Center, Korea Institute of Science and Technology, Seoul, 02792 Republic of Korea

5 Department of Chemical and Biomolecular Engineering, Yonsei-KIST Convergence Research Institute, Yonsei University, Seoul, 03722 Republic of Korea

6 Department of Integrative Energy Engineering, Korea University, Seoul 02841, Republic of Korea

7 KU-KIST Graduate School of Converging Science and Technology, Korea University, 145 Anam-ro, Seongbuk-gu, Seoul, 02841, Republic of Korea

8 Institute for Multiscale Matter and Systems (IMMS), Ewha Womans University, Seoul 03760, Republic of Korea

Dohun Kim, Suyun Lee, and Seeun Jung Contributed equally to this work.

*Corresponding authors. E-mail: chanyeon@dgist.ac.kr (Chanyeon Kim); chchoi@postech.ac.kr (Chang Hyuck Choi); sback@korea.ac.kr (Seoin Back)

Supplementary Figures and Tables

Table S1 | The systematic comparison of candidate co-solvent

| Solvent | CO2 solubility [S1, S2] | Aprotic, H-bond accepting Characteristic [S3] | Electrochemical Stability [S4] | Boiling Point [S5] |
| --- | --- | --- | --- | --- |
| Water | ~34 mM | Protic, H-bond acceptor/donor |  | 100 ℃ |
| Dimethylformamide (DMF) | ~200 mM | Aprotic, H-bond acceptor | Unstable | 153 ℃ |
| Tetrahydrofuran (THF) | ~200 mM | Aprotic, H-bond acceptor | Stable | 66 ℃ |
| Diglyme (DiG) | ~160 mM | Aprotic, H-bond acceptor | Stable | 162 ℃ |

Fig. S1 | XRD analysis before CO2RR. XRD patterns of Cu, Naf/Cu, Naf/DiG/Cu on CP before CO2RR.

Fig. S2 | SEM analysis for (a) Cu, (b) Naf/Cu, and (c) Naf/DiG/Cu.

Fig. S3 | XPS depth profile spectra of Naf/Cu. a-c, XPS spectra of C 1s (a), Cu 2p (b), and F 1s (c) based on Ar etching time.

Fig. S4 | XPS depth profile spectra of Naf/DiG/Cu. a-c, XPS spectra of C 1s (a), Cu 2p (b), and F 1s (c) based on Ar etching time.

Fig. S5 | EIS measurements for Cu and Naf/DiG/Cu. (a) Nyquist plots over the full frequency range and (b) enlarged view of the high-frequency region.

Fig. S6 | NMR analysis to confirm the dissolution of Diglyme in water. NMR spectra of DiG/Cu after immersion in water for 30 min.

Fig. S7 | NMR analysis to identify the Nafion protective effect on dissolution of Diglyme. NMR spectra of anolyte and cold trap after electrolysis at 2.7 and 3.6 V using Naf/DiG/Cu.

Fig. S8 | NMR analysis to identify the Nafion protective effect on dissolution of Diglyme. NMR spectra of the used MEA after CO2RR was deliberately torn apart and immersed in water.

Fig. S9 | Candidate products derived from the decomposition of ethanol.

Fig. S10 | Online DEMS spectra for ethanol fragment under Ar flow at 3.6 V over 30 min.

Fig. S11 | Nafion effect on hydrophobicity. Contact angle analysis for (a) Cu/CP, (b) Naf/Cu/CP, and (c) Naf/DiG/Cu/CP.

Fig. S12 | In situ SEIRAS spectra. a-b, In situ SEIRAS spectra of interfacial water during the CO2RR on Cu (a) and Naf/DiG/Cu (b). The spectra were deconvoluted into four components representing different hydrogen-bonding environments: strongly bound (purple), ice-like (green), asymmetric (blue), and isolated/free (red) water species [S6]. c, Fractions of the water species at various applied potentials. In all potential ranges, the Naf/DiG/Cu shows a higher contribution of ice-like water, and a corresponding lower contribution of asymmetric and isolated/free water compared to the bare Cu. This fitting result aligns well with the trend obtained from the center of mass frequency (νCOM). However, to avoid the potential ambiguities associated with multi-component fitting, we employed νCOM for further discussion in the main text.

Fig. S13 | Isotope analysis to investigate the correlation between water activity and CO2RR selectivity. a-b, FE (a) and partial current density (b) of H2 depending on H2O/D2O ratio.

Fig. S14 | Representative structures from the slow-growth AIMD simulations of the (a) ER mechanism and (b) LH mechanism on the DiG/Cu surface. The DiG molecule and the atoms actively participating in the reaction are shown in ball-and-stick representation, while the background water molecules are depicted as faded sticks for clarity.

Fig. S15 | Hetero-solvent effects on Cu-Ag electrode. Partial current densities for H2 of Cu-Ag and Naf/DiG/Cu-Ag.

Fig. S16 | (a) Partial current density and (b) selectivity for ethanol production.

Fig. S17 | SEM images of Cu, Naf/DiG/Cu, Cu-Ag, and Naf/DiG/Cu-Ag before/after CO2RR.

Fig. S18 | CO2RR performance in 1 M KOH. a-c, CO2RR product distribution of Cu (a), Naf/Cu (b), and Naf/DiG/Cu (c). d, Selectivity of C2H5OH compared to C2H4. e-f, Partial current density for C2H5OH (e) and C2H4 (f).

Fig. S19 | Ionomer effect on CO2RR based on hetero-solvent incorporated Cu electrode. a-b, CO2RR performance of Sus/Cu (a) and Sus/DiG/Cu (b).

Fig. S20 | Ionomer effect on CO2RR based on hetero-solvent incorporated Cu electrode. a-d, Partial current density for H2 (a), C2H4 (b), C2H5OH (c), and C2+ (d).

Fig. S21 | Substrate effect on CO2RR based on hetero-solvent incorporated Cu electrode. a-c, CO2RR performance of Cu (a), Naf/Cu (b), and Naf/DiG/Cu (c) using PTFE substrate.

Fig. S22 | Substrate effect on CO2RR based on hetero-solvent incorporated Cu electrode. a-d, Partial current density for H2 (a), C2H4 (b), C2H5OH (c), and C2+ (d).

Fig. S23 | Selectivity for C2/C1 under various KHCO3 concentrations. C2/C1 ratio of (a) Naf/Cu and (b) Naf/DiG/Cu electrodes.

Fig. S24 | HER performance under various KHCO3 concentrations. FE and partial current densities for H2 at (a) 1 M, (b) 0.5 M, and (c) 0.1 M KHCO3.

Fig. S25 | Selectivity for EtOH/C2H4 under various KHCO3 concentrations. EtOH/C2H4 ratio of (a) Naf/Cu and (b) Naf/DiG/Cu electrodes.

Fig. S26 | Long-term stability measurement of Cu. Cell voltage and FE of H2, C2H4, C2H5OH under 150 mA cm-2 during long-term CO2RR.

Fig. S27 | Long-term stability measurement of Naf/DiG/Cu. Cell voltage and FE of H2, C2H4, C2H5OH under 250 mA cm-2 during long-term CO2RR.

Fig. S28 | CO2RR performance in long-term stability. CO2RR average FE of Cu and Naf/DiG/Cu under 150 and 250 mA cm-2.

Fig. S29 | XPS spectra for Cu and Naf/DiG/Cu after long-term CO2RR

Fig. S30 | XRD analysis after CO2RR. XRD patterns of Cu, Naf/Cu, Naf/DiG/Cu on CP after CO2RR.

Fig. S31 | NMR spectra during long-term CO2RR of Naf/DiG/Cu under (a) 150 and (b) 250 mA cm−2.

Fig. S32 | NMR spectra after long-term CO2RR for 100 h of membrane/Naf/DiG/Cu under (a) 150 and (b) 250 mA cm −2.

Table S2 | State-of-the-art literature on ethanol production by MEA CO2RR in neutral media

| Catalysts | Anolyte | Cell voltage (V) | JEtOH (mA cm-2) | EtOH/C2H4 | Strategy |
| --- | --- | --- | --- | --- | --- |
| Naf/DiG/Cu-Ag | 1 M KHCO3 | 3.6 | 184.2 | 2.6 | Microenvironment engineering (Hetero-solvent) |
| FeTPP[Cl]/Cu [S7] | 0.1 M KHCO3 | 3.7 | 49.2 | 1.1 | Molecule-metal interface engineering |
| Defect-rich Cu [S8] | 0.1 M KHCO3 | 3.5 | 95 | 0.5 | Defect engineering |
| Sputtered Cu [S9] | 0.1 M KHCO3 | 4.9 | 46 | - | Porous layer for ethanol separation |
| Porous Cu/QAPEEK [S10] | H2O | 3.54 | 65.7 | 0.1 | Bifunctional ionomer coating |
| Cu2OZn [S11] | H2O | 4.29 | 148.2 | 2.3 | Alloy |
| Cu-poly-1 [S12] | 1 M KHCO3 | 3.98 | 88.9 | 0.4 | Functionalized Cu NPs with fluoric polymer |

Supplementary References

- M. Jödecke, Á. Pérez-Salado Kamps, G. Maurer, An experimental investigation of the solubility of CO2 in (N, N-dimethylmethanamide + water). J. Chem. Eng. Data 57(4), 1249–1266 (2012). https://doi.org/10.1021/je300105q

- X. Yin, J. Wang, S. Shen, Solubility of N2O and CO2 in dimethyl sulfoxide, 2-(butylamino)ethanol, and their water-lean blends. J. Chem. Eng. Data 69(4), 1668–1676 (2024). https://doi.org/10.1021/acs.jced.4c00015

- S. Joerg, R.S. Drago, J. Adams, Donor–acceptor and polarity parameters for hydrogen bonding solvents. J. Chem. Soc., Perkin Trans. 2 (11), 2431–2438 (1997). https://doi.org/10.1039/a701041i

- R.J. Gomes, C. Birch, M.M. Cencer, C. Li, S.-B. Son et al., Probing electrolyte influence on CO2 reduction in aprotic solvents. J. Phys. Chem. C 126(32), 13595–13606 (2022). https://doi.org/10.1021/acs.jpcc.2c03321

- P.J. Linstrom, W.G. Mallard, The NIST chemistry WebBook:   a chemical data resource on the Internet. J. Chem. Eng. Data 46(5), 1059–1063 (2001). https://doi.org/10.1021/je000236i

- C. Liang, Y. Katayama, Y. Tao, A. Morinaga, B. Moss et al., Role of electrolyte pH on water oxidation for iridium oxides. J. Am. Chem. Soc. 146(13), 8928–8938 (2024). https://doi.org/10.1021/jacs.3c12011

- F. Li, Y.C. Li, Z. Wang, J. Li, D.-H. Nam et al., Cooperative CO2-to-ethanol conversion via enriched intermediates at molecule–metal catalyst interfaces. Nat. Catal. 3(1), 75–82 (2020). https://doi.org/10.1038/s41929-019-0383-7

- Z. Gu, H. Shen, Z. Chen, Y. Yang, C. Yang et al., Efficient electrocatalytic CO2 reduction to C2+ alcohols at defect-site-rich Cu surface. Joule 5(2), 429–440 (2021). https://doi.org/10.1016/j.joule.2020.12.011

- R.K. Miao, Y. Xu, A. Ozden, A. Robb, C.P. O’Brien et al., Electroosmotic flow steers neutral products and enables concentrated ethanol electroproduction from CO2. Joule 5(10), 2742–2753 (2021). https://doi.org/10.1016/j.joule.2021.08.013

- W. Li, Z. Yin, Z. Gao, G. Wang, Z. Li et al., Bifunctional ionomers for efficient co-electrolysis of CO2 and pure water towards ethylene production at industrial-scale current densities. Nat. Energy 7(9), 835–843 (2022). https://doi.org/10.1038/s41560-022-01092-9

- T.-U. Wi, R. University, Z.H. Levell, S. Hao et al., Selective and stable ethanol synthesis via electrochemical CO2 reduction in a solid electrolyte reactor. ACS Energy Lett. 10(2), 822–829 (2025). https://doi.org/10.1021/acsenergylett.4c03091

- T. Zhao, X. Zong, J. Liu, J. Chen, K. Xu et al., Functionalizing Cu nanoparticles with fluoric polymer to enhance C2+ product selectivity in membraned CO2 reduction. Appl. Catal. B Environ. 340, 123281 (2024). https://doi.org/10.1016/j.apcatb.2023.123281