Supporting Information for

On-Site Periodontitis Diagnosis via Room-Temperature Oral Exhalation H2S Sensor Based on Yb-Doped Bi₂S₃ Nanoribbon

Ping Guo 1, Kai Wang 2, Xuyang An 1, Xuanyu Ren 3, Xinxin He 1, Yinhua Hu 1, Lijie Zhou 4, Guohua Cai 5, Lifeng Wang 6, Tiezhu Liu 1*, Wenyu Ge 2*, Jia Zhang1, 7*

1 State Key Laboratory of Robotics and System, Harbin Institute of Technology, Harbin 150080, P. R. China

2 Department of Stomatology Center, Heilongjiang Provincial Hospital, Harbin 150036, P. R. China

3 Key Laboratory of Bio-Based Material Science and Technology of the Ministry of Education, Northeast Forestry University, Harbin150040, P. R. China

4 School of Mechanical and Power Engineering, Harbin University of Science and Technology, Harbin, 150080, P. R. China

5 The Second Affiliated Hospital of Harbin Medical University, Harbin, 150081, P. R. China

6 School of Science, City Campus Australia, RMIT University, 124 La Trobe Street, Melbourne VIC 3000, Australia

7Key Laboratory of Micro-Systems and Micro-Structures Manufacturing, Ministry of Education, Harbin Institute of Technology, Harbin 150080, P. R. China

*Corresponding authors. E-mail:  zhangjia@hit.edu.cn (Jia Zhang);  liutiezhu@hit.edu.cn (Tiezhu Liu); gwysci@163.com (Wenyu Ge)

Supplementary Figures and Tables

Fig. S1 Schematic diagram of the gas sensing test system.

Fig. S2 SEM images of (a) Yb-Bi2S3-0.2%, (b) Yb-Bi2S3-0.5%, (c) Yb-Bi2S3-1.0 %, (d) Yb-Bi2S3-2.0%.

Fig. S3 TEM images of Yb-Bi₂S₃-1.5%.

Fig.S4 Comparison of high-resolution C 1s spectra between Yb-Bi₂S₃ derived from CAU-17 and Yb-Bi₂S₃ synthesized by a conventional one-step hydrothermal method.

Fig. S5 Work functions measured by Kelvin probe force microscopy (KPFM). (The relationship between the contact potential difference (CPD) and the work function (Φ) is given by CPD sample =CPD Au+(Φ Au−Φ sample), where CPD Au=−0.18, and Φ Au=5.10 eV. The measured CPD values for the Bi2S3 and Yb-Bi2S3 were approximately 0.08 eV and 0.34 eV, yielding corresponding work functions of 4.84 eV and 4.59 eV, respectively.)

Fig.S6 The optical properties of BS and Yb-Bi₂S₃-1.5%. (a) UV–vis spectra. (b) the calculated band gap.

Fig. S7 The response curve of Yb-Bi₂S₃-1.5% to 5 ppb H2S.

Fig. S8 A single-range fitting of the response as a function of concentration within the range of 0.005–5 ppm.

Fig. S9 Selective response of Yb-doped Bi₂S₃ sensor toward VOCs and VSCs

Fig. S10 Hysteresis characteristic of Yb-Bi₂S₃-1.5% in the range of 0.1-5 ppm.

Fig. S11 Repeatability test of Yb-Bi₂S₃-1.5% for Repeated exhalation exposure. (A specific volume of H₂S standard gas was mixed with high-humidity air to prepare simulated oral breath containing 100 ppb H₂S for testing. A dynamic testing method was employed: the gas in the sample bag was first dried to eliminate humidity interference. A small pump connected to a three-way valve at the outlet of the drying tube dynamically delivered gas from the gas bag to a 200-mL detection chamber for gas sensing.)

Fig. S12 (a) Baseline resistance and response to 100 ppb H₂S for five sensors from the same batch; (b) baseline resistance and response to 100 ppb H₂S for sensors from different batches

Fig. S13 Bader charge of H2S adsorption on the surface of BS and Yb-Bi₂S₃-1.5%, respectively.

Fig. S14 H₂S concentration curves in oral exhalation of periodontitis patients (post-dental prophylaxis).

Table S1 A comparative table of latest representative H₂S sensor based on different sensitive material

| Materials | Operating temperature | Detection limit(ppb) | Response | tres/trec | Detection range | Humidity tolerance | Selectivity | Sensor Integration | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metal Oxides and Heterojunctions |  |  |  |  |  |  |  |  |  |  |
| Amorphous a-SnO2 | 100 ℃ | 210 ppb | 2.4 (1ppm） | 9 min/- | 400 ppb ~ 1.5 ppm | ~20% reduction | - | no | [1] |
| Rh2O3/ WO3 | 157℃ | 250 ppb | ~5.2 (1 ppm) | 12/64 s | 0.25-100 ppm | ~75% reduction | > 22 | no | [2] |
| Bi2MoO6–CuO | 180 °C | 5 ppb | 4.9 (0.1 ppm) | 213s/1069s | 5-250 ppb |  | > 7 | yes | [3] |
| α-Fe2O3/SnO2 | 250 °C | 1 ppm | 4.3 (10 ppm) | 13s/104s | 2–10 ppm | - | >3 | no | [4] |
| Co3O4/β-CoMoO4 | 160 °C | 10 ppb | 1.25 (10 ppb) | 288/731 s | 0.01–20 ppm | - | > 2 | yes | [5] |
| Cu₂O/NiO | RT | 10 ppm | 1.39 (20 ppm) | ~100 s | 10–100 ppm | - | >10 | no | [6] |
| In2O3/SnO2 | RT | 100 ppb | ~5.2 (0.1 ppm) | 600/181 s | 0.1-70 ppm | ~53% reduction | > 15 | yes | [7] |
| WO3/CuO | 150℃ | 0.5 ppm | 0.68 (5ppm） | 24 s / 78 s | 0.5–50 ppm | - | >6 | no | [8] |
| Fe2O3/Ti3C2 | RT | 10 ppb | 1.18 (20 ppm) | 10s/15s | 0.01–500 ppm | ~28% reduction | >6 | no | [9] |
| Transition Metal Sulfides and Heterojunctions |  |  |  |  |  |  |  |  |  |  |
| WS2 | RT | 53 ppb | 0.15 (27 ppm) | 175 s/- | 53 ppb-27 ppm | ~400% increase | > 10 | no | [10] |
| Bi2S3 | RT | 0.5 ppm | 2.03 (10 ppm) | 27 s/21 s | 0.5–50 ppm | - | > 10 | no | [11] |
| MoSe2/ZnO | 150 ℃ | 200 ppb | 2.8 (6 ppm) | 690 s/665 s | 200 ppb–6.1 ppm | - | ~2 | no | [12] |
| MoS2/rGO | RT | 1 ppm | 1.18 (1ppm) | 0.85/12.1 s | 1-100 ppm | ~46% reduction | >5 | no | [13] |
| WS2- ZnO | 250 °C | 0.1 ppm | 0.33 (1ppm) | ~120s/ | 0.1-5 ppm | - | >8 | no | [14] |
| ZIF-L/SnS2 | 125 ℃ | 3.6 ppb | 1.11 (1 ppm) | 413s/2276s | 1-50 ppm | - | >10 | no | [15] |
| Other material systems |  |  |  |  |  |  |  |  |  |  |
| Cs2AgBiCl6 | RT | 5 ppb | 0.16 (0.08pm) | 99.6/94.2s | 5 ppb-10 ppm | - | >40 | yes | [16] |
| Co3(HITP)2/Ti3C2 | RT | 92 ppb | 2.41(10 ppm) | ~200 s/- | 0.1–200 ppm | ~12% reduction | >2 | no | [17] |
| CsPbBr3 | RT | <200 ppb | 1.21 (0.2 ppm) | 73/275 s | 0.2-5 ppm | <5% | >10 | no | [18] |
| This work |  |  |  |  |  |  |  |  |  |  |
| Yb-Doped Bi₂S₃ | RT | 5 ppb | 9.13 (1 ppm) | 11 s/141 s | 5 ppb-5 ppm | ~27% reduction | > 20 | yes | - |

Supplementary References

- V. Paolucci, J. De Santis, V. Ricci, L. Lozzi, G. Giorgi et al., Bidimensional engineered amorphous a-SnO2 interfaces: synthesis and gas sensing response to H2S and humidity. ACS Sens. 7(7), 2058–2068 (2022). https://doi.org/10.1021/acssensors.2c00887

- D. Xu, R. Li, X. Duan, B. Sun, X. Gong et al., In-situ construction of highly sensitive H2S gas sensor based on Rh2O3-loaded WO3 composites derived from WSe2 flower-like structure. Sens. Actuat. B Chem. 460, 139938 (2026). https://doi.org/10.1016/j.snb.2026.139938

- Q. Jing, C. Gong, W. Bian, Q. Tian, Y. Zhang et al., Ultrasensitive chemiresistive gas sensor can diagnose asthma and monitor its severity by analyzing its biomarker H2S: an experimental, clinical, and theoretical study. ACS Sens. 7(8), 2243–2252 (2022). https://doi.org/10.1021/acssensors.2c00737

- X.-Y. Miao, L.-Y. Zhu, X.-Y. Wu, L.-W. Mao, X.-H. Jin et al., Precise preparation of α-Fe2O3/SnO2 core-shell nanowires via atomic layer deposition for selective MEMS-based H2S gas sensor. Sens. Actuat. B Chem. 378, 133111 (2023). https://doi.org/10.1016/j.snb.2022.133111

- S. Cao, Z. Song, Y. Bing, X. Xu, T. Zhou et al., Metal–organic-framework derived co–Mo multimetal oxide semiconductors: selective trace-level hydrogen sulfide detection. ACS Sens. 9(6), 2979–2988 (2024). https://doi.org/10.1021/acssensors.4c00144

- H. Sun, M. Cao, P. Zhang, X. Tian, M. Lu et al., Magnetic-field-enhanced H2S sensitivity of Cu2O/NiO heterostructure ordered nanoarrays. ACS Sens. 7(7), 1903–1911 (2022). https://doi.org/10.1021/acssensors.2c00495

- Y. Sun, K. Qian, J. Yue, X. Zhang, X. Li et al., High-response In2O3/SnO2 heterojunction sensor for detection of food spoilage gas H2S in refrigerators. Sens. Actuat. B Chem. 451, 139341 (2026). https://doi.org/10.1016/j.snb.2025.139341

- C. Qiu, L. Zhu, Q. Li et al., One-step electrospun WO3/CuO p–n heterojunction nanocomposites for ultrasensitive and rapid H2S detection. ACS Sens. 10(9), 6869–6877 (2025). https://doi.org/10.1021/acssensors.5c01761

- D. Zhang, X. Huang, W. Meng, J. Yuan, F. Guo et al., Room-temperature flexible CNT/Fe2O3 film sensor for ppb-level H2S detection. ACS Sens. 9(10), 5197–5205 (2024). https://doi.org/10.1021/acssensors.4c01342

- S. Kundu, G. Gorthala, R. Ghosh, Room temperature detection of H2S by two dimensional WS2 based chemiresistive sensors. Sens. Actuat. B Chem. 416, 136018 (2024). https://doi.org/10.1016/j.snb.2024.136018

- C. Li, S. Ramadan, H. Kan, L. Wang, Light-activated room temperature surface acoustic wave H2S sensor based on Bi2S3 nanoribbons. Sensors 25(4), (2025). https://doi.org/10.3390/s25041122

- R.K. Jha, A. Nanda, A. Yadav, R. Sai, N. Bhat, 2D-MoSe2/0D-ZnO nanocomposite for improved H2S gas sensing in dry air ambience. J. Alloys Compd. 926, 166825 (2022). https://doi.org/10.1016/j.jallcom.2022.166825

- G.M. Hingangavkar, S.A. Kadam, Y.-R. Ma, M. Selvaraj, R.N. Mulik et al., On the behavior of MoS2-rGO nanocomposites for chemiresistive H2S detection at room temperature. Sens. Actuat. B Chem. 399, 134843 (2024). https://doi.org/10.1016/j.snb.2023.134843

- N. Sakhuja, R.K. Jha, R. Sai, N. Bhat, ZnO nanorods grown on WS2 nanosheets for chemiresistive H2S sensing. ACS Appl. Nano Mater. 5(7), 9241–9251 (2022). https://doi.org/10.1021/acsanm.2c01580

- S.M. Lee, Y.J. Kim, S.J. Park, W.S. Cheon, J. Kim et al., In-situ growth of 2D MOFs as a molecular sieving layer on SnS2Nanoflakes for realizing ultraselective H2S detection. Adv. Funct. Mater. 35(12), 2417019 (2025). https://doi.org/10.1002/adfm.202417019

- M. Li, S. University, W. Ye, S. University, et al., Lead-free halide double perovskite Cs2AgBiCl6 for H2S trace detection at room temperature. ACS Sens. 10(3), 2224–2233 (2025). https://doi.org/10.1021/acssensors.4c03532

- Y. Sun, W. Guo, B. Wang, Y. Hou, W. Wang et al., Construction of a Co3(HITP)2/Ti3C2 MXene heterojunction for selective sensing of H2S with high resistance to humidity. Sens. Actuat. B Chem. 450, 139224 (2026). https://doi.org/10.1016/j.snb.2025.139224

- K. Zhou, H. Yang, Z. Du, Y. Yang, C. Zhu et al., Ultrahigh selectivity H2S gas sensor based CsPbBr3 perovskites via Pb–S bonding interaction. ACS Sens. 10(1), 517–525 (2025). https://doi.org/10.1021/acssensors.4c02980