Supporting Information for

Decoupling Ion-Dipole Interactions via Competitive Coordination for Durable Dendrite-free Zinc Metal Batteries

Bixian Chen1, 4, Xiaomin Cheng1, 8, Xiang Li5, Qinghua Guan1, Hao Li2, 3, Yongzheng Zhang6, Shuang Cheng1, Huihua Li2, 3, Yunjian Liu4, *, Jing Zhang7, Hongzhen Lin1, *, Jian Wang2, 3, *

1 i-Lab & CAS Key Laboratory of Nanophotonic Materials and Devices, Suzhou Institute of Nano-Tech and Nano-Bionics, Chinese Academy of Sciences, Suzhou 215123, P. R. China

2 Helmholtz Institute Ulm (HIU), Ulm D89081, Germany

3 Karlsruhe Institute of Technology (KIT), Karlsruhe D76021, Germany

4 School of Materials Science and Engineering, Jiangsu University, Zhenjiang 212013, P. R. China

5 Anhui Provincial Key Laboratory of Green Carbon Chemistry, Fuyang Normal University, Fuyang 236037, P. R. China

6 School of Textile & Clothing, Nantong University, Nantong 226019, P. R.  China

7 School of Materials Science and Engineering, Xi’an University of Technology, Xi’an 710048, P. R.  China

8 Guangdong Institute of Semiconductor Micro-Nano Manufacturing Technology, Guangdong 518103, P. R.  China

Bixian Chen and Xiaomin Cheng contributed equally to this work.

*Corresponding authors. E-mail: lyjian122331@ujs.edu.cn (Yunjian Liu);  hzlin2010@sinano.ac.cn (Hongzhen Lin); wangjian2014@sinano.ac.cn or jian.wang@kit.edu (Jian Wang)

S1 Supplementary Figures

Fig. S1 Schematic diagram of the L-CN molecular structure.

Fig. S2 a Radial distribution functions of Zn2+-O (H2O) in BE. b The 3D snapshot of the BE obtained from MD simulations.

Fig. S3 MSD of Zn2+ in different electrolytes.

Fig. S4 Fitted Raman spectra of -OH in a 0 mmol L-1 L-CN, b 5 mmol L-1 L-CN, c 10 mmol L-1 L-CN, d 20 mmol L-1 L-CN, and e 50 mmol L-1 L-CN. f The summary proportions of strong, medium, and weak H-bonds in the systems.

Fig. S5 Fitted Raman spectra of -OSO3 in a 0 mmol L-1 L-CN, b 5 mmol L-1 L-CN, c 10 mmol L-1 L-CN, d 20 mmol L-1 L-CN, and e 50 mmol L-1 L-CN.

Fig. S6 The long-term cycling performance with L-CN under various concentrations (0-50 mmol L-1).

Fig. S7 Ionic conductivity test with L-CN under different concentrations (0-50 mmol L-1).

The ionic conductivities (σ) were tested by two blocking electrodes (SS) and calculated according to equation S1:

σ=LRS                                                              (S1)

where L represents the diffusion thickness (1.624 mm), and S is the contact area (0.503 cm-2) between SS and electrolyte, R0=5.709 Ω, R5=5.857 Ω, R10=5.901 Ω, R20=6.175 Ω, R50=6.437 Ω.

Fig. S8 Nyquist plots of symmetric cells employed with a BE and b BE-LCN in at different temperatures. c Charge transfer activation energies based on EIS impedance. d Equivalent circuit diagram used for EIS fitting.

The charge transfer activation energies (Ea) were calculated by fitting to the Arrhenius equation:

1Rct=Aexp-EaRT)                                                 (S2)

Where Rct represents the charge-transfer resistance, Ea denotes the activation energy, R is the ideal gas constant, and T represents the temperature in Kelvin.

Fig. S9 The Zn2+ transference number (tZn2+) of a BE and b BE-LCN. c The tZn2+ of various electrolytes.

The tZn2+ is evaluated by the equation S3:

tZn2+=Is(∆V-I0R0)I0(∆V-IsRs)	                                             (S3)

Where ΔV is the applied voltage (20 mV), I0 and Is are the initial and final current, R0 and Rs are the initial and final resistance.

Fig. S10 Contact angle measurements of a BE and b BE-LCN electrolytes on the Zn anode.

Fig. S11 Cyclic voltammetry (CV) tests at different scan rates in a BE and b BE-LCN.

The EDL capacitance was calculated through the equation S4:

C=icv                                                          (S4)

Where ic represents the double-layer current and v denotes the scan rate. The linear relationship between ic and v allows for the calculation of capacitance, with C derived from the slope of the ic versus v plot. Specifically, ic is calculated as ic =(i0+-i0−)/2, which is the average of the current difference between the forward and reverse scans at 0 V.

Fig. S12 Operando EIS evolution and corresponding analysis of DRT during galvanostatic plating in a BE and b BE-LCN. EIS evolutions during plating at 1 mA cm-2 in c BE and d BE-LCN symmetric cells.

The EIS measurements were performed after Zn was deposited at 1 mA cm-2 for 6 min, followed by a 1 min rest period. The total Zn deposition time is 60 min.

Fig. S13 The SEM images of Zn anodes after plating at first cycle with different current densities and 1 mAh cm-2: a 1 mA cm-2, b 2 mA cm-2 and c 5 mA cm-2 in BE; d 1 mA cm-2, e 2 mA cm-2 and f 5 mA cm-2 in BE-LCN.

Fig. S14 The SEM images of the cycled Zn foils in a BE and b BE-LCN.

Fig. S15 XRD results of Zn foil after 20 cycles at 1 mA cm-2, 1 mAh cm-2.

Fig. S16 pH value of BE and BE-LCN electrolytes.

Fig. S17 Intensity comparison of ZnO-, OH- and SO3- species on cycled Zn in BE and BE-LCN.

Fig. S18 Capacity-voltage curves of a BE and b BE-LCN under different cycles.

Fig. S19 a Coulombic efficiency (CE) values of Zn//Cu cells in BE and BE-LCN with a cut-off voltage of 0.8 V at 1 mA cm−2. Capacity-voltage curves of b  BE and c BE-LCN under different cycles.

Fig. S20 a CE values of Zn//Cu cells in BE and BE-LCN with a cut-off voltage of 0.8 V at 5 mA cm−2. Capacity-voltage curves of b BE and c BE-LCN under different cycles.

Fig. S21 GITT profiles of symmetric cells in BE and BE-LCN at 1 mA cm-2 for 3 min and a rest of 3 min.

Fig. S22 Resting-cycle cycling stability of symmetric cells in BE and BE-LCN at 1 mA cm-2.

Fig. S23 EIS evolution of Zn//Zn symmetric cells during 50 cycles with a BE and b BE-LCN electrolytes at 1 mA cm-2.

Fig. S24 Rate performances of symmetric cells in BE and BE-LCN.

Fig. S25 Galvanostatic cycling performance at 11.7 mA cm-2, 11.7 mAh cm-2 under a high depth of discharge (40%) condition (Zn foil thickness: 50 μm).

The high depth of discharge (DOD) is the percentage of the capacity involved in the electrode reaction relative to the overall capacity of the Zn metal anode:

DOD=yCZn*x×10-4*100%                                          (S6)

where CZn is the theoretical volume capacity of Zn (5855 mAh cm-3), x (μm) is the thickness of the Zn foil and y (mAh cm−2) represents the Zn areal capacity used in electrochemical testing.

Fig. S26 CV curves of Zn//V2O5-x full cells with BE and BE-LCN electrolytes at the second cycle.

Fig. S27 Capacity-voltage curves of Zn//V2O5-x full cell in BE.

Fig. S28 CV curves of Zn//PANI full cells with BE and BE-LCN electrolytes at the second cycle.

Fig. S29 a Rate performances of Zn//PANI full cells in BE and BE-LCN. Capacity-voltage curves of Zn//PANI full cells in b BE and c BE-LCN.

Fig. S30 Self-discharge profiles of Zn//PANI full cells in BE and BE-LCN.

Fig.  S31 The SEM images of the cycled V2O5-x cathodes in a BE and b BE-LCN.

Fig. S32 EIS analysis of Zn//V2O5-x full cells in a BE and b BE-LCN before and after 50 cycles.

Fig. S33 The SEM images of the cycled PANI cathodes in a BE and b BE-LCN.

Fig. S34 EIS analysis of Zn//PANI full cells in a BE and b BE-LCN before and after 50 cycles.

Fig. S35 a The long-term cycling performances of  Zn//V2O5-x full cells in BE and BE-LCN at 1 A g−1. Capacity-voltage curves of Zn//V2O5-x full cells in b BE and c BE-LCN.

Fig. S36 a The long-term cycling performances of Zn//V2O5-x full cells in BE and BE-LCN at 10 A g-1. Capacity-voltage curves of Zn//V2O5-x full cells in b BE and c BE-LCN.

Fig. S37 The long-term cycling performances of Zn//V2O5-x full cells in BE and BE-LCN at 0.5 A g-1

Fig. S38 The long-term cycling performances of Zn//PANI full cells in BE and BE-LCN at 3 A g-1.

S2 Supplementary Tables

Table S1 The N/P ratio of full cells

| Type of cells | Zn thickness (cm) | Zn area (cm-2) | Negative Capacity (mAh) | Mass Loading of Cathode (mg) | Positive Capacity (mAh) | N/P Ratio |
| --- | --- | --- | --- | --- | --- | --- |
| Coin | 0.002 | 1.13 | 13.23 | 5.64 | 3.32 | 3.98 |
| Pouch | 0.005 | 14 | 409.84 | 99.96 | 58.88 | 6.96 |

The N/P ratio is calculated by the following equation:

Negative Capacity (mAh) = Zn thickness (cm) * ρZn (g cm-3) * Theoretical specific capacity of Zn (mAh g-1) * Area of the Zn anode

Positive Capacity (mAh) = Mass loading of cathode (g) * Theoretical specificcapacity of V2O5-x (mAh g-1)

Where ρZn, theoretical specific capacity of Zn and theoretical specific capacity of V2O5 are 7.14, 820 and 589, respectively.

Table S2 Performance comparison of symmetrical cells with different electrolyte additives between previous studies and this work

| Electrolyte additive | Current density (mA cm-2) |  | Areal capacity (mAh cm-2) | Lifespan (h) | Reference |
| --- | --- | --- | --- | --- | --- |
| L-CN |  | 1 | 1 | 7000 | This work |
| L-CN |  | 5 | 5 | 2000 | This work |
| PEG-oSDE |  | 1 | 1 | 1400 | [S1] |
| TXA |  | 5 | 5 | 700 | [S2] |
| DA |  | 2 | 1 | 1000 | [S3] |
| SMD |  | 5 | 3 | 1400 | [S4] |
| Na-L |  | 2 | 1 | 1500 | [S5] |
| AS |  | 5 | 5 | 1300 | [S6] |
| PA |  | 2 | 2 | 1200 | [S7] |
| PNO |  | 5 | 5 | 1000 | [S8] |

Table S3 DOD and cycle lifespan comparison of symmetrical cells between previous studies and this work

| Electrolyte additive | Current density (mA cm-2) |  | Areal capacity (mAh cm-2) | DOD (%) | Lifespan (h) | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| L-CN |  | 11.7 | 11.7 | 40 | 7000 | This work |
| L-CN |  | 5 | 10 | 85.4 | 200 | This work |
| CoPcS₄ |  | 10 | 3 | 51.2 | 150 | [S9] |
| NHM |  | 6 | 6 | 60 | 400 | [S10] |
| CTP |  | 8.8 | 8.8 | 50 | 300 | [S11] |
| PN-ps coating |  | 2 | 20 | 68.3 | 400 | [S12] |
| AHRE |  | - | - | 60 | 300 | [S13] |

Table S4 Performance comparison of full cells with different electrolyte additives between previous studies and this work

| Electrolyte additive | Cathode materials | Current (A g-1) | Cycling performances | Reference |
| --- | --- | --- | --- | --- |
| L-CN | V2O5-x | 1 | 500 cycles 95.2% 444 mAh g-1 | This work |
| L-CN | V2O5-x | 10 | 4000 cycles 93.9% | This work |
| L-CN | PANI | 3 | 4000 cycles 86.3% | This work |
| LA | NH4V4O10 | 5 | 2000 cycles 80.35% | [S14] |
| DP | NH4V4O10 | 3 | 3000 cycles 80.3% | [S15] |
| 10% Xos | ZnVO | 5 | 1000 cycles 82.9% | [S16] |
| Zn(BF4)2-AN | PANI | 1 | 2000 cycles 86.72% | [S17] |
| Glu | PANI | 1 | 1000 cycles 91% | [S18] |
| PCA-Zn | PANI | 1 | 2000 cycles 73.33% | [S19] |
| Zn(CF3SO3)2 | MEG/PANI | 2 | 2000 cycles 72.7% | [S20] |

Table S5 N/P ratio and performance comparison of full cells between previous studies and this work

| Work | Cathode materials | Type of cells | Cycling performances | N/P ratio | Reference |
| --- | --- | --- | --- | --- | --- |
| L-CN | V2O5-x | coin | 500 cycles 1 A g-1 | 3.98 | This work |
| L-CN | V2O5-x | pouch | 200 cycles 1 A g-1 | 6.96 | This work |
| FCOF@Zn | MnO2 | coin | 200 cycles 4 mA cm-2 | 5 | [S21] |
| Sorbitol | CNF/MnO2 | coin | 500 cycles 1 A g-1 | 5.55 | [S22] |
| NH4Ac/Et4 NOTF | PANI | coin | 1000 cycles 1 A g-1 | 5~6 | [S23] |
| FPCH-ZI/Zn | MnO2 | coin | 600 cycles 0.5 A g-1 | 7.3 | [S24] |
| Zinc-plated Cu substrate | MnO2 | coin | 640 cycles 5 mA cm-2 | 5 | [S25] |

Supplementary References

- Z. Shi, M. Li, X. Fu, Y. Zhang, S. Jiao et al., Bimodal Block molecule with ether-type and hydroxyl-type oxygen stabilizes Zn anode in super-dilute electrolyte. Adv. Funct. Mater. 34(25), 2316427 (2024). https://doi.org/10.1002/adfm.202316427

- J. Yin, H. Liu, P. Li, X. Feng, M. Wang et al., Integrated electrolyte regulation strategy: Trace trifunctional tranexamic acid additive for highly reversible Zn metal anode and stable aqueous zinc ion battery. Energy Storage Mater. 59, 102800 (2023). https://doi.org/10.1016/j.ensm.2023.102800

- Y. Yang, Y. Li, Q. Zhu, B. Xu, Optimal molecular configuration of electrolyte additives enabling stabilization of zinc anodes. Adv. Funct. Mater. 34(32), 2316371 (2024). https://doi.org/10.1002/adfm.202316371

- S. Zheng, Y. Wang, B. Luo, L. Sun, G. Duan et al., In-situ formation of heterogeneous interfaces inducing surface crystallographic manipulation toward highly stable Zn anode. Chem. Eng. J. 473, 145313 (2023). https://doi.org/10.1016/j.cej.2023.145313

- Z. Hu, F. Zhang, A. Zhou, X. Hu, Q. Yan et al., Highly reversible Zn metal anodes enabled by increased nucleation overpotential. Nanomicro Lett. 15(1), 171 (2023). https://doi.org/10.1007/s40820-023-01136-z

- X. Ma, Q. Wang, X. Zhang, Y. Lin, F. Zhang et al., Highly reversible zinc anode enabled by a trace-amount additive with pH buffering capability. Energy Environ. Sci. 18(2), 982–990 (2025). https://doi.org/10.1039/d4ee04870a

- K. Wang, H. Zhan, X.-X. Liu, X. Sun, Uncovering required molecular properties for interface regulators and modification mechanisms for Zn anode in aqueous batteries. Adv. Funct. Mater. 35(16), 2418993 (2025). https://doi.org/10.1002/adfm.202418993

- Q. Kang, H. Liang, Z. Zhu, F. Xing, B. Zhu et al., Non-substituted aromatic pyridine N-oxide additives with an intrinsic N→O acceptor for ultra-long-life Zn||MnO2 batteries. Angew. Chem. Int. Ed. 64(10), e202420183 (2025). https://doi.org/10.1002/anie.202420183

- Z. Fang, J. Li, L. Xiang, K. Liu, Y. Pan et al., Kinetic regulation of Zn(002) textured interfaces for highly reversible Zn–iodine batteries. Energy Storage Mater. 82, 104592 (2025). https://doi.org/10.1016/j.ensm.2025.104592

- L. You, S. Guo, Y. He, Y. Xie, S. Liang et al., Surface tension-derived electrical double layer modification enables practical zinc-ion pouch cells. Adv. Funct. Mater. 35(31), 2500780 (2025). https://doi.org/10.1002/adfm.202500780

- Z. Chen, Y. Liao, Z. Lu, G. Chen, H.M.A. Hassan et al., Amphiphilic interfacial environment reconfiguration unlocks long-life zinc-ion batteries with lean electrolytes and ultra-low N/P ratios. Angew. Chem. Int. Ed. 65(26), e4128996 (2026). https://doi.org/10.1002/anie.4128996

- Z. Zhang, G. Liao, Y. Lin, W. Du, Y. Zhang et al., Decoupled yet synergistic microdomains via in situ phase separation enabling ultra-stable zinc metal anodes. Adv. Energy Mater. e71136 (2026). https://doi.org/10.1002/aenm.71136

- X. Zhang, Q. Tang, H. Luo, Y. Xu, S. Miao et al., Hydrogen bond reconstruction maneuver in eutectic electrolyte enables ultralong-lifespan zinc-ion batteries. J. Am. Chem. Soc. 147(43), 39440–39451 (2025). https://doi.org/10.1021/jacs.5c12021

- R. Jiang, T. Naren, Y. Chen, Z. Chen, C. Zhang et al., Enhanced hydrogen bonding through strong water-locking additives for long-term cycling of zinc ion batteries. Adv. Funct. Mater. 34(49), 2411477 (2024). https://doi.org/10.1002/adfm.202411477

- M. Wu, Y. Sun, Z. Yang, S. Deng, H. Tong et al., Harnessing ion-dipole interactions for water-lean solvation chemistry: achieving high-stability Zn anodes in aqueous zinc-ion batteries. Angew. Chem. Int. Ed. 63(43), e202407439 (2024). https://doi.org/10.1002/anie.202407439

- W. Guo, L. Xu, Y. Su, L. Zhao, Y. Ding et al., Synchronous modulation of H-bond interaction and steric hindrance via bio-molecular additive screening in Zn batteries. Angew. Chem. Int. Ed. 64(5), e202417125 (2025). https://doi.org/10.1002/anie.202417125

- Z. Zha, D. Li, T. Sun, Q. Sun, J. Hou et al., Electrolyte design via cation-anion association regulation for high-rate and dendrite-free zinc metal batteries at low temperature. J. Am. Chem. Soc. 146(46), 31612–31623 (2024). https://doi.org/10.1021/jacs.4c09524

- Y. Chen, B. Yin, Y. Zeng, H. Wang, B.-B. Xie et al., Ion-dipole-interaction-manipulated bilateral interface chemistry for deep rechargeability and high redox activity of Zn-organic batteries. Chem 11(6), 102411 (2025). https://doi.org/10.1016/j.chempr.2025.102411

- M. Yang, J. Zhu, S. Bi, R. Wang, H. Wang et al., The construction of anion-induced solvation structures in low-concentration electrolyte for stable zinc anodes. Angew. Chem. Int. Ed. 63(15), e202400337 (2024). https://doi.org/10.1002/anie.202400337

- X. Liao, C. Pan, H. Yan, Y. Zhu, Y. Pan et al., Polyaniline-functionalized graphene composite cathode with enhanced Zn2+ storage performance for aqueous zinc-ion battery. Chem. Eng. J. 440, 135930 (2022). https://doi.org/10.1016/j.cej.2022.135930

- Z. Zhao, R. Wang, C. Peng, W. Chen, T. Wu et al., Horizontally arranged zinc platelet electrodeposits modulated by fluorinated covalent organic framework film for high-rate and durable aqueous zinc ion batteries. Nat. Commun. 12, 6606 (2021). https://doi.org/10.1038/s41467-021-26947-9

- Y. Quan, M. Yang, M. Chen, W. Zhou, X. Han et al., Electrolyte additive of sorbitol rendering aqueous zinc-ion batteries with dendrite-free behavior and good anti-freezing ability. Chem. Eng. J. 458, 141392 (2023). https://doi.org/10.1016/j.cej.2023.141392

- X. Zhao, N. Dong, M. Yan, H. Pan, Unraveling the interphasial chemistry for highly reversible aqueous Zn ion batteries. ACS Appl. Mater. Interfaces 15(3), 4053–4060 (2023). https://doi.org/10.1021/acsami.2c19022

- J.B. Park, C. Choi, J.H. Park, S. Yu, D.-W. Kim, Synergistic design of multifunctional interfacial Zn host toward practical Zn metal batteries. Adv. Energy Mater. 12(48), 2202937 (2022). https://doi.org/10.1002/aenm.202202937

- C. Xie, H. Ji, Q. Zhang, Z. Yang, C. Hu et al., High-index zinc facet exposure induced by preferentially orientated substrate for dendrite-free zinc anode. Adv. Energy Mater. 13(3), 2203203 (2023). https://doi.org/10.1002/aenm.202203203