Supporting Information for

Surfactant-Derived Nitrogen-Bridged MoS2/C Heterostructures for Robust Lithium-Ion Storage

Senchuan Huang1, #, *, Kewei Pei1, #, Yunyi Chen1, Yangfei Cao2, *, Jingwen Shangguan1, Shiman He3, Junxia Meng4, and Shanqing Zhang1, 5, *

1 School of Chemical Engineering and Light Industry, Guangdong University of Technology, Guangzhou 510006, P. R. China

2 School of Materials and Energy, Guangdong University of Technology, Guangzhou 510006, P. R. China

3 School of Materials Science and Engineering, Guangdong Provincial Key Laboratory of Advanced Energy Storage Materials, South China University of Technology, Guangzhou 510641, P. R. China

4 School of Physics and Electronics, Gannan Normal University, Ganzhou 341000, P. R. China

5 School of Environment and Science, Griﬃth University, Gold Coast, QLD 4222, Australia

# Senchuan Huang and Kewei Pei contribute to the work equally.

* Corresponding authors. E-mail: huangsch@gdut.edu.cn (Senchuan Huang); caoyf@gdut.edu.cn (Yangfei Cao); s.zhang@griffith.edu.au (Shanqing Zhang)

Supplementary Figures and Tables

Fig. S1 FESEM image of mSiO2@CTAB

Fig. S2 a Nitrogen adsorption–desorption isotherms and b corresponding pore size distribution curve of mSiO2@CTAB

Fig. S3 FESEM images of SiO2@MoS2-N-C composites at different magnifications: a, b SiO2@MoS2-N-C600, c, d SiO2@MoS2-N-C700, and e, f SiO2@MoS2-N-C800

Fig. S4 Digital photographs of mSiO2@CTAB before and after carbonization

Fig. S5 TG curve of CTAB measured under Ar

Fig. S6 TG curve of thiourea measured under Ar

Fig. S7 FESEM images of the MoS2-N-C heterostructures synthesized at different temperatures: a MoS2-N-C600 and b MoS2-N-C800

Fig. S8 a TEM image and b SAED pattern of MoS2-N-C700

Fig. S9 FESEM images of commercial MoS2 at different magnifications

Fig. S10 EDS spectrum of MoS2-N-C700, showing the existence of N-dopants

Fig. S11 a TEM and b HRTEM images of commercial MoS2

Fig. S12 XRD pattern of commercial MoS2

Fig. S13 Full Raman spectra of MoS2-N-C600, MoS2-N-C700, and MoS2-N-C800

Fig. S14 Pore size distribution curves of MoS2-N-C600, MoS2-N-C700, and MoS2-N-C800

Fig. S15 XPS survey spectra of MoS2-N-C600, MoS2-N-C700, and MoS2-N-C800

Fig. S16 a Normalized XANES spectrum and b Fourier transformed k2-weighted EXAFS spectrum of Mo K-edge for MoS2-N-C700

Fig. S17 Structure characterization of Pristine MoS2 control sample. a, b FESEM images at different magnifications, c XRD pattern, and d TG curves

Fig. S18 a N2 adsorption-desorption isotherms and b-d Mo 3d, Mo 3p and S 2p spectra of Pristine MoS2 control sample, respectively

Fig. S19 EPR spectra of MoS2-N-C600, MoS2-N-C700, and MoS2-N-C800

Fig. S20 EPR tests of MoS2-N-C700 electrodes after different cycles at 0.5 A g-1

Fig. S21 a N2 absorption/desorption isotherms and b relative specific area of MoS2-N-C700 electrodes before cycling and after different cycles at 0.5 A g-1

Fig. S22 a CV cures and b corresponding redox peak currents of MoS2-N-C700 electrodes after different cycles

Fig. S23 Deconvoluted XPS spectra of MoS2-N-C700 electrodes after different cycles at 0.5 A g-1: a Mo 3d, and b N 1s + Mo 3p

Fig. S24 Cycling stability of MoS2-N-C600 at 0.5 A g-1

Fig. S25 Cycling stability of MoS2-N-C800 at 0.5 A g-1

Fig. S26 a N2 adsorption-desorption isotherms and b corresponding pore size distribution curve of MoS2/NC control sample

Fig. S27 SEM images of MoS2/NC control sample at different magnifications

Fig. S28 Cycling stability of MoS2-N-C700 at 2 A g-1

Fig. S29 dQ/dV curves at various cycles of a MoS2-N-C600 and b MoS2-N-C800

Fig. S30 dQ/dV curves of MoS2/NC at various cycles

Fig. S31 First three CV curves at 0.1 mV s-1 of a MoS2-N-C600 and b MoS2-N-C800

Fig. S32 First three CV curves at 0.1 mV s-1 of commercial MoS2

Fig. S33 First three CV curves at 0.1 mV s-1 of MoS2/NC

Fig. S34 First three GCD curves of a MoS2-N-C600 and b MoS2-N-C800 obtained at 0.1 A g-1

Fig. S35 First three GCD curves of a commercial MoS2 and b MoS2/NC obtained at 0.1 A g-1

Fig. S36 a Rate performance and b cycling stability at 0.5 A g-1 of MoS2-N-C700 at a high mass loading of ~2.9 mg cm-2

Fig. S37 Rate performance of MoS2-N-C700, commercial MoS2 and MoS2/NC electrodes

Fig. S38 Deconvoluted N 1s XPS spectra for the MoS2-N-C700 electrode after discharging to 0.01 V at 0.1 A g-1

Fig. S39 Nyquist plots of MoS2-N-C600, MoS2-N-C700 and MoS2-N-C800

Fig. S40 Linear relationship between Z′ and 𝜔-1/2 of MoS2-N-C600, MoS2-N-C700, and MoS2-N-C800

Fig. S41 Nyquist plot of MoS2/NC control sample

Fig. S42 a CV curves at scan rates from 0.2 to 1.0 mV s-1, b linear fitting of the logarithmic relationship between peak current log(i) and scan rate log(v), c pseudocapacitive contribution at different scan rates, and d pseudocapacitive contribution at 1.0 mV s-1 of MoS2-N-C600

Fig. S43 a CV curves at scan rates from 0.2 to 1.0 mV s-1, b linear fitting of the logarithmic relationship between peak current log(i) and scan rate log(v), c pseudocapacitive contribution at different scan rates, and d pseudocapacitive contribution at 1.0 mV s-1 of MoS2-N-C800

Fig. S44 Pseudocapacitive contribution of MoS2-N-C700 at different scan rates

Fig. S45 a CV curves at scan rates from 0.2 to 1.0 mV s-1, b linear fitting of the logarithmic relationship between peak current log(i) and scan rate log(v), c pseudocapacitive contribution at different scan rates, and d pseudocapacitive contribution at 1.0 mV s-1 of MoS2/NC

Fig. S46 Equivalent circuits for EIS spectra fitting

Fig. S47 The trends of a Rct and b DLi+ values obtained from in-situ EIS spectra during discharge and charge for MoS2-N-C700

Fig. S48 In-situ EIS spectra of MoS2-N-C600 during the 6th cycle: a discharge process and b charge process

Fig. S49 In-situ EIS spectra of MoS2-N-C800 during the 6th cycle: a discharge process and b charge process

Fig. S50 DRT plots of MoS2-N-C600 based on the EIS spectra: a discharge process and b charge process

Fig. S51 DRT plots of MoS2-N-C700 based on the EIS spectra: a discharge process and b charge process

Fig. S52 DRT plots of MoS2-N-C800 based on the EIS spectra: a discharge process and b charge process

Fig. S53 XRD pattern of the as-synthesized WS2-N-C700 heterostructure

Fig. S54 FESEM image of the as-synthesized WS2-N-C700 heterostructure

Fig. S55 Electrochemical performance of the as-synthesized WS2-N-C700 heterostructure for LIBs. a CV curves, b rate capability, c GCD profiles, and d cycling stability at 0.5A g-1

Table S1 Quantitative analysis of different chemical states of S species obtained from the deconvoluted XPS spectra

| Samples | Chemical states |  | Peak position (eV) | Relative percentage (%) |
| --- | --- | --- | --- | --- |
| MoS2-N-C600 | Sulphate | 2p 1/2 | 169.7 | 16.8 |
|  |  | 2p 3/2 | 168.6 |  |
|  | C-S | 2p 1/2 | 165.2 | 10.2 |
|  |  | 2p 3/2 | 164.1 |  |
|  | Mo-S | 2p 1/2 | 163.5 | 73.0 |
|  |  | 2p 3/2 | 162.4 |  |
| MoS2-N-C700 | Sulphate | 2p 1/2 | 169.8 | 19.8 |
|  |  | 2p 3/2 | 168.7 |  |
|  | C-S | 2p 1/2 | 165.2 | 6.0 |
|  |  | 2p 3/2 | 164.1 |  |
|  | Mo-S | 2p 1/2 | 163.5 | 74.2 |
|  |  | 2p 3/2 | 162.4 |  |
| MoS2-N-C800 | Sulphate | 2p 1/2 | 169.9 | 12.4 |
|  |  | 2p 3/2 | 168.8 |  |
|  | C-S | 2p 1/2 | 165.2 | 2.6 |
|  |  | 2p 3/2 | 164.1 |  |
|  | Mo-S | 2p 1/2 | 163.6 | 85.0 |
|  |  | 2p 3/2 | 162.5 |  |

Table S2 Relative percentages of nitrogen species in the MoS2-N-C heterostructures determined from the deconvoluted N 1s XPS spectra

| Samples | Chemical states | Peak position (eV) | Relative percentage (%) |
| --- | --- | --- | --- |
| MoS2-N-C600 | Mo–N | 397.5 | 17.2 |
|  | Pyridinic N | 398.5 | 33.0 |
|  | Pyrrolic N | 399.9 | 30.4 |
|  | Graphitic N | 401.2 | 19.4 |
| MoS2-N-C700 | Mo–N | 397.6 | 16.4 |
|  | Pyridinic N | 398.5 | 30.0 |
|  | Pyrrolic N | 399.8 | 30.4 |
|  | Graphitic N | 401.3 | 23.1 |
| MoS2-N-C800 | Mo–N | 397.6 | 15.1 |
|  | Pyridinic N | 398.5 | 33.6 |
|  | Pyrrolic N | 399.8 | 26.1 |
|  | Graphitic N | 401.4 | 25.2 |

Table S3 Charge transfer resistance (Rct) and Li+ diffusion coefficient (DLi+) values obtained from fitting the EIS spectra

|  | MoS2-N-C600 | MoS2-N-C700 | MoS2-N-C800 |
| --- | --- | --- | --- |
| Rct (ohm) | 106.7 | 77.1 | 83.1 |
| DLi+ (10-14 cm2 s-1) | 1.2 | 3.8 | 1.4 |

Table S4 Cycling performance comparison of recent state-of-the-art MoS2/C anodes for LIBs

| Anode | Mass loading (mg cm-2) | Current density (A g-1) | Cycle number | Capacity retention | Ref. |
| --- | --- | --- | --- | --- | --- |
| MoS2-N-C700 | 1.1~1.3 | 0.5 | 800 | ~100% | This work |
| MoS2@C | ~2.0 | 1 | 100 | 21.7% | [S1] |
| NG@MoS2@LS-C | ~3.1 | 0.1 | 100 | 55.5% | [S2] |
| B-MoS2–GO | ~0.6 | 0.5 | 200 | 77.9% | [S3] |
| Ni-MoS2/rGO | ~2.0 | 0.1 | 100 | 79.0% | [S4] |
| Co3S4/1T-MoS2@NC | 1.0~1.1 | 1 | 250 | 75.7% | [S5] |
| 1T/2H hybrid phase MoS2-graphene | 2~3 | 0.18 | 100 | 90.0% | [S6] |
| MoS2/C-3 | 1.6~2.1 | 1 | 1300 | 41.4% | [S7] |
| 5% BN-G@MoS2-50@50 | 0.57~0.85 | 1 | 500 | 85.6% | [S8] |
| SnS2/MoS2/DGS | ~2.0 | 0.2 | 200 | 96.9% | [S9] |

Table S5 Comparisons of electrochemical performance of carbon-based LISCs reported previously

| System | Voltage window (V) | Current density (A g-1) | Energy density (Wh kg-1) | Cycling performance | Ref. |
| --- | --- | --- | --- | --- | --- |
| MoS2-N-C700//AC | 0.5-4 | 0.1 | 175.0 | 1 A g-1@10000 cycles@78.2% | This work |
| MC800//HC | 2-4 | 0.25 | 152.2 | 2 A g-1@5000 cycles@80.0% | [S10] |
| Zn80Co20-PC//AC | 2-4 | 0.05 | 123.0 | 1 A g-1@5000 cycles@90.0% | [S11] |
| CAC//NPC | 0.01-4 | 1 | 151.8 | 2 A g-1@1600 cycles@87.0% | [S12] |
| NPC//AC | 2.0-4.2 | 0.1 | 112.0 | 1 A g-1@6000 cycles@72.0% | [S13] |
| CTK-1.0//CTK-1.0 | 0.1-4.2 | 0.1 | 137.6 | 2 A g-1@3000 cycles@75.0% | [S14] |
| NP-HPC//NP-SC | 1-3.8 | 0.1 | 121.0 | 1 A g-1@3000 cycles@80.2% | [S15] |
| PCNs-800//PCNs-800 | 1-4.2 | 0.1 | 112.0 | 1 A g-1@9000 cycles@63.0% | [S16] |
| NHCM-12//NHCM-A | 0.1-4 | 0.1 | 162.0 | 1 A g-1@5000 cycles@86.2% | [S17] |
| DGPC-1//AC | 2-4 | 0.1 | 103.4 | 5 A g-1@5000 cycles@70.2% | [S18] |

Supplementary References

- D. Li, G. Lin, Z. Huang, X. Tang, Z. Wu et al., Effect of different shell structure on lithium storage properties of MoS2 anode. J. Electroanal. Chem. 905, 115972 (2022). https://doi.org/10.1016/j.jelechem.2021.115972

- J. Sun, Z. Xu, W. Wang, S. Sheng, S. Zhao et al., Preparation and electrochemical properties of mesoporous Carbon@ MoS2 anode materials for lithium-ion batteries. Int. J. Electrochem. Sci. 21(3), 101294 (2026). https://doi.org/10.1016/j.ijoes.2026.101294

- H. Lu, B. Wu, Y. Zhang, T. Dong, Q. Duan et al., A simple and scalable method for preparing natural molybdenite-based MoS2–graphene oxide composite anodes via ultrasonic exfoliation combined with a solvothermal process. J. Electron. Mater. 55(3), 2969–2987 (2026). https://doi.org/10.1007/s11664-026-12686-4

- S. Zhang, K. Qi, B. Du, G. Zhu, X. Liu et al., Reduced graphene oxide supported Ni-doped MoS2 nanosheets with enhanced lithium-ion storage performance. J. Electroanal. Chem. 997, 119501 (2025). https://doi.org/10.1016/j.jelechem.2025.119501

- S.-C. Dong, R. Zeng, H. Zhang, S.-T. Zhang, P.-P. Chen et al., Enhancing stable and rapid Li+/Na+ storage performance via interface engineering of confining Co3S₄/1T-MoS₂ heterostructure on nitrogen-doped carbon. Electrochim. Acta 542, 147415 (2025). https://doi.org/10.1016/j.electacta.2025.147415

- K.Y. Jang, Y.A. Lee, S. Lim, S. Park, K.-N. Jung et al., Enhancing lithium-ion battery kinetics and stability leveraging hybrid 1T/2H MoS2–graphene heterostructures. Chem. Eng. J. 520, 165803 (2025). https://doi.org/10.1016/j.cej.2025.165803

- L. Liu, W. Du, Q. Zhang, H. Jiang, Y. Zhang et al., Constructing hollow flower-like molybdenum disulfide nanospheres/carbon nanospheres as anode with enhanced diffusion kinetics for lithium storage. Adv. Compos. Hybrid Mater. 7(6), 195 (2024). https://doi.org/10.1007/s42114-024-01029-8

- B. Chandra Sekhar, A. Soliman, M. Arsalan, E.H. Alsharaeh, A 2D hybrid nanocomposite: a promising anode material for lithium-ion batteries at high temperature. Nanoscale Adv. 6(22), 5612–5624 (2024). https://doi.org/10.1039/d4na00424h

- W. Yu, B. Cui, J. Han, S. Zhu, X. Xu et al., In situ encapsulation of SnS(2)/MoS2 heterojunctions by amphiphilic graphene for high-energy and ultrastable lithium-ion anodes. Adv. Sci. 11(36), 2405135 (2024). https://doi.org/10.1002/advs.202405135

- H. Liu, X. Zhang, C. Li, S. Zhao, Y. An et al., Self-templating synthesis of mesoporous carbon cathode materials for high-performance lithium-ion capacitors. ChemSusChem 18(3), e202401365 (2025). https://doi.org/10.1002/cssc.202401365

- Q. Tang, G. Chu, Y. Xie, C. Yang, F. Tang et al., Zn/Co bimetallic metal-organic framework derived carbon anode with enchanted rate capability for lithium-ion capacitors. Mater. Today Commun. 41, 110224 (2024). https://doi.org/10.1016/j.mtcomm.2024.110224

- Y. Yang, H. Du, A. Wang, C. Lu, D. Sun et al., Excellent capacitive storage performance of N-doped porous carbon derived from the orientation-guidance coupled with in-situ activation methodology. J. Colloid Interface Sci. 673, 657–668 (2024). https://doi.org/10.1016/j.jcis.2024.05.237

- H. Jing, M. Chen, X. Zhang, Y. Yang, X. Zheng et al., CO2-derived nitrogen doped porous carbon as advanced anodes for lithium-ion capacitors. J. Alloys Compd. 983, 173937 (2024). https://doi.org/10.1016/j.jallcom.2024.173937

- J. Jiang, Q. Shen, Z. Chen, S. Wang, Nitrogen-doped porous carbon derived from coal for high-performance dual-carbon lithium-ion capacitors. Nanomaterials 13(18), 2525 (2023). https://doi.org/10.3390/nano13182525

- C. Cao, H. Hu, J. Duan, G. Zeng, X. Cai et al., Phytic acid mediated N, P Co-doped hierarchical porous carbon with boosting capacitive storage for dual carbon lithium-ion capacitor. Electrochim. Acta 470, 143310 (2023). https://doi.org/10.1016/j.electacta.2023.143310

- T. Qian, Y. Huang, M. Zhang, Z. Xia, H. Liu et al., Non-corrosive and low-cost synthesis of hierarchically porous carbon frameworks for high-performance lithium-ion capacitors. Carbon 173, 646–654 (2021). https://doi.org/10.1016/j.carbon.2020.11.051

- J. Jiang, J. Yuan, P. Nie, Q. Zhu, C. Chen et al., Hierarchical N-doped hollow carbon microspheres as advanced materials for high-performance lithium-ion capacitors. J. Mater. Chem. A 8(7), 3956–3966 (2020). https://doi.org/10.1039/c9ta08676e

- G. Zhang, K. Sun, Y. Liu, D. Wu, H. Zhu et al., Double reaction initiated self-assembly process fabricated hard carbon with high power capability for lithium ion capacitor anodes. Appl. Surf. Sci. 609, 155083 (2023). https://doi.org/10.1016/j.apsusc.2022.155083